## Slide 1: Activities and plans of the USTC HGTD group
Yanwen Liu
University of Science and Technology of China

## Slide 2: Introduction to LGAD/UFSD
RD 50 found indications of charge amplification in highly irradiated diodes and strip detectors
Utilize the amplification effect in a controlled way (H.F.-W. Sadrozinski presentation at 20th RD50 workshop in 2012)
NIM A765(2014)7-11
NIM A765(2014)12-16

## Slide 3: UFSD / LGAD
Drift velocity in silicon saturates at about 107 cm/s
Charge collection for 300 um thick silicon ~ 3 ns
Fast silicon detector needs to be thin.
Need amplification layer to achieve high S/N
In early days …

## Slide 4: ATLAS HGTD project
Two double-sided disks at each endcap
At 3435 mm < |z| < 3485 mm
Coverage: 2.4 < || < 4.0
110 mm < R < 1000 mm
Pixel size: 1.3 x 1.3 mm2
Number of channels : 3.54 M
Active area: 6.3 m2
Time resolution per track: 30 ps

## Slide 5: An event of 200 interactions

## Slide 6: Radiation tolerance (TDR draft 2019 no SF)
At R = 12 cm, NIEL = 6.8x1015 neq / cm2 , TID = 2.4 MGy

## Slide 7: USTC HGTD team
Faculty: Hao Liang, Yanwen Liu, Yongjie Sun, Yusheng Wu, Lei Zhao, Zhengguo Zhao (6)
Postdoc: Quanyin Li (1)
Students: Han Chen, Jiajin Ge, Chihao Li, Zhengwei Xue, Tao Wang, Xiao Yang (6)
Blue = Sensor
Red = Electronics
Students 0.8 FTE, Postdoc and faculty members 0.5 FTE on HGTD
Joined the ATLAS HGTD project in January 2019

## Slide 8: USTC HGTD activities
Sensor design and test
Electronics ALTIROC tests
Assembly study (mechanical dummy module, bump-bonding)
Test beam analysis

## Slide 9: Sensor structure
C-stop
Float GuardRing
GuardRing
P-stop
JTE
Field Plate
Field Plate
P-well
N-Electrode
P-Electrode
~70 μm
~50 μm
VBD: 590 V (after 1x1015 neq /cm2, Vmax: 630 V
Leakage current: 1.5x10-8 A

## Slide 10: LGAD fabrication process
MASK: JTE, Guard ring
Phosphorus implant
MASK: c-stop, p-stop
Boron implant
Diffusion
MASK: n+ electrode, gain layer
Boron deep implant
Phosphorus implant
9. Backside Boron implant
10. Anneal
11. Deposit oxide
12. Deposit metal electrode

## Slide 11
LGAD parameters |  |  |  |  |  |  | 备注
 | Process | Mask | Ion | Energy (keV) | Dose(cm^-2) | 容许误差 | 
1 | Implant | JTE,Guard Ring | Phosphorus | 55 | ~4.5E+14 | 0% | 
2 | Implant | C-stop, P-stop/P-spray | Boron | 100 | ~4.0E+14 | % | P-spray 需要 浅,均匀 的注入
3 | Diffusion | 1050 ℃, 900 min (or 1200 ℃, 60 min) |  |  |  | % | 温度越高，时间越长，越好
4 | Implant | P-well | Boron | >1000 | *1.8-2.2 E+12 | %, uniform | p-well 生产时可从 1.8-2.2 设置 3-4个点研究不同profile的表现 p-well 注入对均匀度要求极高
5 | Implant | N-electrode | Phosphorus | 55 | ~4.5E+15 | % | 
6 | Anneal | ~1050℃, 20s |  |  |  | % | 
7 | Deposit | Surface Oxide | SiO2 |  | 0.5 - 2 | % | 
8 | Deposit | Ohm Contact & Field Plate | Aluminum |  | 1 | % | 
LGAD parameters |  |  |  |  |  |  | 备注
 | Process | Mask | Ion | Energy (keV) | Dose(cm^-2) | 容许误差 | 
1 | Implant | JTE,Guard Ring | Phosphorus | 55 | ~4.5E+14 |  | 
2 | Implant | C-stop, P-stop/P-spray | Boron | 100 | ~4.0E+14 |  | P-spray 需要 浅,均匀 的注入
3 | Diffusion | 1050 ℃, 900 min (or 1200 ℃, 60 min) |  |  |  |  | 温度越高，时间越长，越好
4 | Implant | P-well | Boron | >1000 | *1.8-2.2 E+12 |  | p-well 生产时可从 1.8-2.2 设置 3-4个点研究不同profile的表现 p-well 注入对均匀度要求极高
5 | Implant | N-electrode | Phosphorus | 55 | ~4.5E+15 |  | 
6 | Anneal | ~1050℃, 20s |  |  |  |  | 
7 | Deposit | Surface Oxide | SiO2 |  |  |  | 
8 | Deposit | Ohm Contact & Field Plate | Aluminum |  |  |  | 

## Slide 12: Sensor R&D
Failed test/verification
Passed test/verification

## Slide 13: Sensor test
Unirradiated, HPK Type 1-1, 1-2, 2 & 3-2
Envelope Label | Contents |  |  | Total number
Single SET | LG1-SE3 x2 | LG1-SE5 NM | LG1-SE5 x4 | 11
 | PIN1-SE5 | PIN1-SE5 NM | LG1-SE2 x2 | 
2x2 SET | LG 2x2-SE3-IP9 | LG 2x2-SE5-IP9 NM | LG 2x2-SE5-IP9 x4 | 14
 | PIN 2x2-SE5-IP9 | LG 2x2-SE2-IP9 | LG 2x2-SE5-IP7 | 
 | LG 2x2-SE5-IP5 | LG 2x2-SE5-IP3 | LG 2x2-SE3-IP7 | 
 | LG 2x2-SE3-IP5 | LG 2x2-SE5-IP5-IP9 UBM |  | 
LG 5x5-SE5-IP9 | LG 5x5-SE5-IP9 UBM |  |  | 1
Single & 2×2 in each type are measured
4 types
104 sensors in total
USTC is one of the test sites of LGAD sensors

## Slide 14: Inspection with microscope
Inspected all sensors with microscope.
Found glue on the surface of some sensors.
Glue can become very corrosive after irradiation. Feedback to HPK.

## Slide 15: Tests at probe station (I-V)
Sensor | Type 1-1 |  | Type 1-2 |  | Type 2 |  | Type 3-2 | 
 | Single | 2×2 | Single | 2×2 | Single | 2×2 | Single | 2×2
VBD/V | 216.2 | 201.1 | 272.3 | 277.9 | 255.9 | 245.0 | 130.3 | 126.8
Leakage current/nA | 0.45 | 0.69 | 1.18 | 1.11 | 1.41 | 2.41 | 0.79 | 1.27

## Slide 16: C-V and doping profiles
A large number of results reported in June 2019 HGTD mini week
Type | 1-1 | 1-2 | 2 | 3-2
VGL/V | 23.7 | 31.7 | 32.2 | 54.8
VFD/V | 183.3 | 35.4 | 141.2 | 62.9

## Slide 17: Plan for sensor tests
Setup laser TCT and beta source test to determine
  time resolution
  gain
  efficiency
  uniformity
Test of irradiated sensors

## Slide 18: Electronics (testing ALTIROC chip)
Altiroc consists of PA(pre-amplifier), descriminator, TDC and digital parts.
scan test on descriminator threshold, injected charge(Qinj) and input signal delay, to evaluate the performance and mismatch among different ASIC chips. Also, the test results will be a reference for the next version ASIC.
Some new issues are found during the test: such as cross talk form digital controller to analog input, oscillation in analog front-end in some of channels, inconsistency among ASICs.
AMP
DISC
TDC

## Slide 19: Threshold and charge scan
To research trends of TOA (Time of Arrival) and its std-dev due to the variation of injected charge.
Also, the minimum of acceptable charge can be found.
Test efficiency with different threshold and figure out the pedestal and max value of pre-amplifier output. Issues of cross talk and oscillation are found.
Descriminator Threshold Scan:

## Slide 20: Testing of TDC (delay scan)
Delay Scan:
To evaluate comprehensive performance of TOA TDC: linear dynamic range, DNL & INL.
On going：
Irradiation test.
Difference of parameters and performance among channels and their distribution.
Notes: Delay scan: Change the delay of ‘Start’signal with fixed ‘Stop’, i.e. change the input time interval

## Slide 21: Assembly studies
Dummy sensors by SINANO
Bump-bonding
Shear test：> 1kg
X-ray CT at USTC
More details in the talk at May 29 Assembly meeting

## Slide 22: Test beam analysis
March 2019 at DESY, 6 GeV electron beam
Proposed tracking algorithm based on straight line segments
See our presentation in test beam meeting on May 9.

## Slide 23: HGTD Digitization Software
The realistic HGTD digitization (simulation the signal propagation and electronics) is located in LAr software packages
TDR relies on tracking software (in Athena Release 20.20) to produce coherently the extended tracks to HGTD as well as the associated timing information, for physics and performance studies
Currently, the tracking software (PixelDigitization) uses a dummy model (Gaussian smearing) to mimic digitization effects.
To enjoy the realistic digitization in TDR studies, one needs to migrate the actual digitation codes from LAr software to PixelDigitization.
USTC group joined the efforts in late May, in close collaboration with HGTD software and performance group, as well as tracking CP group
  Tao Wang (1st year graduate) and Yusheng Wu
  Already be able to run both LAr and Pixel simulation and reconstruction software
  Currently study the HGTD digitization code in LAr packages and plan to migrate that to PixelDigitization soon, to be followed by performance and validation checks
  After the first project, plan to contribute to other areas of work, including timing information as well as object performance etc.
  In fact, we already participate in a physics study for HGTD earlier this year, may continue once the sufficient progress will be made on the low-level software work

## Slide 24: Conclusion and outlook
USTC joined HGTD in Jan 2019 and has ramped up very efficiently Thanks to the very supportive community
Now actively working on
  Sensor design and tests
  ASIC RD
  assembly studies
  digitization software
Plans
  Continue to expand the test facility to include laser TCT, beta scope, and to handle irradiated sensors
  Continue to develop the sensor design
  Will participate in the detector and object performance studies as well as physics studies

## Slide 25: BACK-UP

## Slide 26: Acceptor removal
Reference: doi.org/10.1016/j.nima.2018.11.121