## Slide 1: Cornell SRF New Materials Program Nb3Sn Development
Sam Posen and Matthias Liepe
Cornell University
TTC Meeting
6 December 2011
Beijing, China

## Slide 2: Motivation: Why Coat Cavities with Nb3Sn?
Great promise shown in experiments at University of Wuppertal in 80s-90s
We can add techniques that improved the performance of Nb cavities
  HPR, EP, 120 deg C bake, CBP, single crystal Nb
Higher Q0 than Nb for surface fields <~30 mT proven
Higher RF critical field than Nb predicted from theory

## Slide 3
Sn vapor arrives at surface
Nb-Sn interdiffusion
Ts = Sn source temperature
=~1200 C
Tf = furnace temperature
=~1100 C
By independently controlling Sn vapor abundance, it can balanced with Nb-Sn interdiffusion rate to achieve desired stoichiometry
Sn Vapor
Heater
Coating Mechanism
Vapor Diffusion
Coating chamber in UHV furnace
Sn
Nb
Nb3Sn

## Slide 4: Nb3Sn Coating Chamber
Nb heat Shields
Power for heater
Copper transition weld from stainless to Nb
Flange to UHV furnace
Coating chamber is inserted into UHV furnace. Separate vacuum system keeps cavity furnace free from tin contamination
UHV Furnace
Top of insert

## Slide 5: Accomplishments: Surface Studies of Samples
SEM shows micron sized grains similar to Wuppertal
Anodization color indicates Nb3Sn on surface
Cornell, 2011
Wuppertal, 1996
Anodized
Not anodized
1”

## Slide 6: Accomplishments: X-ray Analysis
EDX: uniform composition over surface of 24.2±0.5 atm%Sn
XPS: uniform composition to a depth of 1.5 um

## Slide 7: Accomplishments: Low Temperature Tests
Transition at 18.1±0.2 K, close to the highest recorded value of 18.3 K
Negligible RRR degradation from coating process
Tc
RRR

## Slide 8: Current Work: Nb3Sn Samples in TE Mushroom Cavity
Commissioning is under way of 6 GHz TE mushroom cavity with removable bottom plate
Plan: EP and coat 5” plate with Nb3Sn then RF test
5”
For holding during coating

## Slide 9: Current Work: Nb3Sn Coated Single Cell Cavities
Designed upgraded coating chamber capable of loading full single cell 1.3 GHz cavities
Parts acquisition and fabrication has begun
Optimistic estimate for first coating: March
Tube for main body of coating chamber (niobium)

## Slide 10: Outlook
Coat 5” sample with Nb3Sn and RF test in TE mushroom cavity
Fabricate and commission new coating chamber
Coat ILC single cell cavity with Nb3Sn and RF test with full T-map
Use RF performance as feedback to improve coating parameters