## Slide 1
Development of Large Grain Cavities at DESY
Presented by Waldemar Singer

## Slide 2
11 LG Cavities after BCP
11 LG Cavities after EP
Qo of LG Cavities after EP and BCP
LG Pro/Contra

## Slide 3
Chart: Eacc, MV/m
| 0.93999999761581399 | 1.0599999427795399 | 1.20000004768371 | 1.3500000238418499 | 1.5299999713897701 | 1.7200000286102199 | 1.9400000572204501 | 2.1800000667571999 | 2.46000003814697 | 2.7699999809265101 | 3.13000011444091 | 3.5399999618530198 | 4 | 4.5 | 5.0999999046325604 | 5.7600002288818297 | 6.5300002098083496 | 7.4099998474120996 | 8.4499998092651296 | 9.7100000381469709 | 11.2399997711181 | 13.079999923706 | 15.3400001525878 | 18.2399997711181 | 21.530000686645501 | 25.049999237060501 | 27.440000534057599 | 28.4699993133544 | 29.600000381469702 | 29.889999389648398 | 30
AC112 | 20500000768 | 20700000256 | 20899999744 | 21200001024 | 21300000768 | 21400000512 | 21500000256 | 21600000000 | 21699999744 | 21799999488 | 21899999232 | 22000001024 | 22000001024 | 21799999488 | 21799999488 | 21600000000 | 21300000768 | 21099999232 | 20800000000 | 20600000512 | 20500000768 | 20400001024 | 20199999488 | 20199999488 | 19800000512 | 18499999744 | 15500000256 | 12200000512 | 8120000000 | 6980000256 | 6520000000
AC113 | 19399999488 | 19800000512 | 20600000512 | 20800000000 | 19900000256 | 19299999744 | 18800001024 | 18400000000 | 18000001024 | 14400000000 | 13100000256
AC151 after add. HPR | 28400000000 | 28000000000 | 27400000000 | 26900000000 | 26900000000 | 26800000000 | 26400000000 | 26400000000 | 26500000000 | 26400000000 | 26100000000 | 25200000000 | 23400000000 | 21200000000 | 18600000000 | 16500000000 | 14700000000 | 13500000000 | 12700000000 | 12300000000
AC153 | 19200000000 | 20000000000 | 20400000000 | 21300000000 | 21300000000 | 21900000000 | 22100000000 | 22600000000 | 22100000000 | 21800000000 | 21300000000 | 20400000000 | 19400000000 | 18400000000 | 17500000000 | 16800000000 | 16000000000 | 15200000000 | 15100000000 | 14900000000 | 14300000000 | 14100000000
AC154 | 20800000000 | 22000000000 | 22900000000 | 23400000000 | 24400000000 | 25100000000 | 25600000000 | 25900000000 | 26000000000 | 25800000000 | 25700000000 | 25600000000 | 25200000000 | 24000000000 | 22700000000 | 21300000000 | 20400000000 | 19700000000 | 19200000000 | 18300000000 | 17500000000 | 17500000000 | 17500000000
AC155 | 20800000000 | 22300000000 | 23600000000 | 24800000000 | 25300000000 | 25400000000 | 25000000000 | 24100000000 | 22500000000 | 20500000000 | 18500000000 | 17700000000 | 17100000000 | 16700000000 | 16200000000 | 15900000000 | 15000000000 | 14900000000
AC157 | 24000000000 | 25700000000 | 27400000000 | 27900000000 | 28300000000 | 27900000000 | 27500000000 | 27700000000 | 27400000000 | 27000000000 | 25000000000 | 23400000000 | 21800000000 | 20800000000 | 20100000000 | 19400000000 | 19000000000 | 18900000000 | 18800000000 | 18300000000 | 17600000000 | 16900000000 | 16400000000 | 16100000000 | 16000000000
AC158 after add. 2nd HPR | 31200000000 | 31200000000 | 32800000000 | 33500000000 | 33700000000 | 34200000000 | 35200000000 | 36100000000 | 35300000000 | 34200000000 | 34000000000 | 33900000000 | 33600000000 | 33700000000 | 33000000000 | 31300000000 | 30000000000 | 28700000000 | 27100000000 | 25400000000 | 23600000000 | 20900000000 | 17500000000 | 13600000000 | 10900000000 | 8950000000 | 6860000000 | 5380000000 | 4350000000 | 3700000000
AC114 | 21200001024 | 23800000512 | 26000001024 | 26400000000 | 26000001024 | 24400001024 | 23499999232 | 22200000512 | 20800000000 | 19499999232 | 18300000256 | 17400000512 | 16499999744 | 16000000000 | 15600000000 | 15500000256
AC156 after add. HPR | 34500000000 | 36000000000 | 36800000000 | 37200000000 | 37200000000 | 36600000000 | 35800000000 | 34600000000 | 32500000000 | 29700000000 | 26700000000 | 25400000000 | 24300000000 | 23400000000 | 22700000000 | 22200000000 | 22600000000 | 22500000000 | 21700000000 | 21400000000 | 21100000000 | 21000000000
AC152 after add. HPR | 29300000000 | 30700000000 | 31800000000 | 32000000000 | 32300000000 | 32300000000 | 31900000000 | 31000000000 | 29400000000 | 27200000000 | 24700000000 | 22200000000 | 21000000000 | 20000000000 | 19500000000 | 19000000000 | 18800000000 | 18500000000 | 18400000000 | 18000000000 | 18100000000
Q0(Eacc) of the LG cavities AC112- AC114, AC151-AC158 at 2K after BCP.
Test after 100 µm rough BCP, annealing at 800°C for 2h, final BCP of 20 µm and baking at 130°C for 48h. AC112 is not baked; AC113and AC114 are baked after additional 20µm BCP; AC158 after 2nd HPR has FE
Eleven 9 -cell CVs produced at RI from Heraeus Nb with big central crystal

## Slide 4
Chart: AC112-114, AC151-158 BCP
| 275.33333333333331 | 356.33333333333331 | 291.5 | 300 | 374 | 319 | 378.33333333333331 | 318.66666666666669 | 321.33333333333331 | 349 | 352.66666666666669 | 344.33333333333331 | 334.66666666666669 | 345.66666666666669 | 307.5 | 185.5 | 191 | 213 | 167 | 174 | 210 | 182 | 232 | 173
AC112-114, AC151-158 BCP | 30.13 | 35.79 | 30.13 | 29.11 | 29.12 | 30.06 | 28.03 | 34.54 | 28.03 | 28.37 | 30.59 | 28.37 | 29.69 | 34.8 | 29.69 | 31.79 | 30.59 | 30.59 | 28.03 | 29.23 | 29.23 | 30.01 | 32.64 | 32.64
Eacc (max Eacc in mode measurements) vs. average RRR in individual cells, after BCP
AC RRR measurement

## Slide 5
Eacc versus RRR of FLASH (TTF) cavities (ca.1995-2000). RRR average for cavity. Treatment: post purification with Ti at 1400°C and BCP.
Pronounced dependence Eacc on RRR
Chart: AC RRR
| 137 | 444 | 222 | 473 | 504 | 288 | 248 | 526 | 572 | 535 | 520 | 525 | 200 | 620 | 290 | 537 | 256 | 386 | 463 | 517 | 635 | 612 | 227 | 527 | 531 | 465 | 467 | 661
quench | 14.1 | 23.3 | 18.7 | 23 | 27.6 | 23.2 | 14.6 | 22.9 | 20.2 | 24.7 | 25.6 | 25.4 | 7.7 | 20.3 | 13.3 | 24.6 | 16.3 | 25.1 | 22.1 | 14.2 | 22.7 | 24 | 18.9 | 24.5 | 28.4 | 21.2 | 19.4 | 28.3
power limit | 28.6 | 27.8 | 29.3 | 25.3 | 19.7 | 28.4 | 21.9 | 26.7 | 28.4 | 30.9 | 13.3 | 19.9 | 29.9 | 28.3 | 23.3 | 29.1 | 25.3 | 26.7 | 28.4 | 28.6 | 25

## Slide 6
Chart: Eacc, MV/m
| 0.99000000953674305 | 1.2799999713897701 | 1.62000000476837 | 2.0599999427795401 | 2.6500000953674299 | 3.41000008583068 | 4.38000011444091 | 5.6900000572204501 | 7.4299998283386204 | 8.5299997329711896 | 9.8400001525878906 | 11.300000190734799 | 13.0900001525878 | 15.279999732971101 | 17.9699993133544 | 21.590000152587798 | 26.4899997711181 | 29.2299995422363 | 32.5 | 35.180000305175703 | 38.080001831054602 | 40.659999847412102 | 42.529998779296797
AC113 | 28899999744 | 30300000256 | 30599999488 | 30900000768 | 31600001024 | 31800000512 | 31600001024 | 31200000000 | 29899999232 | 28700000256 | 27399999488 | 25400000512 | 23700000768 | 21699999744 | 19800000512 | 18699999232 | 18000001024 | 17799999488 | 17400000512 | 16600000512 | 15800000512 | 14800000000 | 13500000256
AC114 | 21300000768 | 22000001024 | 22699999232 | 23299999744 | 23600001024 | 23600001024 | 23399999488 | 22900000768 | 22300000256 | 21200001024 | 20000000000 | 19100000256 | 18400000000 | 17300000768 | 15400000512
AC112 | 24500000768 | 25500000256 | 26100000768 | 27000000512 | 27299999744 | 27000000512 | 26100000768 | 24500000768 | 23399999488 | 21500000256 | 19600001024 | 17699999744 | 16400000000 | 15900000256 | 15400000512 | 14899999744 | 14200000512 | 13100000256 | 12499999744 | 11400000512 | 12099999744 | 11200000000 | 10400000000
AC155 | 21600000000 | 25800000000 | 27200000000 | 28100000000 | 27800000000 | 25300000000 | 21400000000 | 20100000000 | 19000000000 | 17700000000 | 17100000000 | 16200000000 | 15500000000 | 14700000000 | 13700000000 | 13200000000 | 12600000000 | 12400000000 | 12100000000 | 11900000000 | 11700000000 | 11700000000
AC151 | 20000000000 | 20500000000 | 20900000000 | 21300000000 | 21700000000 | 21900000000 | 22000000000 | 22000000000 | 21800000000 | 21300000000 | 20900000000 | 20600000000 | 20300000000 | 20000000000 | 19800000000 | 19400000000 | 18800000000 | 17900000000 | 16600000000 | 14800000000 | 13000000000 | 11500000000 | 10100000000 | 9000000000 | 7660000000 | 6530000000 | 5640000000 | 4910000000 | 4100000000
AC152 | 31900000000 | 32700000000 | 33700000000 | 33800000000 | 33700000000 | 33100000000 | 32000000000 | 30400000000 | 29300000000 | 28100000000 | 26900000000 | 25700000000 | 24400000000 | 23400000000 | 22600000000 | 22000000000 | 21800000000 | 21500000000 | 21300000000 | 21200000000 | 21000000000 | 21000000000 | 20200000000 | 17800000000 | 14500000000 | 12500000000
AC157 | 33300000000 | 34300000000 | 35200000000 | 35800000000 | 36300000000 | 36700000000 | 36700000000 | 36000000000 | 34700000000 | 32600000000 | 31000000000 | 29100000000 | 26900000000 | 24900000000 | 23200000000 | 22400000000 | 21800000000 | 20900000000 | 20700000000 | 20700000000
AC158 | 30400000000 | 29600000000 | 27100000000 | 25300000000 | 23500000000 | 22200000000 | 21900000000 | 21800000000 | 21800000000 | 21700000000 | 21700000000 | 21600000000 | 21700000000 | 21200000000 | 20800000000 | 19900000000 | 19100000000 | 17900000000 | 17600000000 | 16700000000 | 16300000000
AC153 | 21400000000 | 23300000000 | 25200000000 | 27600000000 | 28900000000 | 29700000000 | 30100000000 | 29600000000 | 28800000000 | 27900000000 | 26700000000 | 25200000000 | 23400000000 | 21900000000 | 21100000000 | 20600000000 | 20300000000 | 20200000000 | 19900000000 | 19700000000 | 18400000000 | 17700000000 | 17800000000 | 18100000000 | 16200000000 | 15600000000 | 17400000000 | 17600000000
AC154 | 34400000000 | 36100000000 | 37500000000 | 37900000000 | 37300000000 | 36300000000 | 34500000000 | 33300000000 | 31900000000 | 30000000000 | 28000000000 | 26100000000 | 24800000000 | 24200000000 | 23700000000 | 23200000000 | 22800000000 | 21800000000 | 20900000000 | 19000000000 | 18200000000 | 18400000000 | 17900000000
AC156 | 16400000000 | 18500000000 | 18900000000 | 18900000000 | 18700000000 | 17700000000 | 17200000000 | 17000000000 | 17000000000 | 16800000000 | 16500000000 | 16200000000 | 16100000000 | 16200000000 | 15400000000 | 16000000000 | 15900000000 | 16000000000
Q0(Eacc) performance of the LG cavities AC112- AC114, AC151-AC158 at 2K after 50-120 µm EP, 800°C , baking.
AC151, AC152 and AC 157 are in retreatment at DESY (add. EP)

## Slide 7
Chart: AC112-114, AC151-158 EP
| 264 | 328.33333333333331 | 288 | 410.66666666666669 | 335.33333333333331 | 343.66666666666669 | 320.66666666666669 | 441.66666666666669 | 404.33333333333331 | 286 | 251 | 341.33333333333331 | 382.5 | 307.33333333333331 | 271.33333333333331 | 294.33333333333331 | 233.66666666666666 | 406.5 | 274 | 304 | 362 | 362.33333333333331
AC112-114, AC151-158 EP | 33.04 | 33.9 | 33.9 | 25.26 | 27.38 | 27.38 | 30.25 | 31.81 | 31.8 | 15.27 | 23.46 | 23.46 | 47.19 | 41.21 | 38.89 | 43.36 | 43.36 | 44.99 | 49.78 | 45.84 | 46.09 | 46.09
Eacc (max Eacc in mode measurements) vs. average RRR in individual cells, after EP
AC RRR measurement

## Slide 8
Chart: Eacc, MV/m
Comparison of unloaded quality factor Q0 at 2K for 11 EP treated LG cavities with Qo at 2K of XFEL prototype cavities (AC115-AC129, best result)

## Slide 9
Chart: Eacc, MV/m
AC112 | 21799999488 | 20600000512 | 20199999488 | 19800000512 | 18499999744
AC113 | 20800000000 | 19299999744 | 18800001024 | 18000001024 | 14400000000
AC114 | 20700000256 | 19499999232 | 19000000512 | 17899999232 | 13000000512
AC151 | 26400000000 | 26100000000 | 21200000000 | 16500000000 | 14700000000
AC152 | 31900000000 | 27200000000 | 21000000000 | 19000000000 | 18000000000
AC153 | 22600000000 | 21300000000 | 17500000000 | 15200000000 | 14100000000
AC154 | 25900000000 | 25200000000 | 21300000000 | 19200000000 | 17500000000
AC155 | 25400000000 | 22500000000 | 17700000000 | 16200000000 | 14900000000
AC156 | 24700000000 | 25400000000 | 21300000000 | 12000000000
AC157 | 27500000000 | 27000000000 | 20800000000 | 18900000000 | 16900000000
AC158 | 34000000000 | 31300000000 | 27100000000 | 20900000000
Comparison of unloaded quality factor Q0 at 2K for 11 BCP treated LG cavities with Qo at 2K of XFEL prototype cavities (AC115-AC129, best result)

## Slide 10
Chart: 
| 0.99000000953674305 | 1.2699999809265099 | 1.62999999523162 | 2.0899999141693102 | 2.6900000572204501 | 3.45000004768371 | 4.4299998283386204 | 5.6799998283386204 | 7.25 | 8.2600002288818306 | 9.4099998474121005 | 10.6599998474121 | 12.1300001144409 | 13.289999961853001 | 14.3400001525878 | 14.949999809265099 | 15.8800001144409 | 17.100000381469702 | 17.4500007629394 | 17.829999923706001 | 18.559999465942301 | 18.870000839233398 | 19.370000839233398 | 19.9500007629394
EP 144 µm, BCP 18 µm, 7xHPR | 24000000000 | 25099999232 | 25799999488 | 26800001024 | 27700000768 | 28299999232 | 28700000256 | 28500000768 | 27700000768 | 26900000768 | 26000001024 | 24600000512 | 23399999488 | 20099999744 | 16700000256 | 13299999744 | 10800000000 | 7560000000 | 6040000000 | 5529999872 | 4470000128 | 4280000000 | 4670000128 | 3890000128
--- | 18900000768 | 20700000256 | 22300000256 | 23200000000 | 23000000512 | 22499999744 | 21200001024 | 19000000512 | 17500000256 | 15400000512 | 12600000512 | 9960000512 | 8240000000 | 6080000000
--- | 33400000512 | 36500000768 | 36999999488 | 33400000512 | 24299999232 | 29799999488 | 35499999232 | 25899999232 | 22800001024 | 20099999744 | 11600000000 | 11500000256
6xHPR | 28999999488 | 29400000512 | 30100000768 | 30400000000 | 30800001024 | 31000000512 | 30599999488 | 29899999232 | 28600000512 | 27499999232 | 26100000768 | 24500000768 | 22800001024 | 21600000000 | 20899999744 | 19399999488 | 18400000000 | 17100000256 | 15600000000 | 14200000512 | 13100000256 | 12099999744 | 10800000000 | 8970000384 | 9669999616
--- | 28899999744 | 29699999744 | 30599999488 | 31200000000 | 31299999744 | 31100000256 | 30699999232 | 29899999232 | 28099999744 | 26699999232 | 25099999232 | 23399999488 | 21799999488 | 20400001024 | 19100000256 | 16899999744 | 14099999744 | 11299999744 | 11299999744
6xHPR | 20600000512 | 21699999744 | 22599999488 | 23600001024 | 24600000512 | 25300000768 | 25899999232 | 25899999232 | 25400000512 | 24000000000 | 22900000768 | 21500000256 | 19900000256 | 18000001024 | 16800000000 | 15800000512 | 14499999744 | 13600000000 | 12700000256 | 5200000000 | 4980000256 | 4670000128 | 4449999872 | 4040000000 | 4030000128
--- | 17500000256 | 18699999232 | 19700000768 | 20800000000 | 21699999744 | 22599999488 | 23399999488 | 23900000256 | 24000000000 | 23399999488 | 21899999232 | 19700000768 | 18699999232 | 17699999744 | 16600000512 | 15299999744 | 14099999744 | 12800000000 | 11600000000 | 10499999744 | 9500000256 | 8609999872 | 7780000256 | 7040000000 | 6830000128 | 6680000000 | 5960000000 | 5360000000 | 4830000128 | 4329999872 | 4010000128 | 3950000128 | 4070000128
--- | 16499999744 | 18499999744 | 20700000256 | 22599999488 | 21799999488 | 20999999488 | 19000000512 | 17300000768 | 15500000256 | 13200000000 | 11000000512 | 8150000128 | 6609999872 | 5110000128 | 4090000128
EP 48 µm, 12xHPR | 28199999488 | 30300000256 | 30900000768 | 31600001024 | 32000000000 | 32099999744 | 31800000512 | 31000000512 | 29200001024 | 27800000512 | 23600001024 | 22000001024 | 19900000256 | 18200000512 | 15299999744 | 14499999744 | 13600000000 | 13500000256 | 12300000256
--- | 27399999488 | 28299999232 | 28700000256 | 29400000512 | 29799999488 | 29300000768 | 29500000256 | 28500000768 | 26499999744 | 23200000000 | 21200001024 | 19499999232 | 18300000256 | 17799999488 | 16800000000 | 15900000256 | 14200000512 | 11100000256 | 10899999744
--- | 27200000000 | 28199999488 | 28800000000 | 29600000000 | 29899999232 | 29799999488 | 29099999232 | 27700000768 | 25099999232 | 23299999744 | 21300000768 | 19600001024 | 18200000512 | 17300000768 | 16000000000 | 13699999744 | 10899999744 | 10200000512
Qo versus Eacc for the XFEL prototype cavity AC117 after different treatment

## Slide 11
1.LG discs are more cost effective as fine grain sheets (32% according estimation for XFEL CVs pre-series)
2.Wire saw procedure allows getting better surface quality and thickness tolerances in discs.
3.Increased thermal conductivity close to 2K due to phonon effect helps to lead the heat away from hot spots.
4.Simplified quality control QC is possible. No danger that during many steps from ingot to sheet the material will be polluted (no RRR degradation). Eddy current scanning is avoidable.
5.Accelerating gradient of 25-30MV/m can be reached by simple preparation with BCP only. Best result of 45 MV/m reached after EP is a world record for this cavity type.
6.Onset of Q-drop in large grain cavities is typically at 10% higher gradients.
7. Baking of BCP - treated cavity at 130°C works.
8.The Q0 is ca. 25-30% higher for EP treated LG- compared to similar FG -cavities
9.The wire saw method caused much less stress at the surface of the disc compared to rolled sheets (reduces damage layer on both sides of the disc).
10.The complete chain of the LG cavity technique beginning with material production and ending with cavity installation into a cryo-module has been proven. Cryo-module of LG cavities for XFEL injectors is in work.
LG: Pro

## Slide 12
LG: Contra
LG is currently not usable for mass production. For example, the industry is not in position to produce in 2 years the required amount of ca. 20 tons of LG material for the European XFEL.
Only one company (RI) has industrial experiences for LG cavity mechanical fabrication.
3. Smaller shape accuracy as for fine grain mechanical fabrication works, but needs additional effort due to not sufficiently precise shape of half-cells (clamping for trimming, trimming accuracy, frequency measurement, assembling of half cells for welding)

## Slide 13
Thank you
For more details see paper
Development of Large Grain Cavities at DESY
W. Singer, S. Aderhold, A. Ermakov, J. Iversen, D. Kostin, G. Kreps, A. Matheisen, W.-D. Möller, D. Reschke, X. Singer, K. Twarowski and H. Weise
Will be published SRF2011 PRST-AB Special Edition

## Slide 14
Surface roughness (averaged values) of the central and close to them crystals with different orientations after ca. 80 µm BCP
Roughness | (211) | (221) | (100) | (111) | (110)
Ra, µm | 0,15 | 0,2 | 0,24 | 0,35 | 0,36
Ry, µm | 0,95 | 1,29 | 1,4 | 2,23 | 2,56