## Slide 1: MULTILAYERS
C. Antoine, Irfu, SACLAY)

## Slide 2: SRF limitations in (brief) summary
Calculation for the superheating model valid only
  near TC
  “perfect material” (no surface defects)
In real life :
  penetration of vortex faster @ low temperature (why?)
  early penetration of vortex possible @ surface defects
  Nb : the best because of its high HC1 ?
Either we are able to produce 0 defect surfaces, either we screen the surface with multilayers !
More theoretical and exp. work needed
Superheating field vs Vortex nucleation
Nb<50 MV/m
+ magn. screening
Nb~ 55 MV/m
Nb3Sn ~ 95 MV/m
Notes: “rf pair breaking” induces non linear corrections which increase when T decreases : at high field : quadratic variation of RBCS w. field and Tp° . Correction due to clean/dirty limits not done yet
Note : RF HC1 should be > to DC HC1 (Gurevich dixit). If you keep below HC1
If you keep below HC1 : no need to draw hypothesis on the origin/ prediction of HSH ( a controversy between Cornell’s theoretician Sethna and Gurevich on the topic)
If you measure DC or low frequency HC1 you have some safety margin concerning RF HC1

## Slide 3
High Tc nanometric SC films : low RS, high HC1
Accelerating Field Eacc (MV/m)
Magnetic field B (mT)
Quality coefficient Q0
composite nanometric SC (multilayers) Nb / insulator/ superconductor / insulator /superconductor…
d<l => high HC1 => no transition, no vortex in the layer
Increasing of Eacc AND Q0 !!!
Best candidates
Nb3Sn
MgB2
Cavity's internal surface →
Outside wall

Happlied
HNb
Notes: Ainsi si on dépose une série de couche de NbN sur du Nb massif, intercalée d’une couche isolante pour les découpler entre elles, on va atténuer le champ qui arrive jusqu’au niobium et rester en dessous de son champ de transition.
Et donc en théorie, en recouvrant une cavité existante on peut à la fois augmenter le champ accélérateur et diminuer la consommation cryogénique, ce qui serait bénéfique pour absolument tous les types de cavités.

## Slide 4: Local magnetometry (1)
increasing I
=
increasing B
3rd harmonic measurement, local measurement : sample size >> excitation/measuring coil
b0cos (wt) applied in the coil
temperature ramp
third harmonic signal appears @ BC1
Excitation/Detection
coil (small/sample)
Differential Locking Amplifier
= T/Tc
Sample SL : third harmonic signal for various b0
TCi at Bi
Notes: Quelques détail exp :
- C’est une mesure locale, et tant qu’on est à bas champ : on peut s’abstraire du facteur de démagnétisation (pas d’effet de bord : on peut considérer l’échantillon comme un plan infini !) : donc même si on mesure en champ perpendiculaire, on a quand même une info pertinente (peux pas rentrer dans le détail ici)
On mesure le BC1 global de l’échantillon, mais vu coté “couches”
T/Tc = 1 correspond à T = 8.57, le Tc de notre Nb. Mais le comportement de l’échantillon SL est bien relatif à CE niobium là. Ce sera néanmoins important de vérifier le comportement de couches similaires déposées sur du Nb massif. En effet les couches Nb déposées par magnétron ont un HC1 ~20 mT << 150mT pour le matériau massif.
Autre détails concernant le multicouche (résultats non présentés ici)
Quand il y a plusieurs signaux, on garde toujours le premier (= première pénétration). Par exemple sur le multicouche, on voit apparaitre en remontant en Tp° les signaux correspondants à la 2em, 3eme, puis 4eme couche respectivement, ce qui est bien la preuve que le champ qui leur arrive est atténué. Difficile à dépouiller, mais je suis sure qu’on pourrait en obtenir une info sur l’atténuation de chaque couche avec des échantillons de meilleure qualité.
On a pu voir aussi certains autres défauts de cette façon : netteté de la transition, élargissement du signal… c’est pas encore directement exploitable, mais on est en train d’y réfléchir, par exemple pour optimiser les épaisseurs…

## Slide 5: Local magnetometry (2)
Chart: T (K)
| 4.5 | 4.96 | 7.4 | 7.6 | 8.27 | 8.56 | 8.64 | 8.68
Référence | 18 | 11 | 4.1 | 3 | 1 | 0.4 | 0.2 | 0.1 | 0.02 | 0.0046
SL | 96 | 16.2089 | 10.8869 | 6.8543 | 5.3954 | 5.0057 | 3.9325 | 3.0735 | 2.3061 | 1.9215 | 1.5503 | 1.1624 | 0.7668 | 0.5771 | 0.4602 | 0.1183 | 0.0381 | 0.003
(B SL_S) B = I/9,4 | 0.58298 | 1.5649 | 2.5489 | 3.3383 | 4.3287 | 4.9223 | 5.9117 | 11.8532 | 15.7894 | 18.4734 | 26.3723
SL sample : 250 nm Nb + 14 nm MgO + 25 nm NbN
8.90K < Tp° < 16K : behavior ~ NbN alone
Tp°< 8.90K, i.e. when Nb substrate is SC , => BC1SL >> BC1Nb
SL @ Saclay 2011
SL @ Naples 2010
SRF 2011

## Slide 6: Local magnetometry (3)
Chart: T
| 15.95 | 15.05 | 14.5 | 14.1 | 13.95 | 13.72 | 12.2 | 11.55 | 9.6 | 9.42 | 9.7100000000000009 | 8.42 | 8.6999999999999993 | 8.3000000000000007
ML4 | 1.8319 | 3.9691 | 6.6117 | 8.2638 | 9.9245 | 11.5787 | 14.7766 | 16.5489 | 19.8904 | 23.2064 | 26.5309 | 32.866 | 37.5543 | 55.8043
SL | 0.58298 | 1.5649 | 2.5489 | 3.3383 | 4.3287 | 4.9223 | 5.9117 | 11.8532 | 15.7894 | 18.4734 | 26.3723
Nb Ref | 11 | 4.1 | 3 | 1 | 0.4 | 0.2 | 0.1 | 0.02 | 0.0046
ML sample : 250 nm Nb + (14 nm MgO + 25 nm NbN) x 4
Multilayer tested for the first time BC1 > 55 mT @ 8K !
NEW !
Notes: Comments : still some technical problems of thermal contact between sample and set up + thermal regulation not precise below 5 K

## Slide 7: Local magnetometry (4)
Chart: BC1
| 15.95 | 15.05 | 14.5 | 14.1 | 13.95 | 13.72 | 12.2 | 11.55 | 9.6 | 9.42 | 9.7100000000000009 | 8.42 | 8.6999999999999993 | 8.3000000000000007
ML4 | 1.8319 | 3.9691 | 6.6117 | 8.2638 | 9.9245 | 11.5787 | 14.7766 | 16.5489 | 19.8904 | 23.2064 | 26.5309 | 32.866 | 37.5543 | 55.8043
SL | 0.58298 | 1.5649 | 2.5489 | 3.3383 | 4.3287 | 4.9223 | 5.9117 | 11.8532 | 15.7894 | 18.4734 | 26.3723
Nb Ref | 11 | 4.1 | 3 | 1 | 0.4 | 0.2 | 0.1 | 0.02 | 0.0046
ML sample : 250 nm Nb + (14 nm MgO + 25 nm NbN) x 4
Multilayer tested for the first time BC1 > 55 mT @ 8K !
NEW !
Notes: let’s dream….

## Slide 8: Participation to Eucard 2 WP11.2: Thin Film
Niobium on copper (µm) (CERN)
  After ~ 20 years stagnation : new revolutionary deposition techniques (e.g. HPIMS)
  Great expectations in cost reduction
  No improved performances/ bulk Nb
Higher Tc material (µm) (CERN)
  Based on superheating model.
  Higher field and lower Q0 expected
  Superheating model questionable @ 2 K, type II SC
Higher Tc material (nm), multilayer (CEA+ INPG)
    Based on trapped vortices model (Gurevich)
  Higher field and lower Q0 expected
  Recent experimental evidences
Specific characterization tools needed
  Local magnetometry (CEA)
  Sample cavity (HZB)
Better understanding of SRF physics needed
Subtask 2
Subtask 3
Subtask 1
Subtask 4
Notes: We need some young physicist taking time to understand the work of theoretician and translating it into practical information