## Slide 1: HF rinsing studies of 1.3 GHz single cells
A. Romanenko

## Slide 2: Motivation
Anodizing experiments (Eremeev et al, SRF’2005, TuAO8; Ciovati et al, PRST AB 10, 062002 (2007)) demonstrated that the depth of the layer modified by 120C baking is about 20 nm
Distribution of lossy layers within this depth can be explored by step-by-step material removal
  HF rinsing as a tool for that
Maybe maximization of medium Q0 possible in the process – “selecting” the highest Q layer

## Slide 3: Anodizing experiments
Eremeev et al, SRF’2005, TuAO8
Fine grain EP cavity
Ciovati et al, PRST AB 10, 062002 (2007)
Large grain BCP cavity

## Slide 4: HF rinse - principle
Nb
Nb2O5
Nb
Nb
Nb2O5
HF acid dissolves natural oxide layer
Water rinse grows new oxide layer
~2nm
~2nm
~5nm
RF layer
RF layer
RF layer
Each HF/water rinse step consumes about 2 nm of niobium from the top of the RF layer determining the surface resistance and moves deeper into the bulk – depth profiling of the losses

## Slide 5: HF rinse procedure
Filling with HF
5 minutes hold
HF dumping
DI water rinse

## Slide 6: Reproducibility

## Slide 7: Results on EP fine grain (tumbled)
Single HF rinse after mild baking significantly improves medium field Q0
Multiple HF rinse cycles do bring the high field Q-slope back
Onset field is still higher than before baking by ~25 mT after total 5 HF rinse cycles
  Further rinses in queue

## Slide 8: Results on EP fine grain cavity
Single HF rinse improves low and medium field Q0
Six HF rinses do bring the high field Q-slope back but with the higher onset (~125 mT vs 100 mT)

## Slide 9: Results on BCP fine grain cavity
Single and double HF rinse cycles significantly improve medium field Q0
High field Q-slope is present after mild baking

## Slide 10
30%
35%
11%
FNAL single cell data -> single HF rinse (5 min) followed by water rinse is beneficial for the medium field Q value – gains of up to 35% measured at 70 mT
Development of higher Q recipe for Project X
T=2K
T=2K
T=2K

## Slide 11
Nb
Baking modified - no HFQS losses
Literature – 120C enhances residual resistance; possibly due to suboxide formation
Single HF rinsing and regrowing oxide – restores residual resistance to pre-bake state while keeping the improvement in RBCS
Nb2O5
~5nm
~20nm
Bulk – susceptible to HFQS
losses
Nb
Baking modified - no HFQS losses
Nb2O5
After 120C
+HF rinse
+5 HF rinses
Nb2O5
Bulk – with HFQS
losses
Bulk – susceptible to HFQS
losses
Layer of high residual losses
Possible interpretation
B=B0exp(-z/l)
An estimate of the remaining thickness from the HFQS onset:
125 mT * exp (-h/l) = 100 mT => h~8nm

## Slide 12: Conclusion
HF profiling results are so far consistent with the layer of 10-20 nm being modified by mild baking
Practically - single HF rinse/DI water rinse after 120C mild baking appears to be a simple route to increase the medium field Q0 by 10-35% in fine grain cavities
  Important for Project X and other CW projects

## Slide 13: Acknowledgements
J. Ozelis – cavity testing
A. Rowe, D. Bice, T. Reid, R. Murphy – cavity processing