## Slide 1: A Brief Introduction to Superconducting Accelerator Magnets and R&D of SPPC High Field Magnets
Qingjin Xu
Institute of High Energy Physics,
Chinese Academy of Sciences
2016.8.1

## Slide 3: Outline
Basic Knowledge of the Superconducting Accelerator Magnets
PRINCIPLES of a Circular Collider
Design of Superconducting Accelerator Magnets
Superconducting Materials for Accelerator Magnets
R&D of SPPC High Field Magnets
Requirements of the SPPC High Field Magnets
Design Study of the SPPC Dipole Magnets
R&D Steps and Status

## Slide 4
Basic Knowledge of the
Superconducting Accelerator Magnets

## Slide 5: Acknowledgement
The materials of this section are based on USPAS (U.S. Particle Accelerator School) courses:
“Superconducting Accelerator Magnets” by Soren Prestemon (LBNL), Paolo Ferracin and Ezio Todesco (CERN), June 2015
“Superconducting Accelerator Magnets” by Paolo Ferracin (LBNL), Ezio Todesco (CERN), Soren O. Prestemon and Helene Felice (LBNL), January 2012
“Superconducting Accelerator Magnets” by Ramesh Gupta and Animesh Jain (BNL), January 2006
“Applied Electromagnetism: Magnet and RF-Cavity Design” by Mau Lopes and Jeremiah Holzbauer (FNAL), January 2016
Learn more at USPAS website: http://uspas.fnal.gov/materials/materials-table.shtml
and textbooks:
  Martin N. Wilson, "Superconducting Magnets", 1983.
  K.-H. Mess, P. Schmuser, S. Wolff, “Superconducting accelerator magnets”, Singapore: World Scientific, 1996.
  Fred M. Asner, "High Field Superconducting Magnets", 1999.

## Slide 6: PRINCIPLES of a Circular Collider
Colliders: two beams with opposite momentum collide
The arcs: region where the beam is bent
  Dipoles for bending
  Quadrupoles for focusing
  Correctors
Long straight sections (LSS)
  Interaction regions (IR)
    Quadrupoles for strong focusing in interaction point
    Dipoles for beam crossing in two-ring machines
  Regions for other services
    Beam injection (dipole kickers)
    Accelerating structure (RF cavities)
    Beam dump (dipole kickers)
    Beam cleaning (collimators)
A schematic view of a synchrotron
The lay-out of the LHC

## Slide 7: PRINCIPLES of a Circular Collider

## Slide 8: PRINCIPLES of a Circular Collider
Arc

## Slide 9
Design of Superconducting Accelerator Magnets

## Slide 10: Field Harmonics
From M. N. Wilson, pg. 28
An ideal cos
A practical winding with one layer and wedges
[from M. N. Wilson, pg. 33]
A practical winding with three layers and no wedges
[from M. N. Wilson, pg. 33]
Artist view of a cos magnet
[from Schmuser]
  Cos: a current density proportional to cos in an annulus - it can be approximated by sectors with uniform current density
Perfect Dipole
Biot-Savart law

## Slide 11: Field Harmonics
  Perfect quadrupole
  Cos2, a current density proportional to cos2 in an annulus- approximated by sectors with uniform current density and wedges
  (Two) intersecting ellipses
    Perfect sextupoles: cos3 or three intersecting ellipses
    Perfect 2n-poles: cosn or n intersecting ellipses
Quadrupole as an ideal cos2
Quadrupole as two intersecting ellipses

## Slide 12: Field Harmonics
Maxwell equations for magnetic field
In absence of charge and magnetized material
If (constant longitudinal field),
then
  and
James Clerk Maxwell,
Scottish
(13 June 1831 – 5 November 1879)
Gauss's law for magnetism
Ampère's circuital law
Cauchy-Riemann conditions

## Slide 13: Field Harmonics
A dipole
A quadrupole
[from P. Schmuser et al, pg. 50]
A sextupole
Each coefficient corresponds to a “pure” multipolar field
The field harmonics are rewritten as (EU notation)

## Slide 14: Field Harmonics
We recall the equations relative to a current line
we expand in a Taylor series
  the multipolar expansion is defined as
  the main component is
Biot-Savart law

## Slide 15: Field Harmonics
We compute the central field given by a sector dipole with uniform current density j
  Taking into account of current signs
  This simple computation is full of consequences
  B1  current density
  B1  coil width w
  B1 is independent of the aperture r
For a cos,

## Slide 16: Field Harmonics
A dipolar symmetry is
  Up-down symmetry (with same current sign)
  Left-right symmetry (with opposite sign)
Why this configuration?
  Opposite sign in left-right to avoid the field created by the left part is canceled by the right one
  In this way all multipoles except B2n+1 are canceled
  The field quality specifications concern only first 10-15 multipoles
    The field quality optimization of a coil lay-out concerns only a few quantities ! Usually b3 , b5 , b7 , and possibly b9 , b11

## Slide 17: Field Harmonics
Multipoles of a sector coil
  for n=2
  for n>2
Main features of these equations
  Multipoles n are proportional to sin ( n angle of the sector)
    They can be made equal to zero !
  Proportional to the inverse of sector distance to power n
    High order multipoles are not affected by parts far from the centre

## Slide 18: Field Harmonics
First allowed multipole B3 (sextupole)
  for =/3 (i.e. a 60° sector coil) one has B3=0
Second allowed multipole B5 (decapole)
  for =/5 (i.e. a 36°) or for =2/5 (i.e. a 72°) one has B5=0
  With one sector one cannot set to zero both multipoles … let us try with more sectors !

## Slide 19: Field Harmonics
Coil with two sectors
  Note: we have to work with non-normalized multipoles, which can be added together
Equations to set to zero B3 and B5
  There is a one-parameter family of solutions, for instance (48°,60°,72°) or (36°,44°,64°) are solutions

## Slide 20: Field Harmonics
Corrective actions: shaping the iron – the RHIC dipole
    The field in the yoke is larger on the pole
    Drilling holes in the right places, one can reduce saturation of b3 from 40 units to less than 5 units (one order of magnitude), and to correct also b5
Field map in the iron for the RHIC dipole, with and without holes
From R. Gupta, USPAS Houston 2006, Lecture V, slide 12
Correction of b3 variation due to saturation
for the RHIC dipoles, R. Gupta, ibidem

## Slide 21: Electro-magnetic Force
The e.m. forces in a dipole magnet tend to push the coil
- Towards the mid-plane in the vertical-azimuthal direction (Fy , F < 0)
- Outwards in the radial-horizontal direction (Fx , Fr > 0)
Tevatron dipole
HD2

## Slide 22: Electro-magnetic Force
LHC dipole at 0 T LHC dipole at 9 T
Usually, in a dipole or quadrupole magnet, the highest stresses are reached at the mid-plane, where all the azimuthal e.m. forces accumulate (over a small area).
Displacement scaling = 50

## Slide 23: Electro-magnetic Force
The e.m. forces in a quadrupole magnet tend to push the coil
Towards the mid-plane in the vertical-azimuthal direction (Fy, F < 0)
Outwards in the radial-horizontal direction (Fx, Fr > 0)
TQ
HQ

## Slide 24: Electro-magnetic Force
In the coil ends the Lorentz forces tend to push the coil Outwards in the longitudinal direction (Fz > 0)
Similarly as for the solenoid, the axial force produces an axial tension in the coil straight section.

## Slide 25: Electro-magnetic Force
Nb-Ti LHC MB (values per aperture)
  Fx = 340 t per meter
    ~300 compact cars
    Precision of coil positioning: 20-50 μm
  Fz = 27 t
    ~weight of the cold mass
Nb3Sn dipole (HD2)
  Fx = 500 t per meter
  Fz = 85 t
  These forces are applied to an object with a cross-section of 150x100 mm !!!
    and by the way, it is brittle

## Slide 26: Electro-magnetic Force
The e.m. forces in a solenoid tend to push the coil
  Outwards in the radial-direction (Fr > 0)
  Towards the mid plane in the vertical direction (Fy < 0)
Important difference between solenoids and dipole/quadrupole magnets
  In a dipole/quadrupole magnet the horizontal component pushes outwardly the coil
    The force must be transferred to a support structure
  In a solenoid the radial force produces a circumferential hoop stress in the winding
    The conductor, in principle, could support the forces with a reacting tension

## Slide 27: Quench Protection
Quench
Normal zone growth
Detection
Power supply switched off
Protection heaters
Extraction
Quenchback
Trigger protection options
The faster this chain happens the safer is the magnet
Current decay in the magnet
Magnetic energy
Converted to heat by Joule heating

## Slide 28: Quench Protection
In most accelerator magnets, the “natural” resistance growth is insufficient to provide a good protection => Need to enhance the resistance
Method 1:
  Add an external resistor
Method 2:
  Protection heaters mounted on the coils
    Optimized to minimize thermal diffusion time
Method 3:
  Use of couple secondary circuits
    Can be external or internal to the coil
    Quench back
Method 4:
  Coil subdivision
Cold

## Slide 29: Quench Protection
In the LHC main ring, the dipoles are connected in series. The principle is
  to “by-pass” the quenching magnet to avoid dumping all the string energy in one magnet
  To de-excite the rest of the magnets into a dump resistor
Combination of various methods: heaters, dump resistor, diodes

## Slide 30
Superconducting Materials for Accelerator Magnets

## Slide 31: Superconducting materials
Nb-Ti
Nb3Sn
Critical surfaces

## Slide 32: Superconducting materials
Typical operational conditions (0.85 mm diameter strand)
Cu
Nb3Sn
Nb-Ti
Je ~ 5 A/mm2
I ~ 3 A
B = 2 T
Je ~ 600-700 A/mm2
I ~ 300-400 A
B = 8-9 T
Je ~ 600-700 A/mm2
I ~ 300-400 A
B = 12-13 T

## Slide 33: Superconducting materials
The superconducting materials used in accelerator magnets are
  subdivided in filaments of small diameters
    to reduce magnetic instabilities called flux jumps
    to minimize field distortions due to superconductor magnetization
  twisted together
    to reduce interfilament coupling and AC losses
  embedded in a copper matrix
    to protect the superconductor after a quench
    to reduce magnetic instabilities called flux jumps
NbTi LHC wire (A. Devred, [1])
Nb3Sn bronze-process wire (A. Devred, [1])
NbTi SSC wire (A. Devred, [1])
Nb3Sn PIT process wire (A. Devred, [1])

## Slide 34: Superconducting materials
Flux jumps
  An external magnetic field penetrates in a type-II superconductor in the mixed state through fluxoids.
  If the superconductor is subjected to a thermal disturbance, the local change in Jc produces a motion or “jump” of fluxoids, which is accompanied by power dissipation.
  The stability criteria for a slab in the adiabatic condition
  where a is the half-thickness of the slab, jc is the critical current density [A m-2],  is the density [kg m-3], C is the specific heat [J kg-1], and c is the critical temperature.
  Nb-Ti filament diameters are usually less than 50 µm.
  High conductivity copper reduces instability.

## Slide 35: Superconducting materials
Superconductor magnetization
According to the critical state model, when a filament is in a varying external field, its inner part is shielded by a current distribution in the filament periphery.
The shielding currents are proportional to the amplitude of the applied field and do not decay when the external field is held constant.
  When the filament is fully penetrated, the magnetization M is proportional to Jcrf.
  Field distortions are proportional to rf. LHC filament diameter 6-7 µm; HERA filament diameter 14 µm.
K.-H. Mess, et al., [5], p. 84.

## Slide 36: Superconducting materials
Interfilament coupling
  When a multifilamentary wire is subjected to a time varying magnetic field, current loops are generated between filaments.
  If filaments are straight, large loops are generated, with large currents
    Big losses
  If the strands are magnetically coupled the effective filament size is larger
    Flux jumps
  To reduce these effects, filaments are twisted with a twist pitch of the order of 20-30 times of the wire diameter.
M.N. Wilson, [4], p. 148.

## Slide 37: Superconducting materials

## Slide 38: Superconducting materials
Quench protection
  Superconductors have a very high normal state resistivity. A filament of Nb-Ti, if quenched in free space, could reach very high temperatures in few ms.
  If the filament is embedded in a copper matrix, when a quench occurs, the current redistributes in the low-resistivity matrix and the peak temperature can typically be maintained below 300 K.
  The copper matrix facilitates quench protection: it allows the quench to propagate and it provides time to act on the power circuit.
  In the case of a small volume of superconductor heated beyond the critical temperature (for instance because of a flux jump), the current can flow in the copper for a short moment, allowing the filament to cool-down and recover superconductivity.
    The matrix also helps stabilizing the conductor against flux jumps (dynamic stability).
by L. Bottura

## Slide 39
R&D of SPPC High Field Magnets

## Slide 40: Requirements of the SPPC Magnets
Main dipoles
Field strength: 20 Tesla
Aperture diameter: 40~50 mm
Field quality: 10-4 at the 2/3 aperture radius
Outer diameter: 900 mm in a 1.5 m cryostat
Tunnel cross section: 6 m wide and 5.4 m high
6-m Tunnel for CEPC-SPPC. Left: SPPC collider. Right: CEPC collider (bottom) and Booster (top)
SPPC accelerator complex
The CEPC-SPPC ring sited in Qinhuangdao,
50 km and 100 km options .
Refer to CEPC-SPPC Pre-CDR, Mar. 2015: http://cepc.ihep.ac.cn/preCDR/volume.html
SPPC
50/100 km in circumference
C.M. energy 70 TeV or higher
Timeline
Pre-study: 2013-2020
R&D: 2020-2030
Eng. Design: 2030-2035
Construction: 2035-2042
Qinhuangdao

## Slide 41: Why 20-T Dipole Is Difficult ?
Dipole vs Solenoid
Different coil configurations
Limited coil width for dipole
Magnetic shielding
Cost
Martin Wilson
Solenoid
Lucio Rossi
LHC dipole
Dipole
Je – Current density
t – Coil thickness
Je – Current density
t – Coil thickness

## Slide 42: Performance of Superconductors
NbTi:
11 T @ 1.9K
Nb3Sn (Nb3Al)
17 T @ 4.2 K
500 A/mm2
WHOLE WIRE critical current density of main superconductors @ 4.2 K
Peter Lee

## Slide 43: R&D History of Nb3Sn Dipole Magnets
HTS
NbTi
Nb3Sn
(no bore)
(no bore)
20 T
IHEP
LBNL(RD3C)
(Two 35 mm bore)
Results achieved with Nb3Sn dipole technology test
16 T achieved with block type configuration (HD1 @ LBNL, 2003)
15 T achieved with common coil configuration (RD3 @ LBNL, 2001)
Results achieved with accelerator level field quality and bore
14 T achieved with block type configuration (HD2 @ LBNL, 2007)
13 T achieved with Cos-theta configuration (D20 @LBNL, 1997)
(LHC NbTi dipole 8.3 T)
(Single bore)
D.R. Dietderich, A. Godeke, Cryogenics 48, (2008)

## Slide 44: Challenges and R&D Focus of the 20-T Accelerator Magnets
Jc and cost of Superconductors: Based on the present Jc level, thousands of tons of Nb3Sn and HTS superconductors are needed to fabricate SPPC magnets. Significant increase of Jc and reduction of cost of superconductors are expected.
HTS coils for accelerator magnets, especially tape conductors: field quality (current distribution, magnetization effect,…), quench protection and fabrication method.
Magnetic force in superconducting coils at 20 T: F ̴ B2. And both Nb3Sn and HTS superconductors are strain sensitive! Needs innovative strain management for superconducting coils.

## Slide 45: Design Study of the SPPC Dipole Magnets
Chart: 
| 0 | 30 | 60 | 90 | 120 | 150 | 180 | 210 | 240 | 270 | 300 | 330 | 360 | 390 | 420 | 450 | 480 | 510 | 540 | 570 | 600 | 630 | 660 | 690 | 720 | 750 | 780 | 810 | 840 | 870 | 900 | 930 | 960 | 990 | 1020 | 1050 | 1080 | 1110 | 1140 | 1170 | 1200 | 1230 | 1260 | 1290 | 1320 | 1350 | 1380 | 1410 | 1440 | 1470 | 1500
b3 | -0.39506 | -0.16327 | -0.0029767 | 0.080907 | 0.18246 | 0.3156 | 0.439 | 0.5482 | 0.66092 | 0.78202 | 0.90267 | 1.0279 | 1.1648 | 1.3206 | 1.5091 | 1.7498 | 2.0946 | 2.6288 | 3.5771 | 5.2487 | 5.7841 | -5.7987 | -44.674 | -68.098 | -33.263 | 46.267 | 104.97 | 92.844 | -10.311 | -47.905 | -30.782 | -15.193 | -7.0212 | -3.3196 | -1.658 | -0.87994 | -0.49435 | -0.29205 | -0.18021 | -0.11545 | -0.076387 | -0.05198 | -0.036248 | -0.025827 | -0.018755 | -0.013853 | -0.01039 | -0.0078993 | -0.0060811 | -0.0047347 | -0.0037247
b5 | 0.65047 | 0.63445 | 0.61856 | 0.60411 | 0.58834 | 0.57153 | 0.55626 | 0.54083 | 0.52531 | 0.51043 | 0.49419 | 0.479 | 0.46378 | 0.44851 | 0.43298 | 0.41904 | 0.40531 | 0.38867 | 0.3786 | 0.36235 | 0.20873 | -0.53251 | -4.2528 | -4.9148 | 0.75387 | 9.2111 | 9.8532 | 10.795 | 2.2384 | 1.501 | 0.5939 | 0.16091 | 0.048947 | 0.016093 | 0.0056422 | 0.0021176 | 0.00085143 | 0.00036553 | 0.00016666 | 8.0217e-05 | 4.0525e-05 | 2.1376e-05 | 1.1719e-05 | 6.6496e-06 | 3.8919e-06 | 2.3424e-06 | 1.446e-06 | 9.1333e-07 | 5.8915e-07 | 3.8739e-07 | 2.5923e-07
b7 | -0.22665 | -0.23626 | -0.24758 | -0.259 | -0.27031 | -0.28164 | -0.2928 | -0.3039 | -0.31497 | -0.32618 | -0.33686 | -0.34786 | -0.35868 | -0.36961 | -0.38036 | -0.39051 | -0.40017 | -0.41225 | -0.42338 | -0.43247 | -0.44817 | -0.52327 | -1.2989 | -1.178 | -0.45591 | 0.65702 | -0.043029 | 0.29947 | -0.30842 | -0.062959 | -0.036257 | -0.0045847 | -0.00045843 | -6.5972e-05 | -1.4417e-05 | -3.924e-06 | -1.1927e-06 | -3.9146e-07 | -1.3723e-07 | -5.1049e-08 | -2.0095e-08 | -8.2992e-09 | -3.5846e-09 | -1.6598e-09 | -7.6064e-10 | -3.7496e-10 | -1.929e-10 | -9.8611e-11 | -7.1372e-11 | -1.3994e-11 | -4.2101e-11
a2 | -1.1192 | -1.0202 | -0.8741 | -0.77335 | -0.73424 | -0.75942 | -0.86529 | -1.0855 | -1.4598 | -2.0196 | -2.8128 | -3.9196 | -5.4435 | -7.5269 | -10.39 | -14.351 | -19.871 | -27.503 | -37.464 | -47.747 | -51.105 | -43.953 | -50.387 | -145.19 | -275.55 | -306.33 | -145.78 | 144.42 | 327.96 | 268.94 | 175.29 | 104.93 | 61.661 | 37.113 | 23.241 | 15.171 | 10.288 | 7.2145 | 5.2078 | 3.8542 | 2.9147 | 2.2458 | 1.7591 | 1.398 | 1.1253 | 0.9163 | 0.75382 | 0.62594 | 0.52416 | 0.44231 | 0.37589
a4 | -0.8716 | -0.90035 | -0.93672 | -0.97346 | -1.0108 | -1.0487 | -1.0869 | -1.1254 | -1.1637 | -1.2028 | -1.2414 | -1.2804 | -1.319 | -1.3578 | -1.3958 | -1.4314 | -1.4642 | -1.4952 | -1.5293 | -1.6163 | -1.8603 | -3.7839 | -11.221 | -24.239 | -33.011 | -25.068 | 0.16219 | 25.63 | 37.024 | 12.95 | 2.8588 | 0.061841 | -0.23637 | -0.14871 | -0.074522 | -0.036319 | -0.018131 | -0.0094114 | -0.0050941 | -0.0028701 | -0.0016778 | -0.0010142 | -0.00063167 | -0.00040417 | -0.00026495 | -0.00017751 | -0.0001213 | -8.4384e-05 | -5.9669e-05 | -4.2826e-05 | -3.1161e-05
a6 | 0.72944 | 0.7265 | 0.72279 | 0.71915 | 0.7153 | 0.71099 | 0.70752 | 0.70353 | 0.69948 | 0.69478 | 0.69118 | 0.68679 | 0.68241 | 0.67799 | 0.67377 | 0.66895 | 0.6641 | 0.66009 | 0.65533 | 0.64722 | 0.62069 | 0.40548 | -0.95309 | -3.0827 | -4.0809 | -2.769 | -0.86304 | -1.1226 | 0.21362 | -0.77316 | -0.22862 | -0.042185 | -0.0051362 | -0.00035434 | 6.6143e-05 | 5.039e-05 | 2.2979e-05 | 9.7271e-06 | 4.145e-06 | 1.8215e-06 | 8.3132e-07 | 3.9451e-07 | 1.9445e-07 | 9.9283e-08 | 5.239e-08 | 2.8495e-08 | 1.5916e-08 | 9.1718e-09 | 5.3922e-09 | 3.2638e-09 | 1.9977e-09
Integrated bn/an | Value (10-4)
b3 | 0.14
b5 | 1.42
b7 | -0.40
a2 | -0.29
a4 | -1.81
a6 | 0.03
Q. Xu, K. Zhang, C. Wang et. al., 20-T Dipole Magnet with Common Coil Configuration: Main Characteristics and Challenges, IEEE Trans. Appl. Supercond., VOL. 26, NO. 4, 2016，4000404
With common coil configuration
20-T dipole magnet with common coil configuration two Φ50 mm beam pipes; load line 80% @ 1.9 K
Q. Xu, K. Zhang, C. Wang et al.

## Slide 46: Design Study of the SPPC Dipole Magnets
Lorentz force per aperture:
Fmag_x=23.4 MN/m
Fmag_y=2.38 MN/m
Stress in coil after excitation
Stress in shell after excitation
K. Zhang et. al., 2-D Mechanical Design Study of a 20-T Two-in-One Common-Coil Dipole Magnet for High-Energy Accelerators, IEEE Trans. Appl. Supercond., VOL. 26, NO. 4, 2016, 4003705
D.R. Dietderich, A. Godeke / Cryogenics 48 (2008) 331–340
Direction of Magnetic force
K. Zhang, Q. Xu, C. Wang et al.
With common coil configuration

## Slide 47: Design Study of the SPPC Dipole Magnets
Cos-theta dipole
Highest efficiency, complicated ends with hard-way bending
Common coil dipole
Simplest structure with large bending radius, lower efficiency
Canted cos-theta dipole
Lowest stress level in coil, lowest efficiency
Efficiency, field quality, stress management, fabrication method…
Block type dipole
Simpler structure with hard-way bending, lower efficiency
Comparison of different coil configurations

## Slide 48: Design Study of the SPPC Dipole Magnets
Different coil configurations for 20-T dipole magnet
Left: Common coil
Right: Cos-theta
Common coil
Cos-theta
Coil ends
Common coil
Cos-theta
C. Wang et al.
Common coil vs Cos-theta
Comparison of different coil configurations

## Slide 49: R&D Steps and Status
a
b
c
1st step ongoing
Fabrication of 15-T Nb3Sn and Nb3Sn+HTS subscale magnets, to test the stress management method for Nb3Sn & HTS coils and the quench protection method for HTS coils;
By the end of 2018.
2nd step
Fabrication of 15-T Nb3Sn and Nb3Sn+HTS operational field dipole magnet with two Φ50 mm beam pipes and 10-4 field quality, to test the field optimization method for HTS coils;
To be funded.
3rd step
Fabrication of the 20-T magnet with Nb3Sn+HTS or only one of them, if we can get significant progress on the performance of Nb3Sn or HTS superconductors, i.e., their Jc level is 3~6 times increased or even more, and the cost is significantly reduced.
Q. Xu, K. Zhang, C. Wang et. al., 20-T Dipole Magnet with Common Coil Configuration: Main Characteristics and Challenges, IEEE Trans. Appl. Supercond., VOL. 26, NO. 4, 2016，4000404
Q. Xu, K. Zhang, C. Wang et al.
With common coil configuration

## Slide 50: R&D Steps and Status
Northwest Institute for Non-ferrous Metal Research (NIN, Xi’an) & Western Superconducting Tech. Co, Ltd (WST, Xi’an)
Qualified Nb3Sn supplier for ITER; R&D and production of High Jc Nb3Sn and Bi-2212 superconductors.
Shanghai JiaoTong U.& Shanghai Superconductor Tech. Co., Ltd (SSTC, Shanghai)
R&D and production of ReBCO superconductor.
Tsinghua U. & Innova Superconductor Tech. Co., Ltd (INNOST, Beijing)
R&D and production of Bi-2223 superconductor.
Institute of Plasma Physics, Chinese Academy of Sciences (IPP, Hefei)
Test stand with 12-T background field, Nb3Sn CICC cable fabrication;…
High Magnetic Field Laboratory, Chinese Academy of Sciences (CHMFL, Hefei)
Development of High field solenoids;…
Institute of High Energy Physics, Chinese Academy of Sciences (IHEP, Beijing)
30+ years R&D and production of conventional accelerator magnets, plus 10+ years R&D and production of superconducting magnets for particle detectors and industries.
and USTC, IMP, CIAE…
Welcome new members to join us!
20-T Magnet Working Group in China

## Slide 51: R&D Steps and Status
Super High Jc Nb3Sn
Over-pressure HTS Bi-2212
HTS YBCO Jc estimation
Magnet field Vs. Conductor Jc
Principle: increase of Nb3Sn pinning force at high field through grain refinement: Jc(12 T, 4.2K) from 3.5 kA/mm2 @ 100+ nm to 9.6 kA/mm2 @ 35 nm !
X. Xu et al, Appl. Phys. Lett. 104 082602 & ASC14
D. C. Larbalestier et al, NATURE MATERIALS DOI: 10.1038/NMAT3887, 2014
D.R. Dietderich, A. Godeke, Cryogenics
48 (2008) 331–340
R&D of advanced superconductors: Nb3Sn & HTS
HTS YBCO cost estimation
And, other materials
like …
Iron-based superconductor?

## Slide 52
Nb3Sn Bpeak
14.5T @4.2K
Main parameters of the cables
Main parameters of the strands
For per meter of such magnet, the required length of the strand: YBCO: 0.6 Km; Nb3Sn in total: 9.12 Km
Coil configuration in the 1st quadrant
Field distribution in the cross section of the magnet
Strand | diam. | cu/sc | RRR | Tref | Bref | Jc@ BrTr | dJc/dB
IHEPWCJC | 0.82 | 1 | 100 | 4.2 | 12 | 2400 | 400
IHEPWYBCO | - | - | - | 4.2 | 12 | 1020 | 40
I=358A (YBCO)
I=9930A(Nb3Sn)
Main field: 14.6T
YBCO Bpeak
14.7T @4.2K
Cable | Hight | Width-i | Width-o | Ns | Strand | Filament | Insulation
IHEPW1 | 5.8 | 1.5 | 1.5 | 14 | IHEPWCJC | Nb3Sn | 0.15
IHEPW3 | 12 | 1.5 | 1.5 | 29 | IHEPWCJC | Nb3Sn | 0.15
IHEPWYBCO4 | 4 | 0.2 | 0.2 | 1 | IHEPWYBCO | YBCO | 0
Iron yoke OD:
600mm
Clear bore diameter 15mm Inter-aperture spacing 156 mm
To fabricate a 14-T dipole magnet (with two apertures) with HTS and Nb3Sn superconductors, to test the field optimization method of HTS & Nb3Sn coils.
R&D Steps and Status (2016-2018)

## Slide 53: R&D Steps and Status
Superconducting Rutherford Cable fabricated by Toly Electric with WST ITER type Nb3Sn strand
With Nb3Sn conductors (ongoing), and with HTS conductors (to be done)
Collaboration with WST, Toly Electric, and Changtong Electric
Superconducting Rutherford Cable fabricated by Changtong Electric with WST ITER type Nb3Sn strand

## Slide 54: R&D Steps and Status
Pitch length | Filling factor (%) | Ic degradation(%) | Average Ic degradation(%) | Comments
60 | 90.6 | 9.39~16.04 | 12.48~12.67 | Not acceptable
45 | 90.7 | 3.84~10.33 | 6.31~7.42 | Almost acceptable
52 | 87.4 | 3.18~10.39 | 6.51~6.76 | 
52 | 83.7 | 0.33~6.2 | 3.13~3.60 | Acceptable
Y. Zhu (WST) et al.
With Nb3Sn conductors (ongoing), and with HTS conductors (to be done)
Collaboration with WST, Toly Electric, and Changtong Electric

## Slide 55: Summary
SPPC needs thousands of 20-T level magnets to bend and focus the high energy proton beams .
To achieve the challenging 20-T accelerator magnets, a 10~15 years long term R&D is necessary.
A working group is being organized for the 20-T magnet R&D in China, and expecting international collaboration with worldwide labs.
R&D of advanced superconductors and magnets for SPPC are ongoing. Welcome more collaborators to join us!

## Slide 56
Thanks