## Slide 1
BINP
Workshop on High Energy Circular Electron Positron Collider, November 6-8, IHEP, Beijing
Cryogenic temperature for SPPC
Alexander Krasnov
Budker Institute of Nuclear Physics (BINP), Novosibirsk, Russia
E-mail address: a.a.krasnov@inp.nsk.su

## Slide 2
BINP
Contents
Vacuum requirements
Role of surface and radiation
Cold beam pipe. Hydrogen accumulation. PSD
Equations for residual dynamic gas density prediction
CB and BS temperatures
FCC BS new proposal
NEG coating
Solution with NEG application
Activation, surface impedance
Summery

## Slide 3
BINP
Vacuum requirements
LHC arc vacuum upper limit:
  Life time limit due to nuclear scattering ~ 100 h
  n ~ 109 H2/cm3
  ~ 80 mW/m heat load in the cold mass due to proton scattering (two beams!)
  - What is the heat load limit for the 12T (24T) HTS magnets???
Gas | Total cross-section [mb] | Deansity [cm-3] for 100h
H2 | 100 | 1·109
He | 126 | 8·108
CH4 | 540 | 1.9·108
H2O | 540 | 1.9·108
CO | 780 | 1.3·108
CO2 | 1220 | 0.8·108

## Slide 4
BINP
Surface
Metallic surface contains 10 ÷ 100 ML (1 ML ≈ 1015 cm-2 ) of
Chemically bound: MxOy, Mx(OH)y, Mx(HOC3)y, carbon clusters
Physically adsorbed: H2O, organics
Example: Surface of a tube with D=5 cm contains on 107 ÷ 108 times more molecules than ones inside the tube in gas phase at density 109 cm-3 !
Radiation can provoke dissociation of the molecules which causes desorption of:
H2 - most critical for cryogenic beam pipe because H2 can re-desorb on surface with very low binding energy
CO, CO2
Saturated hydrocarbons CxHy (due to catalytic reactions on surface)

## Slide 5
BINP
Dynamic density of hydrogen in cold pipe in presence of SR
Experiments at BINP (25 years ago!) in collaboration with SSC (20 TeV per beam) and CERN vacuum groups
100 h
LHC SR spectra

## Slide 6
BINP
PSD
Experiments with BS prototype at BINP
(JVSTA-A14-4-1996-p2618)
BS temperature 77K, Ec=45 eV

## Slide 7
BINP
Phenomena in cold beam pipe
CB T=1.9K
ID=50mm
Screens against e-
p+
Slots
Cooling tubes
BS T=5 ÷ 20K
OD=49mm
Saw tooth!
γ
γd
e-
e-ph
e-
γd
Molecular physisorption
onto cryogenic surfaces
(weak binding energy)
Cross-section of arc LHC beam pipe in dipoles
Electron Cloud
- fluxes of photons, electrons and ions correspondingly
- primary desorption yields at irradiation by photons, electrons and ions correspondingly
- secondary desorption yield (re-cycling)
- Sticking probability
7
-Equilibrium density
re-cycling
ai - surface density of phisisorbed molecules
l – perimeter of the beam pipe cross-section

## Slide 8
BINP
Increasing temperature of CB
Tmax=3.3K
n=1E9 1/cm3

## Slide 9
BINP
Cryosorber connected to BS in LHC LSS (Tcb=4.5K)
Possible solution for SPPC: connect a cryosorber to CB!
But how?
During Superconducting Magnet assembly?

## Slide 10
BINP
BS temperature
What about CO, CO2 and CH4 ?
Variation of BS temperature should not provoke a pressure rise!
M. Angelucci, R. Cimino, WP4 EuroCircol meeting, Geneva, 9th October 2017

## Slide 11
BINP
SPPC cold beam pipe
Current approach
The practically same solution under consideration at CERN.
Disadvantages:
Very complex
Needs large space for cooling and SR absorption

## Slide 13
BINP
BS new proposal
WP4 EuroCircol meeting, Geneva, 9th October 2017
simplified design from production point of view
does not need precise beam tuning

## Slide 14
BINP
Investigation of TiZrV.
During activation part of molecules evaporate but most part solve (diffuse) in bulk of the material. Rest number of impurities on surface is less than one monolayer.
Effect of activation. Photon flax 4Е16 ph/m/s

## Slide 15
0
-L/2
L/2
Pend
Pc
CO
CO
Pend
=0, s=sm
Experiment with saturated NEG
BINP
L=150 cm, d=2.5 cm
SR stimulates diffusion of molecules into NEG film!
– prolongation of lifetime!
- No re-cycling!

## Slide 16
BINP
NEG at low temperature
H2 sticking probability versus temperature
H2 dynamic pressure rise at presence of SR flux 4·1016 ph/s versus temperature

## Slide 17
BINP
SPPC arc beam pipe
Main idea: separation beam pipe from CB of the magnet
Mandatory:
NEG coating for pumping and EC mitigation (activated NEG has low (?) SEY)
Heater and thermo-insulation (needs less than 1mm gap) between beam pipe and CB (to do NEG activation at 220 C)
Cooling: LN2 (undercooled, 10 atmosphere(?))
Main advantages: no connections between He vessels/pipes and beam vacuum!
Cooling tubes
Insulating vacuum

## Slide 18
BINP
NEG activation inside CB
(CB at RT)
Simple experiment
Tube OD40. Thermo-insulation 1mm thickness
(6 layers of Kopton and aluminum foil).
Temperature inside 220C reached at P=250 W/m
There are materials with thermal conductivity less than 0,005 W/K/m
P<150 W/m

## Slide 19
BINP
NEG surface impedance
Example:
Roughly, NEG specific electrical conductivity 1E-6 Ohm*m
Skin depth at 10 GHz is
It means that 1 micrometer NEG film will not influence on surface impedance at frequencies up to 30 GHz (1cm wavelength)

## Slide 20
BINP
Summery
There are two solutions
LHC style
An absorber has to be connected to CB if its temperature > 3,3K
Possible He leak into Beam Vacuum because many weld connections in He system
A coating or laser treatment is needed to suppress EC (or long conditioning)
A conditioning is necessary due to PSD, ESD and recycling
Insulated Beam Vacuum
CB temperature does not matter
The use maximum horizontal aperture!
- There are No direct connection between He cooling system
NEG coating and its activation is needed to get pumping and EC suppress (needs less than 1mm gap between beam pipe and CB to do NEG activation at 220 C)
A conditioning is NOT necessary
Must be thin to avid influence on HF impedance
Laboratory experiments are necessary to check vacuum and emission properties of beam pipe prototypes

## Slide 21: Thanks for your attention

## Slide 22
BINP
SPPC cold beam pipe
Possible solutions
Mandatory:
Coating for EC mitigation (may be strip-like to keep impedance)
Short bending magnets ( 5 – 7 meters – very preliminary estimation)
SR water cooled absorbers
placed between magnets
A – absorber for hydrogen
BS
A

## Slide 23
BINP
Summery
Vacuum tightness!
Mechanical stability against external pressure or quenching
Low SEY & PEY: Electron Clouds (EC) problems – beam instability
Impedance: LF - resistive instability (LHC, SPPC/FCC), HF: TMI (anti- EC coatings, roughness)
Power absorption: SR, EC, Image Current

## Slide 24
BINP
Surface conditioning (SEY must be less 1.3 for LHC arcs)
SEY measurements at CERN for copper samples:
Pure copper: δ = 1.35

## Slide 25
BINP
Relation between SEY and ESD during conditioning!
B.Henrist, N.Hilleret, C.Scheuerlein, M.Taborelli, G.Vorlaufer. The variation of the secondary electron yield and of the desorption yield of copper under electron bombardment: origin and impact on the conditioning of the LHC. Proceedings of EPAC 2002, pp. 2553-2555, Paris, France.

## Slide 26
BINP
Equations for residual dynamic gas density prediction
Most popular NEG composition is TiZrV – low activation temperature 180 °C
Advantages: low and low SEY, high pumping speed
Disadvantages: Needs baking, low sorption capacity (lifetime ?)
Limited by ui
100 l/s
10000 l/s
re-cycling
NEG coating!
z
Sp-1
Sp
Sp+1
zp-1
zp
zp+1
Sorption capacity 1 ML. Lifetime ?

## Slide 27
BINP
Important solutions made for LHC arc beam pipe
0.02÷0.03
0.5
SR
Slots
Decreasing number of diffusely scattered photons
decreasing number of photo-electrons (3 ÷ 5 times!) and increasing of conditioning effectiveness
Open question: conditioning is slow in compare with laboratory experiments (10 times at least!)
Beam screen: screening of CB against SR and EC, power absorption
Copper co-lamination: high electrical conductivity at cryogenic temperature
Saw tooth!