## Slide 1: Discussion on the LF 110 nm CMOS CIS process
Ying ZHANG
2019-11-25

## Slide 2: Process features (1)
LFoundry 110 nm CMOS CIS technology (quad-well, both PMOS and NMOS), high-resistivity bulk
Custom patterned backside, process developed in collaboration with LFoundry
  No info about the standard process, i.e. available sensor geometry/thickness
Pixel size 25 μm x 25 μm process, back-side pattern and geometry validated in silicon (both MATISSE and pseudo-matrices, electrical, laser, radioactive source and microbeam)
  Investigated sensors with thicknesses of 100 µm, 200 µm, 300 µm.
  How about a 50 µm thick sensor: possible sensing diode size? Depletion voltage? SNR? Charge sharing…

## Slide 3: Process features (2)
Pixel capacitance ~20 fF
  Capacitance vs. sensing diode size? Same case in a 50 µm thick sensor than in 100/200/300 µm thick sensors?
  Capacitance seems 5-7 larger than in the TowerJazz process, the higher Q/C the better in our application (for low power design)
In-pixel electronics located in the deep-pwell
  smallest pixel size (sensing diode + Front-end + digital logic)? 25 µm achievable?
  In-pixel electronics occupies 576 µm2 in 180 nm process

## Slide 4: Summary of our concerns
Are the developed sensor designs by INFN applicable to the CEPC vertex ?
  “no sensor engineering or TCAD design would be foreseen” as stated by Manuel
  Sensor thickness should be less than 50 µm in our case. Compatibility with INFN’s project?
Possibility of a full chip design migration from TJ180 to LF11?
  High back-side voltage required for the sensor in LF case, while not in TJ case
  In-pixel analog circuit needed to be redesign, due to the different sensor capacitance (more than 5 times larger), power supply (1.5 times lower)
  Whether the migration of in-pixel digital logic is possible may depend on the pixel area?
  Others: number of metal, available (MIM) capacitor, etc.
Own access to the LF 110 nm process for IHEP (in future)? Submission possibility?
  To allow more designer to easily involve for a long-term collaboration. Limitations on IHEP visiting scientist and/or joint PhD student. Submission from IHEP side possible? MPW/ENR

## Slide 5: References
M. Darocharolo, CEPC Workshop IHEP, 2019

## Slide 6: References
A. Rivetti, TREDI 2019

## Slide 7: References
A. Rivetti, TREDI 2019
MATISSE