## Slide 1
μSR study on a doped magnetic
Weyl semimetal Co3-xNixSn2S2
Huiqian Luo (罗会仟)
Institute of Physics, CAS
2019.12.13 Hefei
第二届CSNS缪子源多学科应用研讨会

## Slide 2
Science 345, 657(2014)
http://sc8.iphy.ac.cn/
2009-2019
中国科学院物理所 SC8 组
Neutron scattering on correlated electron materials
翠竹
Bamboo

## Slide 3
IOP，CAS: Chang Liu, Xiaoyan Ma, Jianlei Shen,
Enke Liu, Hongming Weng, Youguo Shi
Instrument Scientists :
Pabitra Biswas、D.T. Adroja (ISIS, RAL, UK)
Collaborators
MUSR

## Slide 4
Background: Hall effect
H. Weng et al., Adv. Phys. 64, 227 (2015)

## Slide 5
Quantum anomalous Hall effect
Science 329, 61 (2010), Science 340, 167 (2013)
Cr doped (Bi,Sb)2Te3

## Slide 6
Anomalous Hall effect
E. Liu et al., Nature Phys. 14, 1125 (2018)
anomalous Hall angle (AHA)
vs. anomalous Hall conductivity (AHC)
Extrinsic mechanism: skew scattering side jump mechanisms
Intrinsic Kaplus–Luttinger mechanism
Q. Wang et al., Nature Commun. 9, 3681 (2018)

## Slide 7
Magnetism and AHE
S. Itoh et al., Nat. Commun. 7, 11788 (2016)

## Slide 8
From Tl to magnetic WSM

## Slide 9
Co3Sn2S2
E. Liu et al., Nature Phys. 14, 1125 (2018)
Ferromagnetic half metal
Layered structure
Ordered moment 0.3 μB/Co
M// c on Co kagome lattice
Strong magnetic anisotropy
B//c ~0.1 T
B//ab ~26 T

## Slide 10
Band structure and Weyl nodes
E. Liu et al., Nature Phys. 14, 1125 (2018)
Only spin up cross EF
Weyl points are 60 meV above EF
6 pairs of Weyl ferminon
Strong Berry curvature

## Slide 11
ARPES and STM results
Q. Wang et al., Nature Commun. 9, 3681 (2018), N. Morali et al., ArXiv: 1903.00509, J.-X Yin et al., Nature Phys. 15,443 (2019)
Fermi arc on
surface state
Negative
magnetism

## Slide 12
ARPES and STM results
Science 365, 1282 (2019). Science 365, 1286 (2019).

## Slide 13
Anomalous Hall effect
E. Liu et al., Nature Phys. 14, 1125 (2018)

## Slide 14
Elastic neutron scattering on single crystal
1.5 g
Liu, Shen, Gao et al., unpublished manuscript

## Slide 15
What can μSR do in this material ?
arXiv: 1904.09353

## Slide 16
What can μSR do in this material ?
arXiv: 1904.09353

## Slide 17
What can μSR do in this material ?
arXiv: 1904.09353
In-plane antiferromagnetic order ?

## Slide 18
Doping effect on magnetism
PhD. Dissertation of Dr. M. A. Kassem, Kyoto University (2017).

## Slide 19
Doping effect on magnetism
J. Cryst. Growth. 426, 208 (2015). J. Solid State Chem. 233, 8 (2016).
Physica B 378, 1142 (2006). Physica Status Solidi 10, 1130(2013).

## Slide 20
Doping effect on Co3-xNixSn2S2
Liu, Shen, et al., unpublished manuscript

## Slide 21
Conclusion
Co3-xNixSn2S2 MWSM
3D ferromagnetic interactions with strong SOC;
Complex magnetic structure between Tc and TA ;
Doping suppress ferromagnetism and affect on AHE;
AF order vanishes above x=0.7 (possible FM QCP ?);

## Slide 22
Thanks
http://sc8.iphy.ac.cn/
hqluo@iphy.ac.cn