## Slide 1
Michael Smidman
Center for Correlated Matter and Department of Physics
Zhejiang University, China
Time reversal symmetry breaking in fully-gapped superconductors

## Slide 2
Acknowledgements
Zhejiang University
Z. F. Weng
J. Chen
G. M. Pang
J. L. Zhang
T. Shang
L. Jiao
W. B. Jiang
Y. Chen
L. Yang
F. Steglich
H. Q. Yuan
Theory
S. K. Ghosh
J. Quintanilla
(U. Kent, UK)
J. F. Annett
(U. Bristol, UK)
M. Nicklas
(MPI-Dresden)
T. Shang
J. Verezhak
T. Shiroka
(PSI Facility)
D. Hillier
D. T. Adroja
(ISIS Facility)
G. Balakrishnan
D. M. Paul
(Warwick)
R. P. Singh
(IISER-Bhopal)

## Slide 3
Broken symmetry in unconventional superconductors
In the superconducting state, U(1) gauge symmetry is broken
below Tc
In unconventional superconductors additional symmetries are often broken, e.g.
Rotational symmetry
Time reversal symmetry

## Slide 4
Detecting TRS breaking: μSR
Static Gaussian field distribution P(B) of width σ/γμ
ZF-spectra analyzed considering Lorentzian and Gaussian relaxation

## Slide 5
TRS breaking: ‘Classic examples’
UPt3
Luke et al. PRL 71, 1466 (1993)
U1-xThxBe13
Heffner et al. PRL 65, 2816 (1990)

## Slide 6
Sr2RuO4
Luke et al. Nature 394, 558-561 (1999)
TRS breaking: ‘Classic examples’

## Slide 7
Sr2RuO4
Xia et al. PRL 97, 167006 (2006)
TRS breaking: ‘Classic examples’
UPt3
E. R. Schemm et al. Science 345, 6193 (2014)
Evidence for TRS breaking in Sr2RuO4 and UPt3 from both μSR and Kerr effect
Strongly correlated magnetic systems: unconventional SC anticipated

## Slide 8
Nodal triplet superconductivity: Sr2RuO4 and UPt3
Sr2RuO4
K. Ishida et al. Nature 396, 658 (1998)
UPt3
H. Tou et al. PRL 80, 3129 (1998)
Knight shift measurements indicate triplet pairing

## Slide 9
Or do they?
Sr2RuO4
A. Pustogow et al. Nature 574, 72–75(2019)

## Slide 10
Nodal superconductivity: Sr2RuO4 and UPt3
Bonalde et al. PRL 85, 4775 (2000)
Sr2RuO4: Penetration depth: ~T2.
UPt3: T3 dependence of 1/T1.
Kohori et al. JPSJ 57, 395 (1988)
Evidence for nodal superconductivity

## Slide 11
TRS breaking and triplet superconductivity
Triplet order parameter:
Unitary:
Sr2RuO4: chiral p-wave (Eu)
UPt3: E2u state
N.B. Singlet E1g also break TRS (see also s+id)
Non-zero orbital moment L = +/-1
Not all unitary triplet states break TRS!
e.g Balian – Werthamer phase
c.f. B-phase of 3He
AIP Conf. Proc. 789, 165 (2005)
R. Balian and N. R. Werthamer Phys. Rev. 131, 1553 (1963)

## Slide 12
TRS breaking and triplet superconductivity
Triplet order parameter:
Non-unitary:
E.g. A1 phase of 3He
AIP Conf. Proc. 789, 165 (2005)

## Slide 13
TRS breaking with fully open gaps
Re6Zr
Singh et al. PRL 112, 107002 (2014)
ZF-μSR
TF-μSR
ZF-μSR
TF-μSR
La7Ir3
Barker et al. PRL 115, 267001 (2015)
Lu5Rh6Sn18
Bhattacharyya et al. PRB. 91, 060503(R) (2015)
Non-centrosymmetric
Non-centrosymmetric
Centrosymmetric

## Slide 14
Two nodeless gaps in LaNiC2 and LaNiGa2 – triplet pairing with even parity

## Slide 15
The case of LaNiC2 and LaNiGa2
LaNiC2
Orthorhombic noncentrosymmetric
LaNiGa2
Orthorhombic centrosymmetric

## Slide 16
TRS breaking in LaNiC2 and LaNiGa2
Zero field μSR indicates that TRS is broken in both LaNiC2 and LaNiGa2
LaNiC2
Hillier et al. PRL 102, 117007 (2009)
LaNiGa2
Hillier et al. PRL 109, 097001 (2012)

## Slide 17
Penetration depth and superfluid density
J. Chen et al. New J. Phys. 15, 053005 (2013)
Z. F. Weng et al. Phys. Rev. Lett. 117, 027001 (2016)
TRS breaking and nodeless, two gap superconductivity are common features of LaNiC2 and LaNiGa2

## Slide 18
TRS breaking in LaNiGa2 and LaNiC2
TRS breaking spin-singlet or unitary triplet pairing
All the irreps of Gc are one dimensional and the TRS breaking states are all non-unitary triplet
[PRL 102, 117007 (2009), PRL 109, 097001 (2012)]
Symmetry analysis of the point group:
All the odd parity, triplet TRS breaking states have nodes
2. Odd parity, non-unitary spin triplet states.

## Slide 19
TRS breaking in LaNiGa2 and LaNiC2
Cf. Unitary chiral p-wave state in Sr2RuO4 – point group D4h
AIP Conf. Proc. 789, 165 (2005)
Two dimensional Eu representation:
TRS breaking chiral p-wave state: (a1,a2) = (1,i)

## Slide 20
TRS breaking in LaNiGa2 and LaNiC2
3. Multiband superconductivity with a non-trivial phase difference, e.g. s+id, d+id
Two-bands
Multidimensional order parameter required to break TRS
Need a 2D or higher dimensional irrep
Orthorhombic structures of LaNiC2 and LaNiGa2:
Gc only has 1D irreps
SC state must correspond to 3D triplet irrep of SO(3)

## Slide 21
TRS breaking in LaNiGa2 and LaNiC2
4. Singlet-triplet mixing due to ASOC
For LaNiC2 with significant ASOC:"double group"
Irreps of the "double group" have the same dimensions as irreps of Gc - all are 1D
TRS breaking at Tc implies that the effect of ASOC in LaNiC2 is very weak - negligible singlet-triplet mixing.
LaNiGa2 is centrosymmetric - singlet-triplet mixing is forbidden
Quintanilla et al. PRB 82, 174511 (2010)

## Slide 22
Reconciling TRS breaking and two fully open gaps in LaNiC2 and LaNiGa2
Conventional multiband superconductivity
Z. F. Weng et al. Phys. Rev. Lett. 117, 027001 (2016)
Non-unitary triplet with even parity
Same spin pairing between orbitals: Two fully open gaps
Orbital: antisymmetric
Spin: symmetric
Parity: even

## Slide 23
What about when there are higher symmetries?

## Slide 24
Re-based noncentrosymmetric superconductors
Cubic Re-based NCS (α-Mn structure):
TRSB + Singlet-triplet mixing not forbidden
Singh et al. PRL 112, 107002 (2014)
Re6Zr
T. Shang et al. PRB 97 020502 (2018)
Re24Ti

## Slide 25
Re-based noncentrosymmetric superconductors
Re6Zr: Superfluid density consistent with single-gap s-wave superconductivity.
G. M. Pang et al. PRB 97, 224506 (2018)

## Slide 26
TRS breaking with conventional pairing?
S. K. Ghosh et al. arXiv:1803.02618
More than two atoms per cell related by certain symmetries
Onsite conventional electron-phonon pairing interaction
Change of phase of pairing wavefunction in real space
Circulating loop currents => broken TRS

## Slide 27
Importance of Re element?
Nb0.18Re0.82 (α-Mn structure) and Re element:
Broken TRS below Tc
Re is centrosymmetric and loop current cannot explain TRS breaking
Local electronic structure of Re important?
T. Shang et al., PRL. 121, 257002 (2018)

## Slide 28
T. Shang et al., PRL, 121, 257002 (2018)
Correlation with nuclear moments?

## Slide 29
Summary
Growing number of materials show evidence for broken TRS with a fully open gap
Open questions:
What is the origin of the TRS breaking?
What is the nature of the pairing state?
Are the pairing states/mechanism conventional?
Low symmetry of LaNiC2/LaNiGa2 means that broken TRS at Tc implies non-unitary triplet pairing => even-parity triplet state
Other systems have more possibilities, e.g. cubic Re-based NCS, can these be explained by a conventional pairing mechanism?

## Slide 31
LaNiC2: Specific heat and upper critical field
Specific heat and Bc2(T) also indicate two-gap superconductivity
J. Chen et al. New J. Phys. 15, 053005 (2013)

## Slide 32
LaNiGa2: Specific heat and upper critical field
Specific heat and Bc2(T) further support two-gaps
 | Δ1 | Δ2 | x
LaNiC2 | 1.2kBTc | 2.0kBTc | 0.3
LaNiGa2 | 1.29kBTc | 2.04kBTc | 0.43

## Slide 33
Prediction of spontaneous magnetization below Tc
Some evidence for this in measurements of LaNiC2 single crystals but no reports yet of LaNiGa2 single crystals
Further evidence for unconventional superconductivity

## Slide 34
Fermi surface of LaNiGa2
D. Singh PRB 86, 174507 (2012)

## Slide 35
Mean field theory
Two mean fields:
Z. F. Weng et al. Phys. Rev. Lett. 117, 027001 (2016)

## Slide 36
GL theory for paramagnetic non-unitary triplet
Condition for non-unitary triplet:
Hillier et al. PRL 109, 097001 (2012)

## Slide 37
T. Shang et al., PRL, 121, 257002 (2018)

## Slide 38
Penetration depth
Specific heat
I. Bonalde et al. PRL 85.4775 (2000)
K. Deguchi et al. PRL 92.047002 (2004)
Penetration depth: ~T2.
Evidence for nodal SC in Sr2RuO4.
Classic examples of SC with broken TRS: Sr2RuO4
Specific heat: Ce/T~T.

## Slide 39
NMR
Specific heat
Y. Kohori et al. JPSJ.57.395 (1988)
S. Kittaka et al. JPSJ.82.024707 (2013)
T3 dependence of 1/T1.
H1/2 field dependent specific heat at low temperatures.
 Evidence for line nodes in UPt3.
Classic examples of SC with broken TRS: UPt3

## Slide 40
Singh, Phys. Rev. B 96, 180501 (2017)
Re6Hf
Re24Ti5
Shang, Phys. Rev. B 97, 020502 (2018)
Asymmetry
Mg10Ir19B16
Aczel, PRB, 82, 024520(2010)
Nb0.5Os0.5
Singh, JPCM, 30 075601 (2018)
Onset of spontaneous magnetic field at Tc in Re24T5.
TRS is preserved in some isostructural compounds!
Local electronic structure is crucial for TRS breaking.
Re6Zr
Singh, PRL 112, 107002 (2014)
Re24T5 (T=Zr, Ti, Nb, Hf…) :
A family of TRS breaking Non-centrosymmetric SCs