## Slide 1: CEPC HTS plan and Radiation thickness calculation
Ning Feipeng
2020-06-03

## Slide 2: CEPC HTS plan
HTS SOLENOID FOR IDEA Detector
  Based on the LTS plan of IDEA detector.
Property | Value
Magnetic field in center (T) | 2
Free bore diameter (m) | 4
Cold mass inner radius (m) | 2.2
Cold mass length (m) | 6

## Slide 3: CEPC HTS plan
Cable development
LTS
HTS
Rutherford Cable
NbTi wire
Al Stabilized Rutherford Cable
ReBCO tape
ReBCO Stack Cable
Al Stabilized ReBCO Stacked Tape Cable
It is developing

## Slide 4: CEPC HTS plan
Coil winding
LTS
HTS
vertical configuration
horizontal configuration

## Slide 5: Radiation thickness calculation
IDEA LTS part
Ultra-light 2T/4m bore Detector Solenoid for FCCee-the Solenoid in the IDEA detector -Herman ten Kate, FCC Annual meeting Amsterdam, April 9-14, 2018
IDEA: a detector concept for CepC, F. Bedeschi, INFN-Pisa,CEPC CDR International Review, Beijing, September, 2018

## Slide 6: Radiation thickness calculation
IDEA LTS version
  How to calculate the radiation thickness?
1
2
Trajectory
2:
Trajectory
1:
Material | Thickness | Radiation thickness |  | Nuclear Interaction length | 
 | X, mm | X0, mm | X/X0 | λ0, mm | λ=X/λ0
NbTi | 0.675 | 15.028 | 0.0449 | 204.5 | 0.0033
Cu | 0.675 | 14.36 | 0.0470 | 153.2 | 0.0044
Stabilizer,Al | 30 | 88.9 | 0.3375 | 397 | 0.0756
Glass/epoxy | 5 | 286 | 0.0175 |  | 
Total, Xtot |  |  | 0.4469 |  | 0.083
Material | Thickness | Radiation thickness |  | Nuclear Interaction length | 
 | X, mm | X0, mm | X/X0 | λ0, mm | λ=X/λ0
NbTi | 10 | 15.028 | 0.6654 | 204.5 | 0.0489
Cu | 10 | 14.36 | 0.6964 | 153.2 | 0.0653
Stabilizer,Al | 10 | 88.9 | 0.1125 | 397 | 0.0252
Glass/epoxy | 5 | 286 | 0.0175 |  | 
Total, Xtot |  |  | 1.4918 |  | 0.1394
Cryostat (25 mm Al): X0= 0.28, λ= 0.07
Total | X0 | λ
Track 2 | 0.73 | 0.153
Track 1 | 1.77 | 0.21

## Slide 7: Radiation thickness calculation
IDEA HTS version
  35 layers HTS tape
1
Material | Thickness | Radiation thickness |  | Nuclear Interaction length | 
 | X, mm | X0, mm | X/X0 | λ0, mm | λ=X/λ0
Cu | 0.35 | 14.36 | 0.0244 | 153.2 | 0.0023
Fe | 1.75 | 17.57 | 0.0996 | 167.7 | 0.0104
Ag | 0.07 | 8.543 | 0.0082 | 154 | 0.0005
YBa2Cu3O7 | 0.07 | 12.49 | 0.0056 | 296.5 | 0.0002
MgO | 0.00000035 | 78.28 | 0.0000 | 274 | 0.0000
Al2O3 | 0.0000028 | 70.38 | 0.0000 | 247.9 | 0.0000
CeO2 | 0.0000105 | 16.54 | 0.0000 | 230 | 0.0000
Al stablizer | 15 | 88.97 | 0.1686 | 397 | 0.0378
MLI, Fiber glass | 0 | 286 | 0.0000 | 415 | 0.0000
Glassepoxy | 2 | 286 | 0.0070 | 428.9 | 0.0047
Total, Xtot |  |  | 0.3134 |  | 0.0559
Cryostat (25 mm Al): X0= 0.28, λ= 0.07
Total | X0 | λ
Track 1 | 0.5934 | 0.1259

## Slide 8: Radiation thickness calculation
IDEA LTS and HTS Comparison
Consider using the same Cryostat (25 mm Al): X0= 0.28, λ= 0.07
1
2
Total | X0 | λ
LTS Track 2 | 0.73 | 0.153
LTS Track 1 | 1.77 | 0.21
HTS Track 1 | 0.59 | 0.126
1

## Slide 9: HTS plan R&D
Need to develop the Al stabilized HTS stack cable or other HTS cable.
Got fund (3 million yuan)from CAS to develop the cable and prototype coil.

## Slide 10: Future
CEPC 3T inside calorimeter version, the coil parameter? Radius, length?
Radiation length requirement?
The most important thing is to develop the HTS cable.