## Slide 1: The LTS and HTS detector magnet design
Zhao Ling
On behalf of superconducting magnet group

## Slide 2: Outline
Solenoid design in the CDR
Progress of thin solenoid magnets
New design of solenoid(LTS)
New design of solenoid(HTS)
Next plan

## Slide 3: History of High Energy Physics Detector Magnets
1969 CERN –BEBC, Big European Bubble Chamber (solenoid)
1972 CERN –Omegamagnet (large aperture dipole)
1977 CERN/ISR –Solenoid
1978 DESY –CELLO (solenoid)
1983 SLAC/PEP4 –TPC solenoid
1985 KEK/TRISTAN –TOPAZ, VENUS (solenoids)
1988 CERN/LEP –ALEPH, DELPHI (solenoids)
1990 DESY/HERA –ZEUS (solenoid)
1997 SLAC –BABAR (solenoid)
2004 KEK –BESS-Polar (ultra-thin solenoid)
2007 CERN/LHC –CMS (solenoid), ATLAS (Toroids, solenoid)
Revised August 2017 by Y. Makida (KEK)
Main parameters of detector magnets
T. M. Taylor, CERN Summer Student Lecture, 2006
Notes: Not an exhaustive list!
Historically detector magnets were the first application of superconductivity (Bubble Chambers)
• As early as late 60s and beginning of 70s big magnet in LHe pool, boiling: Argonne and BEBC (CERN); concept of cryostabilisation (Stekly criterion)
1978 CELLO, Pure aluminum as stabiliser was employed for thin solenoids; then also for outer solenoids, toroids and now is becoming the standard stabiliser.
• Remarkably in 30 years the magnetic field increased only a factor 2: from 2-3 T to 6 T peak field of CMS.

## Slide 4: Design of LTS DETECTOR MAGNET in CDR
Solenoid central field ：3T
Working current：15779A
Coil inner radius：3600mm
Cable length：30.1km
CMS
Pure Al+Alloy
CEPC
Pure Al+Alloy
Pure aluminum stabilizer
Aluminum alloy reinforcement
By Guoqing Zhang

## Slide 5: New Yoke Design of LTS DETECTOR MAGNET
CDR version
New Yoke version
 |  | CEPC CDR version | CEPC New version
Central field (T) |  | 3 | 3
Operating current (A) |  | 15779 | 16796
Inner diameter of coil (mm) |  | 7200 | 7200
Length of coil (mm) |  | 7606 | 7600
Barrel yoke inner diameter (mm) |  | 8800 | 9200
Barrel yoke outer diameter (mm) |  | 14480 | 12120
Total length of yoke (mm) |  | 13966 | 12020
Weight of barrel yoke (t) |  | 5940 | 3137
Weight of each end cap (t) |  | 3316.6 | 1144
Total weight of yoke (t) |  | 12,573 | 5,425
By Feipeng Ning

## Slide 6: New requirement
The detector magnet will be located between the Hadron calorimeter and Electromagnetic calorimeter ；
Reduce mass : Increase coil current density，and superconductor were reduced from four layers to two or three layers.
Reduce the radial space occupied by superconducting magnet.
Central field: 3T
Magnet inner bore: >4 meter
Coil Length: about 6 meter.

## Slide 7: Progress of thin solenoid magnets

## Slide 8: Comparison: Thickness of thin solenoid
 | CMS | BESIII | ALEPH | DELPHI | BESS-POLAR | WASA | SDC PROTOTYPE | IDEA* | CDR(CEPC) | NEW DESIGN
Central field (T) | 4 | 1 | 1.5 |  | 0.8 | 1.3 | 1.5 | 2 | 3 | 3
Operating current (A) | 19600 | 3369 | 5000 |  | 380 | 900 | 12000 | 20000 | 16796 | 16956
Inner diameter of coil (mm) | 6360 | 2960 | 5300 |  | 900 | 553.6 |  | 2200 | 7200 | 4600
Length of coil (mm) | 12480 | 3520 | 6350 |  | 1400 | 465 | 1900 | 6000 | 7606 | 5000
Outer shell external diameter(mm) | 7600 | 3292 | 5840 | 3080 | 1060 | 650 | 4012 |  | 8700 | 5600
Inner shell inside diameter(mm) | 5940 | 2750 | 4960 | 2600 | 800 | 490 | 3400 |  | 6800 | 4400
Thickness of cryostat (mm) | 830 | 271 | 440 | 240 | 130 | 80 | 306 | 300 | 950 | 300~400?

## Slide 9: New design of solenoid(LTS)
Coil with two layers superconductor ：weight of superconductor is 11.4t。
Coil with three layers superconductor：weight of superconductor is 17.2t.
By Guoqing Zhang

## Slide 10: New design of solenoid(LTS)
Central field：3.0T；
Max field on coil：3.73T/3.495T；
Stored energy：0.3959GJ/0.40024GJ；
Working current：16956A/11338A；
Field Distribution
Two layers coil
three layers coil
By Guoqing Zhang

## Slide 11: New design of solenoid(HTS)
Coil parameters:
Coil inner radius | 2.2 m
Coil length | 6 m
Cable layers | 2
Tape layer of each cable | 35
Tape width/thickness | 10 mm/80 μm
Operating current | 29700 A
Operating temperature | 5 K
20
10
15
5
By Feipeng Ning

## Slide 12: Radiation thickness calculation
35 layers HTS tapes of each cable.
Material | Thickness | Radiation thickness |  | Nuclear Interaction length | 
 | X, mm | X0, mm | X/X0 | λ0, mm | λ=X/λ0
Cu | 0.7 | 14.36 | 0.0244 | 153.2 | 0.0023
Fe | 1.75 | 17.57 | 0.0996 | 167.7 | 0.0104
Ag | 0.07 | 8.543 | 0.0082 | 154 | 0.0005
YBa2Cu3O7 | 0.07 | 12.49 | 0.0056 | 296.5 | 0.0002
MgO | 0.00000035 | 78.28 | 0.0000 | 274 | 0.0000
Al2O3 | 0.0000028 | 70.38 | 0.0000 | 247.9 | 0.0000
CeO2 | 0.0000105 | 16.54 | 0.0000 | 230 | 0.0000
Al stablizer | 10 | 88.97 | 0.1686 | 397 | 0.0378
MLI, Fiber glass | 0 | 286 | 0.0000 | 415 | 0.0000
Glassepoxy | 2 | 286 | 0.0070 | 428.9 | 0.0047
Total, Xtot |  |  | 0.2815 |  | 0.0455
 | X0 | λ
Single cable | 0.2815 | 0.0455
Double layers cable | 0.563 | 0.091
Radiation thickness of HTS cable
(don’t include cryostat):
By Feipeng Ning

## Slide 13: HTS cable development
ReBCO Stack Cable
Compact stack structure:
Al film thickness and width
Winding stress
Other materials
Prototype cable:
Tape Width: 4 mm, thickness: 80 μm; tape layer: 20
Expected operating current: 6000 A

## Slide 14: Next Plan
For LTS:
R&D of High strength superconducting cable with self supporting structure;
For HTS:
R&D of HTS cable;
R&D of Large HTS coil;
For both:
Optimization of coil support system;
Optimization of coil cooling structure;
Optimization of vacuum vessel structure;
Thin solenoid

## Slide 15: Comparison
LTS:
more experience on cable and coil winding；
small temperature margin(4.5~6K)；
more mass(coil thickness 60mm)；
HTS
more R&D on cable and coil winding；
Higher temperature margin(4.5~20K)；
lower mass(coil thickness 30mm)；

## Slide 16: Funds and personnel
Funds: 1.5millon(IHEP)+3millon(0-1)+3millon
Personnel: Zian Zhu/Ling Zhao/Feipeng Ning
Part time: Meifen Wang/Huan Yang/Guoqing Zhang
Students: 1~2
More R&D is needed for detailed design.

## Slide 17: Thanks for your attention!

## Slide 18
BESS-Polar solenoid
Back Up

## Slide 19
Back Up

## Slide 20
Back Up

## Slide 21
A shared cryostat for solenoid and electronic calorimeter.
Back Up

## Slide 22
绕制生产线布置
回转平台
成型机
缓冲支撑
矫直机
放缆桶
成型机桁架
超导磁体Dummy线圈及绕制工艺装备设计
生产线占地：22mx16m；
生产线搭建前在产线所在区域布置靶标测量点，便于产线设备安装调试。
控制系统控制整个系统的运行，各子系统可单独运行，也可联动。
通过单机调试及联动调试使整个生产线得以平稳运行。
已矫直导体：高度2.2米
Dummy线圈设计
Back Up
Dummy线圈包括一个铝支撑筒和dummy线圈；
内径7.2米，长度约0.3米；
采用56*22mm的Dummy铝合金缆进行绕制，共4层，每层十匝；
匝间绝缘大于500V；
对地绝缘大于1000V。

## Slide 23: Coil Cooling Design
 | Internal section size(mm) | Wall thickness(mm) | Length(mm)
Cooltube | Φ8 | 1 | 400
Feed pipe | Φ12 | 2 | 600
Exhaust pipe | Φ12 | 2 | 140
The phase separator | Φ100 | the upper plate 6，the bottom palte 10，cylinder 6 | 106
Steam tank、Sump | 50×20 | 2 | 203
Back Up

## Slide 24
Back Up

## Slide 25: Back Up