## Slide 1
Noise distribution of TaichuPix1
Tianya Wu
CEPC Meeting
twu@ifae.es
01-02-2021
1

## Slide 2
Sector1+Sector2
Sector1+Sector2
Sector2
Sector2
Sector1
Sector1
Measure several columns by hand and analyze the distribution.
With the same fitting parameters, results looks fine but not so perfect. Some curves will be failed to the fitting function.
There are 4 different analog pixels design, the performance of Sector2 seems better.
DBCOL24~31
DBCOL0~7
DBCOL15/23
DBCOL0~7
+
DBCOL15/23
DBCOL24~31

## Slide 3
Fitting Failure
Fitting Success
Fitting parameter：
μ= 310 mV
sigma= 9mV
Fitting parameter：
μ= 295 mV
sigma= 9mV
μ= 288.69 mV
sigma= 3.18mV
μ= 286.38mV
sigma= 8.68 mV
DBCOL7-R28
DBCOL7-R28

## Slide 4
Sector1：DBCOL0~7
Sector2：
DBCOL24~31
Sector1：DBCOL0~7
Sector2：
DBCOL24~31
Fig.1 Threshold
distribution
Fig.2 noise
distribution
Fig.1 shows the threshold distribution, the FPN for sector1 is ~35e- and ~24.15e- for sector2 .
Fig.2 depicts the noise distribution, the TN noise for sector1 is 15.96e- and 12e- for sector2.
Use two kinds of the fitting parameter, the histogram seems better.