## Slide 1: Study of beam energy measurement for CEPC
Jianyong Zhang
on behalf of BEMC group

## Slide 2: BEMC group
Huang Yongsheng, Tang Guangyi, Chen Shanhong, Si Meiyu, Mo Xiaohu, Zhang Jianyong ……
1, Experiment physics divisions, IHEP, CAS
Duan Zhe, Wang Yiwei, Chen Yuan ……
2, Accelerator center, IHEP, CAS
Shen Zhongtao, Luo Laifu, Yu Hanlin, Liu Shubin ……
3, University of science and technology china
Cividec ……

## Slide 3: Outline
Motivation
Design of diamond micro strip detector
Manufacture of diamond micro strip detector
Preliminary performance test
Design and test of readout electronics
Next to do

## Slide 4: Motivation
In order to determine the MHiggs at the level of σMHiggs~ 1 MeV ，the beam energy should be determined at σEBeam ~ 1 MeV.
It is an international problem to calibrate the beam energy accurately (10-5) at the energy level of 100 GeV. There is no successful experience to learn from.

## Slide 5: BEMS@BEPCII
Ebeam：1 ~ 2.3 GeV
Co2 Wave Length，10.59 μm
ORTEC HPGe detector, ~30%
ORTEC Dspec Pro

## Slide 6: BEMS@BEPCII（II）

## Slide 7: BEM@CEPC
Plan to use laser Compton Scattering method
Assuming Ebm=120GeV, ω0=1.24ev,
Eγ=84GeV, Esbm=36GeV, No energy detector can
measure such high energy accurately
Accurately measure beam position and accurately determine
beam energy
The new detectors were investigated :
  Silicon micro strip detector,
  Silicon pixel detector,
  Diamond micro strip detector
The beam energy of CEPC is high, the performance of silicon detector is significantly reduced at 1017n/cm2, and the radiation resistance of diamond microstrip detectors is one order of magnitude higher
Diamond micro strip detector should be studied carefully
103/bunch
105/bunch

## Slide 8: Design of diamond micro strip detector
According to our simulation, If the position resolution of the diamond micro strip detector is 10 microns, the CEPC beam energy accuracy is about 1.2╳10-5
Select diamond micro strip samples with a width of 50 microns and a gap of 50 microns for research

## Slide 9: Design of diamond micro strip detector
40 channels
Single crystal diamond plate, CVP

## Slide 10: Design of diamond micro strip detector

## Slide 11: Manufacture of diamond micro strip detector
Cooperate with Cividec (Austrian)to help us manufacture diamond micro strip detectors
Specifications
60╳60╳8mm3
HV: 250V
HV
Signal readout

## Slide 12: Preliminary performance test
L.V. power supply：GWINSTK-GPD3303S
H.V. power supply：CAEN 4ch NIM/Desktop Programmable
Oscilloscope：Tektronix MDO 3034
Radioactive source：Am-241
Test process
Diamond
R. source
H.V.
L.V.
Oscil.
Amp.

## Slide 13: Single channel
Detector :10204，Amplifier：141
1
3
5
8
7
6
4
2

## Slide 14: Cross talk
Channel 1 trigger
Channel 2 trigger
Channel 3 trigger
Cross talk in adjacent 3 channels

## Slide 15: Design and test of readout electronics
The amount of charge corresponding to the minimum deposition energy :
Current signal readout scheme
  Charge sensitive
  Trans-impedance amplification
    High power consumption, high digital requirements
  Resistance-voltage conversion and voltage-voltage amplification
    The first stage conversion gain is low and the signal-to-noise ratio is poor
Luo Laifu from USTC

## Slide 16: Design and test of readout electronics
The overall scheme of charge sensitive readout
To improve s/n ratio，Front End Board and Back End Board

## Slide 17: Design and test of readout electronics
Front End Board
Back End Board

## Slide 18: Electronics debugging
Calibration、noise test
  14-bit ADC, 40MSPS sample rate
  Noise at output stage: ~23 ADC Code;
  Slope between output amplitude and input charge:
  Slope difference between channels

## Slide 19: Electronics debugging
Equivalent noise charge （ENC）
  The ENC of all channels is about

## Slide 20: Detector electronics joint debugging
Beta rays using 90-Sr radiation source
H.V.
90-Sr
FEB
L.V.
BEB

## Slide 21: Detector electronics joint debugging
Pedestal and noise
  Pedestal: about 8100 ADC Code, half of full range (14bit, 16383 ADC Code)
  The equivalent noise increases by ~、~
Pedestal of 20 channels
Noise of 20channels

## Slide 22: Detector electronics joint debugging
Ch1
Ch2
Ch3
Ch4
Ch5
Ch6
Ch7
Ch8
Ch9
Ch10

## Slide 23: Detector electronics joint debugging
Ch11
Ch12
Ch13
Ch14
Ch15
Ch16
Ch17
Ch18
Ch19
Ch20

## Slide 24: Detector electronics joint debugging
90-Sr test results
  E，a
  Deposited energy shared among multi-channels

## Slide 25: Next to do
Make the new board to ensure a 40-channel readout system
Prepare a new trigger algorithm according to the actual situation
Investigate the situation where the deposited energy of a single case is shared among multiple strips
Position measurement related experiments
… …
Thank you for your attention!

## Slide 26
90-Sr理论沉积能量
  90-Sr β衰变释放的最大能量为0.546MeV，由此得：
  其在碳中的电离能损：
  在500um厚的金刚石中，损失能量：
  对应电荷量：