## Slide 1
Progress of the High Field Magnet R&D
for CEPC-SPPC
Qingjin Xu
Oct 14, 2021
中国科学院高能物理研究所
Institute of High Energy Physics, CAS

## Slide 2: Outline
SPPC high field magnet design scope
Status of the high field IBS coils by IHEP & IEE
Status of the high field model dipole magnets
Development of a novel HTS transposed cable
Status of the China-CERN HL-LHC CCT project
Summary

## Slide 3
Magnet Design Scope for SPPC
High Energy Circular Colliders for next decades | SPPC | FCC
Proposed institution | IHEP-CAS, China | CERN, Europe
Proposed dates | 2012 | 2014
Site of the project | China | Europe
Baseline technology | IBS 12~24 T to reach 75-150 TeV, Nb3Sn etc as options | Nb3Sn 16 T to reach 100 TeV
Timeline | Construction at 2040s | Construction at 2050-60s
Cost | * | **

## Slide 4
Je of Practical Superconductors Presently
Chart: Applied Magnetic Field (T)
| 5 | 10 | 15 | 20
REBCO: B ∥ Tape plane | 4599.7996 | 4264.0246 | 3416.6751 | 3085.9004
REBCO: B ⊥ Tape Plane | 3664.9998 | 2919.9995 | 2379.9996 | 1796.1537 | 1447.6924 | 1188.462 | 1034.3652 | 956.923 | 851.8301 | 780.8449 | 719.9995 | 679.4359 | 626.087 | 593.2388 | 563.4783 | 535.3843 | 516.5215 | 469.5647 | 433.0766 | 406.956 | 391.3041 | 367.6926 | 360.0003 | 344.3473 | 328.6954 | 322.3077
Bi-2212: 50 bar OP | 2187.8458 | 2018.5437 | 1897.0961 | 1799.3564 | 1729.1673 | 1666.7736 | 1608.1837 | 1558.7923 | 1516.4066 | 1473.2906 | 1436.5687 | 1398.9095 | 1365.3787
Nb₃Sn: Internal Sn RRP® | 1754.8557 | 1454.9349 | 1190.9814 | 1072.6374 | 957.7741 | 855.0933 | 757.6336 | 268.0143 | 190.8587 | 118.9241 | 65.5533 | 28.3097
Nb₃Sn: High Sn Bronze | 166.6431 | 137.8146 | 111.0954 | 84.3762 | 60.8212 | 40.0788 | 19.3362 | 8.0861
Nb-Ti: LHC 4.2 K | 5106.8846 | 4054.1538 | 3180.5962 | 2710.2269 | 2217.4577 | 1724.6885 | 1411.1115 | 1187.1231 | 918.3423
Nb-Ti: High Field MRI 4.22 K | 393.4783 | 291.3043 | 194.203 | 104.3478
Exponential Y-axis Labels | 10 | 100 | 1000 | 10000
Nb-Ti midrange maximal | 971.9231 | 687.3077 | 448.4615 | 393.4783
2212 Fitted Line for 50bar | 1379.4097 | 1269.0093 | 1128.2455 | 1107.3276
YBCO B perp ln extrap | 322.2305 | 315.4585 | 296.3443 | 267.862 | 242.7389
YBCO par ln extrap | 3024.7539 | 2573.1471 | 2188.967 | 2051.8662
IBS 2016
(short sample)
500A/mm2
IBS
100-m tape

## Slide 5
100-m Long Ba122 Tapes by Rolling Process
In 2020, Jc of a 100-m 7-core tape using the new fabrication technique reached 500 A/mm2 @ 4.2 K, 10 T.
Tape width 4.8 mm, tape thickness 0.3 mm. Ic > 200 A, Je>140 A/mm2.
In 2018, Jc of such tape is 300 A/mm2 @ 4.2 K, 10 T.
Prof. Y. Ma’s
Group, IEE-CAS

## Slide 6
4.2 K, 10 T (short sample): Jc=1100 A/mm2
Performance of HIP Ba122 Tapes with Cu/Ag Sheath
Size of the grains was around 0.5 um, smaller than that in the Hot-pressed samples.
The Jc may be improved with the increase the grain size.
Liu 2021 Sci. China Mater.
Doi:10.1007/s40843-020-1643-1
Prof. Y. Ma’s
Group, IEE-CAS

## Slide 7
Preparition of bent IBS tape
Jc of Bent IBS Tapes
Cracks appear regularly in part of the superconducting cores under tensile stress !
Ic of bent IBS tapes decreases with smaller bending diameters.
OMI of D10 bent tape
Sample results by ASIPP in 2018
Sample results by IHEP in 2021

## Slide 8
Fabrication of D20-17 turn-double pancake coils with IBS tapes
Series IBS double pancake solenoids
High Field IBS Insert Solenoids
Coil winding of the IBS double pancake solenoids with 20-mm inner diameter
IBS double pancake solenoids after heat reaction
Impregnated Series IBS solenoids

## Slide 9
High Field IBS Insert Solenoids
Performance test of the series IBS solenoids at 20 T background field
Ic of the series IBS solenoids reached 75 A at 20 T, and stable operation with 100 A.

## Slide 10
Performance test of the double pancake IBS solenoid at 30 T background field
Ic of the IBS solenoid reached 67 A at 30 T. New world record!
D20-17turn-IBS double pancake coil
30T background magnet @ Hefei
High Field IBS Insert Solenoids

## Slide 11
Parameter | Value
Background field | 0-10 T
Rate | 1 A/s
Maximum pressure on IBS | 120 MPa
Racetrack Coils with 100-m Long IBS Tapes

## Slide 12
Zhang, et al., SuST,. 34 (2021) 035021
Two racetrack coils have been made using the 100 m length IBS tapes.
The coils reached 86.7% of critical current of the short sample at 4.2 K and 10 T.
with highest compressive stress of 120 MPa.
Racetrack Coils with 100-m Long IBS Tapes
Comments from SUST reviewers：
…the new results that can have a strong impact on the conductor and magnet community.
…demonstrated the great potential of Iron-Based Superconductor in the development of next-generation accelerators.
It is of certain significance in the path of applications of Iron-Based Superconductor…

## Slide 13
2008.02
2008.09
2016
2018
Discovery of IBS
2008.04
Discovery of
122 phase IBS
2020
100-m 7-core IBS tape fabricated
Challenges and Outlook of the IBS Magnets
Tc reached 55K
IBS solenoid at 24 T
Racetrack at 8 T
The engineering current density of the long-length IBS still needs a significant improvement, to reach the similar level as ReBCO or Bi-2212 conductors.
The materials of stabilizer should be shifted to copper or any other low-cost metals to realize the low cost of IBS.
Structure and fabrication methods of IBS and corresponding coils should be further optimized to minimize the Jc degradation at high field and high stress.
And many other issues like detailed magnetic and mechanical properties study of IBS, quench detection and protection of the IBS coils / magnets and etc.
IBS solenoid at 30 T
Racetrack at 10 T
2022

## Slide 14
超导线材
Impregnation quality control
Thermal stress control
Mechanical strength and stability
Quench protection
Hot spot, voltage,…
Material,
Cross section, Processing,…
Jc, RRR, Cu ratio,
Filament size,
Jc and RRR degradation
Stress and dimension control
线圈制作
磁体组装
性能测试
磁体设计
Magnetic field strength,
EM force, quench protection,…
Magnetic field quality,
Persistent current effect,
Coil stress,…
Jc & strain curve of the superconductor
Pre-stress control
Dimension control,
Mechanical Stability
Training, Thermal-magnetic instability,
Thermal cycle,…
R&D Route for High-field Accelerator Magnets

## Slide 15
R&D of the 1st NbTi+Nb3Sn Model Dipole Magnet
Development of the LPF1 NbTi+Nb3Sn dual-aperture model dipole magnet from 2017.
Dipole field reached 12 T in 2*Φ14 mm apertures in May 2021 and 12.47 T in July after a thermal cycle.

## Slide 17
Ongoing: Development of the 16-T Hybrid Dipole Magnet
Nb3Sn 12~13 T + HTS 3~4 T

## Slide 18
Development of a NOVEL HTS Transposed Cable
Ongoing: Development of the 16-T Hybrid Dipole Magnet
SuST letter
under review

## Slide 19
Ongoing: Development of the 16-T Hybrid Dipole Magnet
Development of a NOVEL HTS Transposed Cable

## Slide 20
R&D Roadmap for next years

## Slide 21
Status of the China-CERN HL-LHC CCT Project
Layout of the HL-LHC Magnets and Contributors
  The prototype has been delivered to CERN, and the series magnets are being developed by 2023.
  Performance of the 1st full-length prototype magnet from China: Fabrication completed in May 2020, and the performance test at 4.2K completed in August 2020. both apertures reached the ultimate current.

## Slide 22
Status of the China-CERN HL-LHC CCT Project
02-Aperture-1
02-Aperture-2
02-Aperture 1
02-Aperture 2
The 1st series magnet passed all the performance test at 4.2K!
The 1st series magnet
Practice coil
1-Aperture-02
1-Aperture-01

## Slide 23
Status of the China-CERN HL-LHC CCT Project
Field quality measurement results of the 1st series magnet
All field errors are within the requirement, less than 5 units for most cases.

## Slide 24
Strong domestic collaboration in China for the advanced superconductor R&D (HTS & Nb3Sn): to significantly raise their performance and lower their cost.
Jc of 100-m long 7-core Iron-Based Superconducting tape has reached 500 A/mm2 @ 4.2 K, 10 T, corresponding to Ic >200 A, Je>140 A/mm2.
Quench current of the Iron-Based Superconducting double pancake solenoid coil reached 67 A at 30 T, new world record!
10+ T dual-aperture model dipoles being developed at IHEP, reached 12.47 T at 4.2 K in July 2021, aiming to reach 16 T (Nb3Sn+HTS) in 3 years, and 20 T in 10 years.
HL-LHC CCT magnet project: the 1st series CCT magnet has passed all the performance test at 4.2 K, to be shipped to EU in October 2021. China & CERN Collaboration on accelerator technology started with HL-LHC CCT magnets, to be expanded in future.
Summary

## Slide 25
IHEP-CAS: Chengtao Wang, Yingzhe Wang, Juan Wang, Chunyan Li, Rui Kang, Huanli Yao, Zhen Zhang, Jinrui Shi, Ze Feng, Wei Li, Ao Feng, Ling Zhao, Zhilong Hou, Huan Yang, Zhongxiu Liu, Quanling Peng,…
IEE-CAS: Dongliang Wang, Xianping Zhang, Yanwei Ma,…
HIPS-CAS: Huajun Liu, Tao Zhao, Yanlan Hu,…
IMP-CAS: Wei Wu, Yu Liang, Wenjie Liang, Dongsheng Ni,…
WST: Bo Wu, Yanmin Zhu, Xiang Guo, Jianwei Liu, Jianfeng Li, Meng Li, Chao Li, …
Toly Electric: Yu Zhao, Hean Liao, Bingxing Lu,…
Baoding Tianwei Electric: Tao Xing, Xiongzhuang Li, Jun Jiao,…
CERN：Ezio Todesco, Glyn Kirby, Andrea Musso, Arnaud Devred,…
*Work supported by the Strategic Priority Research Program of the Chinese Academy of Sciences (CAS) Grant No. XDB25000000, the National Key Research and Development Program of China No. 2018YFA0704200, and National natural Science Foundation of China Grant No. 11675193, 11575214, 11604335.
Team Members & Collaborators
Thanks for your attention