## Slide 1
Status of new technologies exploration
  On behalf of the pixel detector study group
  2022.2.16
  ZHOU Yang

## Slide 2
diffusion
A brief sketch of technology moving used by CMOS pixel sensors developed for vertex detector
Technology nodes used was shrinking with industry progress. Brings benefits like: more functions integrated, faster charge collection, lower power per function.
diffusion
~2008
~2010
~2014
Non-depleted, thick epi substrate: several Ω·cm
AMS 0.6 μm
Semi-depleted, HR epi substrate 500 – 2k Ω·cm
AMS 0.35 μm
Quadruple-well CMOS: both type of transistors admitted in the pixel array
> 1k Ω·cm
TOWER 0.18μm
Fully depleted
> 1k Ω·cm
ESPROS 0.15 μm
TOWER 0.18 μm modified
Charge collection: mainly on diffusion
diffusion drift
Epi-thickness: 14-20 μm
Epi:~20 μm
Leading-edge technology node
TOWER 65 nm
HLMC 55 nm
~2020
drift，
Epi: ~10cm？
> 10 years of development, the main technology for ALICE-ITK2, CBM-MVD, and CEPC vertex detector R&D
？

## Slide 3: Sensor performances achieved in Jadepix series：
1×0.6 cm2
512×192 pixels
Layout of Jadepix4，submitted： 2021.11.5
1.48×0.86 cm2
356×498 pixels
  Test performances:
  Noise：~15e-
  Readout speed：98.3μs/frame；
  Average power dissipation：~52.8mW/cm2；
  Spatial resolution：σx ~2.7-4.4 μm, σy ~3.4-5 μm
While the pixel analogue FE and periphery circuits keep similar with JadePix3：changed the pixel readout structure.
time resolution improved：~100 μs -> ~1 μs;
paid by pixel size increased： 16μm×23μm -> 20μm×29μm
*Design details have been reported by Yunpeng on 2021/10/27
@developed by MOST1 Vertex detector study group
Layout of Jadepix3

## Slide 4: Interested performances may directly affected by new technologies
23.11 μm
16 μm
Layout of a pixel in JadePix3
Layout of a pixel in JadePix4
Specifications required by CEPC vertex sensor (from CDR) | 
Spatial resolution≤ 3µm | Required a pixel size ≤ 16 ×16 µm2
Material budget ≤ 0.15%X0 /layer | Sensor back thinned down to ~50μm
Average power dissipation | <50 mW/cm2
Time resolution | ~1μs
Radiation tolerance | < 3.4 Mrad / year , <6.2 × 1012 neq/ (cm2 year)
20 μm
29 μm
New technologies exploration introduced in this talk:
3D technology;
2. Smaller technology node;
3. Stitching technique
may reduce the material budget to 1/3 of the requirement by removing the supporting structures.
bring opportunities to shrink the pixel size of current design:

## Slide 5: 1. 3D technology： SOI-3D
5
Device Layer (40nm)
Buried Oxide (200nm)
Substrate (50-500μm)
Sputtered Al Layer (200nm)
Sandwiched structure of SOI
Layout of a pixel in JadePix4
20 μm
29 μm
The idea is: split the pixel into two parts, then connected them vertically, so the pixel layout size could shrink to half.
Extra requirements for the 3D technology:
1. The bump size should be small enough to integrated at least two in the small pixel area;
2. The final thickness should meet the low material budget requirement.
First try was on the SOI 0.2μm 3D technology,
Supported buy :“高精度SOI像素顶点探测器研究”, NSFC key program, 2020-2024
3μm diameter Au bump

## Slide 6
Layout of CPV4-3D
Upper
Lower
AERD
readout
Hit
D-FF
Control register
Test-EN
Mask
A-Pulse
D-Pulse
Strobe
Amplifier/
Comparator
State
Reset
PDD
Lower tier
Upper tier
Division of upper and lower functionalities
Lower tier: PDD sensing diode + amplifier/comparator
Upper tier: Hit D-Flipflop + Control register + AERD readout
2 vertical connections in each pixel: comparator output and test switch;
Analog and Digital power/ground are also separated
Pixel size | 17.24×21.04 μm2
Time resolution | ~1 μs or ~3 μs in different operation mode
Pixel array | 128×128
Chip size | 4.5mm×4.5mm
Delivered | Nov. 2020
@ design details was introduced by Yunpeng on 2020/12/28
1. 3D technology： CPV4-3D design overview

## Slide 7: 1. 3D technology : basic functions of the two sensors have been validated
1. Leakage current on CPV4, the analogue sensor can be biased at -200V.
2. Pulse inject test of analogue sensor.
Amplifier output
Digital signal to digital sensor
3. Pulse inject test of digital sensor.
-Valid signal from sensor (white line)
-Reset signal after read the pixel addresses. (yellow line, 4 pixels was fired)
CPV4 digital sensor bonding on test system

## Slide 8: 1. 3D technology: ongoing work
Ordered an extra wafer for 3D integration
Alignment mark on the two sensors
3D integration (by foundry in Japan) order is still in-progress;
A DAQ and test control system is in developing;

## Slide 9: 2. Smaller technology node： more possibilities
Layout of a pixel in JadePix4
20 μm
29 μm
Digital part: 133 transistors, ~324 μm2
6*3 μm2
1.6*1.4 μm2
Layout of a standard digital cell “and” in Tower 0.18μm (left) and HLMC 55nm process (right).
Digital part may be reduced to: ~16*2.5 μm2
~1/8
~1/8
It seems possible to realize current pixel design in 16*16 μm2, using a smaller technology node around 65/55nm.
Per digital function: smaller layout size; lower power consumption (dynamic power could reduce 2.25 times if the core VDD reduced form 1.8V to 1.2V)

## Slide 10
2. Smaller technology node： HLMC 55nm
Basic information:
55nm CIS process;
Voltage for core transistor 1.2V， for IO transistor: 3.3V;
Epi thinness: 5.4 μm
Resistance: 10Ωcm
Quadruple-well process:
  Deep P-well and deep N-well injection parameters were customer designed。(by TCAD simulation)
Supported by : 中俄“重离子超导同步加速器”国际合作研究项目, National key research and development program, 2020-2025
Design team from: IHEP, CCNU, IMP
Some studies have been started in HLMC 55nm process:
  1. Process modification;
  2. Diode, and charge collection study;
  3. Necessary electronic function blocks design: DAC , buffer, PLL and so on.
Epi.

## Slide 11
Layout of the first prototype on HL55nm process to study diode and charge collection，submitted: 2021.6
2.2×4 mm2
Diode and charge collection study:
Including 42 sub pixel arrays：
3 type of pixel pitch size: 8 / 16 / 24 μm;
6 type diode structures: different surface and footprint size;
3 type of in-pixel circuits:
One pure diode matrix for leakage current/equivalent capacitances test
In-pixel circuits in block1: for charge collection amount study;
In-pixel circuits in block2: for charge collection time study;
2. Smaller technology node： 1st prototype overview

## Slide 12: 3. Stitching technique: wafer-scale sensor
Supported by “基于大面积超薄CMOS像素传感器BESIII内径迹室关键技术研究”NSFC KEY Program, 2021 - 2024
Design aiming for the application of BESIII inner tracking system;
Deign team from: IHEP, Shandong University, Harbin Institute of Technology , Dalian Minzu University
Floor plan of our first chip design with large scale.
  Chip size 11cm *11cm,
  XFAB 0.35μm process;
  Rowling-shutter readout mode;
  Plan to submitted in Apr.
~11cm
~10cm
Material budget of one layer is possible down to ~0.05% X0 （1/3 of CEPC expectation in CDR）
Wafer-scale sensor, after thinned down to 50μm，can bend like a A4 paper，so the so-called “self-support”would be possible；
Material budget of the tracking detector system could be significantly reduced，less affect to particle multiple scattering。
Normally a chip size is limited by the mask size: < ~2cm×2cm；
Stitching-technique could extend the chip size ~100 times larger: < ~30cm ×30cm;
Beyond CEPC expect:

## Slide 13: 3. Stitching technique: general experiences
A wafer-scale sensor may include: ~100 MC, ~10 ML/MR/TC/BC, and 1 TL/TR/BR/BL;
The block layout with a same name have to be exactly the same. Need special consideration for the periphery/pixel circuits design, not only the function but also how to realize physically;
Parasitic Capacitances on long signal lines may increase from several ~pf to ~tens of pf. Has to do something to reduce this influence to the power and speed.
Power-ring, IR drop should be taking care;
Sketch map of how masks organized for a wafer-scale large sensor

## Slide 14: Summary and Outlooks
Beside Towerjazz 0.18μm CIS process, 3 new technologies/techniques exploration is ongoing, which may bring more possibilities for CEPC vertex detector R&D: eg. Higher spatial resolution, lower power dissipation/per function, less material budget…….
An ideal technologies may have features like:
  65/55nm CIS;
  ~10μm thick, high resistance epi.
  Quadruple-well process;
  Custom process modification possible;
  Stitching technique support;
Outlooks:
  Looking for an accessible foundry provide the technology has close features we expect;
  Design experiences in smaller technique node: eg. leakage current, average power, time resolution…….
  Design experiences and ideas for a wafer-scale chip;
  Further test of the CPV4-3D : eg. “yield”

## Slide 15
Thank you for your attention！