## Slide 1: Recent Progress of the High Field Superconducting Magnet R&D
2022.03.25
中国科学院高能物理研究所
Institute of High Energy Physics, CAS
中科院高能所超导磁体组
Superconducting Magnet Group, IHEP
Superconducting Magnet Group
Accelerator Division
IHEP-CAS

## Slide 2
Outline
Progress of LPF3: a 16-T dipole magnet with graded common-coil configuration
Conceptual design of the 16-T dipole magnet with CCT coil configuration
Development status of the HTS transposed cable
Development status of the high field IBS coils
Performance study of a new epoxy resin IR-3 for high field applications
Development status of the HL-LHC CCT series magnets

## Slide 3
01
中科院高能所超导磁体组
Superconducting Magnet Group, IHEP
Progress of LPF3: a 16-T dipole magnet with graded common-coil configuration

## Slide 4
Performance of LPF1-U
Picture of LPF1-U
A maximum field of 12.47 T was achieved recently for the upgraded magnet of LPF1-U, beyond the dipolar field baseline required in SPPC.
New record

## Slide 5
Electromagnetic design of LPF3
The cross-section of LPF3
Coil layout (yoke 1/8)
OD:640 mm
120 mm
AP:30 mm
Field and flux distribution in coils
58
42
58
24
54
24
50
20
1
2
3
4
5
6
Main field: 16 T
Nb3Sn
YBCO
Nb3Sn
LTS (13 T) + HTS (3 T)
Current | 7580/143 A |  | Blocks | Block 1 | Block 2 | Block 3 | Block 4 | Block 5 | Block 6 | Block 7
Main field | 16.03 T |  | Peak field (T) | 12.81 | 10.68 | 10.82 | 10.58 | 10.48 | 10.38 | 16.18
 |  |  | LL ratio (%) | 77.66 | 75.61 | 77.56 | 76.15 | 78.45 | 77.87 | -
Peak field | 16.74 T |  | Blocks | Block 8 | Block 9 | Block10 | Block11 | Block12 | Block13 | Block14
 |  |  | Peak field (T) | 15.98 | 16.18 | 15.95 | 16.64 | 16.25 | 16.74 | 16.56
Harmonics | Max: 5.27 U |  | b3: -4.4 | b5: -5.27 | b7: -0.3 | b9:-1.62 | a2:-1.15 | a4: 2.77 | a6:-0.95 | a8:-0.15
Main parameters of LPF3

## Slide 6
Electromagnetic design of LPF3 – HTS insert
Block with SC
The angle between the flux direction and the tape wide surface has been optimized
The effect of persistent current has also been analyzed and optimized
Harmonics | b3 | b5 | b7 | b9 | a2 | a4 | a6 | a8
Unit | -3.2 | -7.7 | -3.8 | -0.9 | 0.9 | -5.5 | -2.5 | -0.6

## Slide 7
Mechanical design of LPF3
Magnet structure
Stress distribution in different loading steps
After assembly at RT: Peak stress on shell- 128 Mpa; On rod- 468 Mpa; On coils- 28.1 Mpa
Cooling down at 4.2 K: Peak stress on shell- 215 Mpa; On rod- 618 Mpa; On coils- 72.3 Mpa
Excited to 13 T: Peak stress on shell- 218 Mpa; On rod- 612 Mpa; On coils- 93 Mpa

## Slide 8
A simplified circuit was established in COMSOL
A 1-dimensional adiabatic model was established
Varistor and heaters are applied to the quench protection of LPF3
Quench protection analysis
Simplified circuit
 | Thickness of stainless steel /μm | Resistance/Ω | Power（W/cm^2) | Charging voltage/V | Resistivity
coil1 | 50 | 2.505 | 50 | 389.76 | 0.5μΩ·m
coil2 | 100 | 1.698 | 50 | 339.6 | 
coil3 | 100 | 1.878 | 50 | 375.6 | 
Parameter of heaters
Main parameter of the magnet
Heaters
Temperature distribution near hot spots
The calculation indicates that the temperature of hot spot is 237 K and the max voltage is 952 V. Safe.

## Slide 9
Fabrication status of LPF3
Nb3Sn Rutherford cable fabrication
Coil fabrication
Heat treatment test
Inner splice soldering
Pre-assembly
Nb3Sn Rutherford cable has been fabricated for LPF3
A dummy coil has been fabricated and heat treated to test the furnace property
The inner joints fabrication test and the pre-assembly of LPF3 has been carried out.
The coils of LPF3 is under construction and the fabrication of the LPF3 is expected to be competed in July.

## Slide 10
02
中科院高能所超导磁体组
Superconducting Magnet Group, IHEP
Conceptual design of the 16-T dipole magnet with CCT coil configuration

## Slide 11
Designing a 16 T CCT Dipole with four coil modules
Module No. | Tilt angle | Inner Radius [mm] | Outer Radius [mm] | Slot width [mm] | Slot depth [mm] | Strand number | Pitch [mm] | Turn No. | Coil length [m] | Strand length [km] | Peak field [T]
1 | 15° | 30 | 68.6 | 2 | 16.8 | 40 | 12 | 88 | 1.36/1.51 | 5.9 | 16.2
2 | 22.5° | 69.6 | 103 | 2 | 14.2 | 34 | 7.2 | 145 | 1.43/1.51 | 10.3 | 14.7
3 | 29° | 104 | 127.6 | 2 | 9.3 | 22 | 5.5 | 193 | 1.46/1.51 | 9.9 | 13.1
4 | 34° | 128.6 | 159 | 2 | 12.7 | 30 | 4.5 | 234 | 1.46/1.51 | 18.2 | 11.3
Iron York | \ | 180 | 300 | \ | \ | \ | \ | \ | 1.6 | \ | \
High lights:
Canted-Cosine-Theta (CCT) technology;
  Superior field quality;
  Stress management
  Developed industrial assembly line;
Graded Nb3Sn Rutherford cables;
Multiple replaceable coil modules;
Major Geometry Parameters (To be optimized)
The geometry of the 4 module CCT magnet
BI
BO
BM
Ribs
Spar
CCT subscale

## Slide 12
Designing a 16 T CCT Dipole with four coil modules
At 4.2 K, the magnet produces 16 T at 100% of the load-line, with 8.8 kA operating current.
Field distribution at the middle cross section
Load-line of the 4 coil modules

## Slide 13
Harmonics： 10-4 | b2 | a2 | b3 | a3 | b4 | a4 | b5 | a5 | b6 | a6 | b7 | a7 | b8 | a8
Cross section-2D | 0.6259 | 0.0119 | 2.9824 | -0.0006 | 0.0537 | 0.0002 | 0.5189 | 0.0002 | 0.0183 | -0.0020 | -0.0845 | 0.0016 | -0.0036 | 0.0009
Integrated-3D | 1.5989 | 0.0101 | 3.8649 | -0.0320 | 0.3047 | 0.0802 | 1.4069 | -0.0175 | 0.0750 | -0.3695 | 0.1163 | 0.0734 | -0.0223 | -0.2090
The CCT magnet has an intrinsic good field quality
Designing a 16 T CCT Dipole with four coil modules
High-order harmonics along axis - Bn
High-order harmonics along axis - An

## Slide 14
03
中科院高能所超导磁体组
Superconducting Magnet Group, IHEP
Development status of the HTS transposed cable

## Slide 15
Recent progress of HTS transposed cable
Time chart of research progress of transposed cables
Cable design
Schematic illustration of the transposed cable and the fabrication steps
The advantages of the designed cable:
High current-carrying compacity
Low dynamic loss
High mechanical stability
Dynamic loss of transposed cable
Figure 3. (a-c) Hysteresis loss and coupling loss of the X-cable at different magnetic field change frequencies and contact resistances.
(d-f) Dynamic loss of the X-cable and the simple stack with the same cross-section and current-carrying capacity as X-cable at different magnetic field change frequencies and contact resistances.

## Slide 16
Recent progress of HTS transposed cable
IBS transposed cable
REBCO transposed cable
strand
cable
heat treatment
Terminal fabrication
test
The measured V-I curves of the IBS transposed cable
The measured V-I curves of the REBCO tapes in the four samples cut from the prototype cable
10-m cable samples were firstly fabricated
Most of the tapes extracted from the cable showed almost no degradation.

## Slide 17
04
中科院高能所超导磁体组
Superconducting Magnet Group, IHEP
Development status of the high field IBS coils

## Slide 18
Zhan Zhang et al 2021 Supercond. Sci. Technol. 34 035021
Development of Racetrack Coils with 100-m Long IBS Tapes
Two racetrack coils have been made using the 100 m length IBS tapes. The coils reached 86.7% of critical current of the short sample at 4.2 K and 10 T with highest compressive stress over 100 MPa.
Wang, et al., Supercond. Sci. Technol,. 2019(32) 04LT01
Ic of the IBS coil at 24 T reach 40% of that at zero magnetic field.
The IBS is promising for the high-field magnet application.

## Slide 19
Development of IBS solenoid pancake coils
Effect of bending before annealing on the Ic of IBS tapes
The attenuation curve of Ic with decreasing bending diameters for IBS tapes was obtained.
Cracks appear regularly in part of the superconducting cores under tensile stress.
Chunyan Li et al IEEE TAS, VOL. 32, NO. 6, 2022

## Slide 20
Development of IBS solenoid pancake coils
First Performance Test of IBS Solenoid Coil under 32 T
The Ic value for Φ34mm-17 turns-DPC is 60 A under 4.2 K and 32 T, which is a new breakthrough！
Ic measurement at 32 T
IBS coil with balloon ends are under construction.
Ic: 75A

## Slide 21
05
中科院高能所超导磁体组
Superconducting Magnet Group, IHEP
Performance study of a new epoxy resin IR-3 for high field applications

## Slide 22
Background
Fig.1 Chemical structures of components of IR-3.
Fig. 2. Thermal shock samples of (a) IR-3 and (b) CTD-101K.
Fig. 3. (a) Pot life and (b) DSC curves of IR-3 and CTD-101 K.
Fig. 4. The (a) tensile, (b) Compressive, and (c) Impact strength of IR-3 and CTD-101K at 77 K after Co-60 γ radiation.
Can IR-3 be used in ReBCO superconducting coils ?
Almost all epoxy materials have to be imported.
For ReBCO coated conductors, epoxy impregnation often leads to performance degradation.
An appropriate epoxy formulation is therefore urgently required to prevent degradation.
Fig.1 Structure of ReBCO.
Cleavage
Stress
< 1 MPa
Conductor
Epoxy
Transverse tensile Stress
<10 MPa
… …
Fig.2 Performance degradation of ReBCO.
Low viscosity
High crack resistance
Good mechanical properties
Sufficiently radiation resistant
Long pot life
Advantage
of IR-3

## Slide 23
Performance of IR-3 impregnated ReBCO double-pancake coils
Fig.1. (a) Coil tooling, (b) Stainless-steel (SS) co-wound coil, and (c) Kapton insulation (KI) coil.
(a)
(b)
(c)
Table 1. Parameters of the SS ReBCO coils.
Fig.2. Cool-down tests
Fig.4. Ic of KI coils
Table 2. Parameters of the KI ReBCO coils.
Fig.3. Ic of SS coils
Fig.5.Thermal cycle of SS coils
Fig.6.Thermal cycle of KI coils
Fig.7.Over-current test results of KI coils
Fig.9. Analysis result for the radial stress.
Fig.8. Ic tests at 4.2K under (a) 5T and (b) 10T.
At 77 K in self-field, after thermal cycle tests, and at 4.2 K even to 10 T under about 15 Mpa tension stress, the IR-3 impregnated coils can avoid performance degradation.
IR-3 impregnated coil enabled the best cooling performance and the IR-3 impregnated coil showed superior electrical and thermal stabilities.

## Slide 24
Performance of IR-3 impregnated ReBCO balloon-end coils
At 77 K in self-field, the IR-3 impregnated SS and KI ReBCO double-pancake coils can avoid performance degradation.
Upper layer
Lower layer
Table 1 Parameters of the Balloon-end ReBCO coil
Fig.4. Ic test of SS coil at 77K (a) before and (b) after IR-3 impregnation
(a)
(b)
Fig.1. Coil tooling and schematic diagram
Fig.2. Schematic distribution of voltage tapes on the coil.
Fig.3. Ic test at 77 K.
Fig.5. Process of IR-3 impregnation
(b)
(a)
Fig.6. Ic test of KI coil at 77K (a) before and (b) after IR-3 impregnation

## Slide 25
06
中科院高能所超导磁体组
Superconducting Magnet Group, IHEP
Development status of the HL-LHC CCT series magnets

## Slide 26
Development of CCT dipole magnets for HL-LHC
Fabrication of a full size prototype magnet MCBRDP2 was completed in May, 2020. Both apertures reached the ultimate current.
MCBRDP2
MCBRD02
MCBRD01
The first set of CCT superconducting magnets MCBRD01 with satisfactory field strength and field quality, has been shipped to Europe in October, 2021.
The assembly of the 2nd set of HL-LHC CCT superconducting magnets has been finished in Jan, 2022, and now the magnet is tested at IMP

## Slide 27
Development of CCT dipole magnets for HL-LHC
2+9 apertures has been fabricated. Most of them can reach the design current, but with very long training history.
From CB09 an important modification to the design has been adopted, to improve the training performance of the CCT coils
CB05 and CB09 will be tested at IHEP next week
Test results of coils CB01 to CB06
CB05 and 09 ready for stand-alone test at IHEP

## Slide 28
中国科学院高能物理研究所
Institute of High Energy Physics, CAS
中科院高能所超导磁体组
Superconducting Magnet Group, IHEP
Summary
As the next step of the high field accelerator magnet R&D, a 16-T dipole magnet named LPF3 has been designed and is under fabrication now.
As a candidate, a 16-T dipole magnet with CCT coil configuration has been proposed with lots of potentials.
The new HTS transposed cable under development shows promising performance for high field applications
Ic of the Iron-Based Superconducting coils reached 60 A at 32 T background field, a new breakthrough!
2 series plus 1 prototype CCT magnets have been developed for the HL-LHC project at CERN. The others are under fabrication. An important modification to the design has been adopted from CB09 to improve the training performance of the CCT coils

## Slide 29
Thanks for your attention!