## Slide 1: Improvement to the vacuum status by NEG coating as the solutions for the high lumi. Z & tt operation
Yongsheng Ma
2022.3.25

## Slide 2: outline
Problem in vacuum of electron ring
Solution: Al vacuum chamber NEG coating

## Slide 3: Preview of CEPC vacuum system
 | Material | Vacuum/ Torr | Cross Section
Booster | Extruded aluminum 6061 | 3 × 10-8 | φ56
Electron Ring | Extruded aluminum 6061 | 3 × 10-9 | 56×75 to φ56
Positron Ring | Extruded copper, NEG film |  | 56×75 to φ56
MDI | Copper/tungsten alloy, NEG film | 3 × 10-10 | φ20
Vacuum of Electron Ring 6m long pipe
 | E | I | ρ
 | Gev | A | m
Higgs | 120 | 0.0167 | 10700
W | 80 | 0.084 | 10700
Z | 45.5 | 0.803 | 10700
tt | 180 | 0.0033 | 10700
Machine and Vacuum Parameters
CDR Vacuum requirements
Notes: Vacuum of Booster 、storage ring, MDI are all considered and under technical design. Conventional technical such as ion pump /Al will be used in CEPC. There is no especial issue exceed our control, except to balance the impedance and gas absorb ability of NEG film

## Slide 4
[4] MALYSHEV O B. Vacuum in Particle Accelerators [J]. 2020,
PSD （photon-stimulated desorption）as a Function of Critical Energy of SR
 | E | PSD
 | Gev | molecules/photon
Higgs | 120 | 2.00E-05
W | 80 | 1.00E-05
Z | 45.5 | 4.00E-06
tt | 180 | 1.35E-03
Problem

## Slide 5
CEPC 30MW |  |  |  |  |  |  |  |  |  |  | 
 | E | I | I | ρ | Psr | PSD | qtd | qlsr | q | Ps | Pmax
 | Gev | A | A | m | MW | molecules/photon | Torr·L/s·cm2 | Torr·L/s·cm2 | Torr·L/s·cm2 | L/s | Torr
Higgs | 120 | 0.0167 | 0.0167 | 10700 | 28.64 | 2.00E-05 | 1E-12 | 8.21E-12 | 9.21E-12 | 100 | 4.40E-09
W | 80 | 0.084 | 0.084 | 10700 | 28.46 | 1.00E-05 | 1E-12 | 2.75E-11 | 1.48E-11 | 100 | 7.06E-09
Z | 45.5 | 0.803 | 0.803 | 10700 | 28.47 | 4.00E-06 | 1E-12 | 1.50E-10 | 3.09E-11 | 100 | 1.48E-08
tt | 180 | 0.0033 | 0.0033 | 10700 | 28.65 | 1.35E-03 | 1E-12 | 2.43E-12 | 1.65E-10 | 100 | 7.90E-08
CEPC 50MW |  |  |  |  |  |  |  |  |  |  | 
 | E | I | I | ρ | Psr | PSD | qtd | qlsr | q | Ps | Pmax
 | Gev |  | A | m | MW | molecules/photon | Torr·L/s·cm2 | Torr·L/s·cm2 | Torr·L/s·cm2 | L/s | Torr
Higgs | 120 |  | 0.029 | 10700 | 49.74 | 2.00E-05 | 1E-12 | 1.43E-11 | 1.53E-11 | 100 | 7.29E-09
W | 80 |  | 0.147 | 10700 | 49.80 | 1.00E-05 | 1E-12 | 4.82E-11 | 2.51E-11 | 100 | 1.20E-08
Z | 45.5 |  | 1.39 | 10700 | 49.27 | 4.00E-06 | 1E-12 | 2.59E-10 | 5.28E-11 | 100 | 2.52E-08
tt | 180 |  | 0.0054 | 10700 | 46.89 | 1.35E-03 | 1E-12 | 3.98E-12 | 2.70E-10 | 100 | 1.29E-07
[4] MALYSHEV O B. Vacuum in Particle Accelerators [J]. 2020,
No NEG coating
The requirement of vacuum value of Vacuum life time is 3×10-9 Torr
PSD （photon-stimulated desorption）& TD （thermal desorption）

## Slide 6: Molflow module of vacuum pipe
Solution: Al vacuum chamber NEG coating
30MW tt
50MW tt
Sticking factor is 0.002 (pumping speed H2 is 0.088L/s·cm2)
Al vacuum chamber NEG coating
Activation temperature do not permit to exceed 180 ℃；
Pump, gauge
the mechanical stress and deformation due to a 200 °C bake were well within acceptable limits from ESRF tests. [5]
[5] KERSEVAN R. PERFORMANCE OF A NARROW-GAP, NEG-COATED,EXTRUDEDALUMINIUM VACUUM CHAMBER AT THE ESRF [J]
50MW tt

## Slide 7: Pumping speed test of NEG coating
Life time test of NEG coating in Beijing
1 um

## Slide 8
Chart: Activation cycles No.
No63（2）氮气保存11个月 | 0 | 0.1 | 0.14 | 0.2 | 0.21 | 0.23 | 0.27 | 0.28 | 0.33 | 0.37 | 0.39 | 0.45 | 0.45 | 0.45 | 0.46 | 0.46 | 0.53 | 0.55 | 0.56 | 0.59 | 0.6 | 0.59 | 0.59 | 0.6 | 0.66 | 0.59
No63（3）氖气保存7个月 | 0 | 0.1 | 0.15 | 0.15 | 0.18 | 0.19 | 0.2 | 0.2 | 0.27 | 0.29 | 0.31 | 0.32 | 0.38 | 0.38 | 0.4 | 0.38 | 0.46 | 0.29 | 0.35 | 0.37 | 0.36 | 0.37 | 0.46 | 0.46 | 0.45
No63（2）低真空度激活降温立刻测 | 0.3
激活温度 | 160 | 180 | 180 | 180 | 180 | 180 | 180 | 180 | 200 | 200 | 200 | 200 | 200 | 200 | 200 | 200 | 225 | 225 | 225 | 225 | 225 | 225 | 225 | 250 | 250 | 250
No63（2）降温27小时后测
150h
130h
140h
140h
After 11 months N2 storage
After 7 months Ne storage
Absorbing speed of NEG coating at different activation temperature vs time

## Slide 9
NEG coating | Total length | Price | Cost
TiZrVHf | m | CNY/m | Million CNY
1:1:1:1 | 100,000 | 0.15 | 150
Cost increase due to NEG coating of electron ring

## Slide 10
Thank You