## Slide 1
SYNTHESIS, STRUCTURE AND CONDUCTIVITY OF NOVEL ANTIPEROVSKITE Na3(H)(SO4) AND Na3(NH2)(SO4) AS SOLID ELECTROLYTES IN BATTERIES
KOEDTRUAD Anucha

## Slide 2
All-solid state batteries
High bulk ionic conductivity
(> 10-4 S/cm)
Compatibility with a positive electrode and negative electrode
Stability against ambient atmosphere and high voltage
Low electronic conductivity
Required properties for solid electrolytes
Anode
Cathode
Cathode
Anode
Solid Electrolyte
Ref: Wu, B.; Wang, S.; Xiao, J. J. Mater. Chem. A, 2016, 4, 15266 - 15280.
A solid electrolyte is considered a key factor for efficient all-solid stae batteries
2

## Slide 3
The reported results are limited with oxide-based antiperovskites.
Rotational dynamics of cluster anions facilitate ionic mobility
Na3OBH4
Na3ONO2
Ref: J. Am. Chem. Soc. 2019, 141, 5640−5644
Ref: J. Mater. Chem. A, 2020, 8, 21265–21272
3
Na3OX
(X = Cl, Br, BH4, NO2, SO4)
Solid Electrolytes

## Slide 4
[1] J. Mater. Chem. A, 2019, 7, 21985
[2] Energy Storage Materials, 2020, 31, 87-94
This work
Novel Na3(H)SO4 and Na3(NH2)(SO4) antiperovskites
Na3(F/Cl)(SO4)
Solid Electrolytes
Stable structure and good Na-conductivity
- Ionic size
- Weak ionic H-Na bond
- Local dynamics of H
4
 | Ea (eV) | σ (mS/cm) at 300 K
Na3(F0.5Cl0.5)(SO4) | 0.21 | 1.086
Na3(Cl)(SO4) | 0.2 | 2.328
Calculated Ea and conductivity of Na3(F/Cl)(SO4)

## Slide 5
Materials Synthesis and Characterization
Synthesis
High Pressure High Temperature Technique
1 GPa
200 – 400 C
Na2SO4
NaNH2/NaH
Characterization
-Phase identification by laboratory XRD,
-Detailed structure analysis by synchrotron XRD and neutron diffractometry
-Conductivity by impedance spectroscopy
5

## Slide 6
Structure analysis with synchrotron XRD data
Na3(H)(SO4)
Tetragonal, P4/nmm
Rwp = 11.67
Na3(H)(SO4) = 88% wt
Na2SO4 = 12%wt
Na3(NH2)(SO4), Tetragonal, P4/nmm
Na3(NH2)(SO4) = 96% wt
Na2SO4 = 4%wt
Rwp = 13.69
Na
SO4
H/NH2
Typical RT SXRD patterns of Na3(H)(SO4) and Na3(NH2)(SO4), and their refinement results
Proposal No. | 2021B1437
Proposal Title | Study of the structure behavior of Na-ion conducting Na3(H)(SO4) and Na3(NH2)(SO4) antiperovskites
Beamline | BL02B2 at SPring-8, Japan
6

## Slide 7
Both compounds are thermally stable: Na3(H)(SO4) ~ 207 C, Na3(NH2)(SO4) ~147 C
27 oC
47 oC
67 oC
87 oC
107 oC
127 oC
147 oC
167 oC
187 oC
207 oC
Na3(H)(SO4)
Typical temperature-variable SXRD
Structure analysis with synchrotron XRD data
Temperature-dependent lattice parameters of the compounds
Na3(H)(SO4)
Na3(NH2)(SO4)
7

## Slide 8
Structure analysis with neutron diffraction data
MEM analysis will be implemented to get visualization of Na, H and NH2 dynamics
Correlation between H/NH2 dynamics and Na-mobility will be discussed with NPD
Proposal No. | 2022A0055
Proposal Title | Study of the H and NH2 dynamics in Na3(H)(SO4) and Na3(NH2)(SO4) antiperovskites as solid electrolytes for Na-ion batteries
Beamline | BL-09 SPICA at J-PARC
Na3(H)(SO4), RT
Tetragonal, P4/nmm
Na3(H)(SO4) = 91% wt
Na2SO4 = 9%wt
Rwp = 3.75
d
Na
SO4
H
Na3(H)(SO4): RT and 200 C
Na3(H)(SO4): RT and 150 C
8

## Slide 9
Summary
The compounds were successfully prepared by a high pressure high temperature technique
Their phases and detailed antiperovskite structure were confirmed with SXRD and NPD techniques
The compounds show good thermal stability
The ionic conductivity will be next measured, and the conduction pathway/mechanism and structure-property relationship will be discussed with SXRD and NPD data
Novel Na3(H)(SO4) and Na3(NH2)(SO4) have been studied for solid electrolytes in batteries
9