## Slide 1: CEPC SRF Cavities Studies Peng Sha (IHEP) The 2022 International Workshop on the High Energy Circular Electron Positron Collider

## Slide 2
Specifications of CEPC cavities: Extremely high Q & Eacc
1.3 GHz 9-cell cavity
650 MHz 2-cell cavity

## Slide 3: Outline
1.3 GHz cavity
650 MHz cavity
Nb3Sn cavity
Conclusion

## Slide 4
1.3 GHz 1-cell cavities nitrogen doped
“3/60” recipe is adopted for nitrogen doping. 2.6E10@30MV/m has been achieved for 1.3 GHz 1-cell.
Vertical test results of 1.3 GHz 1-cell cavities
XPS
XRD
Depth profile
NIM A 993 (2021) 165080

## Slide 5
Mid-T furnace baking of 1.3 GHz 9-cell cavities
N5 - N10 (in 2020)
N11 - N16: only one EP (in 2022)
Simplification
Supercond. Sci. Technol. 34 (2021) 095005

## Slide 6
Vertical test results of 1.3 GHz 9-cell cavities
Vertical test results of 1.3 GHz 9-cell cavities at IHEP
First batch (6 cavities): N5-N10
Four cavities (N5/7/9/10) delivered to SARI in early 2022 for SHINE prototype high Q cryomodule assembly
Second batch (6 cavities): N11-N16
Best Cavity (N11): 4.6E10@21 MV/m, 4.3E10@31MV/m
One of the best high Q 1.3 GHz 9-cell cavities and cavity batches in the world.
Will install to high Q cryomodule at IHEP PAPS for DALS R&D
2 K VT | 1st batch average | 2nd batch average
Eacc (MV/m) | 24 | 27.7
Q0@16 MV/m | 3.8E10 | 4.1E10
Q0@21 MV/m | 3.8E10 | 4.1E10

## Slide 7: Outline
1.3 GHz cavity
650 MHz cavity
Nb3Sn cavity
Conclusion

## Slide 8
650 MHz 2-cell cavities BCP processed (1)
Three 650 MHz 2-cell cavities were fabricated, buffered chemical polished (BCP) and tested, which all exceeded 3E10@20MV/m.
BCP
Inspection
Vertical test
Vertical test results of 650 MHz 2-cell cavities

## Slide 9
650 MHz 2-cell cavities BCP processed (2)
All the three 2-cell cavities were welded with helium vessel, two of which have been integrated into a 650 MHz test cryomodule at PAPS.
2-cell cavities jacketed
650 MHz test cryomodule for CEPC
Cavity string

## Slide 10
650 MHz 2-cell cavities BCP processed (3)

## Slide 11
CEPC 650 MHz single-cell cavities
Cavity | Before May, 2022 |  | After May, 2022 | 
 | Process | Result (Q0 at max Eacc) | Process | Result (Q0 at max Eacc)
650S4 (Fine Grain) | Bulk BCP 200 um + 800C 3h + light BCP 30 um + Light EP 20 um + 950C 3h + light EP 20 um (17.5 °C) + mid-T furnace baking (300C 3h) | 7.6E10@ 24MV/m | Cold EP 30 um (12 °C) + 2-step low-T baking (75C 4h + 120C 48 h) | 1.6E10@ 42MV/m
650S5 (Fine Grain) | Bulk BCP 200 um + 800C 3 h + light BCP 30 um + EP commissioning 215 um + bulk EP 100 um (17.5 °C) + 900C 3h + mid-T furnace baking (300C 3h) | 1E11@ 20MV/m, 6.3E10@ 31MV/m | Cold EP 30 um (12 °C) + low-T baking (120C 48 h) | 2.3E10@ 42MV/m

## Slide 12
Mid-T furnace baking
Mid-T furnace baking of 650 MHz
single-cell cavity
Vacuum, temperature and RGA during mid-T furnace baking

## Slide 13
Cold EP
More uniform removal achieved by cold EP.
The average removal at the equators (3, 4) is 71% of beam pipes (1, 6) during the EP process (17.5 °C) in 2021, while 75% is perfect.
The average removal at the equators (3, 4) is 86% of beam pipes (1, 6) during the EP process (12 °C) in 2022.
Red arrows and numbers indicate the locations for thickness measurements
Surface removal of the EP
(17.5 °C) in 2021
Surface removal of EP
(12 °C) in 2022
EP of 650 MHz
single-cell cavity

## Slide 14
Vertical test results of CEPC 650 MHz single-cell cavities. The max Eacc was limited by quench during the tests.
CEPC 650 MHz single-cell cavities
Bpeak=176mT!

## Slide 15
Cover Article for NST 2022 issue 10
P. Sha et al., NUCL SCI TECH 33, 125(2022)

## Slide 16: Nitrogen doping
Two 650 MHz single-cell cavities have received nitrogen doping, “3/60” recipe was adopted.
Nowadays, the cavities nitrogen doped are awaiting for the light EP, which have been delayed because of the COVID-19.
Nitrogen doping of 650 MHz single-cell at the same furnace as well as mid-T furnace baking

## Slide 17: Outline
1.3 GHz 9-cell cavity
650 MHz cavity
Nb3Sn cavity
Conclusion

## Slide 18
A small furnace for Nb3Sn film coating was developed at IHEP. Nb3Sn film is coated with 1.3 GHz 1-cell niobium cavity by vapor diffusion.
Setup
Furnace for Nb3Sn coating.
Curve of coating process

## Slide 19
Samples were used for microscopic analysis, which showed formation and superconducting transition of Nb3Sn.
Microscopic analysis
Nb3Sn grain (SEM)
1
2
3
4
#1: Tc0 = 18.03K
#2: Tc0 = 17.78K
#3: Tc0 = 17.96K
#4: Tc0 = 17.87K
Samples position
TC of Nb3Sn (R-T)

## Slide 20
Max gradient: 5~7 MV/m; Max Q: ~3E9 (@4.2K). The coating process still needs optimization.
Various cooling rates were tried, which demonstrated very different results. It verified that slow and uniform cooldown resulted in high Q and low surface resistance of Nb3Sn cavity.
1.3 GHz 1-cell Nb3Sn cavities
Physica C: Superconductivity and its applications 600 (2022) 1354107
Before Nb3Sn coating
After Nb3Sn coating
4.2 K
Vertical test results of 1.3 GHz 1-cell Nb3Sn cavities

## Slide 21
Conclusion
The CEPC superconducting cavities are keeping up with state-of-the-art SRF over the world. World-leading 650 MHz and 1.3 GHz superconducting cavities with High Q and high Eacc have been achieved successfully.
New and novel technology are applied: mid-T furnace baking, cold EP, large grain niobium, nitrogen doping/infusion, etc. Nb3Sn coating has gained preliminary progress.
Sergey Belomestnykh and Hans Weise, SRF activities discussed within Snowmass and European HEP strategy process - TTC Aomori, Oct 2022

## Slide 22: Thanks for your attention!