## Slide 1: Low gain Avalanche diode (LGAD) for 4D-tracking
M. Ferrero
INFN Torino
The 22 International Workshop on the High Energy Electron Positron Collider
PRIN
4DInSiDe
Extensive collaboration with other groups and with the RD50 CERN collaboration

## Slide 2
Outline
Basic concepts for an excellent timing
Basic concepts on Low Gain Avalanche Diode (LGAD)
Design innovations in LGAD:
  LGAD optimized for timing
  LGAD for High irradiation level ( > 1015 neq/cm2)
  LGAD with high fill factor: trench-isolated LGAD (TI-LGAD)
  LGAD with 100% fill factor: AC-Coupled Resistive Silicon Detector (RSD)
  Materiel budget
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 3
Time-tagging detector
The time of arrival is set when the signal crosses the comparator threshold
Time Performance depends on:
Characteristic of the signal at the output of the preamplifier
Preamplifier noise
TDC binning
Strong interplay between the sensor and the read-out electronic
Sensor
Read-out electronic
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 4
Temporal resolution, the key ingredients
+
Negligible compared with other terms
The Noise induces amplitude variation around the comparator threshold
Large and fast signal with moderate noise is needed:
  Need moderate internal gain
  Need sensors with thin active thickness
Amplitude and signal shape variations due to non homogeneous energy deposition
Signals as uniform as possible
Ramo’s theorem 
Saturated drift velocity of charge carriers
 Electric field > 30 kV/cm
Weighting field as uniform as possible
 parallel plate geometry
Amplitude variation
Shape distortion
Not uniform Ionization fixes the low limit to time resolution
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 5
Traditional silicon sensors vs Low Gain Avalanche Diode
The gain layer:
a parallel plate capacitor with high field
zoom
Drift area with gain
0.5 – 2 mm long
E field Traditional silicon sensors Low Gain Avalanche Diode E field
p+ implant creates a high electric field underneath the Junction (~300kV/cm), that accelerates electrons enough to start avalanche multiplication (same principle of APD but with much lower gain)
The moderate gain allows:
Segmentation of the readout pattern
Shot noise below the electronic noise
The moderate gain in a high resistivity thin bulk (50 µm) is the key point to excellent temporal resolution ()
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 6
LGADs’ manufacturers
CNM (National Center of Micro-electronics de Barcelona), first time producer of LGADs:
 300 µm-thick LGADs in 2014 (4’’ wafer)
 50 µm-thick LGAds in 2015 (4’’ and 6’’ wafer)
HPK (Hamamatsu Photonics):
 50 µm-LGADs from 2018 (four batches on 6’’ wafer)
FBK (Fondazione Bruno Kessler):
 300 µm-thick LGADs in 2016 (6’’ wafer)
 50 µm-thick LGADs in 2017 (nine batches on 6’’ wafer):
      LGADs radiation resistant up to 1015 neq/cm2 (carbonated LGADs from 2018)
      LGADs with resistive read-out (from 2019)
      Trench-isolated LGADs (2021)
      LGADs for Extreme fluences ( > 1015 neq/cm2), Q4/2022
IHEP-IME (Institute of High energy Physics - Institute of Microelectronics of the Chinese Academy of Sciences):
   Carbonated LGADs (three batches on 6’’ wafer from 2020):
TELEDYNE
 50 µm-thick LGADs in 2021
MICRON
   Low material budget 50 µm-thick LGADs in 2021
Foundries involved in sensors prototyping for MIP Timing Detector (MTD) of CMS and High Granularity Timing Detector of ATLAS (HGTD)
First LGADs produced by CNM in 2014
UFSD4 production by FBK (2021)
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 7
Strategies in gain layer design
Each foundry developed its own gain layer design
The gain layer design affects:
behaviour and the radiation resistance of LGADs
uniformity of the production
cost of the production
E field
E field
E field
Broad
Shallow
Deep
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 8
Temporal resolution in LGADs sensors
Silicon sensors without gain
50 µm thick LGADs reach 30-35 ps of temporal resolution
25 ps
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 9
State of the art of temporal resolution in LGADs sensors
Current sensors choice for timing detector of CMS and ATLAS
Hundreds of measurements demonstrate the temporal capability of 50µm-thick LGADs
50 µm thick LGAD is a reliable technology developed by several foundries in dozes of batches from 2015
Spread due to different gain layer designs
Temporal resolution at -30°C on unirradiated LGADs
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 10
Radiation resistance
Three main effects caused by radiation in silicon sensors:
Increased leakage current and shoot noise
Decrease of charge collection efficiency due to charge trapping
Variation in doping concentration (acceptor creation and removal)
The main effect in LGADs is the acceptor removal into the gain layer
Acceptor removal,
internal gain decrease
Reduction of the gain doping, decreasing the internal gain
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022
Carbon implantation in the volume of the gain layer decreases the acceptor removal
The right dose of carbon improves the radiation resistance of gain layer by a factor 3

## Slide 11
Performance of irradiated LGADs
new
8E14 neq
1.5E15 neq
2.5E15 neq
new
8E14 neq
1.5E14 neq
2.5E15 neq
Example of carbonated LGAD irradiated wit neutrons
Carbonated LGADs:
Unchanged temporal resolution (30 ps) up to 1-2E15 neq
Charge provided > 5 fC up to 2.5-E15 neq
Current electronics achieve the best temporal performance for total charge > 5fC
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 12
Pixelated LGAD and large device
p-stop
VBias
p bulk
oxide
Gain layer
JTE
No gain
50-100 mm
JTE
No gain region
Traditional LGAD
Pixel edge:
JTE: junction termination extension
p-stop
No-gain region of 50-100 µm
 not suitable for small pixel
HPK2
16x16 array
2.1 cm
Mature technology to cover large area
ATLAS and CMS timing detectors will cover 20-30 m2.
Sensor production will start in 2024.
Sensor prototype for ATLAS HGTD and CMS MTD
16 x 16 array; pitch 1.3 mm;
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 13
LGAD with very high fill factor: Trench isolated LGAD
p-stop
VBias
p bulk
oxide
Gain layer
JTE
No gain
50-100 mm
JTE
trench
VBias
p bulk
oxide
Gain layer
JTE
trench
No gain
5-10 mm
No gain region
No gain region
Traditional LGAD
Trench Isolated LGAD
Pixel edge:
JTE: junction termination extension
p-stop
No-gain region of 50-100 µm
 not suitable for small pixel
Pixels isolation with deep trenches
No-gain region of 5-10 µm
 Suitable for small pixel and high
occupancy
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 14
LGAD with very high fill factor: Trench isolated LGAD
Deep trench, < 1 µm wide filled with oxide
Excellent pixel-pixel isolation
Low inter-pixel capacitance (100 fF/mm)
Radiation resistant technology
  Neutron: up to 1-21015 neq/cm2
  X-Ray: up to 10 MRad
SEM image
250x375 µm2
Prototype od 2 pixels devices
Trench Isolated LGAD is a project of RD50 collaboration --- TI-LGAD produced by FBK
Pixel
Pixel
No gain
region
Charge injection
Position scanning
Collected charge [a.u.]
Scanning position [µm]
Fill factor > 80% for pixel pitch of 100 µm or wider
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 15
LGAD with 100% fill factor: Resistive Silicon Detector
p++ electrode
AC coupling oxide
Resistive n+ electrode
Gain layer
RSD is a new paradigm in the read-out of silicon sensors:
Continuous resistive n++ electrode
AC coupling read-out
Unsegmented gain layer to maintain 100%
Bipolar signal
Read out pixel
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 16
LGAD with 100% fill factor: Resistive Silicon Detector
RSD is a new paradigm in the read-out of silicon sensors:
Continuous resistive n++ electrode
AC coupling read-out
Unsegmented gain layer to maintain 100%
Bipolar signal
Particle
+
+
+
+
+
-
-
-
-
-
Typical RSD Signal
Positive lobe determined by AC coupling
Signal duration determined by resistivity of n++
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022
Two batches of RDS by FBK: i)RSD1 in 2019; ii)RSD2 in 2021

## Slide 17
Charge sharing in Resistive Silicon Detector
50 µm thick LGAD with Internal gain 20
Pad 1
Pad 2
Pad 4
Pad 3
0 2 4 6 8
Time [ns]
0 2 4 6 8 10
Time [ns]
0 2 4 6 8 10
0 2 4 6 8 10
60
40
20
0
-20
Amplitude [mV]
60
40
20
0
-20
60
40
20
0
-20
Amplitude [mV]
60
40
20
0
-20
1
2
4
3
P 1
Pad 1
Signal sharing between the four read-out pixels
RSD works as a current divider:
The signal sees parallel impedances between hit point and the read-out pixels
Signal is split according to Ohm’s law
Each pads get a fraction of the total signal
RSD is suitable for:
 tracking with excellent spatial
resolution
 low occupancy
Charge injection with IR laser pulse
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 18
Spatial resolution of RSD: laboratory setup
Laser beam
x-y stage
Particulars Transient Current Technique laser setup
IR pulsed laser (Pulse duration hundreds ps)
Laser beam size 10 µm
Movable x-y stage with 1 µm of precision
Sensors are read-out with 16-channe analogue board developed by FNAL
Signal acquired with 16-channel CAEN digitizer; sampling: 5 Gs/s
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 19
Spatial resolution of RSD: sensors
Pitch = 1300 mm
Pitch = 450 mm
200 x 340 mm2
Investigation of spatial resolution of RSD with crosses AC-electrode
FBK RSD2 production includes several different AC-pad geometries and pitch size
Read-out pixels
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 20
Spatial resolution of RSD: results
Chart: RSD2 crosses: spatial resolution for 4 different pitch sizes
| 29 | 53 | 69 | 154
1300 um | 95 | 50 | 33 | 15.4
450 um | 34 | 25.3 | 19.9 | 15.5 | 10.6 | 10.1 | 8.4 | 7.9 | 10.6
340 um | 44.8 | 34.1 | 21.87 | 19.9 | 13.85 | 12.8 | 10.6 | 7.4 | 6.33
200 um | 45.9 | 26 | 24.13 | 18.5 | 15.9 | 10.5 | 8.5 | 7.8 | 5.2 | 4.4
The effect of radiation on position resolution must be investigates
RSD provides excellent spatial resolution: 2-3% of the pitch size at gain 30
Position resolution comparison
RSD vs standard pixel
 | Pitch [µm] | Position resolution [µm]
RSD | 1300 | 40
 | 450 | 10
Standard pixel | 1300 | 920
Standard pixel | 450 | 320
 | Pitch [µm] | Position resolution [µm]
RSD | 1300 | 
 | 450 | 
Standard pixel | 1300 | 920
Standard pixel | 450 | 320
Position resolution in RSD is not given by the formula for binary read-out
Gain 30
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 21
RSD performance summary
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022
Unchanged temporal capability (
Position resolution improves as pitch decreases

## Slide 22
A complete new tracker based on RSD
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022
Standard Silicon Detector
Resistive Silicon Detector
Resistive implant
~ 50 mm
---
- --
++
+++
Pixel size
~ 250 x 250 mm2
Silicon bulk
Contacts
Electronics
~ 150 mm
Gain implant
--
---
- --
+
++
+++
Pixel size
~ 25 x 25 mm2
The innovative design of a tracker based on RSD
It delivers ~ 30 -40 ps temporal resolution
For the same spatial resolution, the number of pixel is reduced by 50-100
The electronic circuitry can be easily accomodated
The power consumption is much lower, it might even be air cooled (~ 0.1-0.2 W/cm2)
The sensors can be really thin

## Slide 23
Matching RSD capabilities with lepton colliders
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022
Internal gain
Thin
Low material budget
Large signals
100% efficiency
Excellent temporal precision
Resistive read-out
Continuous gain layer
100% fill factor
Signal sharing
Excellent spatial precision
Large pixels
Reduced power consumption
Space for electronics
Continuous cathode
Uniform weighting field
Uniform carriers drift velocity
Innovation
Sensor property
Experimental feature

## Slide 24
Front-end design for Resistive Silicon Detector
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022
Charge integrator
Trans-Impedance
ADC
Time over Threshold
Multiple
Time over Threshold
Wafeform sampler
Increasing power
(i) Excellent spatial resolution, very low material budget.
(II) Combined good spatial and temporal resolutions, moderate material budget.

## Slide 25
Summary on LGAD sensors families
 | Traditional LGAD (JTE/p-stop) | Trench isolated LGAD | Resistive silicon Detector
Fil factor 100% | No | Almost 100% | Yes
High occupancy | Yes | Yes | No
Excellent temporal resolution | Yes | yes | yes
Spatial resolution | No | Typical of pixel sensors | < 10µm with large pixels
Radiation hardness (up to 21015 neq) | Yes | Yes | Under investigation
 | Traditional LGAD (JTE/p-stop) | Trench isolated LGAD | Resistive silicon Detector
Fil factor 100% | No | Almost 100% | Yes
High occupancy | Yes | Yes | No
Excellent temporal resolution | Yes | yes | yes
Spatial resolution | No | Typical of pixel sensors | < 10µm with large pixels
 | Yes | Yes | Under investigation
Traditional LGAD
Trench isolated LGAD
Resistive Silicon Detector
Each design fulfils specific requirements
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 26
Material budget
~200 mm
50 mm
~150 mm
Present design: not optimized for material budget
Present design:
Sensors active thickness 50µm
thick “handle wafer” (handle wafer 200µm)
~10-20 mm
50 mm
~150 mm
Thinned handle wafer Handle wafer: 200 um  10-20 um
The tinning of handle wafer is a well know technology
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 27
Acknowledgement
We kindly acknowledge the following funding agencies, collaborations:
INFN - Gruppo V, UFSD, RSD and ExFlu projects
INFN – FBK agreement on sensor production (convenzione INFN-FBK)
Horizon 2020, grant UFSD669529
U.S. Department of Energy grant number DE-SC0010107
Dipartimenti di Eccellenza, Univ. of Torino (ex L. 232/2016, art. 1, cc. 314, 337)
Ministero della Ricerca, Italia , PRIN 2017, progetto 2017L2XKTJ – 4DinSiDe
Ministero della Ricerca, Italia, FARE, R165xr8frt_fare
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 28
Backup

## Slide 29
Shot noise and power consumption
Power consumption and shot noise can be mitigated operating thin sensors (small volume) a low temperature
Irradiation increases leakage current
Two component of the current:
Surface current
 Defects at the silicon-oxide interface
Bulk current
 deep levels generated by neutrons and charged particles
Power consumption
P =
Shot noise is due to excess noise factor
Oxide

## Slide 30
Effect of radiation on silicon sensors
Radiation creates defects that change macroscopic properties of the detector

## Slide 31
Main technique to decrease acceptor removal
Bs + I  Bi
Bi + O  BO
Acceptor removal mechanism
 Fluence
 Concentration of substitutional
acceptors
c  Acceptor removal coefficient
Carbon implantation in the volume of the gain layer decreases the acceptor removal
Cs + I  Ci replaces Bs + I  Bi
The right dose of carbon improves the radiation resistance of gain layer by a factor 3
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 32
LGADs for fluence in the interval 2-51015 neq/cm2
Carbon shield LGAD  Defect engineering strategy to enhance the gain layer radiation
resistance of carbonate LGAD up to 51015 neq/cm2
→ A Carbon shield will be infused below the carbonated gain layer volume to further protect it from the diffusion of defect complexes from the bulk region and the support wafer
A spray of Carbon will be introduced below the carbonated gain layer region to protect the gain layer atoms from defects moving towards the n++ electrode during process thermal loads or exposure to particle radiation
n++
p+
p
p++
Carbonated GL
Carbonated GL + Carbon Shield
n++
p+
p
p++
O2i
Carbon spay layer
Carbonated gain layer
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022

## Slide 33
LGADs for extremes fluences ( > 11016 neq/cm2)
Doping Profiles of gain layer from Process Simulation
× 4
× 5
Effective Doping
n+ p+ n p
1E+19
0
-1E+19
Higher the acceptor density,
lower the removal
Compensated LGAD:
Compensated gain layer implant to exploit the relationship between acceptor removal rate and doping concentration of boron atoms
Higher acceptor concentration  lower acceptor removal rate
Gain layer design based on compensation:
 doping of gain layer obtained by Phosphorus (n+) and
Boron (p+) implants
 Boron concentration > Phosphorus concentration
First batch of compensated LGAD will be delivered by FBK in November 2022
Marco Ferrero, INFN, CEPC2022 workshop, 24-28 October 2022