## Slide 1: Status and R&D plan of the CECP muon detector
Xiaolong Wang
Fudan University
CEPC Physics and Detector Plenary Meeting, 2022.7.13

## Slide 2: Scintillator based muon detector
Extruded scintillator
WLS fibre
SiPM
Front-end readout
R&D for readout system
  ASIC
  Chips
  Readout board
  DAQ

## Slide 3: NDL SiPM:
Looks good.

## Slide 4: New design on the FE and NDL SiPM
Laser pulse triggering
Very good p.e. peaks!
The preams are tuned at FDU for different kinds of SiPMs.
Laser source
SiPM

## Slide 5
Dark Count Rate
NDL-EQR15
Single p.e.：37.5mV
Threshold>6p.e. DCR<10 Hz
Threshold>7p.e. DCR<1 Hz

## Slide 6
New NDL SiPM with
HV：28 V
Keep laser constant
HV：30 V
HV/ V | Pedestal | ADC | of time difference
28 | 1.2 | 140，90 | 65
30 | 2.9 | 400,270 | 46
HV/ V | Pedestal | ADC | 
28 | 1.2 | 140，90 | 65
30 | 2.9 | 400,270 | 46
Time resolution =

## Slide 7
Saint_Gobain
Kuraray
Kuraray WLS fibre
Kuraray Y11 WLS, which is used in Belle II KLM.
, matching the MPPC surface well.
About 200 SiPMs arrived Fudan from KEK, along with the fibre.
 |  |  | Saint_Gobain |  |  | Kuraray |  | 
Position | Time | Scintillation sample | Entries | Mean | Entriesean | Entries | Mean | Entriesean
 | 1h | #1 | 10820 | 2617 | 2.83 | 12520 | 4892 | 6.12
 |  | #2 | 10657 | 2462 | 2.62 | 12507 | 5260 | 6.58
 | 10h | #1 | 5872 | 1883 | 1.10 | 6031 | 4216 | 2.54
 |  | #2 | 5838 | 2108 | 1.23 | 5998 | 4608 | 2.76
 |  |  | Saint_Gobain |  |  | Kuraray |  | 
Position | Time | Scintillation sample | Entries | Mean |  | Entries | Mean | 
 | 1h | #1 | 10820 | 2617 | 2.83 | 12520 | 4892 | 6.12
 |  | #2 | 10657 | 2462 | 2.62 | 12507 | 5260 | 6.58
 | 10h | #1 | 5872 | 1883 | 1.10 | 6031 | 4216 | 2.54
 |  | #2 | 5838 | 2108 | 1.23 | 5998 | 4608 | 2.76
Light collection: Kurary:Saint_Goban
Talked to domestic company, and they have the interest to do the R&D for WLS fibre.
Saint_Gobain
Kuraray
ADC/4

## Slide 8
Performance of current design
CR testing with two strips.
High efficiency, similar to the performance of the current Belle II KLM.
Time resolution:
Number of photons collected from WLS fibre is limited.
高能科迪

## Slide 9: The next step for Scintillator+WLS Fibre+SiPM
Need to make a module as prototype
A small detector for cosmic ray tracker has been made.
We need a large prototype for cosmic ray testing in the near future.

## Slide 10: Need to start the R&D for readout/DAQ systems
What we need:
Frond-end readout board
  Integrate preams;
  Maybe integrate HV generator;
  Handle a stations;
Back-end motherboard
  Digitization with new chips, sampling rate;
  Highly integrated ASICs;
  Data transition rate and connection: cable, fibre cable or 5G/6G?
Maybe front-end and back-end should be combined,
  see Belle II upgrade:
How about DAQ? Standalone or common DAQ?
  arXiv:2203.11349

## Slide 11: Lab for nuclear electronics at 上海理工
University of Shanghai for Science and Technology
Distance between Fudan and USST: 8km
A large and stable lab, very good equipments
PI: Dr. Qibin zheng (郑其斌), got Ph.D from USTC
Need funding to start the R&D.

## Slide 12: Reference of Belle II KLM