## Slide 1: X-ray total scattering method and its applications
Jo-Chi TSENG July 7, 2023 @ WIN2023, synchrotron section
Jochi.tseng@spring8.or.jp

## Slide 2
Scattering v.s. diffraction
Courtesy of max planck institute-PD Dr. Claudia Weidenthaler

## Slide 3
Scattering v.s. diffraction
Courtesy of max planck institute-PD Dr. Claudia Weidenthaler
Diffraction is a very special scattering event when the Bragg’s Law is fulfilled in a periodic structure.

## Slide 4
Scattering v.s. diffraction
Courtesy of max planck institute-PD Dr. Claudia Weidenthaler
Diffraction is a very special scattering event when the Bragg’s Law is fulfilled in a periodic structure.
Crystalline materials
Requirement on accurate peak shape for structure evaluation
Crystalline & Amorphous materials
Requirement on collection of scattering event as much as possible

## Slide 5
Scattering methods
Bragg’s Law: nλ=2dsinθ
θ++  d --
Courtesy of max planck institute -PD Dr. Claudia Weidenthaler

## Slide 6
Scattering methods
Bragg’s Law: nλ=2dsinθ
θ++  d --
Courtesy of max planck institute -PD Dr. Claudia Weidenthaler
For Total scattering method:
High Qmax, high flux
--> high energy X-ray
Bond lengths
Coordination numbers
Local structure

## Slide 7
High energy X-ray beamlines
X-ray energy/photon flux, detector capability

## Slide 8
X-ray energy
In order to have sufficient peak resolution in real space one has to collect diffracted photons up to high magnitudes of scattering vector q.
Courtesy of DESY-Dr. Jozef Bednarčík

## Slide 9
Developments @ Beamline
Perkin Elmer XRD1621
Dectris Pilatus3 2M CdTe
LaB6 (1s exposure)
LaB6 (10s exposure)
BL13XU
Lambda *6
Detector

## Slide 10
High energy X-ray beamlines
X-ray energy/photon flux, detector capability

## Slide 11
BL08W
115KeV, high flux, 5s - 10min/sample
Single scan
Heating (273K - 1100K)
He- Cryostat (15K - 273K)
Ball-milling (5Hz - 25Hz)
Electrochemistry
Gas adsorption

## Slide 12
BL04B2
60KeV/113KeV, 2 hr/sample
Single scan
Heating (273K - 1100K)
He- Cryostat (15K - 273K)

## Slide 13
Future development and trend
XRD + PDF
Vacuum Path
Courtesy of DESY-Dr. Michael T. Wharmby, I15-1@diamond website

## Slide 14: Total scattering data processing
Gudrun
Igor
pdfgetX/pdfgui
GSAS
TOPAS
DAWN

## Slide 15: Combined method

## Slide 16
ACS nano, 2014, 10, 10704-10714
Synthesis Mechanisms
Chem. Eur. J. 2021, 27, 11600
Hydrothermal synthesis process
Photocatalysis process
Octa. Fe linked to citrate molecules
edge-sharing [FeO6] units  Tetra. iron units
Pentahedra Ti-O in solution  building to anatase by a core-shell structure  Ti-O bond shift (Ti3+ and oxygen defects)  crystallized to anatase after 350℃
Notes: precursor crystalline [Fe(H2cit)(H2O)]n,
  corner-sharing octahedrally coordinated Fe3þ in a polymer-like structure linked by citrate molecules.
Nanoclusters consisting of edge-sharing [FeO6] units form immediately during the hydrothermal treatment
Tetrahedrally coordinated iron ions are observed after a short time at 320ºC.

## Slide 17
Deformation mechanism and interface
Anisotropic elastic strain of CuZr metallic glasses
Mixture of amorphous and crystalline phase
https://doi.org/10.1021/acs.chemmater.1c01466
Acta Materialia 57 (2009) 4133–4139
Strain-free at 54.7º Zr-Zr increases along tensile direction while Cu-Zr decreases atomic rearrangement was suggested
During delithiation crystallites turns to amorphous (V-V increase, V-O shift, suggested oct-V tetra-V by RMC)
Notes: Al substitution induces local distortions around the Al/Sn atoms
Oxygen vacancies, induced by the Al substitution, are mostly located on an anion site around the Al atoms

## Slide 18
Courtesy of DESY-Dr. Hermann Franz
Complementary Methods

## Slide 19
Thank you for your attentions