## Slide 1: The Role of X-ray Absorption Spectroscopy in Developing Novel Heterogeneous Catalysts
WIN 2023
Dr. Molly Meng-Jung Li
Assistant Professor
Applied Physics Department
The Hong Kong Polytechnic University

## Slide 2: Outline of talk
Heterogeneous catalysts
Complementary material characterisation techniques
XAS applications for novel heterogeneous catalysts: Some examples
What we wish to do on catalysis research with XAS

## Slide 3: Catalysis and catalyst
Catalysis: Concepts and Green Applications. Gadi Rothenberg, Wiley-VCH, Weinheim, Germany
A chemical reaction occurs at accelerated rate due to the participation of an additional substance (catalyst)
3 |

## Slide 4: Homogeneous/heterogeneous catalysis
One phase homogeneous catalysis
gas+gas, liquid+liquid
Two phases
heterogeneous catalysis
solid+gas, solid+liquid
4 |

## Slide 5: Supported metal catalyst
Support materials: High-surface-area, porous structure, low cost, high stability
For example: metal oxides, zeolites, carbon, etc.
5 |

## Slide 6
http://organicsynthesisinternational.blogspot.com/2015/07/heterogeneous-catalysis-and-catalyst.html
6 |

## Slide 7
http://organicsynthesisinternational.blogspot.com/2015/07/heterogeneous-catalysis-and-catalyst.html
7 |

## Slide 8
Complementary characterisation techniques
Crystal structure, local environment: -XRD: long-range structural order -XAS/EXAFS: short range structural order and bonding configuration -Electron microscopy: local structure and morphology
Catalyst surface properties: -TPR: metal-support interaction -TPD: interactions between the adsorbed molecules and active sites -TPO: oxidation property of catalyst, carbon deposition investigation
Electronic properties: -XAS/XANES & XPS: Oxidation state, charge transfer
Catalyst surface composition: - XPS & HSLEIS (ion scattering), STEM
Very useful when studying extremely small and active metal catalysts
8 |

## Slide 9: X-ray Absorption Spectroscopy (XAS)
An experimental technique at synchrotron radiation facilities
XAS is an element selective probe (very dilute systems can be studied)
Structural and electronic information
Can analyse amorphous powders/solutions
Powerful technique to resolve local structure/environment
Pics from https:// www.nsrrc.org.tw
9 |

## Slide 10: XANES & EXAFS
Pics from XANES: Theory2 - Chemistry LibreTexts, AIMS Materials Science, 2017, 4(4): 856-866
and https://www.pinterest.com/
10 |

## Slide 11
CH4
CH3OH
Rh
Rh+In
H2 deficient condition
angew. chem. int. ed. 2020, doi: 10.1002/anie.202000841
11 |
Add In into Rh
Efficient H2 consumption for methanol synthesis
Rh-In bimetallic interface-activity

## Slide 12
Extended X-ray Absorption Fine Structure
X-ray Absorption Near Edge Structure
angew. chem. int. ed. 2020, doi: 10.1002/anie.202000841
12 |
Rh K-edge
In concentration ↑
Rh absorption edge ↓
Rh-In bimetallic interface: structural analysis

## Slide 13
NAP-XPS experiment procedures
Monitoring changes of electronic structure under catalyst working condition
angew. chem. int. ed. 2020, doi: 10.1002/anie.202000841
13 |
Rh3+
Rh0
Rh-In bimetallic interface-solid/gas interactions

## Slide 14
[a] Ediff (eV): Energy differences of surface adsorbed HCOO* and COOH* species.
Ediff = EHCOO* – ECOOH*
EHCOO* = EHCOO/sub – Esub
ECOOH* = ECOOH/sub – Esub
[b] Eads (eV): H adsorption energies
HCOO
(intermediate of CH3OH formation)
COOH
(intermediate of CO formation)
Preferred!
14 |
angew. chem. int. ed. 2020, doi: 10.1002/anie.202000841
Rh-In bimetallic interface-reaction pathway

## Slide 15
Determine single atom configuration
2.5%
7.5%
Mo atoms and clusters were
uniformly distributed
Isolated Mo atoms
Lowering the Mo loading dramatically
improved the TOF
Reverse water-gas shift reaction
(RWGS, CO2+H2 → CO+H2O)
Sun*, Angew. Chem.Int. Ed.2022,61,e202203836

## Slide 16
Further confirming coordination environment from the XANES features:
The pre-edge feature comes from Mo-N coordination
(Å)
Mo K-edge XANES simulation
As Mo content increases from 2.1 wt.% to 7.1 wt.%:
Mo/NC phases decreased, making less Mo-N3 contribution;
Therefore the pre-edge intensity decreased
Comes from the Mo-N3 configuration
Sun*, Angew. Chem.Int. Ed.2022,61,e202203836
Determine single atom configuration

## Slide 17
Electron transfer from Cd/In2O3 and Cd/In2O3(VO) to *N2H2 is higher than that of In2O3: stronger electron interaction
NRR activity: Cd/In2O3 (OV) is the best
Cd substitutes the In atoms in In2O3 lattice.
Sun Zhenyu (BUCT)*, Adv. Funct. Mater. 2023, 33, 2209843
NH3 Electrosynthesis
Determine the dopant atom configuration

## Slide 18
S vacancy
Sample: When Ag atoms are doped to CdS, where will it stay?
Bond | CN | R, Å
Ag-S | 1.3 ± 0.1 | 2.47 ± 0.01
Ag-Cd | 1.6 ± 0.3 | 2.73 ± 0.04
Ag-Cd | 0.7 ± 0.2 | 2.91 ± 0.01
Ag-S
Ag-Cd
Ag K-edge EXAFS fitting
parameters of AgCdSx
Ag K-edge XANES
Ag K-edge EXAFS
AgCdSx exhibits a nearly identical XANES spectrum to Ag2S, indicating:
Ag atom is surrounded by S atoms
Valance of Ag is nearly 1+.
AgCdSx EXAFS can be well fitted using Ag-S and Ag-Cd bond
(Details see above table)
From XANES and EXAFS features, combined with DFT calculation results
The site of Ag atoms was determined
Unpublished
Determine the dopant atom configuration

## Slide 19
Support-induced local strain in molecular complex
Electrochemical CO2 reduction performance
Curved CoPc has stronger CO binding
1s→4pz: Decline in CoPc/CNTs due to decreased symmetry
1s→4px,y: Lower valence of CoPc/CNTs due to interactions
Co-N1 length: elongated due to high degree of molecular bending for CoPc/SWCNT
Ye*, Nat. Catal., Accepted.
Notes: Phthalocyanine 酞菁

## Slide 20
Identify unique core/shell interfaces
The EXAFS of the post-reaction Co@BaAl2O4 reveals the distinct Co and BaAl2O4 phases, suggesting no migration of Co species at the metal-support interfaces during the long-term testing.
Core@shell configuration
Unpublished

## Slide 21
Our FTIR
Our Mass Spec (on the floor)
In-situ XAS: real time determination of the
local chemical/structural environment
In-situ IR: interrogation of reactants, intermediates,
reactively-formed products bound at nanoparticle surface
Provide quantitative structure-function relationships
21 |
Other techniques:
XAS/Raman
XAS/XRD
XAS with ?
What we wish to do with XAS

## Slide 22: Now 🙁Far away 🙁No regular access 🙁Long waiting time 🙁Costly 🙁Limited gas options
Synchrotron resources
With SILF
🙂Easy access
🙂Great connection
🙂Most advanced
🙂Easy communication