## Slide 1
R&D Status of the High Field
Model Dipoles for SPPC
Qingjin XU
for the Superconducting Magnet Group,
Accelerator Division, IHEP-CAS

## Slide 2
Introduction
This talk is about the high field superconducting magnet R&D for SPPC
This talk relates to the TDR chapter 8.3 HIGH-FIELD SUPERCONDUCTING MAGNETS
The content relates to the following “charge letter” items
1. Are the accelerator system design goals well defined? Have the goals been reached in the TDR?
3. Are the accelerator complex design, the key technologies adopted, and the conventional facilities effective for achieving the performance goals?

## Slide 3
Magnet Design Scope for SPPC
High Energy Circular Colliders for next decades | SPPC | FCC
Proposed institution | IHEP-CAS, China | CERN, Europe
Proposed dates | 2012 | 2013
Site of the project | China | Europe
Baseline technology | IBS 20~24 T to reach 125-150 TeV, Nb3Sn etc as options | Nb3Sn 16 T to reach 100 TeV
Timeline | Construction at 2040s | Construction at 2050-60s
Cost | * | **

## Slide 4
New Record：14.5 T Dipole by Fermilab in 2020
4
A. V. Zlobin, Fermilab
But with ~20% performance degradation after thermal cycle!

## Slide 5
R&D of the High Field Model Dipoles
Challenges: Stress control, quench protection, field quality control,……
Roadmap for High Field
Dipole Magnet R&D
5

## Slide 6
2018
2019
2021
~90% SSL
R&D of the High Field Model Dipoles
6
Training history at 4.2 K

## Slide 7
16 T Model Dipole: Nb3Sn 12~13 T + HTS 3~4 T
R&D of the High Field Model Dipoles
7

## Slide 8
R&D of the High Field Model Dipoles
Stress distribution in different loading steps
Assembly
4.2 K
13 T
8

## Slide 9
R&D of the High Field Model Dipoles
The calculation indicates that the temperature of hot spot is 237 K and the max voltage is 952 V. Safe.
9

## Slide 10
R&D of the High Field Model Dipoles
16-T Dipole with CCT configuration
Canted-Cosine-Theta (CCT) technology;
  Superior field quality;
  Stress management
  Developed industrial assembly line;
Graded Nb3Sn Rutherford cables;
Multiple replaceable coil modules;
The geometry of the 4 module CCT magnet
CCT subscale
10

## Slide 11
R&D of the High Field Model Dipoles
Harmonics：10-4 | b2 | a2 | b3 | a3 | b4 | a4 | b5 | a5 | b6 | a6 | b7 | a7 | b8 | a8
Cross section-2D | 0.6259 | 0.0119 | 2.9824 | -0.0006 | 0.0537 | 0.0002 | 0.5189 | 0.0002 | 0.0183 | -0.0020 | -0.0845 | 0.0016 | -0.0036 | 0.0009
Integrated-3D | 1.5989 | 0.0101 | 3.8649 | -0.0320 | 0.3047 | 0.0802 | 1.4069 | -0.0175 | 0.0750 | -0.3695 | 0.1163 | 0.0734 | -0.0223 | -0.2090
High-order harmonics along axis - Bn
High-order harmonics along axis - An
11

## Slide 12
R&D of the High Field Model Dipoles
J. Wang et al, Superconductivity 3 (2022) 100019
12
Development of a Roebel-like Transposed Cable with the in-plane bending of HTS tapes

## Slide 13
Development of a Roebel-like Transposed Cable with the in-plane bending of HTS tapes
R&D of the High Field Model Dipoles
13

## Slide 14
Chart: Applied Magnetic Field (T)
| 0 | 5 | 15 | 20 | 25 | 30
REBCO: B ∥ Tape plane | 4144.6766 | 3507.9375 | 3148.3332 | 2909.0554 | 2090.4933 | 1888.9952
REBCO: B ⊥ Tape plane, 45 μm sub | 5478.1345 | 5053.3515 | 4372.0346 | 3812.2534 | 3348.8068 | 3146.724 | 2964.7726 | 2801.365 | 2663.2305 | 2530.35 | 2415.161 | 2307.3222 | 2215.5971 | 2121.427 | 2046.7953 | 1970.1838 | 1905.1216 | 1841.6283 | 1784.4676 | 1729.8653 | 1682.3664 | 1631.1403 | 1591.3007
REBCO: B ⊥ Tape plane | 4144.6766 | 1445.8386 | 975.0997 | 767.7508 | 655.6687 | 571.6114 | 526.7777 | 481.944 | 442.7183 | 428.1462 | 403.4904 | 386.6773 | 364.2626 | 341.8457 | 328.3952 | 319.4289 | 318.3073
Bi-2212: OST NHMFL 50 bar OP | 1243.4169 | 1159.7904 | 1097.571 | 1051.5861 | 1014.8275 | 981 | 955.0755 | 928.7776 | 905.6283 | 884.9933 | 865.478 | 846.7181 | 827.3047
Nb₃Sn: Internal Sn RRP® | 1754.8557 | 1454.9349 | 1190.9814 | 1072.6374 | 957.7741 | 855.0933 | 757.6336 | 268.0143 | 190.8587 | 118.9241 | 65.5533 | 28.3097
Nb₃Sn: High Sn Bronze | 166.6431 | 137.8146 | 111.0954 | 84.3762 | 60.8212 | 40.0788 | 19.3362 | 8.0861
Nb-Ti: LHC 4.2 K | 5106.8846 | 4054.1538 | 3180.5962 | 2710.2269 | 2217.4577 | 1724.6885 | 1411.1115 | 1187.1231 | 918.3423
Nb-Ti: Iseult/INUMAC MRI 4.22 K | 393.4783 | 291.3043 | 194.203 | 104.3478
Exponential Y-axis Labels | 10 | 100 | 1000 | 10000
Nb-Ti midrange maximal | 971.9231 | 687.3077 | 448.4615 | 393.4783
2212 Fitted Line for 50bar ASC'16 | 1381.5217 | 1248.5735 | 1162.079 | 1099.1369 | 1050.2486 | 1010.6145 | 977.4929 | 949.1799 | 924.5486 | 902.818 | 883.4258 | 865.9547 | 850.0872 | 835.5764 | 777.6921 | 691.6232
YBCO B perp linear extrap | 312.7055 | 264.5487 | 240.4379
IBS 2016
IBS 2019
IBS 2022
IBS 2025
IBS Technology: Status and Outlook
Stainless-steel stabilized IBS tape achieved the highest Je in 2022!
Significantly reduced the cost and raised the
mechanical properties.
14

## Slide 15
IBS Technology: Status and Outlook
Ic of Φ34mm-17 turns-DPC reached 60 A at 4.2 K and 32 T, world’s highest record up to now.
The First IBS Solenoid Coil at 32 T background field
15

## Slide 16
IBS Technology: Status and Outlook
16
Quench propagation study of the IBS coils
Experimental data shows significant quench propagation in the IBS coils! More testing will be carried out.

## Slide 17
IBS Technology: Status and Outlook
2008.02
2008.09
2016
2018
Discovery of IBS
2008.04
Discovery of
122 phase IBS
2020
100-m 7-core IBS tape fabricated
Je= 100 A/mm2
@ 10 T, 4.2 K
IBS solenoid at 24 T
Racetrack at 8 T
Je= 300 A/mm2
@ 10 T, 4.2 K
IBS solenoid at 32 T
Racetrack at 10 T
1.3 kA transposed cable
Je > 450 A/mm2
@ 10 T, 4.2 K
2022
H. Hosono
IBS (Tc 26K)
Z. Zhao
IBS (Tc 55K)
Je of IBS expected to be similar as ReBCO in 5 years with better mechanical properties and lower cost
17

## Slide 18
All the magnets delivered to CERN passed the performance double-check at 1.9 K.
Test results of the 1st full-length prototype from China:
“Each aperture, individually and combined, arrived to ultimate current without quench”
“Operation range test checked without quench”……
Development of CCT Magnets for HL-LHC
To be installed in the ATLAS & CMS interaction regions, help to raise the luminosity by 5 times
The 1st time CCT type magnets applied to an operating accelerator.
China provides 13 units CCT twin-aperture dipole magnets for HL-LHC
18

## Slide 19
Development of CCT Magnets for HL-LHC
Items | Values
CCT skew angle | 30°
No. of turns per layer | 365
Slot size in former (mm) | 2×5
Spacing per turn | 5.222
Inside/Outside diameter of the former (mm) | Inner former:105.35/119.35 Inner former:120.80/134.85
Inside diameter of the groove/slot(mm) | 1st layer: 109.15/119.15 2nd layer: 124.65/134.65
Reference radius (mm) | 35
Diameter of aperture (mm) | 105
Current (A) | 395
Ø 614 mm
Aperture
Cooling hole
Hole for tie rod
Yoke alignment
CCT Coils
Items | Values
Diameter of yoke (mm) | 614
Thickness of yoke lamination (mm) | 5.8
Diameter of aperture (mm) | 167
Position of aperture (mm) | 94.19
Yoke key slot(mm) | 8(3.01) ×6
Diameter of cooling hole (mm) | 110
Position of cooling hole (mm) | 205
19

## Slide 20: Training of MCBRD01
Aperture1 of the 1st series magnet
Aperture2 of the 1st series magnet
The 1st practice coil from Bama with new fabrication process wet wind plus 5-bar VPI.
The 2nd coil from Bama with direct wind process plus 5-bar VPI, similar to the process of the 1st prototype.
Development of CCT Magnets for HL-LHC
20

## Slide 21
HL-LHC Schedule for the Collaboration Board 2022
Development of CCT Magnets for HL-LHC
21
Successful design upgrade to solve the “long training problem”, significantly reduced the times of quench during training, ensured the project progress “on track”.

## Slide 22: Training of MCBRD02 & MCBRD03
Development of CCT Magnets for HL-LHC
AP1(CB12，25 quenches 526A) reached ±422A after 11 quenches.
AP2(CB09, 33 quenches 530A; after thermal cycle ＞500A) reached ±422A without any quenches.
22

## Slide 23
Milestone of the HL-LHC CCT Magnet Project
Development of CCT Magnets for HL-LHC
23
Agreement signed
btw IHEP and CERN
The qualified prototype delivered to CERN
The CCT magnet from China under test at CERN
All the 12 series CCT magnets delivered to CERN
Installation to tunnel
HL-LHC commissioning

## Slide 24
Summary
Long-term advanced superconducting magnet R&D for future high-energy accelerators is ongoing at IHEP-CAS.
Strong domestic collaboration for the advanced superconductor R&D (HTS & Nb3Sn): Stainless-steel stabilized IBS tape achieved the highest Je in 2022! Significantly reduced the cost and raised the mechanical properties.
10+ T model dipoles being developed at IHEP, reached 12.47 T at 4.2 K in mid 2021. 16 T (Nb3Sn+HTS) model dipole under development, and to be tested in 2023. 20+ T accelerator magnets expected to be realized in 2020s.
China & CERN Collaboration on accelerator technology: development of HL-LHC CCT magnets going well.
Thanks for your attention!
24