## Slide 1
Progress of the High Field Magnet Program
For the Next-generation Accelerators
Qingjin XU
for the Superconducting Magnet Group,
Accelerator Division, IHEP-CAS
Oct 27 2023
CEPC2023, Nanjing, Oct 23-27 2023

## Slide 2
2
High Energy Circular Colliders for next decades | SPPC | FCC
Proposed institution | IHEP-CAS, China | CERN, Europe
Proposed dates | 2012 | 2013
Site of the project | China | Europe
Baseline technology | IBS 20~24 T to reach 125-150 TeV, Nb3Sn etc as options | Nb3Sn 16 T to reach 100 TeV
Timeline | Construction at 2040s | Construction at 2050-60s
Cost | * | **
Design Scope for the Next-generation Accelerators

## Slide 3
Roadmap of the High Field Magnet R&D at IHEP
3
Challenges: Stress control, quench protection, field quality control,……
2018-2021, 12.47T @4.2K
NbTi + Nb3Sn
2021-2023 16T @ 4.2K
Nb3Sn + HTS

## Slide 4
16 T Model Dipole LPF3: Nb3Sn 13 T (Common Coil with 55 mm gap) + HTS 3 T inserts (Block & CCT with 20 mm)
Development of the 16-T Model Dipole LPF3
4

## Slide 5
5
The Nb3Sn coils for LPF3
Chengtao Wang et al
Development of the 16-T Model Dipole LPF3

## Slide 6
6
The ReBCO block insert coils for LPF3
Parameters | Values
L0 | 409.6 mm
L1 | 540.2 mm
Rhard | 800 mm
Aend | 6 °
R1 | 9.5 mm
Z1 | 120 mm
Ze Feng et al
Development of the 16-T Model Dipole LPF3

## Slide 7
7
The ReBCO CCT instert coils for LPF3
典型CCT线圈结构示意
“斜螺线管”型CCT线圈结构示意
Rui Kang et al
Development of the 16-T Model Dipole LPF3

## Slide 8
8
2023.8.29 Assembly completed
8
Stress monitoring during
assembly with FBG
Pre-stress applied with commercial hydraulic jack
Pre-stress and assembly of LPF3
Yingzhe Wang et al
Development of the 16-T Model Dipole LPF3

## Slide 9
9
Current decay curve at the operating current
Varistor plus CLIQ to protect the Nb3Sn coils. The maximum hot spot is ~ 230 K
NI configuration plus dump resistor to protect the 2 HTS insert coils
Quench protection of LPF3
Rui Kang, Hongjun Zhang et al
Feasibility study of applying the no-insulation coil on accelerator magnets
Development of the 16-T Model Dipole LPF3
Jinrui Shi et al

## Slide 10
Preliminary fresh test results just last week!
The 1st preliminary test carried out in the week Sep 3-8 2003. The 6 Nb3Sn coils were firstly ramped
5 quenches occurred from 9 to 10 T, all caused by FLUX JUMP, but with an encouraging upward trend
Test stopped due to the limited size of He recovery gasbag, > 100 m3 He gas was evaporated during the 5th quench
HTS CCT insert was ramped independently, quenched at 90% of the Iop with a linearly increased voltage curve, probably indicating a damage of ReBCO conductor durting the coil fabrication process
~9 T
~10 T
10
Wei Li et al
Development of the 16-T Model Dipole LPF3

## Slide 11
R&D of the HTS transposed cable: X-cable
11
Martin N. Wilson proposed the idea in1997
Siemens developed a transposed cable with in-plane bending Bi-2223 tapes in 2004
IHEP proposed the transposed cable with in-plane bending of HTS tapes in 2017
KIT proposed the Roebel cable concept by punching wide tapes to realize transposition in 2006
IHEP successfully fabricated the first IBS transposed cable in 2021
IHEP successfully fabricated the first in-plane transposed REBCO cable in 2020
In-plane transposed HTS cable
In-plane transposed HTS cable
Punch-assemble transposed HTS cable
Development of a Roebel-like Transposed Cable with the in-plane bending of HTS tapes
Juan Wang et al

## Slide 12
12
Development of a Roebel-like Transposed Cable with the in-plane bending of HTS tapes
R&D of the HTS transposed cable: X-cable
Juan Wang et al

## Slide 13
Chart: Applied Magnetic Field (T)
| 0 | 5 | 15 | 20 | 25 | 30
REBCO: B ∥ Tape plane | 4144.6766 | 3507.9375 | 3148.3332 | 2909.0554 | 2090.4933 | 1888.9952
REBCO: B ⊥ Tape plane, 45 μm sub | 5478.1345 | 5053.3515 | 4372.0346 | 3812.2534 | 3348.8068 | 3146.724 | 2964.7726 | 2801.365 | 2663.2305 | 2530.35 | 2415.161 | 2307.3222 | 2215.5971 | 2121.427 | 2046.7953 | 1970.1838 | 1905.1216 | 1841.6283 | 1784.4676 | 1729.8653 | 1682.3664 | 1631.1403 | 1591.3007
REBCO: B ⊥ Tape plane | 4144.6766 | 1445.8386 | 975.0997 | 767.7508 | 655.6687 | 571.6114 | 526.7777 | 481.944 | 442.7183 | 428.1462 | 403.4904 | 386.6773 | 364.2626 | 341.8457 | 328.3952 | 319.4289 | 318.3073
Bi-2212: OST NHMFL 50 bar OP | 1243.4169 | 1159.7904 | 1097.571 | 1051.5861 | 1014.8275 | 981 | 955.0755 | 928.7776 | 905.6283 | 884.9933 | 865.478 | 846.7181 | 827.3047
Nb₃Sn: Internal Sn RRP® | 1754.8557 | 1454.9349 | 1190.9814 | 1072.6374 | 957.7741 | 855.0933 | 757.6336 | 268.0143 | 190.8587 | 118.9241 | 65.5533 | 28.3097
Nb₃Sn: High Sn Bronze | 166.6431 | 137.8146 | 111.0954 | 84.3762 | 60.8212 | 40.0788 | 19.3362 | 8.0861
Nb-Ti: LHC 4.2 K | 5106.8846 | 4054.1538 | 3180.5962 | 2710.2269 | 2217.4577 | 1724.6885 | 1411.1115 | 1187.1231 | 918.3423
Nb-Ti: Iseult/INUMAC MRI 4.22 K | 393.4783 | 291.3043 | 194.203 | 104.3478
Exponential Y-axis Labels | 10 | 100 | 1000 | 10000
Nb-Ti midrange maximal | 971.9231 | 687.3077 | 448.4615 | 393.4783
2212 Fitted Line for 50bar ASC'16 | 1381.5217 | 1248.5735 | 1162.079 | 1099.1369 | 1050.2486 | 1010.6145 | 977.4929 | 949.1799 | 924.5486 | 902.818 | 883.4258 | 865.9547 | 850.0872 | 835.5764 | 777.6921 | 691.6232
YBCO B perp linear extrap | 312.7055 | 264.5487 | 240.4379
IBS 2016
IBS 2019
IBS 2022
IBS 2025
IBS Technology: Status and Outlook
13
90% Stainless-steel & 10% Sliver stabilized IBS tape achieved the highest Je in 2022!
Significantly reduced the cost and raised the
mechanical properties.

## Slide 14
IBS Technology: Status and Outlook
Ic of Φ34mm-17 turns-DPC reached 60 A at 4.2 K and 32 T, world’s highest record up to now.
The First IBS Solenoid Coil at 32 T background field
14
Chunyan Li et al

## Slide 15
IBS Technology: Status and Outlook
15
Quench propagation study of the IBS coils
Experimental data shows significant quench propagation in the IBS coils! More testing will be carried out
Chunyan Li et al

## Slide 16
IBS Technology: Status and Outlook
2008.02
2008.09
2016
2018
Discovery of IBS
2008.04
Discovery of
122 phase IBS
2020
100-m 7-core IBS tape fabricated
Je= 100 A/mm2
@ 10 T, 4.2 K
IBS solenoid at 24 T
Racetrack at 8 T
Je= 300 A/mm2
@ 10 T, 4.2 K
IBS solenoid at 32 T
Racetrack at 10 T
1.3 kA transposed cable
Je > 450 A/mm2
@ 10 T, 4.2 K
2022
H. Hosono
IBS (Tc 26K)
Z. Zhao
IBS (Tc 55K)
Je of IBS expected to be similar as ReBCO in 5 years with better mechanical properties and lower cost
16

## Slide 17
Development of CCT Magnets for HL-LHC
To be installed in the ATLAS & CMS interaction regions, help to raise the luminosity by 5 times
The 1st time CCT type magnets applied to an operating accelerator.
China provides 13 units CCT twin-aperture dipole magnets for HL-LHC
17

## Slide 18
HL-LHC Schedule for the Collaboration Board 2022
Development of CCT Magnets for HL-LHC
18
Successful design upgrade to solve the “long training problem”, significantly reduced the times of quench during training, ensured the project progress “on track”.

## Slide 19: Training of MCBRD02 & MCBRD03
Development of CCT Magnets for HL-LHC
AP1(CB12，25 quenches 526A) reached ±422A after 11 quenches.
AP2(CB09, 33 quenches 530A; after thermal cycle ＞500A) reached ±422A without any quenches.
19

## Slide 20
Milestone of the HL-LHC CCT Magnet Project
Development of CCT Magnets for HL-LHC
20
Agreement signed
btw IHEP and CERN
The qualified prototype delivered to CERN
The CCT magnet from China under test at CERN
All the 12 series CCT magnets delivered to CERN
Installation to tunnel
HL-LHC commissioning

## Slide 21
Summary
Long-term advanced superconducting magnet R&D for future high-energy accelerators is ongoing at IHEP-CAS
10+ T model dipoles being developed at IHEP, reached 12.47 T at 4.2 K in mid 2021. 16 T (Nb3Sn+HTS) model dipole under test in 2023. 20 T accelerator magnets expected to be realized in 2020s
Strong domestic collaboration for the advanced superconductor R&D (HTS & Nb3Sn): Stainless-steel-Silver stabilized IBS tape achieved the highest Je in 2022! Significantly reduced the cost and raised the mechanical properties
China & CERN Collaboration on accelerator technology: development of HL-LHC CCT magnets going well
Looking forward to a world wide synergy on the advanced accelerator magnet R&D in future
21
Thanks for your attention