## Slide 1
中科院高能所超导磁体组
Superconducting Magnet Group
@ Accelerator Division, IHEP
R&D of CEPC Detector Magnet
NING Feipeng*, WANG Menglin, ZHAO Ling, PEI Yatian, CAO Jingli, XU Qingjin
IHEP, CAS
CEPC Detector Magnet HTS version
Magnetic field | 3 T | Current | 28000 A
Inner diameter | 4660 mm | Inductance | 1.27 H
Outer diameter | 4960 mm | Stored energy | 500 MJ
Magnet thickness | 150 mm | Cold mass | 27 ton
Length | 8 m | HTS cable length | 10.7 km
Total weight | 48 ton | ASTC weight | 16.6 ton
Coil layout：
Magnet parameters：
Al stabilized Stacked HTS Tape Conductor (ASTC) development
Small-scale sample cable
Superconducting cables are the key to detector magnets. In 2017, IHEP proposed a high temperature superconducting (HTS) scheme for detector magnet and innovatively designed a aluminum stabilized HTS stacked conductor, then began the development of small-scale sample cable.
Object：single tape core Ic > 100 A@77K；considering the self-field effect, The critical current of a 14-core cable is larger than 830 A@77K, self-field.
Ic = 905A
After three years of research and development, the performance of the cable has met the expected requirements.
Developing process of ASTC：
CEPC Detector Magnet LTS version