## Slide 1: Sensor and electronics design and tests
Ying Zhang
On behalf of the CEPC MOST2 Vertex detector design team
2023-6-19

## Slide 2: Outline
Sensor prototypes design
Readout electronics design
Single chip and multi-chips test results
Summary

## Slide 3: Main specification of the full-scale chip
Project assessment index (考核指标)
  Spatial resolution: 3-5 μm
  Total ionization dose (TID) > 1Mrad
A full-scale pixel chip should be design to build the first vertex detector prototype
  No full-scale pixel chip exists in China before this project

## Slide 4: Additional specifications on the full-scale chip
Additional specifications besides the main goals of project
  High detection efficiency  small dead time
  Assembled on ladder  large sensitivity area
  Low material  low power density
  Bunch spacing: Higgs: 680 ns; W: 210 ns; Z: 25 ns
  Hit density: 2.5 hits/bunch/cm2 for Higgs/W; 0.2 hits/bunch/cm2 for Z  high hit rate
  Major innovation: High data-rate processing maintaining good spatial resolution
Specs | Parameter
Hit rate | 120 MHz/chip
Data rate | 3.84 Gbps (triggerless) ~110 Mbps (trigger)
Dead time | < 500 ns (for 98% efficiency)
Pixel array | 512 row × 1024 col
Chip size | ~1.4 × 2.56 cm2
Power Density | < 200 mW/cm2 (air cooling)

## Slide 5: Structure and process of sensor
Monolithic pixel sensor based on CMOS process
  N-well/P-epitaxial diodes employed collection elements
  Readout electronics integrated on the same Si-substrate
   Low material budget, low pixel capacitor, easy to assembly
Process choice: TowerJazz CIS 180 nm process
  Process split:
    Standard process
      Baseline options, the only choice available in the MPW submission
    Modified process
      Additional modification made on the standard cross-section, to achieve faster charge collection, thus better radiation tolerance
      Very difficult to access, the first time available to a Chinese designer

## Slide 6: TaichuPix sensor architecture
Pixel 25 μm × 25 μm
  Continuously active front-end, in-pixel discrimination
  Fast-readout digital, with masking & testing config. logic
Column-drain readout for pixel matrix
  Priority based data-driven readout
  Time stamp added at EOC
  Readout time: 50 ns for each pixel
2-level FIFO architecture
  L1 FIFO: de-randomize the injecting charge
  L2 FIFO: match the in/out data rate between core and interface
Trigger-less & Trigger mode compatible
  Trigger-less: 3.84 Gbps data interface
  Trigger: data coincidence by time stamp, only matched event will be readout
Features standalone operation
  On-chip bias generation, LDO, slow control, etc.

## Slide 7: TaichuPix prototypes overview
Major challenges for the sensor design
  Small pixel size  high resolution (3-5 μm)
  High readout speed (dead time < 500 ns @ 40 MHz )  for CEPC Z pole
  Radiation tolerance (per year): 1 Mrad TID
Completed 3 rounds of sensor prototyping in 180 nm CMOS process
  Two MPW chips (5 mm × 5 mm )
    TaichuPix-1: 2019.06 ‒ 2019.11
    TaichuPix-2: 2020.02 ‒ 2020.06
  1st engineering run
    Full-scale chip: TaichuPix-3, received in July 2022 & March 2023
6 design variations
TCPX3
15.9 mm
25.7 mm
TaichuPix-1
TaichuPix-2
TaichuPix-3
Pixel size：25 μm × 25 μm

## Slide 8: Test of the data interface (TaichuPix-1)
Data readout in DDR mode
Data interface was tested by the on-chip PRBS source, a high speed oscilloscope (@16Gsps), and code stream verified in FPGA
BER qualified till 3.36 Gbps, failed at 4.48 Gbps
Concerning the highest data rate for triggerless at 4 Gbps, at least 2 SER interface ports needed
Thus bit rate @2.24 Gbps is safe and power optimized
@2.24Gbps
@3.36Gbps
Bit rate | 2.24Gbps | 3.36Gbps | 4.48Gbps
Clk freq | 1.12GHz | 1.68GHz | 2.24GHz
BER | 6.59e-18 | 9.14e-13 | 3.23e-5
Tj@e-12 | 141.63ps | 123.27ps | 147.14ps
Rj | 5.39ps | 4.84ps | 5.35ps
Dj | 64.77ps | 54.26ps | 70.90ps

## Slide 9: Functionality of complete signal chain of TaichuPix2
Functionality of the complete signal chain (including sensor, analog front-end, in-pixel logic readout, matrix periphery readout and data transmission unit) was firstly proved with an X-ray source and a laser source.
TaichuPix-2
Measured
Hit map of the TaichuPix-2 under X-ray from the X-tube voltage of 8 kV for 5 min.
Letter imaging obtained with a 1064 nm laser spot scanning on the TaichuPix-2
TaichuPix2 response to X-ray tube (cutting energy @ 6keV)
Measured
Simulated analog output with different input signal

## Slide 10: TaichuPix2 test with 90Sr
TC2 exposure to 90Sr source at different threshold setting (ITHR)
Analog output of one pixel under 90Sr exposure
Average cluster size vs. threshold
Shape and amplitude of analog signal as expected, but peaking time and pulse length larger than simulation.
Average cluster size decreases with threshold as expected
Average cluster size for S1-S4 less than 3 as expected
  Indicates the estimated maximum hit rate (36 MHz/cm2) reasonable
  Cluster size >1, benefits the spatial resolution (better than = 7.2 µm)
S1-S4 features different thresholds for the same DAC code

## Slide 11: Laser test of TaichuPix-2
Setup: a three-dimensional translation stage with a 1064 nm laser
Distribution of residual X
Distribution of residual Y

## Slide 12: Large-scale sensor TaichuPix-3
12 TaichuPix-3 wafers produced from two rounds
  One wafer thinned down to 150 μm and diced
  11 wafers were tested on probe-station before dicing  chip selecting & yield evaluation
Probe card for wafer test
Wafer after thinning and dicing
Thickness after thinning
8-inch wafer
Wafer T212141-02E3
An example of wafer test result
8-inch wafer
Wafer num. | Yield | Wafer num. | Yield
1 | 0.65 | 4 | 0.475
2 | 0.725 | 5 | 0.625
3 | -- | 6 | 0.525
7 | 0.775 | 10 | 0.675
8 | 0.725 | 11 | 0.6
9 | 0.275 | 12 | 0.35
Wafer #3
1st round
2nd round

## Slide 13: Threshold and noise of TaichuPix-3
Pixel threshold and noise were measured with selected pixels
  Average threshold ~215 e-, threshold dispersion ~43 e-, temporal noise ~12 e- @ nominal bias setting
Measured
Measured

## Slide 14: TID test on TaichuPix-3
  The energy of X-ray is set to 12 KeV
  Ionization chamber is used to calibrate irradiation dose rate
  The irradiation dose is regulated by aluminum foil
Aluminum (Al) | Irradiation dose rate
96 layers | 0.02rad/s
64 layers | 3 rad/s
32 layers | 394 rad/s
28 layers | 722 rad/s
24 layers | 1321.6 rad/s
1 layers | 42927 rad/s
Attenuation of Aluminum (thickness of Al foil is 0.01 mm/layer)
Beamline Specifications
Analog signal of the pixel monitored by the oscilloscope
Chart: 
| 0 | 0.01 | 0.02 | 0.03 | 0.05 | 7.0000000000000007E-2 | 0.08 | 0.14000000000000001 | 0.16
 | 481.3123 | 410.5311 | 353.9061 | 318.5155 | 240.6561 | 184.0312 | 169.8749 | 56.625 | 42.4687
Al thickness (mm)
Dose rate（Gy/s）

## Slide 15: TID test on TaichuPix-3
TaichuPix-3 irradiated at BSRF 1W2B beamline (12 keV X-ray)
Position1
Position2
Position3
Full image of the X-ray beam spot(position 1)
Pixel threshold vs. TID
Preliminary
Preliminary
Pixel noise vs. TID
Chip was exposed with full working condition: power, bias, clk, …
Dose rate ~1.2 rad/min for the first 12 min, in order to find the position of beam spot.
   The size of beam spot agrees with the expectation of 1 mm × 0.6 mm
Dose rate ~43.3 krad/min for 69 min until total dose over 3 Mrad.
All three irradiation regions indicated a good performance to 3 Mrad TID

## Slide 16: TaichuPix-3 telescope
The 6-layer of TaichuPix-3 telescope built
  Each layer consists of a TaichuPix-3 bonding board and a FPGA readout board
TaichuPix-3 telescope achieved the expected goal in the DESY testbeam
  The best spatial resolution could be 4.8 μm
  The resolution gets better when decrease the pixel threshold, due to the increased cluster size
Spatial resolution @ threshold of 218 e-
6-layer TaichuPix-3 telescope
TCPX3 chip
Spatial resolution vs. pixel threshold
preliminary
preliminary
Details go to talk ”test beam and results”

## Slide 17: Ladder readout
Completed detector module (ladder) design
  Detector module (ladder) = 10 sensors + readout board + support structure + control board
  Sensors are glued and wire bonded to the flexible PCB, supported by carbon fiber support
  Signal, clock, control, power, ground will be handled by control board through flexible PCB
Challenges
  Long flex cable  hard to assemble & some issue with power distribution and delay
  Limited space for power and ground placement  bad isolation between signals
Solutions
  Readout from both ends, readout compose of three parts, careful design on power placement
Ladder readout system
853 mm
U8
U7
U6
U5
U4
U3
U2
U1
U9
U10

## Slide 18: Laser test result of ladder flex with two chips
One flex equipped with chip U10 & U9
  Config U9/U10 respectively: minimum ITHR is 64 for U10, 96 for U9
  Laser test: U9 and U10 can work simultaneously, NO error code/cross-talk found
U10 @ ITHR=64
U9 @ ITHR=96
U9 & U10 @ ITHR = 96
Gap ≈ 175 um = 7 pixels
U10
U9

## Slide 19: Summary
The full-scale and high granularity pixel sensor prototype, TaichuPix-3, has been designed and tested
The main design indicators achieved
Readout electronics for the sensor test and the ladder readout was developed
  Performed the sensor characterization in the lab successfully
  Completed beam tests for the sensor prototype and the detector prototype at DESY
 | Project indicators | Test results
Spatial resolution | 3-5 μm | 4.8 μm (best)
TID | > 1Mrad | > 3 Mrad

## Slide 20: Backup

## Slide 21: Pixel analog front-end
Based on ALPIDE* front-end scheme
  modified for faster response
  ‘FASTOR’ signal delivered to the EOC (end of column) when a pixel fired, timestamps of hit recorded at pos. edge of ‘FASTOR’
*Ref: D. Kim et al. DOI 10.1088/1748-0221/11/02/C02042
Delay time of FASTOR with respect to the pulse injection vs. injected charge. The delay time was measured by the timestamp of a step of 25 ns.
time walk
Pixel analog output
Pulse injection
“FASTOR” at EOC, derived from pixel digital output
pulse length
delay time
Schematic of pixel front-end

## Slide 22
Simplified column-drain readout:
  Each double column shares a common Fast-Or bus for hit indication
  Common time stamp register @40MHz will record the hit arrival time
  Hit pixels in the same cluster will share a common time stamp as the Trigger ID
Two parallel digital readout architectures were designed:
  Scheme 1：ALPIDE-like: benefit from the proved digital readout in small pixel size
    Readout speed was enhanced for 40MHz BX
  Scheme 2：FE-I3-like: benefit from the proved fast readout @40MHz BX (ATLAS)
    Fully customized layout of digital cells and address decoder for smaller area
Pixel architecture – parallel digital schemes

## Slide 23
Designed for low power
  Only the hit (fastor) info & address are fannout from the pixel array
  Only the read (acquisition) signal is fanned in to the pixel array
    Clock & time stamp are localized only in the EOC, different from FE-I3
Optimized @ CEPC hit rate
  Common time stamp recorded for a full double column
    For low power
    Column is hit every 8.3us / pixel is readout in 2 clocks (50ns) / cluster size 3 pixels
    Dead time 500ns – 98% trigger efficiency
Readout & Periphery
Time stamp recorded when Fastor is valid
Each pixel readout by 2 clocks (50ns)
  Worst delay ~ 25ns
    Sim by 512 rows (full size)
    TDA: read sent –addr come
  Address latch @ 37.5ns
    @1.5 clock
    Enough headroom for all corners

## Slide 24: Readout system of TaichuPix chips
Readout system for single-chip includes
  A dedicated test board for chip wire-bonding and power link
  A readout board loaded with a FPGA to perform chip configuration and data readout
  A DC power supply
  A PC
Test board
Readout board
Structure of the readout system

## Slide 25: Electrical test
Electrical performance verified by injecting external voltage pulses into pixel front-end
Analog output of a pixel @ Vin = 0.9 V
Measured “S-curve” for 128 pixels
Threshold
Threshold dispersion
Noise (peak-to-peak )
Chip periphery

## Slide 26: Performance of threshold and noise of TaichuPix2
Pixel array includes 4 sectors with different transistor parameters/layout for analog front-end, S1 chosen for the full-scale design.
Threshold can be tuned by changing ‘ITHR’ (a global current bias)
Chip4 | Threshold Mean (e-) | Threshold rms (e-) | Temporal noise (e-) | Total equivalent noise (e-)
S1 | 267.0 | 49.8 | 29.3 | 57.8
S2 | 293.4 | 54.5 | 26.9 | 60.8
S3 | 384.9 | 58.4 | 24.4 | 63.3
S4 | 411.9 | 56.6 | 26.5 | 62.5
Mean threshold of Sector1 vs. ITHR setting
Sector1
Noise hit rate < 10-10/event/pixel for the measured threshold range

## Slide 27: TID test on TaichuPix-2
Chip was exposed with full working condition: power, bias, clk, …
Dose rate ~17.63 krad/min for the first 2.5 Mrad, then 211.56 krad/min for 51 min, then 1.24 Mrad/min for 15 min
Normal chip functionality and good noise performance proved up to 30 Mrad TID
Pixel threshold vs. TID
TaichuPix-2
TaichuPix-2 irradiated at BSRF 1W2B beamline (6 keV X-ray)
beam
Pixel noise vs. TID

## Slide 28: Overview of the full-scale prototype
Process: 180 nm CMOS Imaging Sensor process (7 metal layers)
Pixel cell copied exactly from MPW + scaled logic with new layout Periphery + debugged/improved blocks + enhanced power network
Pixel array 1024*512
Periphery
DAC & Bias generation
Data interface
LDO (test blocks)
Chip inter-connection features
Scribe-able top power connection features
1
2
3
4
5
6
7
25.7 mm
15.2 mm
0.6 mm

## Slide 29: TaichuPix-3 specification & performance
 | Design specs. | Measured
Spatial resolution* | 3~5 μm | 4.8 μm (best)
TID* | > 1 Mrad | > 3 Mrad
Pixel pitch | ≤ 25 μm | 25 μm
Chip size | ~1.4 × 2.56 cm2 | 1.59 × 2.57 cm2
Dead time | < 500 ns | ~ 300 ns
Data rate | 110 Mbps (trigger) 3.84 Gbps (triggerless) | Not tested Currently 160 Mbps tested
Power density | < 200 mW/cm2 | 89 – 164 mW/cm2
*project indicator

## Slide 30: Flex cable design consideration
Design goals & considerations for the Flex PCB
  Minimum material budget
    Minimum dead zone extension, limited height of PCB
      Minimum set of signals on Flex
      Inter-chip connection for slow controls through wire bonding  save some space & metal on PCB
    Robust power supply
  Manufacturability
Power
Slow bus
Signals
2mm margin for wire bonding and PCB Pads

## Slide 31: Design of the flex board
Option1
  2 layers + stiffener
  Inter-conn signal used
  worse signal integrity
    Noise
    Ground bounce
Option2
  4 layers flex + stiffener
  Dedicated GND and power plane
  better signal integrity

## Slide 32: New batch of flex boards
25 2-layer flex from FASTPRINT company received, same as previous bunch
  Thickness: 0.31 mm (from the delivery list)
15 2-layer flex and 15 4-layer flex from SCC company received
  Thickness: 0.161 mm for 2-layer; 0.213 mm for 4-layer (from the final inspection report)
Old 4-layer
stiffener on backside of socket
New 4-layer
No stiffener

## Slide 33: TC3 beam test results
Detection efficiency vs. threshold (4 GeV)
  The efficiency decreasing with increasing threshold

## Slide 34: Ladder readout design
Two versions of flex board designed
  Version 1 (baseline): 2 layers, less material, limited layout space leads to worse signal integrity, thickness ~0.2 mm, in production
  Version 2: 4 layers, more material dedicated GND and power plane gain better signal integrity, thickness ~0.4 mm, production done
Interposer board
553 mm
FPGA board
  Communication with chips
  Data processing and package data
  Readout to PC via 1Gbps Ethernet
  Capability of 6 Gbps readout and 2GB internal DDR memory

## Slide 35: Design of DAQ
Considering 6 double-sided ladders

## Slide 36: TowerJazz process
Standard & modified process