## Slide 1
Progress of CEPC Detector Magnet
Ning Feipeng
2023.07
中国科学院高能物理研究所
Institute of High Energy Physics, CAS

## Slide 2
Outline
Introduction of CEPC detector magnet
Progress of HTS cable
Other progress
Other HTS detector magnets
Summarize

## Slide 3: 1. Introduction of CEPC Detector Magnet
Magnetic field | 3 T | Current | 28000 A
Inner diameter | 4660 mm | Inductance | 1.27 H
Outer diameter | 4960 mm | Stored energy | 500 MJ
Magnet thickness | 150 mm | Cold mass | 27 ton
Length | 8000 mm | HTS cable length | 10.7 km
Total weight | 48 ton | ASTC weight | 16.6 ton
A large ultra-thin & transparent HTS solenoid magnet:
Coil layout
support
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 33, NO. 6, SEPTEMBER 2023
The 4th Conceptual Detector Design: The solenoid magnet locates between Hcal and Ecal.

## Slide 4: 2. Progress of HTS cable
铝稳定体高温超导叠型电缆
ASTC(Al stabilized HTS Stacked Tape Conductor) development
Advantage: Simple structure, easy to process, has experience and processing equipment;
Disadvantage: uneven current distribution, High dynamic loss, great influence of shielding current, large AC loss, and so on.
Pure Al stabilizer

## Slide 5
ASTC(Al stabilized HTS Stacked Tape Conductor) cable development
2. Progress of HTS cable
Small size cable: 15*10mm2 , Tape Width: 4 mm, tape thickness: 80 μm, tape Ic > 120A@77K;
Object：single tape core Ic > 100 A@77K；14-core cable Ic > 830 A@77K, self-field.
Pure Al stabilizer
HTS stack
HTS tape
Ic = 905A
Significant progress has been made in the development of HTS cable.

## Slide 6
ASTC(Al stabilized HTS Stacked Tape Conductor) cable development
Problems during development:
Wrapping tape breakage
Core wire breakage
High temperature duration too long
Adhesion of Superconducting tape
Core twisting and misalignment
2. Progress of HTS cable
The process of cable development in the past three years:
1，How to process cables?
2，How to improve cable performance?

## Slide 7: 2. Progress of HTS cable
10 m ASTC prototype cable
Small size cable: 15*10mm2 , Tape Width: 4 mm, thickness: 80 μm
2021.09.29
1，How to process cables?

## Slide 8
2. Progress of HTS cable
2，How to improve cable performance?
High temperature and high pressure caused severe performance degradation of HTS superconducting tapes
The critical current of 20-layer cable is only 180A, Severe degradation of superconducting tape performance.

## Slide 9
2. Progress of HTS cable
cable performance improvement
single tape core Ic > 100 A@77K, self-field

## Slide 10
Chart: 
| 44468 | 44667 | 44729 | 44803 | 44807 | 44907 | 44989 | 44996 | 45029 | 45062 | 45069 | 45086
电缆电流 | 180 | 560 | 350 | 705 | 740 | 600 | 450 | 700 | 745 | 580 | 755 | 905
2. Progress of HTS cable
cable performance improvement：The performance of the cable meets the expected requirements.
7 layers
20 layers
16 layers
15 layers
14 layers
16 layers
14 layers
14 layers
16 layers
16 layers
14 layers
Object：single tape core Ic > 100 A@77K；considering the self-field effect, The critical current of a 14-core cable is larger than 830 A@77K, self-field.

## Slide 11: 2. Progress of HTS cable
Future work of HTS cable: From small size cable to full size cable
  Continued optimization of cable performance;
  Aluminum coating of large-sized superconducting stack using high-strength pure aluminum;
  Research on High Strength Pure Aluminum, 4N8Al+0.025Er%？Other choices？
  Welding of aluminum coating cables and high-strength aluminum alloys, electron beam welding? Friction welding?

## Slide 12: Future plan of ASTC cable
Detector magnet
Small magnet
Accelerator magnet
Fusion magnet

## Slide 13
High Energy physics, detector magnets
Small magnets, high field
insert coil, Instead of NbTi
High field accelerator magnets, SMES
NMR
MRI
ITER
SMES
CMS
EAST
ASTC (Al stabilized Stacked ReBCO Tape Conductor)
Rutherford Cable
CICC
CEPC
Fusion magnets

## Slide 14: Other process of HTS cable
Fcc IDEA
CEPC HTS
High strength and High RRR pure aluminum stabilizer
CMS

## Slide 15: Other process of HTS cable
R&D of High Strength and High RRR Aluminum- Stabilizer for Superconducting Cable
LTS: Yield strength > 100 MPa@4.2K, 74 MPa at room temperature, RRR value > 400
By doping Ni-0.025% Be-0.025%, annealing, cold-working and curing.
The Al-0.025%Ni-0.025%Be alloy prepared from 4N8-aluminum achieved high 0.2% yield strength of 75MPa (R.T.) with RRR of 417 after cold working of 21% and annealing at 130℃ for 15hrs.
HTS: Yield strength > 140 MPa, RRR value > 200
By doping Er-0.025.
The 4N8Al-0.025%Er achieved high 0.2% yield strength of 144MPa with RRR of 208
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 33, NO. 2, MARCH 2023

## Slide 16: Optimization of HTS detector magnet
Optimization of HTS cable structure.

## Slide 17: Optimization of HTS detector magnet
 | Before optimization (MPa) | After optimization (MPa)
ReBCO tape | 461 | 375
Pure Al | 239 | 114
Al-alloy in cable | / | 182
Al-alloy support | 167 | 176
30mm
2*15mm
Why we changed the HTS cable structure:
Need high strength cable.
Maximum stress on the coil

## Slide 18: Mechanical structure
Aluminum alloy support
How to layout the 150mm thickness：
Cable: 20*25mm2
Including: vacuum cryostat, thermal shield, cold mass, Multi-layer insulation, support structure, liquid helium pipe, liquid nitrogen pipe, wires and so on.

## Slide 19: Mechanical structure
Three working conditions: vacuum, cooling, and excitation
vacuum：

## Slide 20: Mechanical structure
cooling：
Cooling to 4.2k, radial deformation
Cooling to 4.2k, axial deformation

## Slide 21: Mechanical structure
Cooling to 4.2k, excitation, radial deformation
Cooling to 4.2k, excitation, axial deformation
excitation：

## Slide 22
Winding method of Large HTS coil
Research of winding method of large HTS coil：
  Much difference from LTS. Research on coil winding technology that more suitable for large HTS magnets.
  No epoxy impregnation? No-insulation?
HTS长缆

## Slide 23
Wind method study
Is No-insulation winding method suitable for large coil using cable？
No epoxy impregnation? No-insulation?
Epoxy impregnation & insulation
NI
NI
Insulation
Insulation
MI
No-epoxy impregnation & No-insulation

## Slide 24
Cable joint study
Research on HTS cable Joint Technology：
  Cable-cable joints
    Inner joint：turn the cable joints into tape joints, evenly distributed in the cable.
    Realize long cables.
    Outer joints：coil-coil joints
    Making joints between cables with small volume, low resistance, and convenient processing.

## Slide 25
Cable joint study
Cable-current leads joints
    Step welding allows each tape contact with the copper lead, the current evenly enter the cable

## Slide 26
Cable joint study
Other HTS cable joints：
Bridge-type mechanical lap joint of HTS STARS conductors
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 26, NO. 2, MARCH 2016
HTS Stacked Tapes Assembled in Rigid Structure (STARS) conductors

## Slide 27
Cable joint study
Bridge-type mechanical lap joint of HTS STARS conductors
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 26, NO. 2, MARCH 2016

## Slide 28
Cable joint study
Bridge-type mechanical lap joint of HTS STARS conductors
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 26, NO. 2, MARCH 2016
The joint resistance was 1.8 nΩ at 100 kA, 4.2 K,0.45 T.
Heat per joint：Q = 18W
Fusion Engineering and Design 146 (2019) 590–593

## Slide 29
Cable joint study
BES III LTS cable joint：
Cable-cable joint
Cable-current leads joints

## Slide 30
Cable joint study
CMS LTS cable joint：
In order to achieve joint electrical resistance lower than 10-9Ω, Metal Inert Gas (MIG) welding are performed.
The reinforcement of the conductors must be machined out in the joint area as the weld is performed to join the pure aluminum stabilizing matrix of both conductors. The conductor lengths are welded together side by side on a length of about 2 m.
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 16, NO. 2, JUNE 2006
0.39 n at B=0T and B=1T, and 0.454 n at B=2T

## Slide 31
Quench detection and protection
Quench detection study：
quench propagation characteristics of the ASTC cable, quench propagation speed, minimum quench energy，the role of aluminum stabilizer.
Partial quench or overall quench? Quench propagation speed？
CMS Equivalent electrical circuit

## Slide 32: Detector magnet needed in the future
 | Experiments | Site | B [T} | Size, ID x L [m] | Note | Fabrication Expected
Collider | EIC-Detector | BNL | 1.5~3 | 2.5~3.2 x 8.5 | Solenoid | 2025 ~
 | ILC-ILD | Japan | 4 | 6.88 X 7.35 | Solenoid | 2030 ~
 | ILC-SiD | Japan | 5 | 5 X 5 | Solenoid | 2030 ~
 | CLIC-ILD | CERN | 4 | 6.8 X 8.3 | Solenoid | 2035 ~
 | CLIC-SiD | CERN | 5 | 5.4 X 6.5 | Solenoid | 2035 ~
 | CLIC | CERN | 4 | 7 X 8.3 | Solenoid | 2035 ~
 | FCC-ee IDEA | CERN | 2 | 4.2 X 6.0 | Solenoid | 2035 ~
 | FCC-ee CLD | CERN | 2 | 7.4 X 7.4 | Solenoid | 2035 ~
 | FCC-hh | CERN | 4 | 10 X 20 | Solenoid | 2060 ~
 | ALICE-3 | CERN | 2 | 3 x 7.5 | Solenoid | 2027 ~
Others | M2e | Fermilab | 5 ~ 2.5 | 1.5 X 4 | Production | Under construction
 | Muon-g-2 | Fermilab | 1.473 | 0.09 X 14.22▪2 | Storage solenoid | Reuse after BNL
 | COMET | J-PARC | 5 ~ 3 | 1.3 X 1.6 | Capture Sol. | Under const.
 | Muon-g-2 | J-PARC | 3 | 0.66 X 0.33 | Solenoid | 2025 ~
 | BabyIAXO | DESY | 2 | 0.7 X 10 | D. Racetrack | TBD
 | IAXO | DESY | 5 - 6 | 5 X 25 | Toroid | TBD
 | Panda | GSI | 2 | 1.8 x 3.1 | Solenoid | TBD
 | Madmax | DESY | 9 | 1.35 x 1.2 | Dipole | TBD

## Slide 33: Aluminum stabilized superconducting cables
Future

## Slide 34: FCC-ee HTS detector magnet design
IDEA detector
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 33, NO. 5, AUGUST 2023

## Slide 35: FCC-ee HTS detector magnet design
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 33, NO. 5, AUGUST 2023

## Slide 36: AMS-100 HTS detector magnet
AMS-100 Alpha Magnetic Spectrometer on the International Space Station
Magnetic Spectrometer to be send to Lagrange Point 2 (1.5 Mkm from earth).
Probing high energy cosmic rays, in particular anti-protons and anti-deuterons.
Geometric acceptance of 100 m2 sr.
Main magnet is a 6 m long, 4 m diameter HTS ultra-thin solenoid.
No active cooling, only passive cooling using radiators.
Electrical/thermal/mechanical challenge.
Compensation coil needed to correct magnetic torque during operation.
Comp. coil is a 1.5 m long, 8 m diameter HTS solenoid.
12 mm
4 mm
12 mm
12 mm

## Slide 37
Summarize
Significant progress has been made in the development of HTS cable.
Many other challenges need to be studied:
  From small size cable to full size cable；
  Ultra-thin and transparent mechanical structure；
  Winding methods of large HTS solenoid, No-insulation?
  Joint of HTS cables；
  Quench detection and protection of HTS.