## Slide 1: Development of aerogel based RICH detectors
Alexander Barnyakov
on behalf of BINP Aerogel group
Budker Institute of Nuclear Physics & Novosibirsk State Technical University , Novosibirsk, Russia
Aerogel RICH in the HEP
Aerogel R&Ds at the BINP
  FARICH technique progress
  FARICH with dual aerogel radiator concept
  Aerogel RICH with Fresnel lens
Summary
23 August 2023
Institute of High Energy Physics, Chinese Academy of Sciences, Beijing, China

## Slide 2: Aerogel RICH in the HEP

## Slide 3: Aerogel is a classical nanomaterial
Aerogel – is a porous material with pore dimension less than visible light wavelength.
It is a classical nanomaterial. The most interesting for physics experiments are silicon dioxide (SiO2) based aerogels:
1.008 | 0.84 | 1.1 | 3.9 | 7.4
1.03 | 0.43 | 0.56 | 2.0 | 3.8
1.05 | 0.33 | 0.43 | 1.5 | 2.9
1.13 | 0.2 | 0.26 | 0.94 | 1.8
1.008 | 0.84 | 1.1 | 3.9 | 7.4
1.03 | 0.43 | 0.56 | 2.0 | 3.8
1.05 | 0.33 | 0.43 | 1.5 | 2.9
1.13 | 0.2 | 0.26 | 0.94 | 1.8
Aerogel was first synthesized by Samuel Stephens Kistler in 1931
S.S.Kistler, "Coherent Expanded Aerogels and Jellies“, Nature, 1931,vol. 127, p. 741

## Slide 4: How it all began?
1973
n=1.01—1.06 (1.2 using sintering)
Lsc(400) = 6 mm
There is a Cherenkov light from aerogel!
‘The are no evident signs of scintillations in aerogel’!

## Slide 5: Ring Imaging Cherenkov detectors with aerogel radiators
If the Cherenkov radiation angle is measured, the precision in the determination (identification) of particle masses will be higher than in threshold counters.
In the 1980s and 1990s, a whole series of RICH detectors were constructed:
  CRID, SLD detector, SLAC(C6F14 n=1.277, C5F12/N2 n=1.0017)
  RICH, Delphi detector, CERN, (C5F12|C6F14, C4F10)
  RICH, CLEOIII detector, Cornell, (LiF, n=1.50)
  DIRC, детектор BaBar, SLAC, USA (SiO2, n=1.47)
Main problem – they do not provide π-K identification in the momenta range 4÷10 GeV/c
Material with n=1.03-1.05 is needed. Aerogel!
A.Roberts, NIM 9(1960)55
J.Seguinot and T.Ypsilantis, NIM 142(1977)377

## Slide 6: Peculiarities of aerogel use in RICH detectors
For a long time, it was considered impossible to use aerogels in RICH detectors owing to the strong scattering of light.
1991 – the first experimental observation of Cherenkov ring from aerogel using photography method
A.I.Vorobiov, V.P.Zrelov, J.Ruzichka, “On some peculiarities of Vavilov-Cherenkov radiation in aerogels”, In Frascati 1991, Physics and detectors for DAPHNE, the Frascati Phi-factory* 551-556
The first RICH with aerogel was proposed Douglas Fields in 1994
D.E.Fields et al., NIM A349(1994)431
1995 – Aerogel RICH for LHCb was suggested. The requirement on minimal light scattering length was elaborated.
J.Seguinot, T.Ypsilantis, NIM A368(1995)229)
1995-1996 – two-step aerogel production was optimized, (400 mm)=40÷50 mm
A.R.Buzykaev et.al, NIM A379(1996)465)

## Slide 7: Why Aerogel RICH?
The difference of Cherenkov angles for different particles is larger
Aerogel refractive index dispersion is smaller
The large number of detected photons from high refractive index radiators can not compensate these effects ()

## Slide 8: The first aerogel RICH
Hermes RICH (DESY, Gamburg)
π/K/p – separation at 2÷15 GeV/c
aerogel, n=1.03 -> π/K – separation 2÷7 GeV/c
C4F10, n=1.0014 -> π/K – separation 7÷15 GeV/c
Start of the design – 1996
1020 aerogel tiles 114x114x11mm3
Start of the operation -- 1998
Investigate spin structure of nuclons
Y.Miyachi, NIM A502(2003)202

## Slide 9: Aerogel in LHCb (LHC-CERN)
measure the parameters of CPV in the interactions of b-hadrons
BIC/BINP production, n=1.03, 20x20x5 cm tiles
Aerogel did not work – small number of photoelectrons in the ring + strong pile-up noise

## Slide 10: Aerogel RICH at AMS-02 at ISS
Measurement of Z of the nucleon, Npe~Z2
BIC/BINP production, n=1.05
More than 10 years in operation since 2010
Very well agreement experimental measured parameters with expected (required) in the project
F.Giovacchini et al., NIM A970 (2020) 163657

## Slide 11: Belle II: ARICH
T.Iijima et al., NIM A548 (2005) 383
Proximity focusing aerogel RICH
Stack of two blocks with different n:
  n1=1.045 / 20 mm
  n2=1.055 / 20 mm
Focal distance 200 mm
Increase Npe due thickness increase without σΘc degradation
Exper. | 93.5±0.6% | 10.9±0.9% | 87.5±0.9% | 5.6±0.3%
MC | 96.7±0.2% | 7.9±0.4% | 91.3±0.3% | 3.4±0.4%
Exper. | 93.5±0.6% | 10.9±0.9% | 87.5±0.9% | 5.6±0.3%
MC | 96.7±0.2% | 7.9±0.4% | 91.3±0.3% | 3.4±0.4%
The first application of technique in Belle2 ARICH
-separation better up to 4 GeV/c
248 aerogel tiles in 2 layers 2+2 cm
420 HAPD; 144 pixels with 5х5 mm2 per each
Y.-T. Lai et al 2020 JINST 15 C07039
PTEP 2016, 033H01
Belle II
TBeam results
Notes: Идея ФАРИЧ появилась в 2004 г.
Точность измерения черенковского угла связана с точностью измерения скорости, а значит с качеством разделения частиц.

## Slide 12: CLAS-12 RICH (J-Lab, Newport)
Investigate spin structure of nuclons
π/K/p-separation at 3÷8GeV/c
Aerogel n=1.05
2 sectors with 102 tiles 20x20x3(2)cm3/each
M. Contalbrigo et al., NIM A964 (2020) 163791

## Slide 13: Aerogel R&Ds at the BINP

## Slide 14
History of aerogel radiators in Novosibirsk
SND ASHIPH system (VEPP-2000 – BINP):
  𝜋/K-separation in the momentum range 300÷870 MeV/с.
  Aerogel (V~9 L).
KEDR ASHIPH system (VEPP-4М – BINP):
  𝜋/K-separation in the momentum range 0,6÷1,5 GeV/с.
  Aerogel (V~1000 L).
DIRAC-II (PS – CERN):
  𝜋/K-separation in the momentum range 5,5÷8,0 GeV/с.
  Aerogel (V~9 L).
LHCb aerogel RICH (LHC – CERN):
  𝜋/K-separation in the momentum range 5,5÷8,0 GeV/с.
  Aerogel (S~0,5 m2), aerogel tile 20х20х5 см3.
CLAS-12 aerogel RICH (J-Lab):
  𝜋/K- & K/p-separation at level 4𝜎 with several momentum GeV/с.
  Aerogel (S~6 m2), aerogel tile 20х20х2-3 см3.
AMS-02 aerogel RICH (ISS):
  Search for antimatter, study of cosmic rays.
  Aerogel (S~1 m2).
Aerogel RICH for CLAS12

## Slide 15: Novosibirsk aerogels is hydrophilic!
Aerogel with bulk density 0.24 g/cm3 has internal surface area by 106 times larger than external.
There are a lot of OH−groups at the aerogel SiO2 surface. These groups are primary adsorption centres which are able to attract hundreds of the H2O molecules per each.
In the hydrophobic aerogels OH−groups are exchanged by hydrophobic radicals such like Si(CH3)3
Influence of adsorbed water on optical parameters of hydrophilic aerogels produced in Novosibirsk are very well studied already.
Heating of hydrophobic aerogel up to above 175℃ makes it hydrophilic. Also more active radicals are able to replace Si(CH3)3 – groups and change aerogel optical parameters.
Before the finalization of any aerogel based counters design it is necessary to investigate influence of materials (such like WLS, hermetics or second gas/liquid Cherenkov radiators) which are going to be used in the construction on aerogel transparency.

## Slide 16: Water adsorption by aerogel
Adsorption
Desorption
Water adsorption and desorption are the fast processes with time constant about 1 hour.
Amount of adsorbed water depends on relative humidity of invironment.

## Slide 17: Refractive index
For theoretical dependence Lorentz-Lorentz formula
was used, which was expressed to calculate refractive
index of gases mixtures but it very often works for other
mixtures.
dependence on water adsorption
Impirical relation is used for fast determination of

## Slide 18: Aerogel transmittance and parameters of Rayleigh light scattering
Hunt formula to fit the transmittance (T) usually are used in two variations:
or
where – aerogel thickness, – light scattering length at 400 nm and – so called clarity, – coefficient responsible for light absorption and scattering at the surface of aerogel samples.

## Slide 19: Influence of adsorbed water on Raleigh light scattering
Raleigh light scattering in aerogel strongly dependce on amount of adsorbed water the effects of light scattering length decrease in normal conditions doesn’t exceed 10% (Lsc(400 nm) drops from 43 to 38 mm).
T. Bellunato, et al., NIM A 527(3) (2004) 319

## Slide 20: FARICH – 19 years of R&Ds (since 2004)

## Slide 21: FARICH technique
T.Iijima et al., NIM A548 (2005) 383 and A.Yu.Barnyakov et al., NIM A553 (2005) 70
n=1.030 6.0mm
n=1.027 6.3mm
n=1.024 6.7mm
n=1.022 7.0mm
The first 4-layer monolithic sample
Increase Npe due thickness increase without σΘc degradation
2004÷2005
Excellent PID capability were shown at CERN beam test in 2012
A.Yu. Barnyakov, et al., NIM A 732 (2013) 352
The Belle II (ARICH) is the first application of the method
2017
Two 4-layer focusing aerogel blocks
230x230x35 mm
2022÷2023
Notes: Идея ФАРИЧ появилась в 2004 г.
Точность измерения черенковского угла связана с точностью измерения скорости, а значит с качеством разделения частиц.

## Slide 22
GEM
MaPMT H12700 (Hamamatsu)
with mask 3х3 mm2
2 aerogel pcs
230x230x35 mm
The largest 4-layers focusing aerogel samples
Refractive index profile is measured with help of didgital X-ray setup at the BINP.
Single photon Cherenkov angle resolution is investigated with relativistic electrons at BINP beam test facilities ”Extracted beams of VEPP-4M complex”.

## Slide 23
BINP beam test facility
4 MaPMT H12700
G N Abramov et al 2014 JINST 9 C08022

## Slide 24
Beam test results
Pixel 6x6 mm
Geom.Eff. ~ 80%
Pixel 3x3 mm
Geom.Eff. ~ 20%

## Slide 25: Cherenkov angle Single Photo-Electron (SPE) resolution
PTEP 2016, 033H01
Belle II
Aerogel: 20+20 mm (Chiba Univ.)
n(400nm): 1.045 +1.055
Pixel: 5x5 mm
4-layers (Novosibirsk) –>
1.039 ÷ 1.046
6x6 mm
Simulation
TBeam
–
–
3x3 mm
4-layers (ideal profile)
1.041 ÷ 1.050
3x3 mm
Geom.Eff. ~ 80%
Geom.Eff. ~ 20%
The excellent single photon Cherenkov angle resolution ~7÷8 𝑚𝑟𝑎𝑑 was achieved with the 4-layer focusing aerogel tiles
with dimensions 23x23x3.5 cm for the first time in 2022!!!
This circumstance allows us to consider the FARICH detector design based on 4-layer focusing aerogel tiles with large dimensions (23x23x3.5 cm).
Geom.Eff. ~ 90%

## Slide 26: FARICH system for the SCTF
275 tiles 200x202x35 in barrel part
2x55 trapezoidal tiles in end caps:
2x12 – inner radius
2x18 – medium radius
2x25 – outer radius
Aerogel layout
Proximity focusing RICH
4-layer focusing aerogel
  nmax = 1.05 (1.07?), total thickness 35 mm
21 m2 – total area of photon detectors
  • SiPMs – barrel part (16 m2)
  • MCP-PMT – endcap parts (4 m2)
~106 pixels 3х3 mm2 with pitch 4 mm
SHAPE |  | Aerogel size, mm |  |  | 
 |  | 200 | 100 | 75 | 50
Parallelepiped | 6 | 0.86 | 0.74 | 0.62 | 0.5
Trapezoidal | 1 | 0.96 | 0.94 | 0.92 | 0.9
SHAPE |  | Aerogel size, mm |  |  | 
 |  | 200 | 100 | 75 | 50
Parallelepiped | 6 | 0.86 | 0.74 | 0.62 | 0.5
Trapezoidal | 1 | 0.96 | 0.94 | 0.92 | 0.9
GEANT4 simulation
of edge effects
Notes: Идея ФАРИЧ появилась в 2004 г.
Точность измерения черенковского угла связана с точностью измерения скорости, а значит с качеством разделения частиц.

## Slide 27: FARICH edge effects: simulation & experiment
Parallelepiped shape aerogel G4sim
Tracks are in a midle of aerogel tile
Tracks are in 6±4 mm from aerogel tile edge
Beam test & sim. results
Black paper between aerogel blocks

## Slide 28: FARICH proposal for SPD-NICA experiment

## Slide 29: NICA: Nucleon Ion Colliding fAcility
https://nica.jinr.ru/complex.php

## Slide 30: SPD: Spin Physics Detector
http://spd.jinr.ru
• Polarized (or )
• 2E = 27 GeV (or 13.5 GeV/nucl)
• L = 1032 cm-2s-1 (or 1031 cm-2s-1)
PID:
• π/K/p - separation
• ToF (60ps) + Aerogel

## Slide 31: FARICH option for SPD
π/K – separation in wide momenta range
Improve momentum resolution
A.Yu. Barnyakov, et al., NIM A 732 (2013) 352
A.Yu. Barnyakov, et al., NIM A 639 (2011) 290
Recent TBeam results:
π/K @ 8 GeV/c :
Precise mesurement of velocity with FARICH
improves momentum resolution: @1 GeV/c
DC (Straw tubes): @1 GeV/c

## Slide 32: Aerogel layout
For two endcap FARICH detectors it is required:
– 136 ”good” aerogel tiles 23x23x3.5 cm (5.44 m2);
– Produce, select and characterise aerogel tiles with help of digital X-ray setup and other laboratory satnds including electron beam test facilities* at BINP;
– Cutt off 136 tiles in 4 different trapziodal shapes;
– 106 ”good” aerogel tiles 23x23x3.5 cm (4.24 m2);
– Produce, select and characterise aerogel tiles with help of digital X-ray setup and other laboratory satnds including electron beam test facilities* at BINP;
– Cutt off 106 tiles in 2 rectangular and 2 trapziodal shapes;
2.5÷3 years for production
2÷2.5 years for production

## Slide 33: FARICH with dual aerogel radiator

## Slide 34: PID options for – separation
  up to 0.6 GeV/c
  up to 0.9 GeV/c
Focusing Aerogel RICH (FARICH)
(4 layer @ =1.05) from 0.5 to 6 GeV/c
ASHIPH@SiPM (n1=1.03 and n2=1.015) from 0.6 to 3.5 GeV/c
A.Yu. Barnyakov, et al., NIM A 732 (2013) 35
Parametric simulation
A.Yu. Barnyakov et al 2020 JINST 15 C04032
EPJ Web of Conferences 212, 01012 (2019),
A.Yu. Barnyakov et al 2020 JINST 15 C04032

## Slide 35: PID options for µ – separation
  up to 0.15 GeV/c
  up to 0.25 GeV/c
TOF with 100 ps up to 0.2 GeV/c, e.g. Chernkov light from entrance window of MCP-PMT
FARICH (4-layer, =1.05) from 0.5 to 1.5 GeV/c
A.Yu.Barnyakov et al., NIMA 1039 (2022) 167044
Results of parametric simulation tuned with results of beam test campaign in 2021:
– SPR= 1.63 mm
– SPR= 1.36 mm
FARICH with dual aerogel radiator is proposed
to provide µ – separation for 0.2≤P≤0.5 GeV/c

## Slide 36: RICH with dual radiators is not very new idea!
Liquid + Gas:
  RICH – DELPHI
  CRID – SLD
    C6F12(n=1.278@190nm) + C5F10(n=1.00174@190nm)
Aerogel + Gas:
  HERMES
  RICH1 – LHCb
    Aer.(n=1.03@400nm) + C4F10(n=1.00137@400nm)
Aerogel + Crystal:
  RICH+ToF – SuperB:
    Aer.(n=1.05@400nm) + Quartz (n=1.47@400nm)
  FARICH – SuperB:
    3-layer aer. nmax=1.07@400nm + NaF (n=1.33@400nm)
Aerogel + Aerogel:
  FARICH – SCTF:
    4-layer aer. nmax=1.05@400nm + aer (n=1.12@400nm)
P=2 GeV/c
Aerogel is material with easy tunnable refractive index!

## Slide 37: Aerogels with high optical density
Sintering approach
ZrO2 addition approach
230 мм
230 мм
n=1.05
n=1.12
n=1.2
n=1.25
n=1.13
The main flaw
of this approach
Lsc(400nm)
Refractive index
The first sample of
SiO2–ZrO2 aerogel
The addition of small amount (0.03÷0.06 mol) of ZrO2 in SiO2 based aerogel alow us to produce highly transperant aerogels with high optical density:
Refractive index up to n=1.12
Rayleigh light scattering length Lsc(400nm) up to 30 mm

## Slide 38: Beam tests results of FARICH with dual radiator
GEM2
GEM3
GEM1
GEM1–GEM2
GEM1–GEM2–GEM3
Photon detector
ZrO2 aerogel
ZrO2–SiO2 aerogel:
Thickness 12 mm & ø20 mm;
Lsc(400nm)=21±0.5 mm;
4-layer SiO2 aerogel:
100x100x35 mm;
Lsc(400nm)=37±0.3 mm;
Photon detector
4 MaPMT H12700 (Hamamatsu);
256 pixels with 3x3 mm size;

## Slide 39: G4 simulation vs beam test results
TBeam results
G4 simulation results
Optical parameters for G4 simultion
PDE for H12700 from data-sheet
Pixel 3x3 mm with pitch 6mm
Focal distance L=172 mm
The main difference between G4sim and TBeam is a photon small angle scattering effect on aerogel surfaces and inside. These effects have not implemented in G4sim yet.

## Slide 40: µ/π-separation via G4 simulation
FARICH: "ideal” profile
FARICH (“ideal”)+ZrO2–aer. (=1.12/12 mm)

## Slide 41: RICH with Fresnel lens

## Slide 42: EIC project
Key EIC Characteristics (parameters)
– High particle collision rate
– Large center-of-mass energy range
– electrons
– protons
– Polarized beams of electrons and ions
– Large range of ion species
– At least one large-acceptance detector
– Projected budget: – Start date:
Almost approved concept since begin of 2022

## Slide 43: ECCE-PID & mRICH system concepts
Physics requirements
  pion, kaon and proton ID
  over a wide range |η| ≤ 3.5
  with better than 3σ separation
  significant pion/electron suppression
Momentum-rapidity coverage
  forward: up to 50 GeV/c
  central: up to 6 GeV/c
  backward: up to 10 GeV/c
Demands different technologies
Cherenkov detectors:
  dRICH = dual RICH (aerogel + gas)
  hpDIRC = high-performance DIRC (synthetic fused silica)
  mRICH = modular RICH (aerogel + Fresnel lens)
ECCE = EIC Comprehensive Chromodynamics Experiment
68 modular counters oriented to IP:
– aerogel n=1.03 100x100x40 mm3
– acrylic Fresnel lens with focal distance 6”
– position sensitive photon detector HRRPD (MCP-PMT) or SiPM arrays

## Slide 44: Aerogel RICH with Fresnel lens
Such approach allows us to improve Cherenkov angle resolution and optimize photo detectors area!

## Slide 45: The thick aerogel for mRICH – EIC project
In both cases there is no reason to make the aerogel thickness more than
In case of approach “stack” the additional Cherenkov photons loss is occurred due to reflectance and scattering on the additional surfaces
There are two not cut off surfaces in aerogel
  “Optical surface” – it contacts only with air during the production
  “Bottom” – it contacts with metallic frame during the production processes
Several configuration of the aerogel Cherenkov radiators were tested with relativistic electron beams at BINP beam test facilities in 2022.
230
230
40
op460f11
n=1.027
FermiLAB 2021: stack of three 1 cm thickness
blocks with n=1.03 from Chiba University
BINP 2022:
single block 23x23x4 cm
with n=1.027
from BIC

## Slide 46: Cherenkov angle single photon resolution (SPR)
19.0+17.6 mm
457f3+457f4
17.6 mm
457f4
40. mm
460f11_22
19.0 mm
457f3
50. mm
460f15_3
30.0 mm
460f4_3
Photon detector
Cherenkov light
t
L=175 mm
,
,
 | 457f4 | 457f3 | 460f4_3 | 457f3_f4 | 460f11_22 | 460f15_3
t/L, mm | 17.6/185 | 19.0/175 | 30.0/185 | 36.6/185 | 40.0/185 | 50.0/185
, mrad | 14.46±0.06 | 15.92±0.06 | 16.96±0.05 | 20.8±0.1 | 24.0±0.1 | 26.7±0.1
Npe* – 60% of the ring | 4.01±0.01 | 4.16±0.01 | 7.69±0.02 | 5.51±0.02 | 8.22±0.03 | 8.05±0.02
,mrad | 7.2 | 7.8 | 6.1 | 8.9 | 8.4 | 9.4
, mm | 1.11±0.03 | 1.08±0.04 | 1.20±0.02 | 1.33±0.06 | 1.35±0.04 | 1.37±0.07
 | 5.9 | 6.15 | 6.65 | 7.5 | 7.7 | 8.1
 | 457f4 | 457f3 | 460f4_3 | 457f3_f4 | 460f11_22 | 460f15_3
t/L, mm | 17.6/185 | 19.0/175 | 30.0/185 | 36.6/185 | 40.0/185 | 50.0/185
 | 14.46±0.06 | 15.92±0.06 | 16.96±0.05 | 20.8±0.1 | 24.0±0.1 | 26.7±0.1
Npe* – 60% of the ring | 4.01±0.01 | 4.16±0.01 | 7.69±0.02 | 5.51±0.02 | 8.22±0.03 | 8.05±0.02
 | 7.2 | 7.8 | 6.1 | 8.9 | 8.4 | 9.4
 | 1.11±0.03 | 1.08±0.04 | 1.20±0.02 | 1.33±0.06 | 1.35±0.04 | 1.37±0.07
 | 5.9 | 6.15 | 6.65 | 7.5 | 7.7 | 8.1
How much effect from Fresnel lens is expected?!

## Slide 47: Position-sensitive photon detectors

## Slide 48: Photon detector options
SiPM arrays
There are several manufacturer in the world including China.
There is no comercially available SiPM arrays produced in Russia for the moment, but some R&Ds are going now.
Estimated cost of such detector option is about 100$/cm2
It is required to develop and produce special R/O electronics and cooling system to operate with SiPMs in SPD detector conditions
MCP-PMT
There are several manufacturer in the world including China.
There is no comercially available position-sensitive MCP-PMTs produced in Russia for the moment, but R&Ds are going now in (Baspik&Ekran FEP).
There is a very large spread of prices for rectangular position-sensitive MCP-PMT. The best price is about 200$/cm2
PDE is not so high, it is limited by photoelectron collection efficiency (~60%) and geometrical efficiency is worse than for SiPM option.
Specialised R/O elctronics is already developed for other experiments and could be adopted for the SPD experiment requirements
There is no such a big problem with intrinsic noise rejecion in comparison with SiPM option
HAPD
Due to axial magnetic field the SiPM is only one possible candidate for the cylindrical part of the FARICH system!!!
For the endacp regions there are three options of photon detectors.
Only Hamamtsu produced such devices for the Belle II experiment and now it doesn’t produced anymore!
There is no comercially available HAPDs in Russia for the moment, but R&Ds are going now in ISP SB RAS.
Price – ???
Expected PDE of such devices will less than for SiPM option but signficantly (1.5 times) higher than for MCP-PMT option.
Expected gain is about
Development of specialised R/O elctronics is needed. It is possible to adopt some Belle II ARICH system expirience.
The S/N-ratio is about 1000, it means that only thermostabilization system to operate at the room temperature will enough for this option.
59 mm
Planacon XP85112
8x8 pixels with 6x6 mm
Cost: 15
KETEK PA3325-WB-0808
(BroadCom, USA)
26.8 mm
73 mm

## Slide 49: SiPM array option
KETEK-BroadCom, USA
Joinbon Tech., China
– Endcaps: 2x2490 SiPM arrays 2.7x2.7 cm2
– Barrel: 18 000 SiPM arrays 2.7x2.7 cm2
– 1 470.7k pixels with 3x3 mm2
– Geometrical Efficiency
– Highly effective cooling sysytem is required!

## Slide 50: Position-sensitive MCP-PMT
HRPPD (Income)
10x10 cm; pixel 2.5x2.5 mm
Hamamtsu R10754-016-M16(N)
4x4 pixels with 5x5 mm
59 mm
Planacon XP85112
8x8 pixels with 6x6 mm
NNVT (China)
Collector plane of MCP-PMT
Concept of Ekran FEP
(Summer 2022)
Availabilty: until end of 2023?!
Price: until end of 2023?!

## Slide 51: Round vs Square MCP-PMT for the RICH
630 PMTs Ø58 mm (PC Ø50 mm) –>
216 pixels 2.9х2.9 мм
548 PMTs 58х58 mm (PC 50x50 мм) –>
16х16=256 pixels 2.9х2.9 mm

## Slide 52: Round vs Square MCP-PMT for the RICH (2) expected FARICH performance
Square shape MCP-PMT
(for )
Round shape MCP-PMT
(for )
To evaluate expected performance we can use recent FARICH beam test data:
– photoelectron collection efficiency ()
– Geometrical Efficiency of Test Beam setup (is determined by fill factor of photon detectors for the experimental setup)
µ/π @ 1 GeV/c:
π/K @ 6 GeV/c:

## Slide 53: R/O electronics cost estimation
FPG-TDC (GSI)
TOFPET-II (PetSys)
There are two modern approaches in development of specialised R/O electronics:
– ASIC (Application Specialised Integrated Circuits)
– FPGA (Field Programable Gate Arrays)
The differences in performance, power consumption and costs are not sufficient today!!!
if Nch<1000 (2019)
if Nch≤1000
A system with 100kChannel:
(2020)
A system with 30kChannel (HADES):
(2017)
Power consumption:
15mW/chan (ASIC) + DAQ (FPGA)~60mW/chan
Power consumption: ~55mW/chan
Both options are not available for us, we are looking for new solution!

## Slide 54: Summary
The PID systems based on aerogel Chernkov counters hve been developeing at the BINP since 1986 and huge experience is already accumulated
Aerogel based RICH detectors are very demand technique for some future colliding beam experiments
In 2020-2023 the essential progress in aerogel RICH development was achieved in Novosibirsk (BINP/BIC):
  Large (23x23x4 or 5 cm with n=1.03 or 1.05) and higly transperant aerogel blocks were produced and tested
  The 4-layer focusing aerogel sample with 20x20x3.5 cm size were produced for the first time in the world –> the possibility to create full-scale systems based on 4-layer focusing aerogel Cherenkov radiators was demonstrated
  The measured SPR (~7 mrad) of FARICH based on 4-layer focusing aerogel is in good agreement with simulation and expectation
  Recent progress in high opticaly dense aerogel production with help of ZrO2 dope allows us to consider new design of FARICH detector with dual aerogel radiator which able to provide exccelent µ/π – separation from 0.2 up to 1.5 GeV/c
For further progress of the aerogel RICH detectors development of photon detectors and compatible R/O electronics are highly required

## Slide 55: Back up slides

## Slide 56: TBeam simulation with G4: input data.
To perform quntitively comparison TBeam results with G4 simulation it is necessary to implement in simulation very correct data on aerogel parameters (n, Lsc, thick) and also about photon detector parameters such like Geometry and PDE.
As a QE() we will use data for MaPMT H12700 from manufacturier (Hamamatsu) data-sheet (DS) normalized on our own direct measurement QE(=409nm) performed with laser light sourse(see the pictures below: left).
Also it is necessary to take into account that flat-pannel MaPMTs have non 100% photoelectron collection efficiency (CE). According to invetigations (Ref. arXiv:1506.04302v2 [physics.ins-det] 5 Oct 2015) about 20% of photoelectrons are able to give by 5 times smaller amplitude than a single photoelectron peak due to skip of the first dynode stage (see the pictures below: right). It means that if the read out electronics discriminator threshold is set ~0.1-0.2pe we will lose about 20% of photoelectrons.
In the G4 simulation is implemented recalculated photon detection efficiency (PDE):

## Slide 57: Expected e// – separation with FARICH up to 1.5 GeV/с
1100 MeV/c
700 MeV/c
To estimate /-separation capability in wide momentum range results of parametric simulation were used:
Refractive index profile approximation for aerogel sample 453f4 and its focusing distance L=160 mm
Simulation was performed for track angles 0о and 45о.
Number of photoelectrons for relativistic particles (beta=1) is equal to 39 (was taken from G4 simulation).
Single Photon Resolution (SPR) for relativistic particles SPR(=1.63 mm and SPR(ø1 mm)=1.36 mm
(was taken from beam test results).
Quality of particles separation is determined as:
1500 MeV/c
3 level

## Slide 58: Dependence of Npe and on aerogel thickness
Npe dependes on the aerogel thickness as expected and limitted by the Releigh light scattering law.
Some ssytematical increase of Npe (~13÷15%) are observed in new thick aerogels after increase of backing temperature (470˚C –> 600˚C). This effect could not be quantatively explained by increase of refractive indexes (1.027 –> 1.029) and it is contra to Npe decrease (~5÷6%) expected due to Releigh light scattering decrease
(as expected), while for several aerogel samples some deviations from the dependence are observed. The reason of this effect could be in some impurites inside the aerogel which are able to give additional small angle forward scattering.

## Slide 59: FEE based on FPGA-TDC
DC-DC convertor board
goes behind the backplane
51×84 mm2 size
provides power to SiPMs, amplifiers, FPGA
uses air inductive coils to operate in the detector magnetic field
power, trigger & clock connectors
Amplifier board
27×27 mm2 size
14-layer PCB
30x gain, 64 channels
couples to KETEK 8×8 SiPM array
TDC board
64 channels
2 TDC + 4 threshold FPGAs
10ps precision
Simulated single photon pulse shapes from amplifier for different input resistance. ~ 22mV amplitude can be achieved.
• Each module readouts 6 arrays 8x8 pixels and equipped with optical transceiver.
• Thickness of 5-layer design is less than 5 cm.

## Slide 60: The first tests of FaRICH-Auslese-System
ToT
Time, ns
The tests performed bu Mechael Traxler, Matthias Hoek and Merlin Böhm at HIM-Institute in Mainz.
Everything works as expected: ToT(Time) is as expected for single photon distribution.
Single photon detection time resolution without any corrections and proper TDC calibration is about 380ps (it is good enough value for FARICH), while intrinsic resolution of TDC is about 8÷12 ps.
A lot of dark counts are in the data (every 3rd hit is noise). Thermostabilization or cooling is needed for future tests.
FPGA-TDC (FaRICH-Auslese-System) to readout 2304 SiPMs developed and produced in GSI.
Time, ns