## Slide 1
Vadim Grinenko
Tsung-Dao Lee Institute, Shanghai Jiao Tong University, Shanghai
6 November 2023
Workshop on Muon Science Technology and Industry MELODY2023
μSR as a primary tool to search for superconductors with broken time-reversal symmetry

## Slide 2: μSR as the most sensitive bulk magnetic probe:
Discovery of BTRS superconductivity in iron-based superconductors with average spontaneous magnetic fields ~ 0.1 Oe.
Split superconducting and BTRS transition under uniaxial strain in Sr2RuO4.
Strain induced spin density wave (SDW) with magnetic moment ~ 0.1μB.
BTRS superconductivity under hydrostatic pressure.
V. Grinenko et al., Phys. Rev. B 95, 214511 (2017).
V. Grinenko et al., Nat. Phys. 16, 789 - 794 (2020).
V. Grinenko et al., Nat. Phys. 17, 1254–1259 (2021).
Y. Iguchi et al. Science 380,1244-1247(2023)
I. Shipulin et al., Nat Commun 14, 6734 (2023).
V. Grinenko et al., Nat. Phys. 17, 748–754 (2021).
V. Grinenko et al., Nat Commun 12, 3920 (2021).

## Slide 3: Superconductors that break time reversal symmetry (BTRS)
and
T(Z2) – time reversal symmetry: Δ Δ* ≠ | Δα|eiθ
Two energetically equivalent states with Δ ≠ Δ*
meaning spontaneously broken Z2 symmetry.
?
?
V (Δ)
Δ*
Δ
0
T
BTRS state can be described by two component imaginary order parameter: .
Two different phase transitions → Tc ≠ TBTRS.
https://slideplayer.com/slide/5363094/
At Tc broken U(1)
The fundamental symmetry which spontaneously violates by any superconducting state.
Superconducting state below Tc can be characterized by a complex order parameter Δ = |Δ|eiφα, which has amplitude and phase.
The order parameter characterizes how strong the symmetry is broken below transition temperature.

## Slide 4: Phenomenologically, broken time reversal symmetry
Phenomenologically, broken time-reversal symmetry results in the appearance of a spontaneous magnetization (m) when a superconductor is cooled below TBTRS.
V. Grinenko et al., Nat. Phys. 16, 789–794 (2020)
V. L. Vadimov and M.A. Silaev, PRB 98, 104504 (2018)
C. Hicks, MPI Dresden
m
Spontaneous fields appear around inhomogeneities or at the domain walls (no spontaneous fields in infinite homogeneous superconductor).
The structure and value of the fields depend on the type of the order parameter, the anisotropy of the system and the structure of inhomogeneities.

## Slide 5: Discovery of BTRS superconductivity in Ba1-xKxFe2As2
Experiment:
mSR/NQR
Rajib Sarkar, Hans-Henning Klauss,
TU Dresden, Germany
Hubertus Luetkens,
PSI Villigen, Switzerland
Ba1-xKxFe2As2 single crystals
Kunihiro Kihou and Chul-Ho Lee
AIST, Tsukuba, Japan
AC specific heat and ultrasound
Tino Gottschall, Denis Gorbunov,
Sergei Zherlitsyn, Jochen Wosnitza HZDR, Dresden-Rossendorf, Germany
Calorimetry and magnetization
Ilya Shipulin, IFW Dresden, Germany
Thermoelectrical transport
Nadia Stegani, Federico Caglieris,
CNR-SPIN Genova
Christoph Wuttke, Christian Heß,
Bernd Büchner
IFW Dresden, Germany
Theory:
Daniel Weston, Ilaria Maccari
KTH, Stockholm, Sweden
Julien Garaud,
Institut Denis Poisson CNRS-UMR, France
Egor Babaev
KTH, Stockholm, Sweden
Scanning SQUID Microscopy
Yusuke Iguchi
Kathryn A. Moler

## Slide 6: Effect of Lifshitz transition on Ba1-xKxFe2As2 superconductivity
N. Xu et al., PRB 88, 220508(R) (2013)
x ~ 0.7 - 0.9
Hole doping results in topological changes of the Fermi surface (Lifshitz transition) at xL = 0.55 – 0.9.
The superconducting dome is continuous across the Lifshitz transition.
What is the effect of Lifshitz transition on the superconducting state?
electron
hole
hole
D. Evtushinsky at al.,
ARPES (unpublished)
Lifshitz
transition
W. Malaeb et al., PRB 86, 165117 (2012)
Lifshitz transition of
the electron pocket at X-point BZ

## Slide 7: Possible s+is superconductivity at Lifshitz transition
V. Grinenko et al., Nat. Phys. 16, 789–794 (2020).
see also J. Garaud, J. Carlström, and E. Babaev, Phys. Rev. Lett. 107, 197001 (2011), S. Maiti and A. V. Chubukov, Phys. Rev. B 87, 144511 (2013); A. Chubukov, Springer Series in Materials Science, 211, 255 (2015)
Competition between different s± pairing states → intermediate s-state with frustrated phases of the order parameter → Broken Time Reversal Symmetry (BTRS).
Cai et al., Science Bulletin 66 (2021)
D. Wu et al., arXiv:2212.03472v1
Nodal
Isotropic in optimally doped
Lifshitz
transition
N. Xu et al., PRB 88, 220508(R) (2013)

## Slide 8: BTRS superconductivity in Ba1-xKxFe2As2
Moun spin depolarization rate is enhanced for x ~ 0.8
Change of the scaling behavior → two superconducting (SC) phases!
A narrow BTRS dome (0.7 > x > 0.85) close to the Lifshitz transition between two different superconducting states.
V. Grinenko et al., Phys. Rev. B 95, 214511 (2017).
V. Grinenko et al., Nat. Phys. 16, 789 - 794 (2020).
SC1
SC2
SC1
SC2
SC1
SC2
Lifshitz
transition
Average spontaneous field <Bint> = ΔΛ/λμ ~ 0.1 G.
N. Xu et al., PRB 88, 220508(R) (2013)

## Slide 9: Anisotropy of the spontaneous magnetic fields in BTRS state
What is the BTRS order parameter ?
Spontaneous fields are anisotropic → consistent with an s+is state!
V. Grinenko et al., Nat. Phys. 16, 789–794 (2020)
V. L. Vadimov and M.A. Silaev, PRB 98, 104504 (2018)

## Slide 10: What is further evidence for BTRS?
Is it a muon-induced effect?
Is it the interaction of local moments with superconductivity?
For long time a BTRS superconductivity was an extremely rare phenomenon. However, in a recent years “hundreds” of new BTRS superconductors were discovered.
If it is intrinsic:
Why this unusual phenomena is so common?
Do we need “new” theory of superconductivity to understand it?
Extrinsic reasons:
Is BTRS intrinsic or extrinsic to Ba1-xKxFe2As2?

## Slide 11: Discovery of fractional vortices (FV) in the BTRS state
Scanning SQUID Microscopy
FV are mobile un related to defects!
V. Grinenko et al., Nat. Phys. 16, 789–794 (2020)
Y. Iguchi et al. Science 380,1244-1247(2023)
~ 10% of vortices are fractional vortices (FV)
Support for multicomponent superconductivity!
Abrikosov vortices
Fractional vortices
Abrikosov and Fractional vortices pinned at the same location.
FV – quantum objects unrelated to specific defects in the sample.

## Slide 12: Is there a phase transition above Tc?
The splitting between transitions seen by the specific heat and susceptibility is observed for the samples with the “strongest” BTRS phase found in the µSR experiments.
V. Grinenko et al., Nat. Phys. 16, 789–794 (2020).
V. Grinenko et al., Nat. Phys. 17, 1254–1259 (2021)
Specific heat ΔCel/T (mJ/mol•K2)
Critical fields (T)
Temperature (K)
The splitting increases in applied magnetic field.
What is the nature of the transition above Tc?
Is there specific heat anomaly at TBTRS ?

## Slide 13: Criteria for Tc and Z2 transition (TcZ2)
V. Grinenko et al., Nat. Phys. 16, 789–794 (2020).
The specific heat anomaly develops at T* > Tc, preformed Cooper pairs?
V. Grinenko et al., Nat. Phys. 17, 1254–1259 (2021)
Tc is defined by zero resistance.
In the resistive state diamagnetic susceptibility is small.
Tc T*
Evidence for the Z2 transition above Tc from μSR and spontaneous Nernst effect!

## Slide 14: Calorimetric evidence for phase transition above Tc in zero magnetic field
The shoulder-like anomaly above Tc in a narrow doping range around x ~ 0.75.
I. Shipulin et al., I. Shipulin et al., Nat Commun 14, 6734 (2023).
Is there evidence for the BTRS phase?

## Slide 15: Calorimetric evidence for phase transition above Tc in zero magnetic field
In our model phase fluctuations suppress stronger superconductivity (U(1) transition) compared to Z2 transition.
Is there evidence for superconducting fluctuations?
I. Shipulin et al., Nat Commun 14, 6734 (2023).
Monte-Carlo (MC) simulations of two component model with phase fluctuations.
Theoretical simulations are qualitatively consistent with the experimental observations of two transitions.
The spontaneous Nernst signal confirms Z2;
Zero resistivity the superconducting transition.

## Slide 16: Spontaneous Nernst and fluctuations above Tc
In BKFA without BTRS state spontaneous Nernst signal is absent and superconducting fluctuations are weak.
Strong superconducting fluctuations in the samples with BTRS state!
V. Grinenko et al., Nat. Phys. 17, 1254–1259 (2021).

## Slide 17: Conclusions: the phase diagram of the sample with a possible quartic metal phase
TBTRS > Tc
TBTRS≤ Tc
V. Grinenko et al., Phys. Rev. B 95, 214511 (2017).
V. Grinenko et al., Nat. Phys. 16, 789 - 794 (2020).
V. Grinenko et al., Nat. Phys. 17, 1254–1259 (2021).
Y. Iguchi et al. Science 380,1244-1247(2023)
I. Shipulin et al., Nat Commun 14, 6734 (2023).
A new state appear from incoherent Cooper pairs at TcZ2 > Tc which is a bound state of four fermions – correlated state of pairs of Cooper pairs.
At TcZ2 we observe increased muon spin relaxation rate and spontaneous Nernst effect as well thermodynamic signatures.
A lack of the Meissner effect and finite resistance at TcZ2 indicate absence of coherent Cooper pairs.
Preformed Cooper pair exist above TcZ2 up to T ~ 2Tc as evidenced by the observation of the field-dependent Nernst effect and by deviation of the resistivity from the high-temperature behavior.
Conclusions:
Fluctuations suppress faster a continuous U(1) than discreet Z2 symmetry.

## Slide 18: μSR as the most sensitive bulk magnetic probe:
Discovery of BTRS superconductivity in iron-based superconductors with average spontaneous magnetic fields ~ 0.1 Oe.
Split superconducting and BTRS transition under uniaxial strain in Sr2RuO4.
Strain induced spin density wave (SDW) with magnetic moment ~ 0.1μB.
BTRS superconductivity under hydrostatic pressure.
The main collaborators at PSI:
Hubertus Luetkens
Rustem Khasanov
The main participants in the projects:
Hans-Henning Klauss,
TU Dresden
Shreenanda Ghosh
The Johns Hopkins University
Clifford W. Hicks
University of Birmingham
V. Grinenko et al., Phys. Rev. B 95, 214511 (2017).
V. Grinenko et al., Nat. Phys. 16, 789 - 794 (2020).
V. Grinenko et al., Nat. Phys. 17, 748–754 (2021).
V. Grinenko et al., Nat Commun 12, 3920 (2021).
Manfred Sigrist
ETH Zurich

## Slide 19: Motivation
Is Sr2RuO4 a chiral (Δx ± iΔy) superconductor?

## Slide 20: Sr2RuO4 is multiband superconductor
Sr2RuO4 has a complex electronic structure, makes it similar to Fe-based superconductors.
Fermi surface
Crystal structure
C. Hicks, MPI Dresden
Electronic orbitals relevant for conductivity
S. Raghu et al., Journal of Physics: Conference Series 449, 012031 (2013).

## Slide 21: Sr2RuO4 is multiband superconductor
Variety of possible superconducting order parameters in Sr2RuO4
Multi-band nature of the Fermi surface results in a possibility of mixed pairing states with the pairing mediated by spin fluctuations, candidates: s+id, d+ig, s+ip
A. T. Rømer, et al., PRL 123, 247001 (2019); PRB 102, 054506 (2020); PRB 104, 064507 (2021);
S. A. Kivelson, et al., npj Quantum Mat. 5, 43 (2020).
dxz+idyz
Alternatively, the orbital degree of freedom can encode chiral order parameters with a pairing originated from local interactions, candidates: d+id.
A. Ramires, and M. Sigrist, Physical Review B (2019). H. G. Suh et al.,Phys. Rev. Research 2, 032023(R) 2020.
A. Ramires, arXiv:2110.10621.
A chiral p-wave is excluded according to the NMR Knight shift measurements:
A. Pustogow et al., Nature 574, 72 (2019).
K. Ishida, et al., J. Phys. Soc. Jpn. 89, 034712 (2020).
A. Chronister et al., PNAS 118 (25) e2025313118 (2021).
The reduction of the NMR Knight shift below Tc
Mixed pairing or chiral
?

## Slide 22: How can we distinguish between chiral and non-chiral superconductivity using µSR?
Accidentally degenerated sates:
Tc and TBTRS transitions must split under uniaxial strain.
Tc and TBTRS transitions must split under symmetry breaking uniaxial strain.
(dxz ± idyz)
(100) direction
x
y
Tetragonal
Orthorhombic
(110) direction
Uniaxial pressure
Splitting of Tc and TBTRS is expected for both: chiral and accidentally degenerated orders.
Important demonstration that Tc and TBTRS are related to a different phase transitions.
V. Grinenko et al., Nat Commun 12, 3920 (2021).
Do not split with the hydrostatic pressure and isotropic disorder.
Do split with the hydrostatic pressure and disorder.

## Slide 23: Sr2RuO4 under the (100) strain
Tetragonal
Orthorhombic
V. Grinenko et al., Nat. Phys. 17, 748–754 (2021).
along (100)
Experimental setup for the μSR:
S. Ghosh et al., Review of Scientific Instruments 91, 103902 (2020).
Tc is measured by AC susceptibility.
TBTRS by zero-field µSR.
A. Steppke, et al., Science 355, eaaf9398 (2017).
What is the effect of van Hove on BTRS state?
Can van Hove induce magnetism?

## Slide 24: BTRS superconductivity of Sr2RuO4 under the (100) strain
A. Steppke, et al., Science 355, eaaf9398 (2017).
Relaxation rate, λ (µs-1)
Temperature (K)
AC susceptibility
Tc
TBTRS
V. Grinenko et al., Nat. Phys. 17, 748–754 (2021)
Relaxation rate, λ (µs-1)
Temperature (K)
AC susceptibility
TBTRS
Significant splitting of TBTRS and Tc!
BTRS state exists above van Hove singularity!
Tetragonal
Orthorhombic

## Slide 25: Strain induced SDW phase in Sr2RuO4
A. Steppke, et al., Science 355, eaaf9398 (2017).
Tetragonal
Orthorhombic
An incommensurate SDW phase well above the van Hove singularity with TN ~ 7 K;
van Hove
V. Grinenko et al., Nat. Phys. 17, 748–754 (2021)
Small internal magnetic fields correspond roughly to 0.1 µB (similar to Sr3Ru2O7);
The SDW internal field is 100 times stronger than spontaneous fields due to BTRS superconductivity.

## Slide 26: μSR measurements of Sr2RuO4 under uniaxial strain
Superconducting Tc and TBTRS split by uniaxial strain → two distinct phases!
V. Grinenko et al., Nat. Phys. 17, 748–754 (2021).
SDW state
Elastocaloric effect
YS. Li et al., Nature 607, 276–280 (2022).
SDW phase detected by μSR is confirmed by elastocaloric effect measurements.
M. S. Anwar et al., arXiv:2211.14626v1
Spontaneous superconducting diode effect
Split Tc and TBTRS is confirmed by spontaneous superconducting diode effect measurements.
x
y
Tetragonal
Orthorhombic
Uniaxial strain induces spin density wave order (SDW) above the Lifshitz transition in odd with early theoretical predictions.
Lifshitz transition
What is the evidence from other probes in favor of the μSR phase diagram?
TBTRS
Tc

## Slide 27: How can we distinguish between chiral and non-chiral superconductivity using µSR?
Accidentally degenerated sates:
Tc and TBTRS transitions must split under uniaxial strain.
Do split with the hydrostatic pressure and disorder.
Tc and TBTRS transitions must split under symmetry breaking uniaxial strain.
Do not split with the hydrostatic pressure and isotropic disorder.
(dxz ± idyz)
V. Grinenko et al., Nat Commun 12, 3920 (2021).
Disorder effect on Tc
N. Kikugawa et al., Phys. Rev. B 70, 060508(R) (2004)
At small concentrations the dominant effect of La on Tc is related to a pair breaking effect.
La-doping results in isotropic in-plane disorder without anisotropic internal strain.
La-doping is an ideal tool to study the effect of disorder on Tc and TBTRS

## Slide 28: Time reversal symmetry breaking in Sr2-yLayRuO4
The normal state electronic specific heat is nearly the same for all samples, γn ≈ 40 mJ/mol-K2 -> the DOS and correlation effects are unchanged.
Sharp superconducting transition -> homogeneous suppression of superconductivity by a pair braking effect.
1% of La doping suppresses Tc by 50% as compared with a impurity free Tc0
TBTRS = Tc in the sample with a half of the disorder free Tc0;
Together with the splitting between TBTRS and Tc under uniaxial strain
→ evidence in favor of a chiral superconductivity in Sr2RuO4
TBTRS ≈ Tc
V. Grinenko et al., Nat Commun 12, 3920 (2021).

## Slide 29: Theory: Splitting of the Tc and TTRSB under disorder for accidentally degenerated orders
Accidentally degenerated sates:
Tc and TBTRS transitions must split under uniaxial strain.
Do split with the hydrostatic pressure and disorder.
V. Grinenko et al., Nat Commun 12, 3920 (2021).
Fine-tuning is possible that transitions do not split with disorder.
d+ig state
Therefore, additional experiments are needed!
B. Zinkl. & M. Sigrist, arXiv:2009.10089 (2020).
Manfred Sigrist

## Slide 30: How can we distinguish between chiral and non-chiral superconductivity using µSR?
Accidentally degenerated sates:
Tc and TBTRS transitions must split under uniaxial strain.
Do split with the hydrostatic pressure and disorder.
Tc and TBTRS transitions must split under symmetry breaking uniaxial strain.
Do not split with the hydrostatic pressure and isotropic disorder.
(dxz ± idyz)
V. Grinenko et al., Nat Commun 12, 3920 (2021).
Hydrostatic pressure preserves tetragonal symmetry a = b
x
y
Tetragonal
D. Forsythe et al., Phys. Rev. Lett. 89, 166402 (2002)
N. Shirakawa et al., Phys. Rev. B 56, 7890 (1997)
“Fine tuning” is impossible for both disorder and hydrostatic pressure!

## Slide 31: The first μSR measurements of BTRS superconductivity under pressure
TBTRS ≈ Tc due disorder and under hydrostatic pressure
BTRS transition temperature, TBTRS (K)
TBTRS = Tc
Superconducting transition temperature, Tc (K)
V. Grinenko et al., Nat Commun 12, 3920 (2021)
Evidence for two component chiral
superconductivity in Sr2RuO4.
Rustem
Khasanov
Tc
TBTRS
Temperature (K)
Suppression of superconductivity and time-reversal symmetry breaking under pressure.
Tetragonal
Sample +cell
Sample

## Slide 32: Is there any other method to detect the phase transition below Tc?
The BTRS phase transition result in divergence of the coherence length.
This divergence should affect intervortex integration.
J Garaud et al., Phys. Rev. B 98, 014520 (2018)
We studied the vortex structure under uniaxial strain using muon spin rotation experiments.

## Slide 33: Summary: TBTRS under pressure and disorder in Sr2RuO4
BTRS transition temperature, TBTRS (K)
TBTRS = Tc
Superconducting transition temperature, Tc (K)
Taking in to account symmetry consideration the natural possibility is a chiral dxz± idyz superconducting state!
The related µSR publications:
V. Grinenko et al., Nat Commun 12, 3920 (2021).
V. Grinenko, S. Ghosh et al., Nat. Phys. 17, 748–754 (2021).
Problems for chiral dxz± idyz state:
Missing anomaly in the specific heat under uniaxial strain;
Missing cusp in Tc under the strain.
Problems for mixed pairing states:
Unusual fine tuning of Tc and TBTRS under hydrostatic pressure and with disorder;
Reproducible observation of the Kerr effect.

## Slide 34
Polar Kerr effect
J. Xia, A. Kapitulnik et al., PRL (2006)
Some experimental evidences for multicomponent order parameter in Sr2RuO4
Enhanced muon spin relaxation rate below Tc → spontaneous magnetic fields
Luke, G. M. et al. Nature 394, 558–561 (1998)
Decrease of the transverse sound viscosity at Tc, -> elastic constant C66 -> indication for 2D order parameter.
C. Lupien, PhD thesis (2002)
S .Ghosh et al., Nat. Physics (2020) , S. Benhabib et al., Nat. Physics (2020)
Altogether these experiments are consistent
with chiral state.

## Slide 35
Evidences against chiral superconductivity in Sr2RuO4
Are Tc and TTRSB transitions split under uniaxial strain?
Problems with interpretation Josephson effect: S. Kashiwaya et al., PRB 100, 094530, S.-I. Suzuki et al., PRB 101, 054505 (2020), ….
J. R. Kirtley, et al., Phys. Rev. B 76, 014526 (2007)
C. W. Hicks et al., Phys. Rev. B 81, 214501 (2010)
Absence of edge currents?
Scanning SQUID microscopy
It can be explained by the suppression of superconductivity by surface reconstruction.
C. A. Marques et al., arXiv:2005.00071
A. Kreisel et al., arXiv:2103.06188
R. Fittipaldi et al., Nat Commun. 12, 5792 (2021).
C. W. Hicks et al., Science 344, 283-285 (2014).
A. Steppke, et al., Science 355, eaaf9398 (2017).
Missing cusp in Tc under strain
Theory
Experiment
Missing anomaly at TTRSB in the specific heat under uniaxial strain
Y.-S. Li et al., PNAS 118 (10) e2020492118 (2021)

## Slide 36: Two critical temperatures in Ba0.23K0.77Fe2As2 with BTRS state
TcZ2 - formation of bound state and appearance of spontaneous Nernst signal;
Tc - Meissner effect and zero resistance;
TSFlow - freezing all vortices.
V. Grinenko et al., Nat. Phys. 17, 1254–1259 (2021).
The anomaly in the specific heat at TcZ2 is observed in applied magnetic field.
The anomaly is not resolved in zero field.