## Slide 1: Thin film SRF cavity R&D at IHEP
Jin Dai
IHEP, CAS
11th IHEP-KEK SCRF Collaboration Meeting
Beijing, 20 Nov 2023

## Slide 2
Outline
Copper Niobium Sputtering Cavities
Introduction
Substrate cavities
Copper surface preparation
- SUBU chemical polishing
- Centrifugal barrel polishing
- Electrochemical polishing
Inner surface inspections
DCMS coating
HiPIMS coating
Nb3Sn Superconducting Cavities
Setup of the furnace
Nb3Sn coating

## Slide 3
Copper Niobium Sputtering Cavities

## Slide 4
Introduction
Nb/Cu study at IHEP launched in 2017
A small working group (~7 persons, ~2-3 FTEs): physicists, engineers and postgraduates
Main interests: Nb/Cu, Nb3Sn/Cu, NbN/Cu

## Slide 5
Substrate cavities
Copper cavities
- 1.3GHz mono-cell shape with beam pipe extensions
- ASTM C10100 copper, deep drawing + electron-beam welding
- 4 copper cavities produced
Sample holder cavities
- copper samples can easily fixed on beam pipe, cell, iris, equator
- 2 stainless-steel cavities produced

## Slide 6
Centrifugal barrel polishing (CBP)
Centrifugal barrel polishing system previously developed for 1.3GHz 9-cell bulk-Nb cavity was used for copper cavities
The copper cavity is fixed on a cage that rotates around the equipment axis, and then it can rotate on its own. These two rotational degrees of freedom allow the abrasive inside to polish different positions in the cavity

## Slide 7
CBP: original recipe
Before polishing
Ceramic triangles
(50 hours)
RG-22 resin cones
(25 hours)
3µm diamond suspensions & 5mm hardwood blocks
(38 hours)
0.04µm non-stick colloidal silica
(90 hours)
90RPM

## Slide 8
CBP: new recipe
Before
polishing
Corundum angle cut triangles
(6mm*6mm, 240-grit)
(50 hours)
1000-grit resin cones
(10mm*10mm)
(25 hours)
2000-grit resin bullets
(25 hours)
Corncobs & metal polishing paste
(5 hours)
90RPM

## Slide 9
CBP: comparison
Average roughness of the copper cavity surface after each polishing step by using two different recipes
With the new recipe, after 5 hours of final polishing, a mirror-like surface was finally created, and the roughness further improved to be 60 nm
F. Yang et al., Radiation Detection Technology and Methods 5, 33-41 (2021). DOI: https://doi.org/10.1007/s41605-020-00215-8

## Slide 10
SUBU system
Enclosed design
- Single sided polishing, saving half of the acid solution and related post-processing costs
- Prevent acid gas from entering the environment at high-temperature
- The copper cavity is not exposed to the atmosphere, which can prevent internal surface oxidation
SUBU preparation barrel
Passivation barrel
Heating box
Pure water tank
Buffer box
Copper cavity
Waste acid tank
F. Yang, et al., Journal of Instrumentation 16, P06031 (2021).

## Slide 11
SUBU processes
F. Yang, et al., Journal of Instrumentation 16, P06031 (2021).
Activation
SUBU
Cooling
Dilution, rinsing
Passivation
SUBU solution: followed CERN recipe, sulfamic acid, hydrogen peroxide solution, ammonium citrate, n-butanol and deionized water

## Slide 12
SUBU results
Temperature kept at 72 degC during SUBU
Post-SUBU cooling step added to prevent oxidation, 72 degC -> 25 degC in 10’
Copper surface after SUBU was smooth and bright, average Ra = 0.12 µm

## Slide 13
Electrochemical polishing
EP system developed and under commissioning
EP solution: Phosphoric acid (85%), Buthanol (99%), ratio 3:2

## Slide 14
Cavity inner surface inspection
Optical inspection system developed for cavity surface examination (after chemical or sputtering)
- Cavity movement: cavity rotation, cavity translation
- Camera movement: up and down translation, left and right swing
- 8 LED lamps inside the cavity with independent brightness control
Cavity beam tube and cell clearly photographed without dead zone
Iris
Cell

## Slide 15
Magnetron sputtering system (DCMS)
DCMS sputtering system developed for 1.3GHz mono-cell cavity Nb coating
- Vacuum inside the coating chamber: 3E-9 mbar
- Diameter of niobium target: 45 mm
- 2 permanent magnetic rings (width: 20mm, 1.35 Telsa) placed concentrically inside Nb target
- South poles of the two magnetic rings were close to each other, a titanium ring of 15 mm length placed in the middle for isolation and positioning

## Slide 16
Sample coating results
High temperature create cluster morphology with lower Tc
Chose 200 degC as the coating temperature

## Slide 17
Nb coating
Substrate baked at 400 degC for 48 hours, then cooled to 200 degC to start coating
Vacuum inside the coating chamber: 3 E-9 mbar
Krypton pressure: 0.5 Pa
Duty ratio 0.6, discharge current 3 A
Magnet movement speed: 1 mm / s
Target Nb thickness: 2 μm

## Slide 18
Results
Sample coating prior to cavity coating to examine film qualities
SEM results show that the grain growth at the beam tube, iris and equator was compact. However, there were holes in the film at the cell site, and the grains could not grow together completely.
This may be due to the irregular shape of the cell part of the ellipsoidal cavity, the niobium atoms cannot be vertically incident on the cell surface, resulting in the deposition quality of the niobium atoms on the cell is inferior to other positions.

## Slide 19
Rinsing
Ultra-pure water rinsing (18 MΩ) and clean assembly in Class-100 clean room
Cavity rotates at a constant speed of 4 RPM
The spray bar reciprocates on the axis of the cavity. The speed of passing through the beam tube is 70 mm/min, and the speed of passing through the cell part is 30 mm/min
The set pressure was 8 bar for four times of cleaning
Pressure tests also be conducted on the niobium film and found that it did not detach under high pressure water flushing at 50 bar

## Slide 20
VT results
Eacc reached 5 MV/m with Q0 > 1108
Defects on equator found in later inspections after VT

## Slide 21
Cylindrical HiPIMS cavity system
Huttinger Electronics TruPlasma Highpulse DC Unit:
10 kW max average power delivered
voltage up to 1 kV
pulse width up to 1000 us
frequency up to 10 KHz
chamber for 1.3 GHz SRF cavities
Niobium cathode RRR~300
base pressure in the low 10E-9 mbar range
residual gas analyzer
movable magnetrons 1mm/s
Coating temperatures 200℃
Water cooled
Substrate preparation is SUBU
Assembly in clean room
Coating with Kr
Nb/Cu dummy cavities have been produced both by DCMS and HiPIMS

## Slide 22
HiPIMS without bias voltage
94A
tube
iris
cell
equator
cell: FIB-SEM
cell:cross-section
Tc 9.1K
Tc 9.08K
Tc 7.4K
Tc 9.4K
Tc 9.12K
Tc 9.23K
Tc 9.34K
Tc 9.14K
The use of short pulses and increasing the peak current had been found to have limited improvement in the quality of the Nb film.
94A, 531V, 30us, 740Hz, 65KW, 0.72Pa
128A, 456V, 30us, 1000Hz, 135KW, 0.61Pa
272A, 388V, 25us, 653Hz, 300KW, 0.61Pa
128A
272A

## Slide 23
HiPIMS studies with biased substrate
Tc 9.20K
Tc 9.23K
Tc 9.19K
tube
iris
cell
equator
cell: cross-section
copper substrate
cell: cross-section
silicon substrate
0V
50V
100V
HiPIMS with 100V bias voltage can effectively improve the quality of Nb film.
0V, 70A, 674V, 41us, 1200Hz, 59KW, 0.69Pa
50V, 145, 618V, 100us, 308Hz, 101KW, 0.69Pa
100V, 134A, 599V, 100us, 300Hz, 100KW, 0.69Pa

## Slide 24
Nb3Sn Superconducting Cavities

## Slide 25
Setup of the furnace
Manufacturer: Shanghai Sanjing Vacuum Equipment Co., Ltd.
Main Configurations:
two separate vacuum systems and two separate heaters;
heaters, thermocouples and 7-layer thermal shields are installed in the outer chamber;
the outer chamber is evacuated by an dry pump, and the vacuum can reach 1 × 10-3 Pa;
the inner chamber made of Nb (RRR~50) is evacuated by an oil-free molecular pump and a dry pump, and the vacuum can reach 5 × 10-6 Pa at room temperature and 1 × 10-4 Pa at 1200 ºC;
the highest temperature of cavity is 1300 ºC, while the crucible can reach 1400 ºC.
Schematic of the new dual-vacuum furnace developed for the Nb3Sn coating of 1.3 GHz 1-cell cavity.

## Slide 26
Nb3Sn coating
Sn
SnCl2

## Slide 27
Coating process
Degassing: 200ºC, >10h;
nucleation: 500ºC, 5h;
(3) ramp-up: 12ºC/h;
(4) coating:
  furnace1200ºC, 3h;
  Crucible 1300ºC, 3h;
(5) annealing: 1200ºC, 2h;
(6) cool down

## Slide 28
Cooling rate experiment
Various cooling rates were tried during the vertical tests of Nb3Sn, which demonstrated very different results.
Cernox sensors
(Up and down)
Fast cooling
Slow cooling
< 0.1 K

## Slide 29
Vertical test results of S25
~3E9 at low fields
7.6E8 @ 6.4 MV/m, which was limited by RF power.
Low-temperature baking of 120C 48h was also conducted, which had little effects.
Images of the same equator region of S25 cavity before (a) and after (b)
Nb3Sn coating. Several small defects existed on some welding zones are circled
in red (c) and (d).

## Slide 30
S22、S27
The results of S22 and S27 were almost the same as S25.
S22
S27

## Slide 31
Characterization
XRD
Samples #2-#5 were in size for XRD, R-T and SEM measurements.
R-T
SEM
Setup

## Slide 32: Summary
The CBP polishing recipe has been established, the SUBU chemical polishing system has been put into use, and the electrochemical polishing system is under commissioning
DCMS has completed the cavity coating and vertical test, and HiPIMS has entered the sample coating stage
The Nb3Sn coating equipment is operating normally and has completed vertical test of three thin film cavities

## Slide 33
Thanks