## Slide 1
Vertex detector toward TDR
Zhijun Liang (IHEP)
梁志均 （中国科学院高能物理研究所）

## Slide 2: Vertex detector Towards TDR study
Major change from CDR to TDR
  Beam pipe diameter: 28mm (CDR)  20mm (TDR) (reduce 30%)
  Instant Luminosity per IP:
    Z pole: 32×1034 cm-2s-1 (CDR)  192 ×1034 cm-2s-1 (TDR, 50MW) (6 times increase)
    ZH: 5.6×1034 cm-2s-1 (CDR)  8.3 ×1034 cm-2s-1 (TDR) (~1.5 times increase)
Action item
  Need to consider Higgs/Z pole/ WW/ (ttbar ) run
    Accelerator can switch operation mode in a short time scale
  Connection to Physics Optimize the geometry, physics case
      First vertex layer: Radius=12mm (TDR candidate) or Radius =16mm (CDR design) ?
  Connection to MDI 
    Estimate the hit rate from background, Fluence and total ionization dose estimation
    Mechanical and cooling solution
  Connection to DAQ and electronics  Data Rate in Higgs/Z pole/ WW/ ttbar
  Work together to select Technology based on all aspects

## Slide 3: Backup

## Slide 4: Hit rate and radiation from background (input for vertex)
Waiting for the update on background estimation (Haoyu)
First guess of background based on input (Haoyu)
  Instant Luminosity increase  radiation hardness requirement increased, tiny impact on hit density
  Beam pipe diameter: 28mm  20mm : Expect 3-5 times larger hit density and radiation
Hit density per crossing (CDR)
Total ionization dose (CDR)
Fluence (CDR)

## Slide 5: Radiation hardness (Total ionization dose)
First guess on Radiation requirement (need final input from Haoyu):
Taichupix2 was irradiated in-situ tested up to 30 Mrad
Based on LHC experience, chip have potential to survive serval hundred Mrad
Taichupix3 irradiation test
Pixel threshold vs. TID
Taichupix2 irradiation test
Initial input on TID | First layer radius=16mm (CDR vertex design) | First layer radius=12mm (TDR design candidate)
ZH (240GeV) 8 year | ~1 Mrad/year | 3-5 Mrad/year
Z pole (91GeV) 2 year | ~60 Mrad/year | 200-300 Mrad/year

## Slide 6: Hit rate and radiation from background (input for vertex)
Waiting for the update on background estimation (Haoyu)
First guess of background based on input (Haoyu)
  Instant Luminosity increase  radiation hardness requirement increased, tiny impact on hit density
  Beam pipe diameter: 28mm  20mm : Expect 3-5 times larger hit density and radiation
Hit rate and radiation from Background (CDR study, from Haoyu)

## Slide 7: Radiation hardness (Total ionization dose)
First guess on Radiation requirement (need final input from Haoyu):
Taichupix2 was irradiated in-situ tested up to 30 Mrad
Based on LHC experience, chip have potential to survive serval hundred Mrad
Taichupix3 irradiation test
Pixel threshold vs. TID
Taichupix2 irradiation test
Initial input on TID | First layer radius=16mm (CDR vertex design) | First layer radius=12mm (TDR design candidate)
ZH (240GeV) 8 year | ~1 Mrad/year | 3-5 Mrad/year
Z pole (91GeV) 2 year | ~60 Mrad/year | 200-300 Mrad/year

## Slide 8: Radiation hardness (neutron Fluence)
First guess on Radiation requirement (need final input from Haoyu):
CDR requirement: ~2*𝟏𝟎𝟏3𝒏𝒆𝒒⋅ 𝒄𝒎-𝟐 ⋅ 𝒚𝒓
TDR requirement: 1-6 *𝟏𝟎𝟏4𝒏𝒆𝒒⋅ 𝒄𝒎-𝟐 ⋅ 𝒚𝒓 (depending on radius)
  Whether CEPC MAPS sensor can survive 𝟏𝟎𝟏4𝒏𝒆𝒒⋅ 𝒄𝒎-𝟐 ?
neutron fluence 𝒏𝒆𝒒 𝟏𝟎𝟏𝟐 ⋅ 𝒄𝒎-𝟐 ⋅ 𝒚𝒓 | First layer radius=16mm (CDR vertex design) | First layer radius=12mm (TDR design candidate)
ZH (240GeV) | 3 | 9-15
Z pole (91GeV) | 120 | 360-600
  Radiation of Taichu @ CSNS ( up to 1.5*𝟏𝟎𝟏4𝒏𝒆𝒒 )
  DUT is irradiated TaichuPix with modified process
  Preliminary result (by Yiming)
    Efficiency >99% @ 𝟏𝟎𝟏3𝒏𝒆𝒒
    Efficiency >95% @ 1.5* 𝟏𝟎𝟏4𝒏𝒆𝒒

## Slide 9: Hit density
First guess on Radiation requirement (need final input from Haoyu):
CDR : ~2 hits cm-2 BX -1
TDR requirement: 2~10 hits cm-2 BX -1(depending on radius)

## Slide 10: Summary： Action item
Based on initial input of background, compare advantage and disadvantage of different layout
  First layer radius 12mm Vs 16mm
  Still waiting for final input of background from MDI group (Haoyu)
Revisit vertex time resolution and occupancy, spatial resolution requirement
  Roadmap for R & D (Taichu –like/ Jadepix –like architecture)
  Finalize the readout architecture design ( need to consider trigger design)
Integration vertex design with beam pipe in MDI region
  For Cooling design and support structure, Cabling, and frontend boards location