## Slide 1
CEPC Detector Magnet
Feipeng Ning
On behalf of Detector magnet team
Oct. 23-27, 2024, CEPC workshop, Hangzhou

## Slide 2: Content
Introduction of detector magnet
Physical design of the magnet
Mechanical design of the magnet
Cryogenics system design
R&D progress
  Aluminum stabilized superconducting cable development
  Dummy coil development
  High strength and high RRR Al stabilizer
Team and cooperation
Summary

## Slide 3: Introduction of detector magnet
Position and size
Magnetic field
Inner diameter | 7070 mm
Thickness | 700 mm
Outer diameter | 8470 mm
Length | 9050 mm
Energy | t | Higgs | W | Z
Magnetic field | 3T | 3T | 3T | 2T
Energy |  | Higgs | W | Z
Magnetic field | 3T | 3T | 3T | 2T
Magnet
Magnet

## Slide 4
Physical design of the magnet
Design of the magnet
4
Central magnetic field | 3 T
Inner diameter | 7070 mm
Outer diameter | 8470 mm
Thickness | 700 mm
Length | 9050 mm
Cold mass | 185 tons
Yoke weight | 2960 tons
Magnet weight | 290 tons
Magnet parameters:
Yoke + Muon
Solenoid magnet
HCal

## Slide 5
Physical design of the magnet
Physical design of the magnet
5
Central magnetic field | 3 T
Inner diameter | 7300 mm
Operating current | 17000 A
Cable length | 33 km
Inductance | 11 H
Stored Energy | 1.54 GJ
Coil parameters:
Magnetic field distribution on the axis
2D Magnetic field simulation
3D Magnetic field simulation
3D Magnetic field simulation

## Slide 6: Physical design of the magnet
Stress analysis：
Cable structure | 56*22 mm2 | 56*22 mm2 CMS Type | 56*22 mm2 BOX Type | 56*28 mm2 | 68*22 mm2
Coil at 4.2 K |  |  |  |  | 
Aluminum stabilizer | - | 4.7-79.2 | 12.8-96.5 | 54.3-95.6 | 4.4-86.1
SC cable | - | 205-307 | 188-246 | 190-248 | 174-243
Al alloy | - | 2.5-20.8 | 30.2-57.1 | - | -
Support | - | - | - | 3.27-24.7 | 4.6-36.2
Coil at 4.2 K, energized |  |  |  |  | 
Aluminum stabilizer | 103 | 46.7-94.2 | 52.5-102 | 58.3-103 | 42.4-89.1
SC cable | 288 | 111-283 | 80-223 | 88.9-243 | 134-216
Al alloy | - | 46-98 | 46.7-125 | - | -
Support | 126 | - | - | 58.9-152 | 34.4-80.4
 | High strength Al stabilizer | NbTi | 5083 Al alloy
Yield stress@4.2K | 105 MPa | 800 MPa | 500 MPa
More details see Wang Menglin’s talk

## Slide 7
Physical design of the magnet
Physical design of the magnet
7
Material | Von Mises stress (MPa)
Coil at 4.2 K | 
Aluminum stabilizer | 4.4-86.1
SC cable | 174-243
Al alloy support | 4.6-36.2
Coil at 4.2 K, energized | 
Aluminum stabilizer | 41.5-95.9
SC cable | 54.9-221
Al alloy support | 43.2-87.4
Stress analysis
Coil structure
Cable structure
The maximum stress of each part of the coil is controlled within the stress range of the material.
NbTi Rutherford cable
High strength and High RRR Al stabilizer
More details see Wang Menglin’s talk

## Slide 8
Physical design of the magnet
Yoke
8
Yoke parameters：
In order to reduce the detection dead zone of the muon detector, the barrel yoke is designed as a spiral structure.
Barrel yoke: 1560 tons
Single module of the barrel yoke
130 tons
End yoke
700 tons
Barrel yoke (ton) | 1560
Each End yoke (ton) | 700
Total Yoke (ton) | 2960
Diameter(m) & length (m) | 10.37&11.75

## Slide 9
Mechanical design of the magnet
2D
Completed the design of the 2D chain and the space occupied by each component.
3D
Completed the design of the 3D structure, added suspension system, cooling pipes, and connection structure.
coil
Thermal shield
suspension rod
More details see Hou Zhilong’s poster

## Slide 10
Mechanical design of the magnet
Suspension system
Thermal shield suspension system:
6 radial rods each end
Material: titanium alloy
Coil suspension system (185 tons):
8 axial rods each end
6 radial rods each end
Material: titanium alloy
Forces and torques resulting from axial and radial offset, and from angular tilt of the coil.
Axial displacement (cm) | 1 | 3 | 10
Axial force (kN) | 484 | 1498 | 5034
Radial displacement (cm) | 1 | 3 | 10
Radial force (kN) | 34.3 | 236 | 656
Angular tilt (angle) | 1/407.5 =0.14° | 3/407.5 =0.42° | 10/407.5 =1.41°
Torque (kN.m) | 1965 | 6170 | 19935
 | Diameter | Length | amount
Axial rods | 30 mm | 3530 mm | 16
Radial rods | 40 mm | 1700 mm | 8
Main pull rods | 48 mm | 1650 mm | 4
More details see Hou Zhilong’s poster

## Slide 11: Mechanical design of the magnet
Main Technical Challenges:
Large-size and high-strength Aluminum stabilized superconducting cable;
Suspension system of the huge coil (185 tons);
High precision machining and assembly of large scale coil；
There are lots of welds in low-temperature pipes, including pipes and coil supports, pipes and liquid/gas helium tanks.
In summary, most of the challenges are related to processing techniques.

## Slide 12
Cryogenic system
Cooling methods: Thermal siphon
12
Uniform temperature distribution;
High heat transfer efficiency, not limited by source pressure and pressure drop;
Low cost. No need for liquid helium circulation pump
Cooling process diagram
The verification experiment are being design.

## Slide 13
Cryogenic system
Cooling methods: Thermal siphon
13
Cooling structure
Heat loads:
Items | Heat loads@4.2K (W) | Heat loads@60K (W)
Heat radiation | 35 | 373
Suspension rods | 7 | 55
Current leads | 100 | 2000
Cable joints | 4 | 0
Dynamic loads | 193 | 65
Static loads | 30 | 160
Total | 369 | 2653

## Slide 14
R&D progress
Conductors
  Conductor is the foundation of the magnet development. Most of the detector magnets used or will use the Aluminum-stabilized Nb-Ti/Cu conductors.
14
The IHEP and Toly company have jointly established an aluminum coated conductor production line in 2015.
Rutherford Cable
Aluminum stabilized NbTi/Cu conductor
Extrusion machine

## Slide 15
R&D progress
Aluminum coated conductor production line
15
This is the only aluminum coated superconducting cable production line in the world at present.
More details see Zhao Ling’s poster

## Slide 16
Aluminum stabilized superconducting conductors
R&D progress
Dimensions: 15*10 mm2
Number of tapes ：14
Materiel: Al 1100
Complete time: 2023.12
Length: 100 m
HTS: ReBCO cable
Aluminum stabilized Stacked REBCO Tape Cable
100 m
Dimensions: 15*4.7mm2
Number of strands ：14
Materiel : Al(99.99% purity)
Complete time:2017.8
Shear strength (COPPER &Al) > 35MPa
Length: 1.5 km
1.5 km
LTS: NbTi cable
Aluminum stabilized NbTi Rutherford cable
More details see Zhao Ling’s poster

## Slide 17
R&D progress
Dummy coil development
17
Large scale superconducting coil winding platform
Coil winding, vacuum leak detection, epoxy impregnation curing.
Coil winding
Coil winding

## Slide 18
R&D progress
Dummy coil development
18
φ7.2m dummy coil
Dummy coil
4 layers*10 turns
The manufacturing accuracy is controlled within ± 1mm
vacuum leak detection

## Slide 19
R&D progress
R&D of High Strength and High RRR(Residual Resistivity Ratio) Aluminum- Stabilizer for Superconducting Cable
19
Yield strength > 100 MPa@4.2K, 74 MPa at room temperature, RRR value > 400
By doping Ni-0.025% Be-0.025%
The Al-0.025%Ni-0.025%Be alloy prepared from 4N8-aluminum achieved high 0.2% yield strength of 75MPa (R.T.) with RRR of 417
High strength and High RRR aluminum stabilizer
Poisson’s ratio | 0.33/0.34
Young modulus | See the curve
Thermal expansivity | 14.23×10-6 K-1
4.2KRp0.25 | 105MPa

## Slide 20
IHEP: staff 13; engineer 5; post doctor 1; students 3
Cooperative institutes and Universities: SJTU, SWJTU, NCEPU, TSINGHUA, IEE, IPC, IPP and so on.
Cooperative companies: Wuxi Toly (aluminum stabilized conductors), Hefei Keye ( coil winding platform and dummy coil development), Xinjiang Zhonghe ( Aluminum stabilizer), SSCT ( HTS tapes), to be added.
Welcome international cooperation.
Research Team

## Slide 21
R&D plan
R&D items | Time
Further optimize the physical design of the coil, including magnetic field distribution, conductor structure, quench calculation and so on | 2024.11
Optimize the workflow of cryogenic system | 2024.12
Refine the design of mechanical structures | 2025.3
Full size superconducting conductors development | 2025.12
HTS plan R&D | 2027.12

## Slide 22: Summary
1. We carried out the physical design, mechanical design, and cryogenic system design of the CEPC detector magnet.
2. A lot of R&D work is underway.

## Slide 23
Thank you for your attention!
Oct. 23-27, 2024, CEPC workshop, Hangzhou