## Slide 1: A proposal to search for T-violating muon polarization in decay using stopped positive kaons
S. Ide, K. Horie, S. Ide, R. Imai, S. Ishitani, M. Mihara, S. Shimizu, K. Yasuda
Department of Physics, The University of Osaka
K. Kamada, A. Yoshikawa
Institute for Material Research, Tohoku University

## Slide 2: Transverse muon polarization in
Results of E246:
=0.0017±0.0023±0.0017
Δ 10−3
M. Abe et al.,
Phys. Rev. D40 (2006) 072005
J.A. Macdonald et al.,
NIM A 506 (2003) 60
with and decays
Stopped method was adopted in KEK-PS E246. Large solid angle and high resolution of the Toroidal spectrometer and CsI(Tl) calorimeter were used for the muon and photon measurement.
Well-designed detector to suppress systematic uncertainties
However, the finite acceptance for and , small momentum window for

## Slide 3: T-violation experiment using integrated calorimeter and polarimeter system
x
Muon momentum, muon polarization, and momentum are determined by the same electro-magnetic calorimeter using a stopped beam.
We aim at achieving Δ level in this experiment by keeping the cancellation mechanism to reduce systematic uncertainties with 1000 times higher acceptance.
A scintillating material which can preserve the polarization at room temperature.
S. Shimizu et al.,
Nucl. Instrum. Methods
A 945 (2019) 162587
Front
calorimeter
x
~1.5m
~1.2m

## Slide 4: Muon behavior in Fluorine compounds
The polarization in alkali halide such as NaI and CsI is promptly depolarized due to muonium () formation.
In fluorine compounds, a part of muons create a stable F-μ-F diamagnetic state, which can preserve the μ+ polarization.
In zero-field experiments, the SR signal by the fluorine magnetic moment was actually observed.
However, the observed polarization is less than 50% at low temperature.
R. Kadono, Muon Spin Rotation

## Slide 5: Polarized muon beam
muon
Neutrino
(decay time 26ns)
Pion decays into a neutrino and a muon
Neutrinos are always left-handed, so muons produced in decay are 100% polarized
At J-PARC, polarized muon beam can be obtained to confirm the preservation of spin polarization.

## Slide 6: Measurement ofpolarization in Lanthanoid Fluoride materials
CeF3, LaF3, PrF3, and NdF3 crystals with cross section were used.
A 100% polarized beam was stopped in the samples.
The time integrated polarization higher than 90% was obtained
2cm
Magnetic Field
K. Horie et al., Nucl. Instrum. Methods A 1037 (2022) 166932
K. Horie et al., Nucl. Instrum. Methods A 1066 (2024) 169606
J-PARC, MLF
At room temperature
100%

## Slide 7: asymmetry as a function of LF strength
A large CeF3 crystal with cross section was used (provided by K. Kamada, Tohoku Univ.).
The asymmetry was measured as a function of LF strength.
Decoupling feature of the F-μ-F state was clearly observed.
K. Horie et al.,
Nucl. Instrum. Methods A 1037 (2022) 166932

## Slide 8: Properties of CeF₃
density | 6.16g/cm
Radiation length | 1.68-1.7cm
Emission wavelength （peak） | fast=300nm slow=340nm
Decay time | 5-8ns
Luminous amount（NaI） | 4-8.6%
Merit
Possible to preserve
poralization
High time resolution
No hygroscopic
Good radiation hardness
Demerit
The emission wavelength of CeF₃ is around 300 nm. (NaI is around 400 nm.) it cannot be detected by a standard photon readout device.
→Special detector for short emission wavelengths is employed.
Low luminous intensity (8% of NaI)
Decide to use

## Slide 9: Bench test to research CeF3 properties
Cosmic rays
20 mm
CeF3 crystals
Channel
Time (ns)
Backgrounds
The detector system is very close to the beam.
The timing resolution is required to be better than 1 ns.
20 mm
S. Ide
Thesis work

## Slide 10: Further tests to obtain better detector performance
Measurement of spin relaxation time in -YF3 materials.
  chemical formula is same as CeF3, but crystal structure is different
  Photon yield is much higher; nearly same as NaI(Tl).
  A test experiment will be performed at J-PARC MLF in Nov. 2025.
Check of the analyzing power improvement using BGO detector.
  The asymmetry depends on the energy
  The asymmetry is determined as a function of the energy
  The experiment will be performed at TRIUMF in Dec. 2025
BGO detector

## Slide 11: Analyzing power of the polarimeter system
In the proposed T-violation experiment, the energy can be automatically measured.
Since the analyzing power can be determined as a function of the energy, and the polarization can be calculated in each bin.
In the standard polarization measurement, the analyzing power is reduced down to 1/3, integrating over all
The analyzing power of the new system is a factor of 2 higher.
The decay can be used for the calibration of the absolute polarization
asymmetry distribution
Using thin detectors,
A factor of 1/3 attenuation
:analyzing power

## Slide 12: Summary
A new experimental method to search for T-violating transverse muon polarization in decay is proposed.
In this experiment, the muon momentum, the muon polarization, and the momentum are determined by the same electro-magnetic calorimeter using a stopped beam.
We concluded the μ+ residual polarization higher than 90% in LaF3-type crystals is high enough to perform the T-violation experiment at J-PARC.
A test experiment to improve the analyzing power of muon polarization will be performed at TRIUMF. The analyzing power is expected to be highly improved by measuring the energy.
The spin relaxation time in -YF3 materials will be measured at J-PARC MLF.

## Slide 13: Backup

## Slide 14: muSR imagingの話(時間がなければskip)

## Slide 15: CeF3 crystal fabrication for the T-violation experiment
Large CeF3 crystal can be fabricated by K. Kamada et al. @Tohoku University.
It will take a year to produce all of the CeF3 modules.
Cost estimation of the CeF3 calorimeter
  Calorimeter weight is ~1ton
  Cost of raw materials is 0.3-0.4 M$

## Slide 16
 | CeF3 | PWO | CsI(pure) | NaI(Tl)
密度(g/cm3) | 6.16 | 8.2 | 4.86 | 3.67
輻射長(cm) | 1.7 | 0.92 | 1.86 | 2.6
光量相対的 | 4-5 | 0.26 | 4 | 100
光の減衰時間(nsec) | 30 | 15 | 10～1000 | 230
発光波長 (nm) | 340 | 430 | 300～400 | 415
屈折率 | 1.68 | 2.2 | 1.8 | 1.85
放射線耐性(rad) | 106 |  | 104-5 | 103
潮解性 | なし | なし | 少し | あり
CeF３の一般的性質
･光量の温度依存性 0.05(%/℃)
･モリエル半径 2.8(cm)
･圧縮強度 3.1×109(dyn/cm2)
･ヤング率 1.1×1012(dyn/cm2)
･熱膨張率 1.3×10-5(/℃)

## Slide 17: Properties of CeF3 as a scintillating material

## Slide 18: Properties of CeF3 scintillating material
Fast (~300nm)
Slow
density
melting point
refractive index
radiation length
wave length
decay time
photon yield
Moliere radius
hygroscopic
No
very fast
response
(NaI=100%)