## Slide 1: Cavity degradation after vert. test on the way or in the module, James Kerby
~10% agreement in results across laboratories typical
~20% degradation VT to cryomodule typical (DESY number here high as only the 16 'bad' cavities reported
small degradation w/ time (TRIUMPH 3%, CM1? other VT tests...)
for 1300MHz on order 30% ±5% cavities in CMs have large drops or external (tuner, coupler...) failures. 25% desy, 3/8 in both CM1 and S1G, but CM1 and S1G driven by externals?
Questions:
Possible sources of degradation?
What did we investigate?
What do we have to investigate?
What are the necessary improvements?

## Slide 2: Cavity degradation after vert. test on the way to the module
handling procedures
  Cleaning for clean room
  Pump and venting, cleanliness of pumping systems
  Flange opening
  Assembly of accessories
  Leak check
  Transportation
RF Measurement
  Fast power rise
  Multipacting
  FE from neighbor cavity
External systems need same level of rigorous testing as cavities
FE(?) largest suspect of remaining cavities
Lack of instrumentation compatible w/ dressed cavity tests a limit. Ideas?
Cross check of procedures across labs useful.
Documentation of failures very useful; limited statistics, shared knowledge base helps all avoid duplication.

## Slide 3: Questions about Q0, Clair Antoine, Camille Ginsburg
What is the measurement uncertainty of Q0?
Can magnetic shielding be used to improve Q0? At medium field? At high field?
What is the relation of Q0 to surface roughness and surface chemistry? At medium field? At high field?
For fine grain bulk Nb, which surface treatments maximize Q0?
  BCP vs. EP
  Tumbling
  Final HF rinse
Which “new” materials maximize Q0?
  Large grain? Does this depend on surface treatment?
  Multilayers (SC, insulating layers alternate), e.g., Nb3Sn, MgB2, NbN
  Thin films, e.g., Nb3Sn on Nb, Nb on Cu
What post-mortem is recommended for cavities which show high heat load (degradation) in cryomodule test to understand what happened? How do we discriminate between peripheral component heating and cavity surface heating?

## Slide 4: LHe oscillations in cryostats, Tom Petersen
Although large scale systems differ from small test systems, rapid pressure changes may be locally produced at or near the CM. Thus, even in single CM tests could be relevant. Do you see rapid (< 1 sec) pressure changes in your 2 K testing or larger 2 K systems?
If so, do you have some ideas about the sources?
Idea: Cryomodule design for pressure stability could involve not only vapor buffer volume but surface area of liquid-vapor interface for absorbing or desorbing vapor quickly with pressure changes.