## Slide 1
Fumio Furuta,
Georg H. Hoffstaetter
Cornell University
Laboratory for Elementary-Particle Physics
Recent results of VEP’ed cavities.
Analysis on VEP removal.
Temperature oscillation asymmetry.
Updates of Vertical Electro Polishing at Cornell

## Slide 2: What is Vertical Electropolish?
0.5 to 1 Hz
Cavity
PVDF Impeller
Al Electrode
Aluminum Electrode
Does Not Rotate
PVDF Electrode Cover
It Rotates
H. Padamsee & A.C. Crawford, PAC07, WEPMS009

## Slide 3: Why Vertical Electropolish?
Vertical Electropolishing has the Following Benefits:
  Eliminates rotary acid seals
  Eliminates sliding electrical contact
  Eliminates the cavity vertical/horizontal position control fixtures
  Simplifies the acid plumbing/containment
  The outside of the cavity is actively cooled, providing better temperature control of the polishing reaction.
  Lower capital equipment cost.

## Slide 4
Chart: 
| 49.55819125003265 | 56.244199969942 | 62.2157997661594 | 68.01390335271867 | 75.96342153944664 | 90.91862880616331 | 96.02077396540375 | 105.8633819355707 | 109.9514129335755
NR1-2, bulk-VEP+degas+micro-VEP+Bake, 1.8K | 17445518755.8522 | 17122065612.0001 | 16948201495.3541 | 16613625359.9272 | 16404126628.7479 | 14682319841.7617 | 13439539877.6812 | 12410115666.3043 | 11142832269.4716
NR1-3, bulk-VEP+degas+micro-VEP+Bake, 1.4K | 22400000000 | 20800000000 | 22300000000 | 23900000000 | 25500000000 | 26700000000 | 24700000000 | 24800000000 | 21100000000
AES1-002, bulk-VEP+degas+micro-VEP w/ circulation+Bake, 1.8K | 28466642428.0449 | 30517888367.3616 | 29766447932.5601 | 28358261647.2955 | 26479444836.2782 | 25888523620.7005 | 25004597813.8085 | 24829989105.8569 | 23091332117.4921 | 22475368163.08 | 17866725427.8886 | 16758686773.9243 | 18588834912.5814 | 19866458523.8539
AES1-006, bulk-VEP+degas+micro-VEP+Bake, 1.4K | 87589775677.7813 | 74865568376.9434 | 36955824116.9074 | 17825835279.3084 | 13856528618.018 | 13353697772.561 | 13610298300.3553 | 13733061032.8882 | 82293995680.4614 | 90322357291.7973 | 57136894943.7298 | 14481404662.8903 | 72580730767.4269 | 77361203578.2533 | 84501522414.3841
LR1-3(RE 60mm), CBP+bulk-VEP+degas+micro-VEP+Bake, 1.6K | 74925906471.2657 | 75597085122.3637 | 75665569439.1245 | 72936716321.569 | 67714941010.0663 | 64460549300.4566 | 59795820901.5647 | 52339736517.9858 | 45441954921.27 | 40147481326.9732 | 33940015889.1161 | 29431941967.9631 | 23932231596.4749 | 13226666824.3863 | 8256084353.1792 | 5154023243.1948 | 3312760957.0799
Hpk [mT]
Qo
Recent results of single cell + VEP
*NR, AES: TESLA shape
*LR: re-entrant shape

## Slide 5
Recent results of 9-cell + VEP
Chart: 
| 15.55631139000401 | 21.72505095467779 | 31.00942971702703 | 42.41420479369111 | 56.26025602006711 | 66.68830019284086 | 79.05884361625239 | 87.31875857567009 | 95.36765131631797
A10_VEP140um+degas+VEP30um+Bake, 2K | 26131347610.3217 | 25620021136.9141 | 25330134991.7008 | 23827569005.923 | 20604161659.2119 | 19091073914.3406 | 17319815984.6832 | 15903909318.4615 | 14771590368.8281
AES5_VEP140um+degas+VEP30um+Bake, 2K | 14135093266.5185 | 14420972716.0688 | 14350491508.7818 | 14483302133.9166 | 14204011838.8832 | 14019003920.4169 | 13618841387.8579 | 12881243026.3722 | 11898318956.4256 | 11502889927.1179 | 10865840584.9592 | 10354715322.4355 | 9890802851.5218 | 9495751470.6576 | 9120265272.9961 | 8446178008.1127 | 8000453682.5818
A9_tumbling+VEP140um+degas+okypolish+bake, 2K | 17164891497.614 | 16324535534.2541 | 16844624326.9442 | 17206254573.6822 | 17512047273.8572 | 17353748112.9536 | 17550459704.445 | 17366923881.1372 | 17320808303.3949 | 17063658794.7889 | 16835007108.1801 | 16258075365.4849 | 16156178304.0096 | 15665972348.1645 | 15705528346.774 | 14914756623.9018 | 14578990223.8077 | 13087949436.3472 | 12176905249.3214 | 11567954177.2631 | 10812232836.8216 | 10234644237.587 | 9666984233.3637 | 8723081218.8887 | 7889845198.0685 | 7331028607.0468 | 6591440267.0558 | 5754988140.4521 | 5101975885.8693 | 4286516507.6443
A9_VEP30um+Bake, 2K | 18014509408.5022 | 18588270266.0595 | 18987414624.5705 | 19568748251.4503 | 19117079610.9174 | 19043066536.1352 | 18500813567.5297 | 18058083186.1926 | 17689967138.5463 | 17192121514.4983 | 16608843535.8999 | 15985428585.667 | 15326270156.4875 | 14754191051.9756 | 14286484897.2646 | 13816416892.5435 | 13168321065.968 | 12558813455.7708 | 12542333034.3928 | 10884241181.6142 | 11741485324.3467 | 11298446494.6255 | 11018091457.6882 | 10899830951.2949
Re-entrant(70mm)_tumbling+VEP140um+degas+VEP30um+Bake, 2K | 16174150064.7575 | 15857288816.8872 | 15800692393.4655 | 15686470520.7417 | 15310269562.4547 | 15147260959.4147 | 14890866965.8777 | 14742441485.1206 | 14464085518.7155 | 14165751862.3203 | 13853922939.2401 | 13514755964.2809 | 13038420740.7052 | 12788483760.0539 | 12204037203.7259 | 11625686011.1456 | 11011525074.1544 | 9962103394.7527 | 9391576201.7385
Hpk [mT]
Qo

## Slide 6
Achievements of VEP for ILC requirements
Chart: 
| 38.64
TESLA single | 21100000000
TESLA 9cell | 4286516507.6443
RE single | 3312760957.0799
RE 9-cell | 9391576201.7385
Eacc [MV/m]
Qo

## Slide 7
Chart: 
| 4.0 | 30.0 | 10.0
single cell | 109.975 | 161.85 | 112.05 | 148.68
single cell* | 124.5
9-cell | 103.75 | 102.0241 | 95.3677 | 103.95
9-cell** | 149.4
>Single cells are NR1-3, AES1-002, AES1-006, Re-entrant(60mm).
>9-cells are A9, A10, AES5, Re-entrant(70mm).
>Cavity treatment: Bulk VEP (140~300um) + hydrogen degas + micro VEP + 110CBake.
>Some cavities tumbled to remove defects.
>*HNO3 in electrolyte, 8ml/3.5L.
>**EP after degas was replaced by 100nm oxypolish.
Hpk [mT]
Micro VEP removal [um]
Analysis on VEP removal
Preliminary

## Slide 8: VEP system with Recirculation
VEP 2.1: Recirculation

## Slide 9: Temp. monitoring setup
Top half cup
bottom half cup
Resolution of thermocouples: 0.02°C
Agitation: 0.85Hz
Acid Recirculation(1Hz)
Location of thermocouples ->
60 second window
Sample rate of
  TC: 1.5 Hz
  Current: 5 Hz
Thermometers

## Slide 10
Temperature Oscillations Asymmetry
VEP of AES2-1 w/ acid circulation
Top half Cup
Bottom half Cup
Preliminary

## Slide 11: Interpretation
Frequency of top ≈ 2 * frequency of bottom
No obvious correlation between temperature & electrolyte motion
Upper cup
  T increase correlated for Type 1 & Type 2 current spike
Lower Cup
  T increase correlated with Type 2 current spike
  T decrease correlated for Type 1 current spike
Meter stick for VEP development
  Top and bottom oscillations must be identical
Further analysis on temperature/current correlation

## Slide 12
Recent results.
>TESLA single cell achieved 39MV/m with Qo of 2.1e10 by VEP.
>Feasibility of VEP + oxypolish was demonstrated with TESLA 9-cell.
36MV/m was achieved so far.
>preliminary results show VEP removal dependence on gradient.
>Temperature oscillation asymmetry was found during single cell VEP.
We will check reproducibility of these processes.
These may have hint to high gradient Q-slope issue of VEP.
Ongoing R&Ds for VEP establishment.
1)Demonstration of high gradient w/ high Qo.
step1. TESLA shape(okay) -> Re-entrant shape.
step2. single cell -> 9-cell.
2) Demonstration of reproducibility and high yield.
3) Optimization of parameters.
voltage, current, temp, removal, agitation, etc.
4) Understanding of VEP process.
Temp. oscillation asymmetry, circulation, etc.
Summary