## Slide 1: Surface Treatment Studies in KEK
S. Kato, M. Nishiwaki, T. Noguchi, T. Saeki, M. Sawabe, H. Monjushiro,
M. Sato, K. Ueno, H. Hayano
KEK, Tsukuba, Ibaraki, Japan
P.V. Tyagi, V. Chouhan
GAUS, Tsukuba, Ibaraki, Japan
TTC meeting@Beijing 12052011

## Slide 2
(1) Surface contaminations on Lab-EP sample coupon.
(2) Surface contaminations on sample coupon in single cell cavity.
(3) Field Emitter Scanning microscope (FES) development.
(4) Formation of Sulfur in EP solutions
(5) Capturing of Sulfur in Cavity EP process
Studies on Nb surface contaminations in EP process

## Slide 3
Surface Analysis System
Analysis chamber consists: electron energy analyzer, ion mass spectrometer, x-ray source, electron gun, ion gun, extractor gauge, residual gas analyzer.
(XPS, SIMS)
Base pressures; analysis chamber: 10-9 Pa, LL1: 10-7 Pa, LL2: 10-8 Pa,
LL3: 10-7 Pa, sample storage chamber: 10-8 Pa.
P.V. Tyagi

## Slide 4
Transferring samples to multi holder carousel, then put into vacuum suitcase.
Vacuum suitcase consists: one battery operated ion pump and one linear motion drive.
The base pressure in suitcase: 10-7 Pa.
Sample carousel is transferred to XPS chamber by load-lock system.
Samples Transportation with clean condition
Vacuum Suitcase With Carousel
Multi Sample holder Carousel
P.V. Tyagi

## Slide 5
Laboratory EP Experiments
P.V. Tyagi

## Slide 6
Laboratory Electropolishing
Assembled Nb plate was electropolished at Lab-EP facility.
Lab-EP experiments were conducted with different current density.
The plate was twisted up to 1800 during the EP in order to agitate the process.
The twisting speed was 5-6 rpm.
P.V. Tyagi
Closer View of Nb Plate in Laboratory Electropolishing
Nb Base Plate (100x100x2.8 mm3)
Attached With
Nb Rectangular Sample (20x14x2.8 mm3)
Laboratory Electropolishing System

## Slide 7
Experiments | Purpose | Average Current Density (mA/cm2) | EP Acid Temperature (0C) | Nb Conc. in EP acid (g/l) | Removal Depth (μm)
Lab EP 1 | To see the effect of low current density with aged EP acid on EP performance at laboratory lavel | 33 | 27 | 7.3 | 20
Lab EP 2 | To see the effect of high current density with aged EP acid on EP performance at laboratory level | 50 | 30 | 7.6 | 20
P.V. Tyagi
Elements | Lab EP 1 Experiment with Low Current Density (atomic %) | Lab EP 2 Experiment with High Current Density (atomic %)
Nb | 16.5 | 5.1
C | 29.7 | 25
O | 53.7 | 60
F | <0.1 | <0.1
S | 0.3 | 10.3
XPS Analysis
Results
Parameters of Laboratory EP experiments

## Slide 8
Comparison of XPS Spectra of the Samples Treated in LabEP 1 and LabEP 2 Experiments
A Peak shift in sulfur as well as oxygen spectrum was again found in case of sample treated with high current density.
The chemical state of sulfur was confirmed as a mixture of SO4-- and SO3-- once again in the same manner as cavity EP 2 experiment.
O
S
F
Intensity [CPS]
Intensity [CPS]
Intensity [CPS]
Binding Energy [eV]
Binding Energy [eV]
Binding Energy [eV]
P.V. Tyagi
XPS analysis on Lab EP 1 (With Low Current Density)
and Lab EP 2 (With High Current Density)

## Slide 9
SEM and EDX Observation of Sample Surfae
Eped in Lab EP 2 (With High Current Density)
SEM Image of Sample Surface
EDX Spectrum of Sample Surface
SEM observations showed that the surface was covered with many particles.
EDX analysis confirmed that these particles are sulfur particles.
In addition, a large amount of oxygen was found in particles.
1 mm
10 µm
P.V. Tyagi

## Slide 10
Cavity EP Experiments
P.V. Tyagi

## Slide 11
Six disc type Nb samples are
required for an experiment.
A real single cell Nb cavity was
drilled with six holes.
Samples were mounted at
cavity holes with holding jig.
Disc Type Nb Sample
Φ = 8 mm, t = 2.8 mm
Nb SRF Cavity Drilled With Three Pairs of Holes
Iris hole
Equator hole
Beam pipe hole
Cavity Electropolishing Experimental Details
Φ = 8 mm
P.V. Tyagi

## Slide 12
Experiments | Purpose | Average Current Density (mA/cm2) | EP Acid Temperature (0C) | Nb Conc. in EP acid (g/l) | Removal Depth (μm)
Cavity EP 1 | To see the effect of fresh EP acid on EP performance | 48 | 25 | 0 | 20
Cavity EP 2 | To see the effect of aged EP acid over the fresh EP acid on EP performance | 48 | 25 | 7.9 | 50
Cavity EP 3 | To see the effect of low current density with aged EP acid on EP performance | 30 | 25 | 6 | 20
P.V. Tyagi
Condition of Cavity EP experiments

## Slide 13
O
Depth Profiles of the Samples
S
Beam Pipe Sample
Iris Sample
Equator Sample
Oxide layer FWHM : 1.5 nm
Oxide layer FWHM : 1.8 nm
Oxide layer FWHM : 2 nm
C
Cavity EP 1 Experiment With Fresh EP Acid
Comparison of XPS Spectra among Equator, Iris and Beam Pipe Samples
Depth [nm]
Depth [nm]
Atomic Compositions [%]
Depth [nm]
Depth [nm]
Atomic Compositions [%]
Atomic Compositions [%]
Intensity [CPS]
Intensity [CPS]
Intensity [CPS]
Binding Energy [eV]
Binding Energy [eV]
Binding Energy [eV]
P.V. Tyagi

## Slide 14
O
S
F
Equator Sample
Iris Sample
Beam Pipe Sample
Oxide layer FWHM : 1.5 nm
Oxide layer FWHM : 2.5 nm
Oxide layer FWHM : 1.9 nm
Equator and beam pipe samples: sulfur and fluorine up to 1 nm.
Iris sample: sulfur and fluorine up to 2 nm.
Cavity EP 2 Experiment With Aged EP Acid
Comparison of XPS Spectra Among Equator, Iris and Beam Pipe Samples
Atomic Compositions [%]
Atomic Compositions [%]
Atomic Compositions [%]
Depth [nm]
Depth [nm]
Depth [nm]
Intensity [CPS]
Intensity [CPS]
Intensity [CPS]
Binding Energy [eV]
Binding Energy [eV]
Binding Energy [eV]
Depth Profiles of the Samples
P.V. Tyagi

## Slide 15
Oxide layer FWHM : 1.5 nm
Equator Sample
Iris Sample
Beam Pipe
Sample
Oxide layer FWHM : 1.8 nm
Oxide layer FWHM : 1.8 nm
O
S
F
The FWHM of oxide layer was similar to cavity EP 1 and 2 experiments but in case of cavity EP 3 experiment, 20 % of oxide layer was found at 5 nm depth also.
Cavity EP 3 Experiment With Low Current Density (Aged EP Acid)
Comparison of XPS Spectra Among Equator, Iris and Beam Pipe Samples
Atomic Compositions [%]
Atomic Compositions [%]
Atomic Compositions [%]
Depth [nm]
Depth [nm]
Depth [nm]
Intensity [CPS]
Intensity [CPS]
Intensity [CPS]
Binding Energy [eV]
Binding Energy [eV]
Binding Energy [eV]
Depth Profiles of the Samples
P.V. Tyagi

## Slide 16
Cavity EP 1 Experiment With Fresh EP Acid
Elements | Equator sample surface (atomic %) | Iris sample surface (atomic %) | Beam pipe sample surface (atomic %)
Nb | 19 | 18 | 16
C | 37 | 40 | 34
O | 44 | 43 | 50
F | <0.4 | <0.4 | <0.4
S | <0.5 | <0.5 | <0.5
P.V. Tyagi
Elements | Equator sample surface (atomic %) | Iris sample surface (atomic %) | Beam pipe sample surface (atomic %)
Nb | 16 | 10 | 20
C | 18 | 16 | 27
N | 2 | 6 | 0
O | 58 | 59 | 49
F | 3 | 3 | 4
S | 4 | 7 | 2
Cavity EP 2 Experiment With Aged EP Acid
Elements | Equator sample surface (atomic %) | Iris sample surface (atomic %) | Beam pipe sample surface (atomic %)
Nb | 18 | 17 | 16
C | 35 | 29 | 33
O | 45 | 54 | 51
F | 0.9 | 0.2 | 0.4
S | 0.5 | < 0.1 | 0.2
Cavity EP 3 Experiment With Low Current Density (Aged EP Acid)

## Slide 17
EPed in Cavity EP 1 Experiment (Fresh EP Acid)
Surfaces were covered with many particles.
Particles size was several sub-micrometers to few micrometers.
A high density of particles was observed on the surfaces treated with aged EP acid.
SEM Observations
EPed in Cavity EP 2 Experiment (Aged EP Acid)
SEM Images of Beam Pipe Sample
P.V. Tyagi

## Slide 18
S. Kato
FES (Field Emitter Scanning microscope) study

## Slide 19
Combined System of FES and SEM-EDX
5 Axis Stage
NEG Modules
200 mm
SEM Object
Lens
5 x
Actuators
FES Support
Sample
Holder
Probe Tip
Cross sectional schematic view of the SEM stage and FES.
S. Kato

## Slide 20
SEM image of petals on Nb surface EPed with a high current density(50mA/cm2) and an aged acid(7.6g/l) (left). SEM image showing one petal, the scanning tip and the scanned area of 100x100 μm2 with 4 lines. (right).
The EP generated a large quantity of sulfate particles which were confirmed with XPS(X-ray Photoelectron Spectroscopy) and SEM-EDX techniques. These sulfate petals seem to be grown product as a result of surface segregation of sulfate.
S. Kato

## Slide 21
FES emission current mapping. The units for the vertical axis and for the X, Y axes are ampere and μm, respectively.
There were some small current peaks in a range of 1-10pA and unfortunately the scanning did not reveal the petal itself on the FES image. However the small peaks might be interestingly corresponding to both the rooted sulfate part at the petal feet that would be (semi)conductive and the small conductive sulfate with a size of 10-100 nm.
3.5kV for 20um distance
( ~ 17.5 MV/m )
S. Kato
2um step scan
for 100 x 100 um

## Slide 22
After the FES mapping, it was observed that strong blast of the petal occurred during the scanning and the main part of this insulating emitter disappeared. There remained some roots of the blasted petal in the Nb sub-surface, the fragments and the round melted particles.
SEM image after the FES mapping.
S. Kato

## Slide 23
Formation of Sulfur in EP solutions
H. Monzyushiro

## Slide 24
only NbF6- is observed in HF + Nb
NbF6- and Sulfur are detected in EP + Nb
Dissolution of Nb Metal powder in EP and HF solutions
H. Monjushiro
Raman spectroscopy

## Slide 25
Observation of Shapes of Sulfur micro-particles
during Nb dissolution in EP solution by Electron Microscope
Nb powder
50 mg
EP solution
5.0 mL
40 ℃
Filtration (0.45mm)
Carbon Adhesive Tape
Electron Microscope
H. Monjushiro

## Slide 26
40℃, 5 hr
40℃, 23 hr
40℃, 45 hr
40℃, 70 hr
40℃, 105 hr
Nb powder dissolution in EP solution
H. Monjushiro
Nb powder
Sulfur
Octahedron + Sphere
Growth of Sphere

## Slide 27
Capturing of Sulfur in Cavity EP process
M. Sawabe

## Slide 28
Sampling at cathode bag
By using carbon adhesive tape, surface contamination of cathode-bag and PTFE flange were sampled and viewed by SEM.
Sampling at PTFE flange
Carbon tape
Carbon tape
M. Sawabe
Capturing residuals after cavity EP process

## Slide 29
Sulfur shapes found in cathode-bag and PTFE flanges
Crystals
(Octahedron)
powder
plate
strings
M. Sawabe

## Slide 30
Before FM-20 Ultrasonic rinse
After FM-20 Ultrasonic rinse
M. Sawabe
Capturing residuals on cavity beam pipe after cavity EP process
During MHI-015 9-cell cavity bulk-EP process
FM-20 : degreaser which is used at STF

## Slide 31
MHI-015: Before FM-20 Ultrasonic rinse
MHI-015: After FM-20 Ultrasonic rinse
Sulfur were almost removed, but a few still there
M. Sawabe
Sulfur rings were observed

## Slide 32
M. Sawabe
MHI-015: Before FM-20 Ultrasonic rinse
MHI-015: After FM-20 Ultrasonic rinse
Sulfur were crystal form, and string form
Sulfur rings were observed

## Slide 33
(1) Surface contaminations on Lab-EP sample coupon.
High current density EP produce much sulfur in Nb surface.
(2) Surface contaminations on sample coupon in single cell cavity.
Aged EP acid EP produce much sulfur and fluorine in Nb surface.
Aged EP acid but low current density EP produce less sulfur.
(3) Field Emitter Scanning microscope (FES) development.
FES is still under development for emitter study on Nb surface.
(4) Formation of Sulfur in EP solutions
growth of sulfur and its shape change are observed.
(5) Capturing of Sulfur in Cavity EP process
sulfur removal by ultrasonic rinse using degreaser is confirmed, but not perfect.
Summary

## Slide 34
END of Slide