## Slide 1
CEPC Detector Magnet
Feipeng Ning
On behalf of SC magnet team
Aug. 7th, 2024, CEPC Detector Ref-TDR Review

## Slide 2: Content
Introduction
Requirements
Technology survey and our choices
Technical challenges
R&D efforts and results
Detailed design of the solenoid magnet
Cryogenic system
Mechanical design
Research team and working plan
Summary

## Slide 3: Introduction
This talk is about the design and development of the detector magnet for the TDR.
This talk relates to the Ref-TDR Chapter 9.

## Slide 4: Requirement
Position and size
Magnetic field
Inner diameter | 7070 mm
Thickness | 700 mm
Outer diameter | 8470 mm
Length | 9050 mm
Energy | t | Higgs | W | Z
Magnetic field | 3T | 3T | 3T | 2T
Energy |  | Higgs | W | Z
Magnetic field | 3T | 3T | 3T | 2T

## Slide 5
Technology survey and our choice
Low Temperature Superconductor (LTS) or High Temperature Superconductor (HTS)
 | LTS | HTS
advantages | Mature cable processing technology Mature coil winding and epoxy impregnation process Mature coil quench detection and protection methods Low cost | High mechanical strength High current density Can work at higher temperature, reducing the operating costs of cryogenic systems
disadvantages | Easy to quench High operating cost of cryogenic system | No effective quench detecting method No good coil winding method High cost

## Slide 6: Main Technical Challenges
Suspension system of the huge coil (140 tons);
High precision machining and assembly of large cylindrical dewar；
There are lots of welds in low-temperature pipes, including pipes and coil supports, pipes and liquid/gas helium tanks.
In summary, most of the challenges are related to processing techniques.

## Slide 7
R&D efforts and results
Conductors
  Conductor is the foundation of the magnet development. Most of the detector magnets used or will use the Aluminum-stabilized Nb-Ti/Cu conductors.
7
The IHEP and Toly company have jointly established an aluminum coated conductor production line in 2015.
Rutherford Cable
Aluminum stabilized NbTi/Cu conductor
Extrusion machine

## Slide 8
R&D efforts and results
Al-stabilized Conductors
8
1.5 km
100 m
LTS: Aluminum stabilized NbTi Rutherford cable
HTS: Aluminum stabilized Stacked REBCO Tape Cable
Aluminum coated conductor production line

## Slide 9
R&D efforts and results
Dummy coil development
9
Large scale superconducting coil winding platform
φ7.2m dummy coil
Coil winding, vacuum leak detection, epoxy impregnation curing.
vacuum leak detection
Dummy coil
4 layers*10 turns
The machining accuracy is controlled within ± 1mm

## Slide 10
R&D efforts and results
R&D of High Strength and High RRR Aluminum- Stabilizer for Superconducting Cable
10
Yield strength > 100 MPa@4.2K, 74 MPa at room temperature, RRR value > 400
By doping Ni-0.025% Be-0.025%, annealing, cold-working and curing.
The Al-0.025%Ni-0.025%Be alloy prepared from 4N8-aluminum achieved high 0.2% yield strength of 75MPa (R.T.) with RRR of 417 after cold working of 21% and annealing at 130℃ for 15hours.

## Slide 11
Detailed design of the solenoid magnet
Design of the magnet
11
Central magnetic field | 3 T
Inner diameter | 7070 mm
Outer diameter | 8470 mm
Thickness | 700 mm
Length | 9050 mm
Cold mass | 140 tons
Yoke mass | 3752 tons
Magnet mass | 265 tons
Magnet parameters:
magnet

## Slide 12
Detailed design of the solenoid magnet
Physical design of the magnet
12
Material | Von Mises stress (MPa)
Coil at 4.2 K | 
Pure Aluminum | 12.8-96.5
SC cable | 188-246
Al alloy | 30.2-57.1
Coil at 4.2 K, energized | 
Pure Aluminum | 52.5-102
SC cable | 80-223
Al alloy | 46.7-125
Central magnetic field | 3 T
Inner diameter | 7300 mm
Operating current | 16702 A
Cable length | 33 km
Inductance | 11 H
Stored Energy | 1.54 GJ
Coil parameters:

## Slide 13
Detailed design of the solenoid magnet
Yoke
13
Barrel yoke (ton) | 2184
Each End yoke (ton) | 784
Total Yoke (ton) | 3752
Diameter(m) & length (m) | 10.97&11.75
Yoke parameters：
In order to reduce the detection dead zone of the muon detector, the barrel yoke is designed as a spiral structure.
Barrel yoke
2184 tons
Single module of the barrel yoke
182 tons
End yoke
784 tons

## Slide 14
Cryogenic system
Cooling methods: Thermal siphon
14
Uniform temperature distribution;
High heat transfer efficiency, not limited by source pressure and pressure drop;
Low cost. No need for liquid helium circulation pump
Cooling process diagram
Verification experiment schematic diagram
Detailed calculations and process designs are currently underway.

## Slide 15
Mechanical design
2D
Completed the design of the 2D chain and the space occupied by each component.
3D
Completed the design of the 3D structure, added suspension system, cooling pipes, and connection structure.
coil
Thermal shield
suspension rod

## Slide 16
Mechanical design
Suspension system
Thermal shield suspension system:
6 radial rods each end
Material: titanium alloy
Coil suspension system (140 tons):
8 axial rods each end
6 radial rods each end
Material: titanium alloy
Forces and torques resulting from axial and radial offset, and from angular tilt of the coil.
Axial displacement (cm) | 1 | 3 | 10
Axial force (kN) | 484 | 1498 | 5034
Radial displacement (cm) | 1 | 3 | 10
Radial force (kN) | 34.3 | 236 | 656
Angular tilt (angle) | 1/407.5 =0.14° | 3/407.5 =0.42° | 10/407.5 =1.41°
Torque (kN.m) | 1965 | 6170 | 19935
 | Diameter | Length | amount
Axial rods | 30 mm | 3530 mm | 16
Radial rods | 40 mm | 1700 mm | 8
Main pull rods | 48 mm | 1650 mm | 4

## Slide 17
IHEP: staff 13; engineer 5; post doctor 1; students 3
Cooperative institutes and Universities: SJTU, SWJTU, NCEPU, TSINGHUA, IEE, IPC, IPP and so on.
Cooperative companies: Wuxi Toly (aluminum stabilized conductors), Hefei Keye ( coil winding platform and dummy coil development), Xinjiang Zhonghe ( Aluminum stabilizer), WST ( LTS wires), SSCT ( HTS tapes), and so on.
Welcome international cooperation.
Research Team

## Slide 18
Experience: BES III detector magnet
Research Team
Design, processing, manufacturing, and assembly experience of BES III detector magnet;
Safe, stable, and accident free operation for nearly 20 years.

## Slide 19
Experiences: 12T Dipole Magnet
Research Team
12T Dipole Magnet
Development of the LPF1 NbTi+Nb3Sn dual-aperture model dipole magnet from 2017.
Dipole field reached 12 T in 2*Φ14 mm apertures in May 2021 and 12.47 T in July after a thermal cycle.

## Slide 20
Experience: Aluminum stabilized superconducting conductors
Research Team
Dimensions: 15*10 mm2
Number of tapes ：14
Materiel: Al 1100
Complete time: 2023.12
Length: 100 m
HTS: ReBCO cable
Aluminum stabilized Stacked REBCO Tape Cable
100 m
Dimensions: 15*4.7mm2
Number of strands ：14
Materiel : Al(99.99% purity)
Complete time:2017.8
Shear strength (COPPER &Al) > 35MPa
Length: 1.5 km
1.5 km
LTS: NbTi cable
Aluminum stabilized NbTi Rutherford cable
This is the only aluminum coated superconducting cable production line in the world at present.

## Slide 21
Working plan
Further optimize the physical design of the coil, including magnetic field distribution, conductor structure, quench calculation and so on; 2024.11
Full size superconducting conductors development; 2025.6
Optimize the workflow of cryogenic system; 2024,12
Refine the design of mechanical structures；2025,3
R&D of HTS coil.

## Slide 22: Summary
1. After comparison, we have selected a solution and carried out the physical design, mechanical design, and cryogenic system design of the magnet.
2. The research team has a lot of experience in developing superconducting magnets. We are confident that we will finish all the required elements and will deliver this part into TDR.

## Slide 23
Thank you for your attention!
Aug. 7th, 2024, CEPC Detector Ref-TDR Review