## Slide 1
INTRODUCTION TO NEUTRON ACTIVATION ANALYSIS AT THE IBR-2 REACTOR, FLNP JINR
Inga Zinicovscaia
inga@jinr.ru/zinikovskaia@mail.ru
1Frank Laboratory of Neutron Physics, JINR, 6 Joliot-Curie Str., 1419890, Dubna, Russia, 2Horia Hulubei National Institute for R&D in Physics and Nuclear Engineering, 30 Reactorului Str. MG-6, Bucharest - Magurele, Romania

## Slide 2
geology
environment
materials science
forensics
archeology
nanotechnology
Elemental analysis

## Slide 3
Analytical techniques applied for element analysis

## Slide 4
Method | Detectable elements | Sensitivity*
ICP-OES/MS/SFMS | Li to U | ppm to ppt
NAA | H to U | ppm to ppt
AAS | Mainly metallic elements, up to 70 elements | ppm
CHNOS | C, H, N, O, S | 0.05–0.1 wt%
XRF | Be to U | 10 ppm–1 at%
SEM-EDX | All except H, He, and Li | 0.1–1 at%
ERDA | H to U | 0.1–0.5 at.%
RBS | Be to U | 0.1 at%
https://measurlabs.com/blog/elemental-analysis-applications-and-method-comparison/
Comparison of elemental analysis techniques

## Slide 5
Neutron activation analysis was first developed by G. Hevesy and H. Levi in 1936. They used a neutron source (226Ra + Be) and a radiation detector (ionization chamber) and promptly recognized that the element Dy (dysprosium) in the sample became highly radioactive after exposure to the neutron source.
George de Hevesy
Hilde Levi
Gamma spectrum of dysprosium-165
4He+9Be→12C+1n
G. Hevesy, Hilde Levi, The Action of Neutrons on the Rare Earth Elements, Det. Kgl. Danske Videnskabernes Selskab, Mathematisk-fysiske Meddelelser XIV, 5 (1936) 3–34
Neutron activation analysis

## Slide 6
Diagram illustrating the process of neutron capture by a target nucleus followed by the emission of gamma rays
The most common reaction occurring in NAA is the (n,γ) reaction, but also reactions such as (n,p), (n,α), (n,n′) and (n,2n) are important.

## Slide 7
Reactor and Radioanalytical complex REGATA

## Slide 8
Reactor and Radioanalytical complex REGATA
2 channels for irradiations, one with Cd shield.
Thermal neutrons flux: ~ 1012 n/cm2.s
Resonance neutrons flux: ~ 1011 n/cm2.s

## Slide 9
Regata Control program interface

## Slide 10
Left photo: KUKA KR 10 R1100 manipulator mounted on a stand. Right photo: Manipulator gripper and cassette holder with containers

## Slide 11
Irradiation channel: Ch 2 (full neutron spectrum)
Weight of samples: 0.05-0.5 gram
Irradiation time: 1- 30 min
Mg, Al, Si, Cl, I, Ti, V, Cu, Mn, Ca, S and Dy
Procedures of samples irradiation
Short irradiation
Long irradiation
Na, K, Sc, Cr, Fe, Co, Ni, Zn, Ga, As, Se, Mo, In, Sn, Br, Rb, Sr, Zr, Sb, Cs, Ba, Ag, Cs, La, Ce, Sm, Tb, Hf, Ta, Nd, Nb, Y, Yb, W, Re, Ir, Hg, Au, Th and U
Irradiation channel: Ch 1 (Cd- screen, epithermal and fast neutrons)
Weight of samples: 0.05-0.5 gram
Irradiation time: 3- 5 days
Cooling -3.5 days/ Repacking
First measurement- 30 min, directly after repacking
Cooling time – 20 days after the end of irradiation/ Second measurement – 2.0 hours

## Slide 12
Показатель | Диапазон измерений, млн-1 (мг/кг) | Показатель внутрилабораторной прецизионности в относительных единицах σRл, %
Na | 100-1000 | 26,0
 | 1000-40000 | 11,5
 | 40000-500000 | 3,86
Al | 1000-500000 | 19,3
Cl | 1000-5000 | 11,2
K | 1000-3000 | 20,5
 | 3000-30000 | 14
 | 30000-100000 | 8,08
Ca | 1000-15000 | 18,8
 | 15000-35000 | 11,4
 | 35000-400000 | 10,1
Sc | 1,0-50 | 11,4
Ti | 100-1000 | 17,9
 | 1000-10000 | 15,3
 | 10000-20000 | 6,78
V | 10,0-50 | 17,3
 | 50-500 | 13,6
Cr | 10-100 | 27,2
 | 100-500 | 15,6
.
Certification of the methodology of INAA

## Slide 13
Software of the SNAAPI

## Slide 14
  Scientific directions

## Slide 15
International Cooperative Programme on Effects of Air Pollution on Natural Vegetation and Crops
UNECE
United Nations Economic Commission for Europe
CONVENTION ON
LONG-RANGE TRANSBOUNDARY
AIR
Working Group on Effects - 1981
Passive biomonitoring

## Slide 16
As
Cd
61.5%
10.9%
2020/2022
3300 sampling sites

## Slide 17
Map of samples exposure in Kemerovo region
Active biomonitoring
Content of the elements in exposed moss samples compared to control

## Slide 19
25 stations along South Africa
KwaZulu-Natal
Mozambique
Namibia
Cape Town
Saldanha Bay
Eastern Cape
Assessment of water pollution

## Slide 20
Al, Sc, V, Cr, Mn, Fe, Co, Th -terrigenous
Na, Mg, K, Cl, As, Br, I - water salinity
Co, Ni, Sb, U - anthropogenic
Ca, Sr - deposition into shell and its construction
Na, Mg, Ca, As, Br, Sr, Cs - terrigenous (resuspension of bottom sediments)
East Polluted stations (harbors at eastern coast of South Africa)
Hazard indices (THQ
and HI)

## Slide 21
Wastewater treatment
Uptake of Er, Ho, and Gd by spirulina biomass cultivated in a medium supplemented with REEs.
Effects of rare earth elements on spirulina productivity

## Slide 22
Location of the Kumluca wildfire (a), soil sampling from the study area according to different fire severity levels and aspects (b)
  Assessment of soil pollution
Element concentrations in unburned and
burned soils

## Slide 23
Leaves-soil: K (TFL/S=3.1), Zn (TFL/S=2.1), Sr (TFL/S =1.9), and Mo (TFL/S =1.1) and Ca (TFL/S=0.96).
Fruits-soil: K (TFF/S= 1.6) and U (TFF/S = 2.1).
Fruits- leaves: TF> 1.0 was obtained for Na, Cl, and Cr.
Apples
Transfer factors in system soil-leaf-apple
 | Apple |  |  | Plum |  |  | Grape |  |  | 
Element | C mg/kg f.w. | DIM, mg/day | HQ, mg/kg/day | C mg/kg f.w. | DIM, mg/day | HQ, mg/kg/day | C mg/kg f.w. | DIM, mg/day | HQ, mg/kg/day | RfD, mg/day
Cr | 3.9 | 1.2 | 0.01 | 0 | 0 | 0 | 0.48 | 0.1 | 0.004 | 105
Co | 0.5 | 0.1 | 0.05 | 0.7 | 0.2 | 0.07 | 0.6 | 0.2 | 0.06 | 3
Fe | 78 | 23 | 0.4 | 151 | 45 | 0.75 | 8.8 | 2.6 | 0.04 | 10-60
Mn | 8.1 | 2.4 | 0.5 | 2.2 | 0.6 | 0.1 | 1.7 | 0.5 | 0.1 | 0.5-5.0
Ni | 6.7 | 2.0 | 1.4 | 1.4 | 0.4 | 0.3 | 1.8 | 0.2 | 0.2 | 1.4
V | 0.6 | 0.2 | 0.1 | 0 | 0 | 0 | 1.3 | 0.4 | 0.3 | 1.8
Zn | 33 | 9.9 | 0.7 | 25 | 7.5 | 0.5 | 6.4 | 1.9 | 0.1 | 15
Estimated daily intake of metal (DIM) and potential health hazards (HQ) from fruit
  Control of quality and safety of foodstuffs

## Slide 24
PCA scores plot for medicinal plants
Discriminant Analysis
TFs for K, Ca, Zn and Mo in medicinal plants
  Medicinal plants
Map of samples collection

## Slide 25
  Nanotoxicology
Microorganisms
Medicinal plants
Animals
Сereals
Accumulation of silver nanoparticles in mice and their offspring brain
1-100 mg/L
AuNPs
The content of gold in soil samples under root irrigation condition (a) and foliar spraying with AuNPs (b)
Spirulina platensis exposed to 0.05 µM AgNPs

## Slide 26
(a) St. Nicholas
(b) St. Basil the Great
(d) Mater Dolorosa
(e) Christ entering
Jerusalem
(c) St. John Baptist
Cultural heritage
Icon | Elements, mg/kg |  |  |  |  |  |  |  |  |  |  | 
 | Na (%) | Mg (%) | Cl (%) | K (%) | Ca (%) | Fe (%) | Zn | As | Sr | Sb | Ba | Au
Christ entering Jerusalem: yellow foil | 0.04 | 0.12 | 0.6 | 0.2 | 42 | 0.2 | 65 | 1 | 1090 | --- | --- | 4
Christ entering Jerusalem: ocher fragment | 0.08 | --- | 0.8 | --- | 39 | 0.1 | 60 | 5 | 950 | 2 | 220 | 1
St. Basil the Great: wood fragment | 0.02 | --- | 0.1 | --- | 0.1 | --- | 10 | --- | 2 | --- |  | 27
The content of major elements and trace elements as determined by NAA in some fragments of Russian icons.

## Slide 27
The content of major (a) and trace elements (b) in Chelyabinsk meteorite
Extraterrestrial materials
Elemental composition of clean and contaminated fragments of the rolled cotton cloth determined by NAA, in µg/g

## Slide 29
May 27
Vladimir Galustov. Dataset preparation software for training a neural network to determine the boundaries of full energy peaks in gamma spectra.
May 29
Marina Frontasyeva. Air pollution studies in Asia and the Pacific based on moss analysis by nuclear and related analytical techniques.
Alexandra Peshkova. Risks assessment of gold nanoparticles exposure for the soil-plant-consumer system.
Margarita Shvetsova. Assessment of the recreational zones in Moscow using neutron activation analysis and atomic absorption spectrometry.
Aleksandra Kravtsova. Copper and nickel accumulation and translocation in leafy vegetables irrigated with metal-containing effluents.
Vladimir Zaichick. Activation by neutrons and related analitical methods as a tool of medical elementology.
Octavian Duliu. INAA and XRD investigation of the Serbian sector of the Danube river and its tributary.

## Slide 30
Thank you for attention!