## Slide 1: Superconducting Magnets for Accelerator Science
CERN LHC

## Slide 2: Item
Accelerator & Magnet
Superconducting Accelerator Magnet
Superconductivity
Superconducting Magnets for Hadron Colliders
Superconducting magnet applications in various accelerators
Summary

## Slide 3: Item
Accelerator & Magnet
Superconducting Accelerator Magnet
Superconductivity
Superconducting Magnets for Hadron Colliders
Superconducting magnet applications in various accelerators
Summary

## Slide 4: Accelerator？
Accelerate Charged Particle
:力
q: Charge
（E=V/d）
V
d

## Slide 5: Ring Accelerator Synchrotron
Bending
Magnet
Focusing
Magnet
Accelerating Cavity
Ring Orbit by Magnetic Field
Reuse Accelerator Cavity
Stronger B Field for Higher Energy
Bent Beam by Magnetic Field
遠心力
EM Force

## Slide 6: Magnets for Synchrotron
Bending Magnet
  Normal Dipole
  Bend Beam
  Uniform Field
Focusing Magnet
  Normal Quadrupole
  Focus Beam
  Gradient Field
S
S
N
N
Accelerating Cavity
Bending
Magnet
Focusing
Magnet

## Slide 7: Multipole Field
Normal Dipole
B1=const. (zero otherwise）
By=B1
Bx=0
Uniform Field
Normal Quadrupole
B2=G0=const. (zero otherwise）
By+iBx=G0/r0(x+iy), G0/r0=g0
By=g0x
Bx=g0y
Uniform Gradient Field
2n-pole field
Bn=Kn=const. (zero otherwise）
By+iBx=Kn/r0n(x+iy)n
On x-axis（y=0）
By=Kn(x/r0)n
S
S
N
N
: Normal 2n-pole、
: Skew 2n-pole
N
S
reference
radius

## Slide 8: LHC: Large Hadron Collider
1 arc = 23 cell
8 x 2.45 km arc, 8 x 545 m straight section
F or DF Magnet
B Magnet
１cell：BM６＋FM１＋DFM１

## Slide 9: Create Uniform Field
x
y

## Slide 10: Create Uniform Field
Left conductor（Current Density=j ）

## Slide 11: Create Uniform Field
Right Conductor（Cj ）
Left Conductor（Current Density=j ）

## Slide 12: Create Uniform Field
Center（Current Density=0）
Right Conductor（Cj ）
Left Conductor（Current Density=j ）

## Slide 13: Cosθ coil
d→0
t = d・
BM (Normal Dipole)：
FM（Normal Quadrupole）： Distribution
θ

## Slide 14: Create Uniform Field：LHC Dipole
j = 400 A/mm2
d = 3 cm
By = 8.3 T
Actual Coil
Inner Cable
Width：15.1 mm
Thickness：1.9 mm
Turn Number：15*2
Current Density：400 A/mm2
Outer Cable
Width：15.1 mm
Thickness：1.48 mm
Turn Number：26*2
Current Density：520 A/mm2
Power consumption：total LHC: 120MW 〜 600W/Tm

## Slide 15: Normal Conducting Magnet
Ohmic Heating：W = VI = RI2 → Cooling limitation：10 A/mm2
1/40 of Superconductor：40 times large coil?：Not real
Real normal magnet：Magnetic circuit with Iron Yoke
Iron Saturation：2 T limit
g
H=NI
B~μ0NI/g
P = ρi(NI)L
~ ρjBLg/μ0
(P: Power consumption、
ρ: Resistivity
j: Current Density,
L: Conductor length / turn）
0.05(gap)*0.1(width)*1(length)m & 2T ~ 15kW (@ 10A/mm2) 〜 7kW/Tm
LHC with Normal Magnet
4 times large accelerator
10 times large Power Cons.

## Slide 16: Item
Accelerator & Magnet
Superconducting Accelerator Magnet
Superconductivity
Superconducting Magnets for Hadron Colliders
Superconducting magnet applications in various accelerators
Summary

## Slide 17: Superconducting Accelerator Magnet
HL-LHC
Nominal LHC
NC D1
IT Quads. w/ Nb3Sn
SC D1
IT Quads.& D1
Corrector
Package
Q1
Q2a
Q2b
Q3
IP

## Slide 18: HL-LHC D1 magnet Lorentz force
Shell (SUS304L)
Iron yoke
(EFE by JFE steel )
key (S45C)
4-way split stainless steel collars
(NSSC130S)
Cu/NbTi cable
(LHC MB outer) +
Apical insulation
Radiation resistant
GFRP wedge
(S2 glass + BT resin)
Brass shoe
QPH + Insulations
Field tuning hole
f60 mm HX hole
Stack tube (S45C)
Mid-plane
High Current in High Field
=Strong Lorentz force
=Strong Structure

## Slide 19: Prestress to support coil
δxi
ki
δxi+1
ki+1
fi
fi+1
fi-1
….
….
X=X0+ΔX
….
….
k1
f1
fn-1
kn
Prestress
~const.

## Slide 20: Error Field
Error Field＝Orbit distortion: small as possible 〜10-4
A2, A6, A10, …
A1, A3, A5, …
+
–
–
+
–
+
–
+
Error due to coil size error
Error due to magnet deformation
High Precision Structure技術

## Slide 21: Magnet Assembly Size Control of Coil Parts
Pole shim and wedges tolerance: ±20 μm
Pole shim and wedges
End spacers
Chart: TY0002
Chart: TY0002
Chart: TY0002

## Slide 22
Magnet Assembly
Coil winding and Curing
Tensioner
Feeder
Turn table
Winding mandrel
Hydraulic rams

## Slide 23
Magnet Assebly
Coil size measurement
コイルサイズを確認して予備応力を制御する

## Slide 24
Magnet Assebly
Collaring
Collar plates were fabricated by fine-blanking.
Good size accuracy in the critical parts:±10 mm
Four-way split collar even for a dipole
Alternate lamination of Fixing- and Spacer-collar
(t2.3 mm, t2.6 mm)
Embossing to control PF to be 96%
Vertical
collar
Horizontal
collar
Collaring press
Sub-stack
Fixing-collar
Spacer-collar
Fixing-collar
Spacer-collar
Four-way split collar
Collar plates fabricated by
fine-blanking

## Slide 25
Upper yoke
Lower yoke
SS collar
GFRP collar
Ramp box
Magnet Assebly
Yoking
Yoke plates were fabricated by fine-blanking.
Alternate lamination of Fixing- and Spacer-yoke (t5.6 mm, t6 mm)
Spacer sheets were periodically inserted to control PF to be 98%
Yoke assembly
Loading
Fixing-yoke
Spacer-yoke
Yoke sub-stack
Keys
Key slots

## Slide 26
2 m long half shells were longitudinally welded.
Magnet assembly was completed after end ring welding and splice work.
Magnet Assebly
Final Assembly
Shell welding
End ring welding
Splice work
Completion of fabrication

## Slide 27: Item
Accelerator & Magnet
Superconducting Accelerator Magnet
Superconductivity
Superconducting Magnets for Hadron Colliders
Superconducting magnet applications in various accelerators
Summary

## Slide 28: Discovery of Superconductivity and Meissner Effect
Heike Kamerlingh Onnes
  1908 Helium liquified
  1911 April 8th Discovery of Hg Supercon.
1933 Meissner Effect

## Slide 29: BCS Theory
BCS Theory（１９５７）
  Cooper Pair
Bardeen, Cooper, Schrieffer

## Slide 30: Normal Conductor
V = RI
W = VI = RI2

## Slide 31: Superconductor
Pair interchange kinetic momentum: no loss

## Slide 32: BCS Theory
Based on Cooper pair
Bose–Einstein condensation
  All Cooper pairs have the same momentum
  Energy Gap
Bardeen, Cooper, Schrieffer
Fermi
Surface

## Slide 33: Superconuductors
Type I Superconductor
  Meissner Effect
    Penetration Depth λ＜ξ Coherent Length
    l: Electron Mean Free Path Pure Metal
  Current Flow only on Thin Surface
Type II Superconductor
  Mixed State (1957 Abrikosov)
    Penetration Depth λ＞ξ Coherent Length
    Alloy, Compound
  Flux penetration in Superconductor
  Current Flow inside Superconductor

## Slide 34: Critical Current and Pinning
Flux Flow
  Flux Move
  Induced Voltage
  Need to stop Flux
Pinning Force
  Week superconducting state
    Easier to turn to normal
  Normal Site = Flux Pinned
  Pinning Force = Critical Current
Pinning potential

## Slide 35: Meissner Effect and Pinning Effect
Stick by Pinning Effect
Enforce flux pinning by pushing
superconductor to magnet rail
Superconductor
Ｓ
Ｎ
Ｓ
Ｎ
Ｓ
Cross Section
Ｎ
Ｎ
Ｎ
Ｓ
Ｓ
Ｓ
Ｓ
Ｎ
Float by
Meissner Effect
Superconductor
Ｓ
Ｎ
Ｓ
Ｎ
Ｓ
Ｎ
Ｎ
Ｎ
Ｓ
Ｓ
Ｓ
Ｓ
Ｎ

## Slide 36: Critical Surface
Critical Current Density is function of
  Temperature
  Magnetic Field
NbTi: 3000A/mm2 @ 4.2K, 5 T

## Slide 37
Billet
Hydrostatic Extrusion
Drawing
Multi Billet
Drawing
Heat Treatment
Twist
Insulation
Cabling
Al stabilized Cable
Rutherford Cable
CICC
Soldered Cable
Real Superconductor：
Multi-filament superconductor
NbTi/Cu
Nb/Bronds
Nb/Al/Cu
NbTi
Nb3Sn
Wire
Cable
dice
Hydrostatic Extrusion

## Slide 38: Multi-filament Superconductor Magnetization
Type-I
Type-II (without Pinning)
Type-II (with Pinning)
Magnetization
＝ Proportional to
Filament Size
–M
H
Shielding Current with Jc
+Jc
+Jc
Coupling between Filaments
Twist to de-couple

## Slide 39: Quench and Protection
Quench = Abrupt phase transition to normal
Current flow in Copper → Still fast temperature rise
Temperature rise depends: MIITs
MIITs/I2: time to reach a temperature
  Cu/NbTi=1, 400 A/mm2 →
Copper
NbTi
Current
Rapid detection of quench and shutting down current is needed
〜10-10 Ωm
〜10-7 Ωm

## Slide 40: Quench Protection
Fast Shutting Down of Current
  External Dump Resistor
    Extract energy to outside
    High terminal voltage
  Quench Protection Heater
    Voltage is distributed in the magnet
    The energy is dumped into the magnet
  In principle combination of these two methods is used
PS
Magnet
Extraction R
Magnet
Heater
PS

## Slide 41
Dump Circuit
  Protect Cold Diodes and SC Bus Bars
  Time Constant: 20 sec
Cold Diode
  Turn On Voltage: 6V
  Forward Voltage: 1V
Quench Protection Heater
  Powered by Capacitor Bank
  Magnet Current τ≈1 sec
Protection Circuit for Accelerator String
Quench Detector
trigger
trigger
Quench Protection of Large Accelerator
Magnet System:
Neutrino Beam Line

## Slide 42: LHC Incident in 2008
Cause
  Bad solder joints
  Insufficient quench detection
  Huge stored energy
Damage: 300MJ dissipated: ~15 magnet damaged
Recovery: 2 years: several thousand solder joints repaired

## Slide 43: Item
Accelerator & Magnet
Superconducting Accelerator Magnet
Superconductivity
Superconducting Magnets for Hadron Colliders
  History
  On going
  Future
Superconducting magnet applications in various accelerators
Summary

## Slide 44: History of Accelerator and Superconductivity
PARTICLE ACCELERATORS by M. Stanley Livingston and John P. Blewett, 1962, p. 6.
1908 Liquid Helium (K. Onnes)
1911 Superconductivity (Hg：K. Onnes)
1933 Meissner Effect (W.Meissner)
1957 BCS Theory (J.Bardeen L.Cooper J.Schrieffer)
1965 First International Symposium of Magnet Technology (SLAC)
1970 Industrialization of NbTi Composite Conductor
1977 FNAL/Tevatron prototype magnet
1979 Industrialization of MRI Magnet
1983 FNAL/Tevatron: 6.3km (4.4T, 6.1m, 774)
1986 High Tc Superconductor (K.Muller, J. Bednorz)
1988 SC Tokamak （TORE SUPRA）
1989 SC Cavity (KEK/TRISTAN)
1990~ Industrialization of MCZ Magnet
1992 DESY/HERA: 6.3km (4.7T, 8.8m, 416)
1993 SSC Cancel: 87.1km (6.6T, 15.8/13.3m, 7956/504)
1998 BNL/RHIC: 3.8km (3.5T, 9.7m, 288)
2001 MgB2 (J. Akimitsu)
2008 CERN/LHC: 26.7km (8.3T, 14.2m, 1232)

## Slide 45: History of Superconducting Magnet Early Days（1960s）
初めての磁石
  1954 G. Yntema 0.71 T
1961 MIT Conference
  J.E.Kunzler (Bell Lab.): Nb3Sn 6.8T Win!
  J.Hulm (Westinghouse): NbZr 6T ！
Kunzlerによる最初の特許
Kunzler:10T Nb3Sn Magnet
Win 2 case of scotti！
But Bell lab. stop SCM R&D
J. Hulm: NbTi !

## Slide 46: NbTi (Alloy) vs Nb3Sn (Compound)
Jc：Nb3Sn is better
Mechanical Property
  NbTi: Alloy → Ductile → Easier to wind coil
  Nb3Sn: Brittle → Difficult to wind coil
Below 8T
  NbTi

## Slide 47: TEVATRON
Energy Doubler (1TeV)
  Higher Field Magnet 4.3 T
Energy Saver
  ~1/2 Overall Power Saving
Tunnel is given (main ring)
SCMs are installed in the same tunnel
main ring (normal conducting) is
used as injector, but reduce energy from 400 GeV to 150 GeV
Overall energy saving ~ ½

## Slide 48: Iron geometric error
FNAL dipole magnet
  Coil support creep → Coil move by -dy
Iron location error：+dy
  Error in image current: (R2/r)
    Radial：-dy/r•sinθ
    Azimuthal：dy/r•cosθ
  Skew quadrupole
  Beam X-Y coupling
  Emittance growth at injection

## Slide 49: Accelerator Superconducting Magnet: HERA & RHIC
1992：DESY/HERA: 6.3km (4.7T, 8.8m, 416 Magnets)
1998：BNL/RHIC: 3.8km (3.5T, 9.7m, 288 Magnets)

## Slide 50: Accelerator Superconducting Magnet: Superconducting Super Collider
Start in 1988 > Terminated in 1993
Fail to control budget 4.4B$→12B$
2B$ already used

## Slide 51: Synchrotron Operation
Storage Ring
  Collider, Photon Factory
  Slow Operation Cycle
Extraction Machine
  Injector, Fixed Target
  Fast Operation Cycle
Injection
Storage (flat top)
Injection
Extraction
(flat top)
Imag
Imag
Time
Time
Accelration
Acceleration
HEB magnets: 15 times faster ramp rate to that of collider

## Slide 52: SSC: Influence of inter-strand coupling current on field quality
Inter-strand coupling current dominated by cross over resistances that are extremely non-uniform across the magnet cross section = non-uniform coupling current = strange field behavior

## Slide 53: Accelerator Superconducting Magnet: LHC
2008：CERN/LHC: 26.7km (8.3T, 14.2m, 1232 Magnets)

## Slide 54
Measured as
  Sextupole field decay and snap back at TEVATRON
  Imbalance current observed as periodic pattern at HERA
  Model to simulate effect established by CERN (LHC)
Magnetization decay
Acceleration
Flat
top
Injection

## Slide 55: Japanese Contribution to LHC MQXA: Interaction Quadrupole
Focus Beam at Interaction Region (Increase Luminosity)
  Field Gradient 280T/m, Maximum Field 8.7 T

## Slide 56: Item
Accelerator & Magnet
Superconducting Accelerator Magnet
Superconductivity
Superconducting Magnets for Hadron Colliders
  History
  On going
  Future
Superconducting magnet applications in various accelerators
Summary

## Slide 57: On going HL-LHC
High Luminosity LHC
Increase Collision Statistics
More detailed physics

## Slide 58: On going HL-LHC
Interaction Region Upgrade
  Smaller beam size at IR
    Quadrupole upgrade by Nb3Sn
  Crab cavity
  Beam separation magnet upgrade
    NbTi superconducting magnet
  Luminosity Upgrade

## Slide 59: IR Quadrupole Upgrade Higher Field by Nb3Sn
Nb3Sn: maximum field 11.4T
Wind and React to handle brittle superconductor
OST RRP strand, 132/169

## Slide 60: Superconducting Transmission Line
Transmission line system for HL-LHC.
Default MgB2
Option HTS
“Development of superconducting links for the Large Hadron Collider machine,” A. Ballarino, Supercond. Sci. Technol. 27, 2014, 044024.

## Slide 61: Beam Separation Dipole Upgrade KEK Contribution
Large Aperture 150mm, 6T Dipole
Sigh of MOU between CERN and KEK
HL-LHC D1 Magnet

## Slide 62: Item
Accelerator & Magnet
Superconducting Accelerator Magnet
Superconductivity
Superconducting Magnets for Hadron Colliders
  History
  On going
  Future
Superconducting magnet applications in various accelerators
Summary

## Slide 63: The FCC-hh: a next energy frontier.
L Rossi @ WAMHTS-2 Kyoto
LHC
27 km, 8.33 T
14 TeV (c.o.m.)
FCC-hh
80 km, 20 T
100 TeV (c.o.m.)
FCC-hh
100 km, 16 T
100 TeV (c.o.m.)
HE-LHC
27 km, 20 T
33 TeV (c.o.m.)
Geneva
PS
SPS
LHC
L. Bottura at WAMHTS-1
Future
Prospects FCC
Future Circular Collider (FCC)
Future 100 TeV Collider
100 km circumference
Or
HE-LHC
(High Energy LHC)
Both needs
20T HTS magnets or
16T Nb3Sn magnets

## Slide 64: FCC Magnet Designs
4300 tons of Nb3Sn + 10200 tons of Nb-Ti
20T version
16T version
1400 tons of HTS + 6600 tons of Nb3Sn + 11300 tons of Nb-Ti
L. Bottura at WAMHTS-1

## Slide 65: Item
Accelerator & Magnet
Superconducting Accelerator Magnet
Superconductivity
Superconducting Magnets for Hadron Colliders
Superconducting magnet applications in various accelerators
Summary

## Slide 66: Superconducting magnet applications in various accelerators
Lepton colliders
Synchrotron radiation facilities
Proton extraction synchrotron
Medical synchrotron
Cyclotron
Ion source, klystron
Detector magnets

## Slide 67: Superconducting magnet applications in various accelerators
Lepton colliders
Synchrotron radiation facilities
Proton extraction synchrotron
Medical synchrotron
Cyclotron
Ion source, klystron
Detector magnets

## Slide 68: LEP and LEP2
LEP: electron positron collider at CERN
27 km circumference
Superconducting magnets for interaction region: focusing quadrupole magnets

## Slide 69: KEK Lepton colliders and SC Magnets TRISTAN, KEKB, S-KEKB
SuperKEKB Quadrupole magnet at Collision point

## Slide 70: ILC Magnets
Undulator
Acceleration Region Quadrupoles
Interaction Region Quadrupoles
ILC magnets
Low field

## Slide 71: Superconducting magnet applications in various accelerators
Lepton colliders
Synchrotron radiation facilities
Proton extraction synchrotron
Medical synchrotron
Cyclotron
Ion source, klystron
Detector magnets

## Slide 72: Synchrotron radiation facilities
Various SR facilities

## Slide 73: SR facilities
Super-Bend
Traditional usage

## Slide 74: SR facilities
Wiggler

## Slide 75: SR facilities
Superconducting undulator
Short period undulator.
HTS tape conductor coil
Nb3Sn high current density coil
Shorter period
Higher brightness
Higher energy
Large fixed aperture

## Slide 76: Superconducting magnet applications in various accelerators
Lepton colliders
Synchrotron radiation facilities
Proton extraction synchrotron
Medical synchrotron
Cyclotron
Ion source, klystron
Detector magnets

## Slide 77: Proton extraction accelerators J-PARC
J-PARC: extraction machine
  Rapid cycle synchrotron
  J-PARC RCS (3GeV 1MW)：25 Hz
  J-PARC MR (30GeV 1MW): ~1 Hz
  Not suitable for superconducting magnets
After extraction: constant beam energy = constant magnetic field: good for superconducting magnet
  J-PARC neutrino beam line
J-PARC RCS Magnets
J-PARC MR Magnets

## Slide 78: Japanese Accelerators and SC Magnets J-PARC Neutrino Facility
Neutrino Facility needed SC magnets due to space limitation
Combined Function Magnet Beam Line（2.6T+19T/m, 28 Magnets）Optimize Cost and Schedule
We need SC Magnets
But it's too expensive

## Slide 79: Muon Capture and Trasportation
Muon at J-PARC MLF: Low Energy (low momentum)
  Trap Muon in helical orbit (cyclotron motion)
  Use solenoid magnet
B
Current +I⦿
Current -I

## Slide 80
Superconducting Curved Solenoid
Superconducting Focusing Solenoids
SC Solenoids in MLF Muon Science Facility
Ultra-Slow Muon Beam Line
Decay Muon Beam Line
Superconducting Solenoid
http://legacy.kek.jp/newskek/2009/julaug/CFCAF.html

## Slide 81: J-PARC g-2/EDM
2900 mm
Muon storage orbit
Dia. : 666 mm
Cold box
NMR probe system R&D
Very high precision solenoid (sub-ppm) for Muon storage: measure muon g-2 and EDM

## Slide 82: COMET at J-PARC
Support to J-PARC Projects
Transfer Line
Muon Transport Solenoid
Helium Refrigerator
COMET SC Magnet System: Helium Transfer Line to Muon Transport Solenoid is under construction.
ColdBox
CurrentLeadBox
Pion
Capture
Solenoid
Muon
Transport
Solenoid
Detector
Solenoid
TransferTube
to MTS
TransferTube
to PCS
Muon production solenoid
Capture muon and pion with large solenoid

## Slide 83: J-PARC MLF Second Target
Utilize HTS to sustain high radiation environment
Secondary Particle Capture Solenoid
MLF Second Target

## Slide 84: Other Extraction Synchrotron TEVATRON, GSI SIS100
TEVATRON (800GeV ~70kW) Originally extraction machine
  Various AC loss reduction method such as ZEBRA cable
  Operation Cycle: ~ 1 min
GSI SIS100 (30GeV ~100kW)
  Superferic: 1.9T, 1Hz(4T/s)
GSI SIS100 Main Dipole Magnet

## Slide 85: Superconducting magnet applications in various accelerators
Lepton colliders
Synchrotron radiation facilities
Proton extraction synchrotron
Medical synchrotron
Cyclotron
Ion source, klystron
Detector magnets

## Slide 86: Superconducting magnet applications in various accelerators
Lepton colliders
Proton extraction synchrotron
Synchrotron radiation facilities
Medical synchrotron
Cyclotron
Ion source, klystron
Detector magnets

## Slide 87: Medical Accelerator
Synchrotron for heavy ion accelerator
  Synchrotron: enables energy scan
  Need rapid cycle: difficult for superconducting magnets
LBNL Bevalac
QST HIMAC

## Slide 88: Medical Accelerator Superconducting Gantry
Compact and light weight with superconducting magnet

## Slide 89: Medical synchrotron Future prospect
Superconducting synchrotron for more compact machine
Fast ramp rate magnet R&D
High field gantry
Future medical synchrotron

## Slide 90: Superconducting magnet applications in various accelerators
Lepton colliders
Synchrotron radiation facilities
Proton extraction synchrotron
Medical synchrotron
Cyclotron
Ion source, klystron
Detector magnets

## Slide 91: RIKEN SRC
World largest superconducting ring cyclotron

## Slide 92: Small Cyclotrons
DC operation: good for superconducting magnets
High field magnet for compact accelerator
Beta Installation at the University of Michigan
Mevion S250 Medical synchro-cycrotron
IBA synchro-cycrotron

## Slide 93: Superconducting magnet applications in various accelerators
Lepton colliders
Synchrotron radiation facilities
Proton extraction synchrotron
Medical synchrotron
Cyclotron
Ion source, klystron
Detector magnets

## Slide 94: Small applications ECR Ion source 、Klystron
High intensity ion source
  Focusing superconducting magnet with solenoid and sexstupole magnets
GyroSERSE OPERA-3D model
Berkeley VENUS Ion Source
CERN CLIC Klystron foucusing solenoid

## Slide 95: Superconducting magnet applications in various accelerators
Lepton colliders
Synchrotron radiation facilities
Proton extraction synchrotron
Medical synchrotron
Cyclotron
Ion source, klystron
Detector magnets

## Slide 96: Detector magnets Spectrometer, Thin solenoid, Toroid
Identify particle momentum and charge

## Slide 97: Detector Magnets Spectrometer
RIKEN SAMURAI
J-PARC SKS
KEK BENKEI

## Slide 98: Detector magnet Thin solenoid
Use aluminum stabilized conductor to realize particle transparency

## Slide 99: Detector magnet Thin solenoid
CDF solenoid:
  FNAL TEVATRON

## Slide 100: Detector magnet Thin solenoid
Japanese solenoids
TOPAZ: TRISTAN
VENUS: TRISTAN
BELLE: KEKB

## Slide 101: Detector magnets Thin solenoid
LHC
ATLAS solenoid
CMS solenoid

## Slide 102: Detector magnets Toroid
J-PARC TREC
LHC ATLAS TOROID

## Slide 103: Item
Accelerator & Magnet
Superconducting Accelerator Magnet
Superconductivity
Superconducting Magnets for Hadron Colliders
Superconducting magnet applications in various accelerators
Summary

## Slide 104: Summary
SC Magnet and Accelerator
Developed supplementary
Reached to NbTi limit
Higher Field by Nb3Sn (or IBS?)
  FCC world wide development
HTS (High Temperature Superconductor)
  Still very expensive
  Needs special usage
    High Radiation
    High Filed above 20 T
Game Change = New Chance!
Kamerlingh Onnes
Find Superconductivity
Alvin Tollestrup
TEVATRON Magnet
Who's next
YOU?