## Slide 1
Theory of RF Superconductivity and Thin Film SRF
Teng Tan
2025.3.27
Institute of Modern Physics, CAS
Linac Center

## Slide 2: Introduction of Lecturer
Dr. Teng Tan
Researcher, deputy director of RF surface group
Linac Center, Institute of Modern Physics, CAS
E-mail: ttan@impcas.ac.cn
Involved projects: CiADS, HIAF, IP-SAFE, (possible) EicC
Research and engineering topics: Cavity Post-processing, Thin Film SRF
Layout of IMP Huizhou Accelerator Complex

## Slide 3: Resources of Fundamental Research Reports
《RF Superconductivity》 by Hasan Padamsee
Top meetings: SRF & TTC
Workshops: TFSRF, LCWS, etc.

## Slide 4
··
01
Why SRF fundamentals
02
Some Physics
03
Some SRF Physics
04
SRF Material beyond Nb
Table of Contents

## Slide 5
Why SRF fundamentals
01

## Slide 6: Quick review about yesterday
Material – Cavity – CM – Accelerator
Higher field, higher efficiency
How to obtain better beam output with fixed tunnel length and acceptable cryogenic cost
Hasan Pandamsee, RF Superconductivity for Accelerators

## Slide 7: Quick review about SRF system
How to accelerate with RF power
Nb
Vacuum
Heat
Helium cooling
CM vacuum chamber
Helium jacket
RF input
Cavity
Beam
LHe
Material: Nb
Hc: 240 mT
Tc: 9.2 K
Aperture d
Cryo. system
RF Amplifier
Cryomodule
Rs ~ nΩ, Q0~1×109-10 , Pcavity ~ W
104~5 times better than Cu cavity
SRF benefits:
Extremely high energy efficiency
PRF ≈ Pbeam+ Pcavity
Pbeam/PRF >99% for cw machine
Large aperture d
Large opening for beam halo, reduce beam loss
Low beam-cavity interaction, increase beam quality

## Slide 8: What are the cavities 40 years before
Runs at 4.2 K
Typical Q0: 1~5 × 109.
Typical Eacc: < 10 MV/m
Simple processes
TRISTAN cavity
Takaaki Furuya, SRF’87
P. Brown, EPAC1992
B. Bonin, SRF’93
Saclay 1.5 GHz
LEP 352 MHz
Part of JLAB SRF’89 report

## Slide 9: What are the cavities now
Runs at 2 K
Typical Q0: 4 × 1010.
Typical Eacc: > 20 MV/m
Established processes with inspection, polishing, baking, clean assembly, etc.
Ultra‑high quality factor and ultra‑high accelerating gradient achievements in a 1.3 GHz continuous wave cryomodule Jin‑Fang Chen, NST, 2025
IMP protocol for low beta cavities

## Slide 10: How Does SRF Cavity Behave
Many influence factors in addition to thermal feedback (details see Fesi’s talk later)
Kenji Saito, Lecture note in Tokyo University on May 2011
Limits in cavity performance Detlef Reschke DESY Tutorial, SRF 2007
https://accelconf.web.cern.ch/accelconf/srf2007/TUTORIAL/PDF/Tutorial_3c.pdf
H. Padamsee, "50 years of success for SRF accelerators — a review," Superconductor
science and technology, vol. 30, p. 05003 (23 pp), 2017.

## Slide 11: What do we want from fundamental SRF research
High Performance
High RAMI
Low cost
Impossible without breakthrough in fundamental SRF technology
High G: High energy with fixed tunnel length
High Q0: High energy and low cryogenic cost.
Link processing protocols with cavities properties
Versatile application targets: Science, Medical, Industry

## Slide 12
Some Physics
02

## Slide 13: What is an RF cavity
Static/DC voltage has shortcomings

## Slide 14: What is an RF cavity
RF field: no need for high-V protection
Major drawback: surface dissipation

## Slide 15: RF surface dissipation on normal metal
Skin effect:
lower ω higher ω
j distribution depends on ω
Skin depth
Electrical Conductivity
Permeability
Surface resistance Rs
OFHC copper:
=58 MS/m, μ=1
1.5 GHz：
=1.7 m，Rs=9.9 mΩ
Can we just increase σ of copper?

## Slide 16: Put copper in LHe
Anomalous skin effect:
When MFP l > δ, the relationship breaks
Rs=1/sd
Anomalous skin effect l>δ
Courtesy: G. Ciovati
Surface resistance of Cu at 1.5 GHz as a function of temperature
RRR = (4.2K)/(300K) = 300
Rs(4.2 K)  1.3 mW
…in spite of the resistivity decreasing by a factor 300 from 300 K to 4.2 K, Rs only decreases by a factor of ~8!

## Slide 17: Some brief history of superconductivity
Discovery of SC:
Kamerlingh Onnes liquified He in 1908
May 1911，Hg’s R “disappeared” at 4.2K
D. Van Delft and P. Kes, Physics Today 63, 9, 38 (2010);
-269℃

## Slide 18: Some brief history of superconductivity
1908 Liquefaction of helium (4.2 K)
1911 Zero resistance
1933 Meissner effect
1935 Phenomenological theory of H. & F. London
1950 Ginzburg – Landau theory
1951 – 2 types of superconductors (Abrikosov)
1957 Bardeen – Cooper – Schrieffer microscopic theory
1960 Magnetic flux quantisation
1962 Josephson effect
1986 High temperature superconductors (Bednorz – Müller)
2001 MgB2 (Nagamatsu)
2008 Iron-based SC (Hosono)
2015 H3S at 200K
2020 C-H-S at 300K
Bardeen – Cooper – Schrieffer (BCS)
Abrikosov
Ginzburg
Bednorz
Müller
Landau

## Slide 19: Superconducting materials
Chao Yao, https://doi.org/10.1016/j.isci.2021.102541,
Tens of thousands of kinds
Most of them only in lab
Only LTS have applied to SRF
HTS have applied to RF electronics

## Slide 20: Physics (Courtesy of T. Junginger)
Overview of theories
London Theory
  Based on Maxwell´s equations. Phenomenological theory that can describe zero resistance and the Meissner effect
  Applicable to Type-II superconductors
Ginzburg Landau Theory
  Can describe non-local effects
  Applicable to Type-I and II superconductors
BCS Theory
  First microscopic theory of superconductivity
  Published 46 years after the discovery of superconductivity
H. & F. London
Pippard

## Slide 21: The London Theory
The London Theory is phenomenological and does not involve the essence of superconductivity. The essence of superconductivity needs to be explained from a quantum perspective, namely the BCS theory.
First assume there are 2 kinds of electrons:
Normal electron
Superconducting electron
Normal electrons: classical electrons like in other normal conductors, induce ohmic losses. Drude model for electrical resistance is still valid.
Superconducting electrons: travel and carry current without any losses. Drude model does not valid any more.
Definition of the current density:
ns(T)+nn(T)=n, where n is the total electron volume density
Js
Jn

## Slide 22: The London Theory
Assume an electron which is freely accelerated by an electric field
F
Lorentz force acting on the particle:
J
No voltage, no Jn, use J for the SC current density
E
E=0
0
1st London Equation
The goal is to obtain a differential equation for B
To explain the Meissner effect we want to derive an equation that relates J to B
Maxwell equation:

## Slide 23: The London Theory
0
Maxwell equation
0
2. B(x)
2 possible solutions:
with
London penetration depth
B0
B(x)
Ampere´s law relates the current density J and the magnetic flux density B
Either a constant B field or an exponentially decay field in SC. Can they both exist?

## Slide 24: No, Meissner Effect
2. B(x)
This is not what we observe in superconductors
Consider a conductor which fulfills these solutions when cooled below its critical temperature

## Slide 25: The London Theory
0
2. B(x)
Only exponential decaying fields are observed
To explain the Meissner effect the Londons postulated:
Finally, we have derived the two London equations:
E
Zero Resistance
Meissner Effect

## Slide 26: The London Theory – Pippard extension
Pippard found that λL depends on the purity of the material and therefore on the electron mean free path l
He introduced of the new parameter coherence length ξ in analogy to the anomalous skin effect in normal conductors
Pippard introduced ξ as a phenomenological parameter. Later explained by the microscopic BCS theory
Non-local relation between current density and vector potential:
A.B Pippard - Proceedings of the Royal Society of London. A Vol. 216, No. 1127 (1953)

## Slide 27: The BCS Theory
What needed to be explained?
Zero Resistance and Meissner Effect
Coherence (Non-local relation between current density and E-field)
Energy Gap (exponential specific heat)
  Suggests a Bose-Einstein condensation like process
The isotope effect
  The transition temperature of mercury depends on the isotopic mass
  This suggests that the lattice is important for superconductivity

## Slide 28: The BCS Theory
Pairing of electrons close to the Fermi level into Cooper pairs through interaction with the crystal lattice
  Boson (no Pauli exclusion principle)
  All cooper pairs condense to the same ground state
  Coherent wave functions  no scattering  zero resistance
Size of a cooper pair is large compared to the lattice constant and is related to the coherence length ξ
Estimated size of a cooper pair:
Relaxation time of the lattice: 2π/ωD≈10-13s
Electrons move with vF≈106m/s
Distance between electrons forming a cooper pair:
vF≈10-7m

## Slide 29: The BCS Theory
The superconducting state consists of electron pairs and elementary excitations, quasiparticles, behaving almost like free electrons
The energy gap Δ separates the energy levels of elementary excitations from the ground state level. At 0K only the ground state is occupied
Density of elementary excitations. There are no states within the energy gap Δ
Temperature dependence of Δ:
The gap has its full value Δ0 at 0K and vansishes at TC
BCS theory
GL theory
The BCS theory has been derived from perturbation theory – valid only close to 0 K
Close to TC the Ginzburg-Landau theory is valid

## Slide 30: The Ginzburg-Landau Theory
To provide a phenomenological description of superconductivity near the critical temperature Tc​.
Order parameters with dependance on T
4th order contribute to phase transition. Higher orders contribute very little and can be neglected.
Vitaly Ginzburg was awarded the Nobel Prize in Physics in 2003 for his work on superconductivity, including the development of the Ginzburg-Landau theory.

## Slide 31: The Ginzburg-Landau Theory
A
London equation:
Minimizing gS wrt to Δy and ΔA (variational method) yields the Ginzburg-Landau equations:
Characteristic lengths:
Penetration depth is the length scale for the variation of the magnetic field
Coherence length is the length scale for the variation of the order parameter
Ginzburg-Landau parameter

## Slide 32: The SC-NC boundary
s.c
Vacuum/n.c
Energy loss:
The density of cooper pairs is suppressed over the distance
Energy gain:
Field does not need to be expelled over the distance
z
x
l
y
B
If it is energetically favourable to create normal-superconducting boundaries above the lower critical field Bc1
These superconductors are referred to as type-II
: Energy difference at a NC-SC boundary compared to the SC state
Bc: crtical thermodynamic field, above Bc the normal conducting state is energetically favorable
=0 and resolve wrt B
Exact result from GL theory

## Slide 33: Two types of superconductors
Type II Superconductors
  Impure metals
  Pure niobium
  Alloys
  For >>1 local electrodynamics (London theory) applicable
Type I Superconductors
  All elements except niobium
  Non-local electrodynamics
Type-I
Type-II
SC
NC
SC
Mixed
NC

## Slide 34: Two types of superconductors
Under DC fields flux tubes can be pinned – no dissipation
    SC magnets are operated between Hc1 and Hc2
Under RF fields flux tubes oscillate – dissipation
  RF cavities are operated in the Meissner state
Can the Meissner state persist metastable beyond Hc1?
Cavities
Magnets

## Slide 35
Some SRF Physics
03

## Slide 36: SRF Physics
Surface Resistance of Superconductors
  Two fluid model vs BCS model
  Influencing factors
  Residual surface resistance and flux
Surface Barrier and Superheating field
  Operate SRF beyond Hc1
  Field enhancement for thin film structure
Field emission
  Causes and F-N theory
Overview of SRF theories

## Slide 37: Surface Resistance of Superconductors
Superconducting currents are transported by Cooper pairs formed of two electrons
  flow without friction  DC supercurrents are lossless
For temperatures above 0 K not all electrons form Cooper pairs
Cooper pairs have a finite inertia. Under RF fields a time-varying E-field is induced in the material. Normal electrons see this field, move and dissipate
Rs > 0
+

## Slide 38: From two fluid model
Basic ingredients for RF superconductivity
  Two fluid model (Gorter-Casimir)
  Maxwell electrodynamics
  London equations
Close to 0 K:
electron density
temperature (K)
Tc
n
ns
Basic assumptions of two fluid model
  all free electrons of the superconductor are divided into two groups:
    superconducting electrons of density ns
    normal electrons of density nn
  The total density of the free electrons is
  n = ns + nn
  As the temperature increases from 0 to Tc, the density ns decreases from n to 0.

## Slide 39: From two fluid model
Electrodynamics of sc is the same as nc, only that we have to change s  s1 – i s2
= s2
s
Penetration depth:
s1 << s2 for sc at T<<Tc
Interesting to note here: -We have derived λL from DC arguments before
- Now we find λL does not depend on f for T<<Tc
London equation:
Two fluid model:

## Slide 40: From two fluid model
Hy(x,t)
Ez(x,t)
x
z
y
+i
Electrodynamics of sc is the same as nc, only that we have to change s  s1 – i s2
Recall the definition of the surface impedance:
Ls: kinetic inductance

## Slide 41: From BCS model
Remember: In superconductivity the relation between current and field is non-local. In 1953 Pippard introduced:
One could use this relation to develop a more complete phenomenological model, which would still be dependent on the temperature dependence of ns and nn from the 2-fluid model
Mattis and Bardeen (1958) used time dependent perturbation theory to derive RS for weak RF fields
Within this theory no simple formula can be derived. Several approximate formula can be found in the literature for some limits. For example for the dirty limit
There are numerical codes (Halbritter (1970) to calculate RBCS as a function of w, T and material parameters (x0, lL, Tc, D, l)
For example, http://www.lepp.cornell.edu/~liepe/webpage/researchsrimp.html
/T

## Slide 42: From BCS model
Be carefureful here. The website suggests 40nm. The input required is πξ0/2, while ξ0≈40nm for Nb

## Slide 43: BCS model vs two fluid model
The treatment within BCS theory and two-fluid model give qualitatively similar results
Quantitatively they can differ by an order of magnitude
  The BCS treatment gives qualitatively correct results for low field
To treat experimental data approximate formulae are useful, e.g.
Here A accounts for all material parameters

## Slide 44: Surface Resistance of Superconductors
This equation implies RS:
Has a minimum for medium purity
Is proportional to
Decreases exponentially with temperature
Vanishes as T0 K
Is independent of RF field strength
In the following we will compare these assumptions to experimental data and modify the formula if necessary

## Slide 45: Surface Resistance of Superconductors
The dependence of the penetration depth on l is approximated as
s1  l
if l >> ξ0 (“clean” limit)
if l << ξ0 (“dirty” limit)
Rs has a minimum for l = πξ0/4
C. Benvenuti et al., Physica C 316 (1999) 153.
Nb on Cu,1.5 GHz, 4.2 K
“clean”
“dirty”
Nb films sputtered on Cu
By changing the sputtering species, the mean free path was varied.

## Slide 46: Surface Resistance of Superconductors
This equation implies RS:
Has a minimum for medium purity
Is proportional to
Decreases exponentially with temperature
Vanishes as T0 K
Is independent of RF field strength
In the following we will compare these assumptions to experimental data and modify the formula if necessary

## Slide 47: Surface Resistance of Superconductors
Normal Conducting
Superconducting
400MHz
800MHz
1200MHz
(T)+Rres
Measurement of the surface resistance at low field of niobium at three frequencies with the Quadrupole Resonator
Frequency dependence for RBCS and Rres are almost identical
Is there a common cause?

## Slide 48: Residual Surface Resistance
BCS DOS
Smeared DOS
Rs never goes to 0 when T goes to 0. Some constant value.
Point contact tunneling experiments on Nb and Nb3Sn have found finite density of states (DOS) inside the energy gap
The physics remains not fully understood, however subgap states will yield a finite RS(0K) irrespective of physical mechanism.
A. Gurevich Supercond. Sci. Technol. 30 (2017) 034004

## Slide 49: Residual Surface Resistance
Possible contributions to Rres:
Trapped magnetic flux and thermal currents
Lossy oxides, metallic hydrides
Normal conducting precipitates
Grain Boundaries
Interface Losses
Magnetic Impurities

## Slide 50: Trapped Magnetic Flux
Well understood contribution to Rres
When a cavity is cooled down in an ambient DC magnetic field not all flux is expulsed – Incomplete Meissner effect
In fact fields of a few µT (order earth magnetic field) can be completely trapped
In cryomodules thermal currents can cause additional magnetic fields which can be trapped

## Slide 51: Trapped Magnetic Flux
for RRR=300
H. Padamsee et al. RF Superconductivity for Accelerators
Simple model with these assumptions:
  Fluxoids are perpendicular to the cavity surface, static and RF currents flow through them
  Flux completely trapped
  Losses are independent on RF field
Additional residual resistance=Ratio nc/sc areaNormal conducting surface resistance

## Slide 52: Surface Resistance of Superconductors
This equation implies RS:
Has a minimum for medium purity
Is proportional to
Decreases exponentially with temperature
Vanishes as T0 K
Is independent of RF field strength
In the following we will compare these assumptions to experimental data and modify the formula if necessary
+Rres

## Slide 53: Surface Resistance vs Field

## Slide 54: Surface Resistance of Superconductors
Not only do RBCS and Rres depend on the RF field strength there can also be additional extrinsic losses limiting the cavity performance
+Rres
This equation implies RS:
Has a minimum for medium purity
Is proportional to
Decreases exponentially with temperature
Vanishes as T0 K
Is independent of RF field strength

## Slide 55: Field vs surface
A semi-infinite type-II superconductor placed in a uniform magnetic field H parallel to its surface.
The lower critical field (Hc1) is defined as the critical field under which a type-II superconductor starts to exhibit vortex penetration.

## Slide 56: Field vs surface
Boundary condition of SC surface: Repulsive force for vortex near surface
Bean-Livingston barrier
C. Bean and J. Livingston, Phys. Rev. Lett. 12(1964).

## Slide 57: Field vs surface
For double-side surface: thin film
H < Hc1, vortex is not favorable anywhere.
Hc1 < H < Hs, vortex is energy-favorable inside the film, but is stopped by the surface barrier from entering the film.
H > Hs, surface barrier disappears, vortex enters the thin film without being hindered.
Both Hs and Hc1 are larger than Hc1 for bulk materials calculated from G-L (x<d<l)
G. Stejic, PRB, 49 1247(1994)

## Slide 58: Superheating field
The superheating field Hsh is set by the competition between magnetic pressure (imposed by the external magnetic field), the energy cost to destroy superconductivity, and the attractive force due to the zero-current boundary condition at the interface.
Hc1 is the field where it is energetically favourable for the flux to be in the superconductor
Hsh is the field where the Bean-Livingston barrier for flux entry disappears
Defects can serve as entry points for flux preventing superheating
Suggested further reading:
B. Liarte et al. - Supercond. Sci. Technol. 30 (2017) 033002

## Slide 59: Field emission
Under high RF fields electrons can be released from the surface and accelerated.
Released electrons will impact on the cavity wall creating x-rays and heating  Reduced Q-value
Field emitters found on dissected cavities (size 0.5-10μm with sharp edges)

## Slide 60: Field emission
Bulk Nb ~mm
NbOx ~10nm
Bulk Nb ~mm
Hydrocarbon ~ 1~2nm
NbOx ~10nm
Adsorbed gas, ~monolayer
Particulates
Ideal RF surface
Real RF surface
Fowler－Nordheim

## Slide 61: In-situ processing
MEBT
HEBT
CM1
CM2
CM3
CM4
Reactive plasma cleaning and helium RF power conditioning

## Slide 62
SRF Material beyond Nb
04

## Slide 63: SRF Material beyond Nb
Courtesy A-M VALENTE-FELICIANO, SRF 2023

## Slide 64: Improve directions
Courtesy A-M VALENTE-FELICIANO, SRF 2023

## Slide 65: Improve directions
  Current Nb SRF performances
    Surface impurity manipulation
    Nb thin film for special purpose
    Limit = magnetic transition of the SC material @ Hpeak
  Superconductivity only needed inside
    Thickness ~ < 1 µm => thin films
    Q0 (∝ 1/RS) ∝ TC Eacc ∝ HRF=> Nb3Sn, MgB2, NbN…
    Multilayer structures
    Coated onto a thermally conductive, mechanically resistant material, e.g. Cu
  Cavity structures
    Composite materials
    Heat management of the entire cavity

## Slide 66: Material Selection

## Slide 67: Nb beyond Nb
A. Grassellino et al, 2013 Supercond. Sci. Technol. 26 102001
Doping – infusing - baking

## Slide 68: Nb beyond Nb
SARI
Bunch of reports on TTC2024 and the next TTC

## Slide 69: Nb beyond Nb – LCLS-II
D. Gonnella, TTC2024 ESS

## Slide 70: Nb beyond Nb – IHEP
P. Sha, TTC2024 ESS

## Slide 71: Nb beyond Nb – SARI
Y. Zong, TTC2024 ESS

## Slide 72: Nb/Cu
From 1980s to now
Both composite material and thin film
JAERI
Suehiro Takeuchi, SRF’87

## Slide 73: Nb/Cu
Recent composite materials
HWR Cu/Nb composite cavity
vs. at 4.2 K
The assembled 9 HWR010 Cu/Nb cavities string

## Slide 74: Nb/Cu
LEP magnetron sputtering
Cost-saving and performance improving:

## Slide 75: Nb/Cu
QWR cavities: PKU, INFN & CERN
PKU
HIE-ISOLDE
INFN

## Slide 76: Nb/Cu
Energetic condensation: ECR, cathodic arc, HiPIMS
AVMF, TTC2024 ESS
ECR
HiPIMS

## Slide 77: Q-slope in thin film cavities
From trapped flux to pair breaking

## Slide 78: Nb3Sn – tin vapor diffusion
Resumed in 2013 at Cornell, followed worldwide
WG2, TTC2024 ESS
U Wuppertal results from 1990s

## Slide 79: Nb3Sn – tin vapor diffusion
Single cell cavity

## Slide 80: Nb3Sn – tin vapor diffusion
Dong, TFSRF2024
IHEP progresses

## Slide 81: Nb3Sn LHe-free machine
Technique progress rapidly before 2020
Gradient reached ~20 MV/m
Good for 4K operation and conduction cooled machine
Compact machine idea at 2019

## Slide 82: Nb3Sn LHe-free machine
IHEP: Conduction cooling of 1.3 GHz 1-cell Nb cavity

## Slide 83: Nb3Sn LHe-free machine
Compact machine realized in many spots
IMP, LHe-free e-machine

## Slide 84: Nb3Sn LHe-free machine
CLASSE, single cell 1.3GHz

## Slide 85: Nb3Sn LHe-free machine
Jlab, CEBAF type 2 cavity
First demonstration of >10 MeV Nb3Sn cryomodule

## Slide 86: Nb3Sn other than tin diffusion
In-situ and ex-situ annealing
Bi-Polar HiPIMS
S. Leith, TFSRF2024

## Slide 87: Nb3Sn other than tin diffusion
Bronze route: FNAL, IMP, HZB

## Slide 88: MgB2
HPCVD
K. Chen, X. X. Xi, TFSRF2024

## Slide 89: Iron based
Lin TFSRF2024
FeSe/Nb
Potential for S/S, SIS structure
Miyazaki, TFSRF2024

## Slide 90: Multilayer S-I-S and SS structure
Vortices in RF field ~ oscillate ~ power dissipation
Thin SC film with d ~ l can remain in Meissner state in a much higher B field than bulk material. Enhanced Hc1.
A few layers of SC thin films separated by insulating layers can shield the magnetic field step by step.
A possible way to utilize SC with low Hc1 in SRF cavities.
A. Gurevich, APL 88, 012511 (2006)
Takayuki Kubo, SUST2016

## Slide 91: Multilayer structure

## Slide 92: Thank you
Questions?

## Slide 93: Appendix: how to calculate Rbcs

Since we will deal a lot with the surface resistance Rs in the following, here is a simple DC model that gives a rough idea of what it means:
Consider a square sheet of metal and calculate its resistance to a transverse current flow:
In this model the surface resistance Rs is the resistance that a square piece of conductor opposes to the flow of the currents induced by the RF wave, within a layer 
current
d
a
a
Courtesy: S. Calatroni
Resistance of a square metal sheet of thickness d:
Surface Resistance of a square metal sheet with penetration depth :

## Slide 94: The RF surface resistance (intuitive approach)
Consider an alternating magnetic field at the surface of a semi-infinite superconductor
Consider Faraday's law of induction
(t)=Byexp(i
J,E
B
Vacuum
Superconductor
y
x
Integration area

## Slide 95: The RF surface resistance (intuitive approach)
B(x)
Ez and By are both independent of y
Ohms law:
J,E
B
Vacuum
Superconductor
y
x

## Slide 96: The RF surface resistance (intuitive approach)
electron density
temperature (K)
Tc
n
ns
Close to 0 K:
Definition of the
Surface resistance