## Slide 1: SRF technology - cavity and tuner
Feisi He
Institute of High Energy Physics (IHEP)

## Slide 2: Outline
The electric and magnetic field in SRF cavity
Cavity design
Cavity fabrication
Post processing: why and how
LFD, microphonics, and tuners
Back to beginning: realistic good cavity design

## Slide 3: Example of SRF cavities
SRF cavity is an empty container, with ~2-5mm thick shell made of superconducting Nb, and it has standing wave electric and magnetic field in the vacuum inside the container
Two types of structures are most commonly used:
  TM class (elliptical cavity, for β>0.6)
  TEM class (QWR, HWR, Spoke, for β<0.6)

## Slide 4: Origin of TM class: pillbox cavity
All elliptical cavities are evolved from an enclosed cylindrical waveguide, which is so called pillbox cavity
The 1st mode TM010 is used for beam acceleration

## Slide 5: From pillbox to elliptical cavity
Two openings for beam to enter and exit the cavity are needed; field leaking from the beam pipe has to be small
Beam in&out
Within beam pipe, field decay exponentially:
NC cavity f>3GHz, R<35mm, Rpipe<25mm;
SC cavity f<1.3GHz, R>100mm, Rpipe>39mm

## Slide 6: From pillbox to elliptical cavity (2)
Input antenna to feed RF power in; pick-up antenna to pick control-signal out
Beam in&out
RF power in
Control signal out
Beam in&out
Coaxial line doesn’t have
cut-off frequqncy

## Slide 7: From pillbox to elliptical cavity (3)
Optimized cavity shape to increase Eacc or reducing heat load
Beam in&out
RF power in
Control signal out
Beam in&out
RF power in
Control signal out
Beam in&out

## Slide 8: From pillbox to elliptical cavity (4)
Multiple cells in one cavity to save longitudinal space
RF power in
Control signal out
Beam in&out
RF power in
Control signal out
Beam in&out

## Slide 9: Field in multi-cell cavity
There are N passband modes for a cavity with N accelerating gaps
Capacitive coupling between cells leads to highest frequency as π mode
Flat field means frequency of each accelerating gap is the same
Iris size ↑, cell-cell coupling coefficient k ↑, frequency separation ↑
N2/k<3000 is a reference for tuning not to be too hard
Hasan Padamsee, RF superconductivity for accelerators, P129-133

## Slide 10: Origin of TEM class: Half wave resonator
All TEM cavities are evolved from an enclosed coaxial line
The 1st mode TEM is used for beam acceleration
-L/2 0 L/2
L

## Slide 11: From coaxial line to HWR cavity
If operating at same frequency, TEM cavity is smaller
With similar size or weight that is not too hard to handle, TEM cavity operates at lower frequency, where Rs is much lower too.
Ports for cleaning
L
RF power in
Control signal out
Beam in&out

## Slide 12: From coaxial line to QWR cavity
Quarter wave resonator use even less space than HWR
Typically QWR places Pin&Pt port at B-field zone
Drawback of QWR:
  Mechanically vibration of the inner conductor
  B field on beam axis is not zero, and it kicks beam
L
B-field
E-field
Vibration
A. Facco, low and intermediate β cavity design, tutorial in SRF2009

## Slide 13: From coaxial line to spoke cavity
Inner conductor of ~λ/2 long is rotated by 90 degrees
More accelerating gaps in one cavity is possible
L

## Slide 14: Field in un-driven cavity
Energy decay exponentially in the cavity
Time constant of cavity response period of RF
Decay time is defined as the time for energy decay to 1/e
Pe
Pt
Pc
Hasan Padamsee, RF superconductivity for accelerators, P145-160

## Slide 15: Equivalent circuit model
With quasi-static approximation of a L-R-C circuit is good enough for cavity both at NC and SC
H. Klein, Transmission line basics I, Cern accelerator school 1992
Pin and Pr
Pt
Ibeam
Pc
When exciting a cavity with incident voltage , the cavity voltage is proportional to transmitted voltage :
,
At steady state:

## Slide 16: Equivalent circuit model (2)
At steady state:
H. Klein, Transmission line basics I, Cern accelerator school 1992
Pin and Pr
Pt
Ibeam
Pc
Reflection coefficient , where , ,
Especially on resonance:
, where upper sign is for >1 (over-coupled) , and lower sign for <1 (under-coupled)
Note: a commonly used relative unit for power[db]:
P1/P2[db]=10*lg(P1/P2)
P1/P2=
e.g. P1/P2=2=3[db]; P1/P2=0.5=-3[db]

## Slide 17: Outline
The electric and magnetic field in SRF cavity
Cavity design
Cavity fabrication
Post processing: why and how
LFD, microphonics, and tuners
Back to beginning: realistic good cavity design

## Slide 18: Cavity design considerations
Nikolay Solyak, Lecture 7a in ILC school 2008

## Slide 19
Resonance frequency f
Optimized beta β0
Number of cells or accelerating gaps
Transient time factor:
Cavity effective length:
Epeak / Eacc, Bpeak / Eacc
Geometry factor:
Ra/Q =
Lorentz force detuning coefficient: LFD = df /
Hellium pressure sensitivity df/dP
Beam
dynamics
related
Technics
related
Some important cavity parameters

## Slide 20: Cavity design procedure
Pre-defined frequency, β0, Ngap and beam-pipe size by beam dynamics (may need several interations)
Define optimization goal:
  Ep/Ea, Bp/Ea, G*R/Q, HOM damping, and so on
Sweep cavity shape: Surface field is minimized by distributing field to larger area
  For spoke cavity, base of spoke and end-cover ↔ B field; central part of spoke ↔ E field; Typically Ep/Ea~3.3 or Bp/Ea ~ 7 is achievable for β>0.2
E
B
  For elliptical cavity, E field ↔ iris, B field ↔ equator; Ep/Ea~2 or Bp/Ea~4.2 is achievable for β=1

## Slide 21: Cavity design procedure (2)
Add cleaning and coupling ports, check antenna length and heating on flange.
Mattia Parise, Lessons learned from fabricating and processing PIP-II SRF Cavities in industry, TTC2024

## Slide 22: Cavity design procedure (3)
Check multipacting:
  E-field minimum is associated with local RF potential well, thus attracting electrons and creating conditions favorable of MP
  Electron trajectory with collision energy < 135eV is safe (soft or no MP). You may need to modify the shape of cavity if collision energy > 150eV
Valery D.Shemelin, Multipactor in Accelerating Cavities, 2020

## Slide 23: Cavity design procedure (4)
Mechanical design:
  Change wall thickness, stiffeners, and helium vessel
  Safety analysis: yielding stress, buckling
 | Flange1 | Flange2 | Cav | LHe | ISO | OUT | T
Cav leak check | Free | Free | Vac | 1bar | 1bar | 1bar | RT
HV leak check | Free | Free | 1bar | Vac | 1bar | 1bar | RT
Pre-tuning | Fix | Pull | 1bar | 1bar | 1bar | 1bar | RT
Iso-vacuum | Free | Free | Vac | 1.23-1.9bar | Vac | 1bar | RT
Operation | Fix | Pull | Vac | 1.23bar | Vac | 1bar | 4K

## Slide 24: Cavity design procedure (5)
Mechanical design: Reduce LFD, df/dP, increase intrinsic vibration frequency
  Makes cavity body stronger
  Stiffening ribs to control distortion as needed
  Connect cavity to He vessel (or not) to cancel unwanted distortion
  Cancel df/dP caused by distortion at E/H zone
Remind: be very careful on correct boundary condition setup

## Slide 25: Cavity design tools
Elliptical cavity RF optimization:
  2D free code Superfish. You have to write input files to use it. https://laacg.lanl.gov/laacg/services/download_sf.phtml
  BuildCavity by Paolo Pierini, VB based user dialog to control superfish (need installation): http://wwwsrf.mi.infn.it/Members/pierini/buildcavity/BuildCavity_v143_exe.zip
  Another superfish user dialog by He Feisi (need Mathmatica8.0 or later): https://docs.google.com/file/d/0B7jeOkUDj9HMUHFyUmJMTzhfRG8/edit?usp=sharing
  Fishpact by Wu Genfa, 2D tracking code for MP analysis (with superfish field)
TEM cavity RF optimization and MP analysis:
  Typically CST is used (paid software)
HOM analysis and damping design:
  Typically CST is used (paid software)
Mechanical design and analysis:
  Typically ANSYS or COMSOL are used (both paid software)

## Slide 26: Outline
The electric and magnetic field in SRF cavity
Cavity design
Cavity fabrication
Post processing: why and how
LFD, microphonics, and tuners
Back to beginning: realistic good cavity design

## Slide 27: Fabrication of the cavity
Fabrication process:
  Deep drawing
  Machining
  Frequency control
  Grinding
  Parts cleaning
  EBW
Notes: 端盖+中间环（内导体两半、相邻两片、圆环）；

## Slide 28: Cavity frequency control before EBW
TEM cavity: un-welded parts are stacked to measure frequency; then length of cylinder is trimmed to tune frequency
How to measure frequency accurately:
  Humidity, air pressure and temperature needs to be calibrated to STP (20C, 50%, 1bar)
  No field leakage in the gap: measuring Q0
  Controlled cavity distortion: fitting the frequency at zero torque
  Trimming sensitivity may need to be re-calculated based on measured critical sizes.

## Slide 29: Cavity frequency control (2)
TM cavity: it is not realistic to stack multiple cells together
So frequency of each dumb-bell and end-cell is measured by perturbation method
The equator is trimmed then

## Slide 30: Surface quality control
Before final EBW it is the last chance to get easy access to the cavity inner surface
Defect, e.g. pits in diameter 0.1mm, could be addressed by eye inspection. Sometimes magnifier or very light BCP helps to find defects.
Notes: Normal aluminum oxide wheels (e.g. 3M-02684) works well on Nb cavity grinding

## Slide 31: Cavity EBW
Welding zones are BCP cleaned 5-20um before EBW
Vacuum better than 5e-5mbar before welding starts
K. Saito, RF technology – superconducting RF, ILC school 2009

## Slide 32: Performance limit:
.
P. Michelato, Cavity processing, SRF13 tutorial

## Slide 33: Outline
The electric and magnetic field in SRF cavity
Cavity design
Cavity fabrication
Post processing: why and how
LFD, microphonics, and tuners
Back to beginning: realistic good cavity design

## Slide 34: Performance limit
Quench (local thermal instability)
  material + fabrication (or cleanliness)
Field emission
  Cleanliness of surface treatment, assembly, handling + vacuum
Multipacting
  Cavity shape + rf surface condition
Hydrogen Q-disease
  Chemical surface treatment; stay at 50-120K for several hours
Increased residual surface resistance
  Cleanliness of surface treatment, assembly, handling + vacuum
Q-drop (without field emission) + Q-slope
  May be defect or insufficient etching
P. Michelato, Cavity processing, SRF13 tutorial

## Slide 35: BCP/EP: remove damaged layer

## Slide 36: BCP: Buffered Chemical Polishing

## Slide 37: BCP system
BCP is an exothermic reaction; temperature ↑, etching rate ↑
BCP at >20C increases H2 in Nb; typically at 15-20OC, ~1μm/min
Nb concentration ↑, etching rate↓; typically Nb < 12-15g/L for bulk BCP, <4 g/L for flash BCP (XFEL)
Typical Eacc 25-30MV/m.

## Slide 38: EP: electron polishing

## Slide 41: Comments on BCP and EP

## Slide 43: High baking

## Slide 44: Ultrasonic cleaning and UPW rinsing
Ultra pure water (18 MΩ.cm ) + detergent (like liquinox 1%), @ 45C – 60C, duration about 20-30 min
It removes grease, particulates, residues from former treatments
US power: 10 W/liter
Component MUST be fully immersed, with no air bubbles inside.
NO partial or two step (top and bottom) cleaning accepted!
Rinsing with UPW, continuous flow
Detergent for large production should be changed many times a week (even once / 1 – 2 days)

## Slide 45: HPR

## Slide 46: HPR: how it works
Direct effects of high speed water on particles:
  Particles are removed if the force of the jet and high speed water (especially the droplet) is > adhesion force of particles
Large particle are more easily removed

## Slide 47: Cleanroom
Clean is the key issue for cavity performance
Typically ISO4 (class 10) for cavity HPR and assembly; ISO6-7 (class 103-104) for ultrasonic cleaning.
The largest cause of contamination is personnel

## Slide 48: Key points for clean room operation
Correct items entering procedure, mainly based on the use of WATER rinsing
Well cleaned components subcomponents (flanges, bolts, nuts, gasket, external parts of cavities, valves, etc) using standardized procedure, if applicable, on all components.
Blowing of components to assembled just in time
Precisely defined procedures
Well-trained and motivated personal
Keep duration of actions at open cavity as short as possible

## Slide 49: Outline
The electric and magnetic field in SRF cavity
Cavity design
Cavity fabrication
Post processing: why and how
LFD, microphonics, and tuners
Back to beginning: realistic good cavity design

## Slide 50: Lorentz force detuning
Electromagnetic fields produces pressures that act on the cavity wall, causing the cavity wall to distort
Distortion changes the resonance frequency of the cavity
When LFD is of the order of bandwidth, ponderomotive instability may occue

## Slide 51: Microphonics (vibration)
Noise sources (.e.g. pumps, cryo-system; seismic waves, etc. ) excite cavity vibrations
Any small shift in the cavity frequency requires significant increase in power to maintain Eacc=const, produces phase errors that affect the beam

## Slide 52: Frequency tuners
Oscillations can be excited
  Deterministically (Lorentz Force)
  Non-Deterministically (Microphonics)
Slow Tuner
  Stepper motor changes length of the cavity to bring it to the desired resonance frequency)
  Compensates Static Detuning Forces
  Techniques: mechanical tuner
Fast Tuner
  Compensates Lorentz Force Detuning & Microphonics
  Techniques: Piezoelectric actuators

## Slide 53: Slow tuner: an example
Requirements for Slow Tuner
  Enough tuning Range
  Small hysteresis
  Group delay small
  High Stiffness
  Boring transfer function
  High enough resolution

## Slide 58: Fast tuner: an example

## Slide 59: Outline
Cavity RF design
Cavtity fabrication
Post processing
Performance limit
LFD, microphonics, and tuners
Back to beginning: realistic good cavity design

## Slide 60: Realistic good cavity design
Reducing Ep/Eacc while keeping Bp < 60-70mT at operation
Easy to fabricate (high reproducibility, low risk of failure, no low quality EBW)
Enough access for BCP/EP and HPR

## Slide 61
Thanks for your attention!