## Slide 1
CEPC vacuum chamber production line
Discussion on vacuum chamber with photon absorber
Yongsheng Ma
Vacuum group, IHEP,CAS
Nov 27th 2024

## Slide 2: Outline
CEPC vacuum chamber NEG coating & spraying production line progress
Layout of production line
NEG coating process
Spraying Process
Discussion on vacuum chamber with photon absorber
Changes to vacuum chamber
Changes to BPM, RF shielding bellows
Changes to the layout of vacuum devices
conclusion

## Slide 3: CEPC vacuum chamber production line
项目 | 设计参数
尺寸 | L 11400-d56-D62
重量 | 50~100kg
NEG 薄膜 | 厚度：200nm±30% SEY<1.1 抽速、容量、寿命
加热层 | 厚度<0.5mm 加热温度<300℃
Important nodes and progress
Technical scheme review
Procurement bidding
2024.10
2024.12
Requirement
Due to the difference in length, two production lines will be used to complete the production of vacuum chambers for the CEPC collider. The quantity of NEG coating and spraying facilities for the two lines varies to match the production speed.
With two production lines, the all vacuum chambers of collider will be finished in 5 years.
Advantages
More stable process, less manpower, less NEG coating facility, more adaptive capacity in production, etc.

## Slide 4
  Layout of production line
Kr+
阴极靶内置磁环
CSNS, BEPCII vacuum chambers;
Nb coating;
4
磁环

## Slide 5
NEG镀膜--真空盒装配、NEG镀膜、真空盒拆卸
真空腔体C
阴极靶水冷运动机构
阴极靶
真空盒
真空炉
真空腔体A
分段轨道升降平台
自动拧紧、放铜垫
NEG coating process
结构组成：
铜真空盒NEG镀膜组装体
真空炉：低真空、加热、测控温系统
真空、水冷、充气、电气控制系统等。

## Slide 6: Spraying Process
喷砂、等离子喷涂、
喷砂机器人
热交换器
室外除尘器
清洁、行程区
底层、电阻层、电极喷涂
喷砂间
上料区
绝缘层喷涂
吹扫清洁区
GTV水电控制箱
下料区
喷涂地轨机器人
室外除尘器
GTV电弧电源
GTV-PPC
热交换器
送粉器，控制端

## Slide 7: Prototype of cathode
23000mm(23 meters)
Magnets
Isolating and supporting ring
Magnetron Cathode
~12000mm(12 meters)
Water cooling pipe
dynamic sealing for water pipe
The magnets will be driven by motor when NEG coating
Motor for magnets driven
7

## Slide 8: Prototype of Spraying heating film and tests
Chart: Temperature vs Heating Power
| 0.10608465608465609 | 0.10661375661375663 | 0.16633597883597886 | 0.16865079365079366 | 0.24285714285714285 | 0.24523809523809523 | 0.28759920634920633 | 0.28888888888888892 | 0.3351851851851852 | 0.33703703703703708 | 0.38690476190476192 | 0.38740079365079372 | 0.44232804232804235 | 0.44550264550264551 | 0.50370370370370388 | 0.50595238095238104 | 0.56726190476190474 | 0.57023809523809532 | 0.63584656084656088 | 0.63961640211640214 | 0.70899470899470907 | 0.71230158730158732 | 0.75000000000000011 | 0.78958333333333341
管外温度 | 37.3 | 53.9 | 62.2 | 90 | 91 | 122.4 | 122.7 | 138.2 | 138.9 | 158 | 158.4 | 175.8 | 176.2 | 196.7 | 197 | 215.7 | 217 | 237 | 237.5 | 260 | 260.3 | 279.2 | 279.1 | 299.4
功率面密度W/cm2
管外温度/℃
Dimension: L400*D24 Substrate: copper
Function | Materials | Thichness/um
Transition-layer | MCrAlY alloy | 50~100
Isolation-layer | Al2O3 cermic | ~150
Conductivity-layer | NiCr alloy | ~100~200
Isolation-layer | Al2O3 cermic | ~150
Contactor-layer | Copper | ~50
Reheating test more than 12 times
Adhesion test in ultrasonic resining

## Slide 9: Discussion on vacuum chamber with photon absorber
The round vacuum chamber convert to antechamber;
Absorber will be welded together with vacuum chamber;
Colling pipe is necessary: the total heat load due to the resistive wall for collider single ring is about 2Mw under 50 mw mode; SR reflection from absorber.
The structure of vacuum chamber will be more complex.
NEG coating , spraying heating layer will be more complex.
Changes to vacuum chamber

## Slide 10: Changes to BPM, RF shielding bellows
The round vacuum chamber convert to antechamber
The structure will be more complex.
BPM
RF shielding bellows
The size of magnet needs to be reconsidered

## Slide 11: Changes to the layout of vacuum devices
Dipole magnet n
Dipole magnet n+i
The length of vacuum chamber: 11.5m changes to 5.5m;
The space for absorber needs to be considered;
Absorbers bear high power density synchronous light deposition, requiring good machining and installation accuracy.
The layout of vacuum devices will be more complex.
SR power from dipole magnet | Power density | Area of absorber | Length of absorber
W | W/mm2 | mm2 | mm
4071.01 | 15 | 271.4 | 407.10
The manufacture of absorbers is very challenging.
SR reflection from absorber.
The heating deposits on VC;
Radiation;

## Slide 12: Cost
Vacuum chamber： unit price increase 30%, Approx. 300 million CNY
Photo absorber： approx. 795 million CNY
RF shielding bellow： unit price increase 20~30% due to antechamber, the quantity may also increases (20819 to 38483)due to high accuracy installation of absorber. approx. 200 million CNY
The total cost increases from 3.4 billion to 4.7 billion
unit price | quantity | total price
10000 CNY | / | 10000 CNY
3.0 | 26500 | 79500

## Slide 13: Conclusion
Production line:
Technical scheme review for production line has been finished;
Procurement bidding will be held in Dec.
Absorber
The structure of vacuum chamber will be more complex, bad to NEG coating process;
The structure of BPM, RF shielding bellows will be more complex;
The space for absorber needs to be considered, and requiring good machining and installation accuracy;
The total cost will be increased from 3.4 billion to 4.7 billion

## Slide 14: Photon absorber models
Qi Li

## Slide 15: Photon absorber prototypes
1 GlidCop-AL15 and SS316L flange brazing in a vacuum furnace.
2 GlidCop-AL15 and SS316L flange brazing in a hydrogen furnace.
3 and 4 CuCrZr copper Integrating flange (no brazing).
1
2
3
4
Qi Li

## Slide 16: Photon absorber prototypes
ABS5
ABS4
ABSR
Qi Li

## Slide 17
4. Vacuum chamber geometry, and related issues
Extensive modelling is needed in order to make predictions of the vacuum commissioning duration
Modern tools, based on coupled ray-tracing Montecarlo simulations allow to do this (SYNRAD+, Molflow+)
It’s easy to prove that a NEG-coated VC has a clear advantage in terms of average pressure and commissioning time over a lumped-pump configuration with no NEG-coating; also, the final cost is lower for a NEG-coated configuration, since it allow large savings in term of a largely reduced number of cables for the lumped pumps
FCC-ee Copper Extrusion
CEPC copper chamber (from TDR)

## Slide 18
LEP:
ellipse 131x70 mm2
FCC-ee:
115 mm wide, 70 mm ID
The specific conductance of FCC-ee is ~1/2 that of LEP, ~100:50 l·m/s
The proposed 60 mm ID version for FCC-ee would have a 37% conductance decrease, i.e. only ~1/3 that of LEP
Lead shielding
Antechamber for NEG strip
Pumping slots
5. Arcs and MDI
The arcs and the MDI share some common design for the vacuum system, but at the same time differ in some key aspects
The arcs’ VCs must present as smooth and continuous as possible cross-section, minimizing the changes of cross-section: LEP already had a continuous elliptical chamber (131x70 mm2), common to dipoles and quadrupoles; CEPC plans to have a circular cross section (impedance), while FCC-ee is looking into a modified SUPERKEKB cross-section, with a round pipe (70 or 60 mm ID) with two “winglets” in the plane of the orbit, to be able to install recessed SR absorbers (SRAs)

## Slide 19
Another example: 3D-PRINTED SR ABSORBER, with INTEGRATED COOLING CIRCUIT AND SWIRL TAPE TO IMPROVE HEAT EXCHANGE
FCC-ee

## Slide 20
FCC-ee: Initial geometry of the SR photon absorber, now superseded by 3D-printed one
A
B
175 mm
300 mm
18 mm
A
B
3D-printed SR absorber, with integrated splitting cooling channel (~300 mm long)

## Slide 21
50 m
45.6
80
120
175
182.5