## Slide 1
Quantum Critical Spin-Liquid in Geometrically Frustrated Kagome Lattice Investigated by Muon Spin Relaxation and Neutron Scattering
Devashi Adroja
ISIS Facility
Rutherford Appleton Laboratory
UK
2nd Workshop on Muon Science Technology and Industry
10-11 Jan 2025
CSNS, IHEP, CAS
Notes: Thanks to Profs. Yu Bao, Jie Ma, Yang Li, H. Luo

## Slide 2
Collaborators
R. Tritahi, A.D. Hillier, S. Sharma, S. Langridge, F. Demmel, D. Keen, H. Walker, G. Stenning, F. Pratt, R. Perry (ISIS Facility)
C. Ritter, M. Koza (ILL, Grenoble)
T. Takabatake, C. Yang (Hiroshima University, Japan)
W. Higemoto, T. Ito (ASRC, JAE, J-PARC, Japan)
A. Sundaresan (JNCASR, India), A. Bhattacharyya (RMVERI, India)
Strydom (Johannesburg University, SA)
Qimiao Si (Rice University, USA)
Notes: A. Severing (Cologne)

## Slide 3
Outline
Introduction
Experimental investigations on CeRh1-xPdxSn
    Structural and Physical properties
    Muon spin rotation and relaxation study
Inelastic neutron scattering (INS)
Neutron powder diffraction study
Conclusions

## Slide 5
Introduction: Geometrical Frustrated Lattice
3D Pyrochlore Lattice
A network of corner-sharing tetrahedra
2D Kitaev Honeycomb lattice Quantm Spin liquid
2D Triangular lattice.
Quantum Spin-liquid
2D Kagome lattice
Topological Flat bands and Dirac cone. CDW superconductivity: AV3Sb5 (A = K, Rb, Cs)
1D spin-chain. Quantum fluctuations, Tomonaga-Luttinger liquid. Spin dimerization and Halden gap:
C14H18CuN4O10
Notes: Experimental identification of QSLs
Japanese weave (kago=basket, mé=eye or hole)
Spin ice materials and magnetic monopoles.
he spins fractionalize into Majorana fermions and form a topological quantum spin liquid (QSL) in the ground state. It was soon recognized that a family of complex iridium oxides, as well as ruthenium chloride, with honeycomb structure are magnetic insulators and accommodate essential ingredients of the Kitaev model, due to the interplay of electron correlation and spin-orbit coupling. This initiated a race to materialize the Kitaev QSL and to capture the signature of Majorana fermions
a A ground-state configuration for collinear spin order when the nearest-neighbour couplings are antiferromagnetic. This ground state is highly degenerate, but lattice distortion may stabilise one configuration. Four antiferromagnetic couplings are satisfied in each tetrahedron and two are frustrated as indicated by ‘sad face’ symbols; this construct is useful for the more complex frustrated configurations shown in Fig. 4. b Non-collinear spin order for situation (a) can give rise to the ‘all-in all-out’ configuration, where all magnetic moments point towards or away from the centre of each B-site tetrahedron, preserving cubic symmetry and with each antiferromagnetic coupling partly frustrated. c Strong dipolar interactions can lead to a related ‘2-in 2-out’ spin ice order, with two spins pointing in and two pointing out of each tetrahedron when spin–spin couplings are weakly ferromagnetic. This is also shown as one of the magnetic phases for γ-Fe2SiO4 in Fig. 5
Monopole 3-in and 1 out
Kagome lattice materials have fascinated scientists for a long time because they provide a window into quantum phenomena such as geometrical frustration, topology, and strong correlations.

## Slide 6
Introduction: Frustration in the Kondo lattice
Phase diagram of the geometrically frustrated Kondo lattice
P. Coleman et al. 2010 J. Low Temp. Phys. 161 182
Kagome lattice
Shastry-Sutherland lattice
CePdAl and YbAgGe
Ce2Pd2Sn and Yb2Pd2Pb
J2
Kondo strength
Frustration
Coleman & Schofield (2005)
Notes: In Ce2.15Pf1.95Sn1-yIny SSL phase exist at x=0 between 4.5 K and 2.2 K

## Slide 7
Magnetic structure of c plane
3D Magnetic structure of CePdAl
Ce ions form an equilateral triangles in the c plane.
2/3 of Ce moments participate in the AFM long-range order
1/3 of Ce moments are disordered below TN = 2.7 K,
Partially geometrically frustrated CePdAl with quasi-kagome lattice
A. Dönni et al. 1996 J. Phys.: Condens. Matter 8 11213
V. Fritsch et al. 2014 Phys. Rev. B 89 054416
Hexagonal ZrNiAl-type structure
Localized
moment
μCe= 1.6 μB // c
TN= 2.7 K
How about frustration effects in isostructural Ce compounds?

## Slide 8
 | a (Å) | c (Å) | - P(K) TK(K)
CeRhSn | 7.443 | 4.089 | ~400 240
CeIrSn | 7.438 | 4.076 | ~300 480
CePdAl | 7.217 | 4.231 | TN=2.7 6
Y. Bando, TT. et al.,
JALCOM. 313,
1 (2000).
TSm
Rh
Ir
High TK  No magnetic order occurs.
For CeRhSn polycrystal, NFL behaviors in c(T) and C/T  T -n (n~0.5) for 1.5 < T < 5 K. A. Ślebarski et al., Phil. Mag. 82, 943 (2002).
Rh
Ir
B. Chevalier et al., Solid State Sci. 8, 1000 (2006).
Thermopower of polycrystals
Inverse (T) for polycrystals
TK(K) = 1.6TSm
CeRhSn and CeIrSn in the valence fluctuation regime
Undistorted kagome lattice for comparison
Notes: We have focused on CeRhSn and CeIrSn possessing a similar quasi-kagome lattice as in CePdAl. The inverse magnetic susceptibility has a large and negative paramagnetic Curie temperature, approximately -300 to -400 K. The thermopower has a broad maximum. These two properties are characteristics of Ce compounds in the valence fluctuating regime. If we estimate the Kondo temperature TK as 1.6 times of the maximum temperature, then TK of 480 K for CeIrSn is twice higher than that for CeRhSn. Because of the high TK, no magnetic order occurs. For CeRhSn polycrystal, NFL behaviors in chai and specific heat were first reported by Slebarski.

## Slide 9
Non Fermi liquid behaviors in CeRhSn,
Magnetic susceptibility
Electrical resistivity
Specific heat
C/T ∝ln T and shows saturation below 0.7 K
not consistent with the
NFL behaviors in r and c
.
Quantum criticality in Quasi-Kagome CeRhSn
χ(T) shows a power-law
behavior T –n (n =1.1, B // c).
ρ(T) decreases with T n(n ≤ 1.5)
M. S. Kim et al. 2003 Phys. Rev. B 68 054416
Notes: CeRhSn single crystal exhibits strongly anisotropic resistivity and magnetic susceptibility. The resistivity is lager along the a axis, and exhibits a broad maximum at 70 K. At low temperatures, the power of T is 1.5 and 1.0.
The susceptibility exhibits an Ising behavior along the c axis and diverges like this. However, the specific heat divided by T becomes constant on cooling to 0.5K, not consistent with the NFL behaviors in rho and chai.

## Slide 10
Zero-field quantum criticality in CeRhSn
C/T : under 2 T, below 0.5 K,
NFL to FL.
A zero-field QCP
C/T diverges, T 0
Y. Tokiwa et al. 2015 Sci. Adv. 1 e1500001
Magnetic Grüneisen ratio
ГH : diverges below 1 K,
saturation under B // c = 0.25 T
A zero-field QCP
Uniaxial thermal expansion
coefficient αa/T diverges
quantum criticality driven by
geometrical frustration in the
c-plane
Quasi-kagome plane
Ce
a
c
Notes: The black dotted line indicates a power-law divergence) and H provide evidence for a zero-field QCP.
The anisotropy of linear thermal expansion coefficient: which only displays quantum critical behavior along the a axis and not along the c axis  geometrical frustration drives quantum criticality in this system

## Slide 11
Structural and Physical properties of CeRh1-xPdxSn

## Slide 12
The structure switches to the orthorhombic TiNiSi-type for x > 0.8.
Structural property of CeRh1-xPdxSn
The results of EPMA are consistent with the nominal composition for x ≤ 0.5.
With increasing x, the quantity of impurity phase Ce(Rh1-XPdX)2Sn2 increased.
The real compositions of x in CeRh1-xPdxSn phase were 0.65 and 0.75 for
X = 0.7 and 0.8, respectively.
c-f hybridization
Kondo screening
Doping with Rh for Pd
AFM order would be induced
4d-electron number
c axis parameter
Electron doping effect

## Slide 13
Magnetic susceptibility (T) of CeRh1-xPdxSn
C. L. Yang et al, Phys. Rev. B 96, 045139 (2017)
Notes: TABLE I. Parameters obtained by the fits with the modified Curie-Weiss form χ = C/(T − θp) + χ0 to the averaged magnetic susceptibility data {χ(B ) + 2χ(B⊥)}/3 at T > 100 K, where χ(B ) and χ(B⊥) were measured, respectively, in external fields of 1 T applied parallel and perpendicular to the samples of CeRh1−xPdxSn preferentially oriented along the c axis. μeff, θp, and χ0 are the effective magnetic moment, paramagnetic Curie temperature, and temperature independent term, respectively

## Slide 14
Heaty capacity of CeRh1-xPdxSn
C. L. Yang et al, Phys. Rev. B 96, 045139 (2017)
R. Tripathi et al, Phys. Rev. B 106, 064436 (2022)
A linear increase in magnetic specific heat is expected at low temperatures in a gapless QSL
Single crystal
Polycrystalline
x = xc = 0.1: C/T ∝ -ln T;
Δρ ∝ T (NFL)
X > Xc=0.1 I AFM
A. Schröder, H. v. Löhneysen
Notes: We can therefore anticipate that the broad peak in the specific heat arises from short-range magnetic correlations, reflecting the fact that the system is close to a magnetic QCP. On the other hand, in a gapless QSL, a linear increase in magnetic specific heat is expected at low temperatures [45]

## Slide 15
Heaty capacity and ac(T) of CeRh0.9Pd0.1Sn
R. Tripathi et al, Phys. Rev. B B 106, 064436 (2022)
Single crystal x=0.1
Single crystal x=0.1
Frequency independent peak for H// c
This confirms that the x=0.1 single crystal does not have a spin-glass transition.
Notes: Tmax increases linearly with increasing the field parallel and perpendicular to the c-axis.
This suggests Zeeman splitting of the Ce ground state doublet, where at zero field, the splitting could arise from the fluctuating internal field due to short-range order.

## Slide 16
Muon spin rotation and relaxation (SR) study on CeRh0.9Pd0.1Sn single crystals
R. Tripathi et al, Phys. Rev. B 106, 064436 (2022)
 || c-axis
  c-axis
Single crystals CeRh1-xPdxSn (x = 0.1) were grown by the Czochralski method in an RF induction furnace with an argon gas atmosphere.
Notes: magnetic moment 3.2 x proton
Decay into positron,  ~ 2.2 s

## Slide 17
ZF-SR study on CeRh0.9Pd0.1Sn single crystals
2D frustrated QSL,  can be described by a power-law, (T) ∝ T−w
R. Tripathi et al, Phys. Rev. B 106, 064436 (2022)
MuSR@ISIS
// c
 c
CeRhSn ZF, A. SCHENCK et al (2004)
t (µs)
Y. Li et al, PRL 117, 097201 (2016)
Notes: Abg=0.117
Region I- λ hardly dependent on temperature  the system is close to its paramagnetic limit.
Region II- Crossover- λ increases steeply with the decrease of temperature evidence for a slowing down of the spin dynamics, likely resulting from the building up of short-range correlations.
Region III- λ(T) levels off slow changes with temperature without a critical slowing down of the electronic spin fluctuations.
This constant low-temperature behavior of λ is an universal characteristic of several SL candidates.

## Slide 18
LF-SR study on CeRh0.9Pd0.1Sn single crystals
Analysis of field dependent 
Redfield equation
Power-law behaviour for LF
Asymmetry
τ is spin auto-corelation time
Fluctuation rate υ = 1/τ
T = 0.1 K τ = 30 ns
υ = 33. MHz
// C
 C
Notes: The LF-µSR results suggest that the out of kagome plane spin fluctuations are responsible for the SL behavior.
For S = 1/2 V-based Kagome SL T=0.02 K
υ = 470 MHz
J. C. Orain et al
JPCM:cs551 012004 (2014)

## Slide 19
ZF-SR study on CeRh1-xPdxSn x=0.2 & 0.5 polycrystals
SL behaviour is observed in x=0.2
While long range magnetic ordering is observed in x=0.5
D1 spectrometer

## Slide 20
Inelastic Neutron Scattering Investigations on CeRh1-xPdXSn
Low energy measurements were carried on IN6 at ILL
High energy measurements were carried out on MERLIN at ISIS Facility

## Slide 21
Low energy INS study on Ce(Rh1-xPdx)Sn (x = 0.1)
Continuous gapless excitations U(1) SL
The low energy inelastic neutron measurements on the powder sample of CeRh0.9Pd0.1Sn do reveal the presence of gapless magnetic excitations, as found in U(1) SL. The low energy INS measurement on the large single crystals are highly essential to further shed light on the nature of the SL ground state for x = 0.1.
R. Tripathi et al, Phys. Rev. B B 106, 064436 (2022)

## Slide 22
Low energy INS study on CeRh1-xPdXSn
IN6 at ILL
X=0.1
X=0.2
A very similar scaling behaviour has also been observed in other non Fermi liquid systems such as
UCu5-xPdx (=0.33), CeRh0.8Pd0.2Sb (=0.77), Ce0.7Th0.3RhSb (=0.33) and CePd0.15Rh0.85 (=0.6), CeCu6-xAux (=0.75) by M. C. Aronson et al., (1995), J.-G. Park et al., (2002), J. So et al., (2002), D. T. Adroja et al., (2007), A. Schröder et al., (1998), respectively.

## Slide 23
Neutron diffraction study on CeRh0.25Pd0.75Sn
D20 at ILL and GEM at ISIS Facility
K1= (0 0 0.4)
K1= (0 0 0.4)
K2= (0 0 0.5)
K1= (0 0 0.4)
K2= (0 0 0.5)
T=1.5 K/2 K
There exist three allowed irreducible representations (IREPS),
Γ11 , Γ21 , Γ32, having respectively 1, 2 and 6 basis vectors (BV)
1.5 K/2K data fit better with Γ21
ord= 1.22 (1) µB/Ce-atom
T= 0.5 K
Two magnetic phases refinment
K1= (0 0 0.4) 76% and K2= (0 0 0.5) 24%
Symmetry analysis of K2 gives five IREPS:
Γ11 + Γ21 + Γ32+ Γ42+ Γ52,
with respectively 1, 1, 1, 4, and 2 BVs. Γ21 give the best fit
ord= 1.37 (1) µB/Ce-atom with assumption the same moment value of Ce in both bases.
K1= (0 0 0.4)
V. Fritsch et al (2016)
CePdAl

## Slide 24
Neutron diffraction study on CeRh0.5Pd0.5Sn
0.06 K
0.45 K
0.85 K
1.3 K
CeRh0.5Pd0.5Sn
Diff=0.06 K -1.3 K

## Slide 25
Conclusions
The ZF-µSR relaxation rate suggests the presence of dynamic spin fluctuations persisting even at T = 0.05 K without static magnetic order in the single crystal sample with x = 0.1.
The ground state of x = 0.1 (namely, a constant λ and a linear T-dependence in C4f) can be attributed to a metallic spin-liquid near the quantum critical point (QCP) in the frustrated Kondo lattice
The LF-µSR results of the single crystal samples of x = 0.1 with the muon beam along and perpendicular to the c-axis suggest that the out of kagome plane spin fluctuations are responsible for the SL behaviour
Low energy INS study in x = 0.1 and 0.2 indicates gapless excitations, a typical behaviour observed for the NFL systems near QCP where the neutron dynamical susceptibility exhibits E/T scaling
ND reveals incommensurate longitudinal spin density wave ground state with Ce moment along the
c-axis below 4 K in x = 0.75 sample and no presence of magnetic frustration.
In x=0.5 we have observed the magnetic diffuse scattering at 0.06 K.
Notes: Our high energy INS shows a very weak and broad scattering in x = 0 and 0.1, which transforms into well-localized CEF excitations with increasing x.

## Slide 26
Thank you very much for your attention

## Slide 27
High energy INS study on CeRh1-xPdXSn
MERLIN at ISIS
CeRh1-xPdXSn
The solid black lines show the fit to the
Lorentzian functions.
CEF analysis
CeRh1-xPdXSn x=0.5
Ce point symmetry is C2v
B20 = – 1.01, B22 = 0.244, B40 = – 0.017,
B42 = – 0.222 and B44 = 0.159 (meV)

## Slide 28
(1/3, 2/3 0)
Muon site from dipolar dipolar coupling
A. SCHENCK et al,
Journal of the Physical Society of Japan
73, 3099 (2004)

## Slide 30
Data of RERhSn, R. Mishra et al., Z. Naturforsch. 56b, 589 (2001).
M.S. Kim , PhD Thesis,
(2003) Hiroshima Univ.
Ce
Rh/Ir2-Sn
c-axis contraction in CeTSn by c-f hybridization
Notes: You see here that the lattice parameters of CeRhSn and CeIrSn are smaller than that expected from the series of trivalent rare-earth compounds. The remarkable shrinkage along the c axis indicates strong hybridization of the Ce 4f sate with the 4d electrons of Rh2 or 5d electrons of Ir2 in the neighboring layers, not in the same layer.

## Slide 31
Harwell Science & Innovation Campus
ISIS – Neutrons and Muons
Diamond –X Rays
Neutrons
X-Rays
Rutherford Appleton Laboratory
Harwell Science and Innovation Campus
Diamond
ISIS
TS2
TS1
Neutrons
Muons
Notes: Total 28 instruments on TS-1
Total 13 instruments on TS-2

## Slide 32
Quantitative investigation of the Kondo interaction in CeRh1-xPdxSn
The experimental data have been compared to simulations of the spectra using calculations including full multiplet (fm) and configuration interaction (CI) using theXTLS9.0 code by A Tanaka For the CI part we use the simplified model by Imer et al. where the valence states are represented by only one ligand stat.
Martin Sundermann and Andrea Severing
O. Niehaus et al Z. Natur forschung B 70, 253264 (2015)
Notes: FIG.3. (Coloronline)(a)Ce3dcore-levelHAXPESdataof CeRh1 xPdxSnwithx=0,0.1,0.3,0.5,0.75. atT=60Kaf ternormalizationtotheintegratedintensitybeforesubtract inganintegratedbackground(BG)(dashedblackline),plas mons(solidblackline),andtheSn3semissionintensity(cyan line).BGandplasmonsarespecimenofthe30%Pdanalysis. (b)Ce3demission linesafter subtractionofBG, plasmons, andSn3s.Theredrulerindexesthecontributing4fcon gu rations,f0,f1,andf2. Insets: enlargedregionsoff0andf2 emission. (c)Resultsof the fmCI simulations for theCe3d emissionusingtheCIparametersaslistedinTableI.

## Slide 36
LF(s-1)

## Slide 37
Resistivity (T)
CeRhSn single crystal: Anisotropic r(T) and c(T)
a(T): maximum at 70 K
a(T)/c(T)  3~5
r  T n, n = 1.5 (ӀӀ a), 1.0 (ӀӀ c)
Susceptibility (T)
Mo-Sung. Kim , TT. et al., PRB 68, 054416, (2003).
c / a  10 at T < 2 K
c  T −n
n = 0.35 (B ӀӀ a), 1.1 (B ӀӀ c)
10倍
T −0.35
T −1.1
Specific heat C/T
C/T  constant as T  0.5 K.
not consistent with the
NFL behaviors in r and c
Notes: CeRhSn single crystal exhibits strongly anisotropic resistivity and magnetic susceptibility. The resistivity is lager along the a axis, and exhibits a broad maximum at 70 K. At low temperatures, the power of T is 1.5 and 1.0.
The susceptibility exhibits an Ising behavior along the c axis and diverges like this. However, the specific heat divided by T becomes constant on cooling to 0.5K, not consistent with the NFL behaviors in rho and chai.

## Slide 38
J. Wein et al, npj Quantum Materials volume 4, Article number: 12 (2019)
Introduction: Experimental identification of QSLs
a
b
c
d
Notes: In addition to 1D system with competing NN and NNN interactions

## Slide 39
J2
Magnetic frustration in metallic systems
Three spins can not be all anti-parallel
Kagome lattice
Triangular lattice
Shastry-Sutherland lattice
J'
J'
J
When J1 / J2 is large enough, AFM order is destroyed
Two-dimensional spin lattice
Competing magnetic interactions among localized moments can not be simultaneously satisfied.
Magnetic frustration with spin fluctuations
P. Coleman et al. J. Low Temp. Phys. 161 182 (2010)
Three-dimensional pyrochlore lattice
FM interaction is frustrated due to
different Ising axes of spins
L. Balents, Nature (London) 464, 199 (2010).
Notes: Magnetic frustration in metallic systems has been less studied compared with insulating systems. The frustration has a geometrical origin. Well known systems are the triangular lattice, Kagome lattice, Shastry Sutherland lattice, and pyrochlore lattice. In a kagome lattice, for example, the nearest neighbor AFM interaction J1 competes with the next nearest neighbor FM coupling J2. When the ratio J1 over J2 is large enough, the AFM order is destroyed.
In these lattices, competing magnetic interactions among localized moments can’t be simultaneously satisfied. So it leads to magnetic frustration with spin fluctuations.