## Slide 1: Searching for Broken Symmetries in Superconductors with Muons
Graeme Luke
Dept. of Physics & Astronomy
McMaster University

## Slide 2: Quantum Materials
Materials whose essential properties go beyond semi-classical particles.
Collective properties governed by fully quantum behaviour
Strong electronic correlations, often resulting in some kind of order such as magnetic, superconducting, topological…
Fundamental degrees of freedom: charge, spin, orbit and lattice become intertwined.
Emergence of novel excitations/quasiparticles/behaviour.

## Slide 3: Quantum Spin Systems
Role of quantum fluctuations in Quantum spin systems (eg. spin 1/2).
  Neel state not an eigenstate of Heisenberg Hamiltonian.
  increasingly bad for low-d, low spin.
Quantum spin liquid: originally suggested by Anderson for 2-D spin 1/2 -RVB.
Spin liquid, Quantum spin liquid states
Emergent excitations include monopoles, spinons, holons.
Balents, Nature 464, 199 (2010).

## Slide 4
No periodic arrangements of moments which can simultaneously minimize energy.
Can have large number of classically degenerate ground states.
Leads to competing low temperature phases and enhanced quantum mechanical spin dynamics.
Possible emergent phenomena, quasiparticles.
Geometrical Frustration

## Slide 5
Lattices Promoting Geometrical Frustration
Pyrochlore
Stacked Triangular
Kagome
Shastry-Sutherland J1-J2

## Slide 6
Superconductivity

## Slide 7
Superconductivity

## Slide 8: Superconductivity in Elements and Compounds
Blundell
Wikipedia

## Slide 9: Unconventional Superconductivity
Conventional
Δ(k) has symmetry of crystal
Usually Δ(k)=Δ (s-wave)
Unconventional
Δ(k) has lower symmetry
Possible nodes in gap.
Other broken symmetries
Ding et al., PRB 54, 9678 (1996)
Bi-2212

## Slide 10: Pairing Symmetry – Penetration Depth
𝜆(0) from 𝜇SR measurements

## Slide 11: Unconventional Superconductivity
Trappmann, Lohneysen, and Taillefer, (1991)
Adenwalla et al., (1990)
Trappmann, Lohneysen, and Taillefer, (1992)
Luke et al., PRL 72, 1466 (1993).
Multiple SC phases vs. B, P
ultrasound

## Slide 12: Routes to Unconventional Superconductivity
Conventional SC (BCS): electron phonon interaction overcomes Coulomb repulsion via retardation.
Strongly correlated metals, electrons retain more localized character (Coulomb > electron-phonon): retardation less effective.
  Other interactions (eg. spin fluctuations)
  Superconductivity near magnetic quantum critical point.
Role of crystal structure, such as presence/absence of inversion symmetry.
  ASOC gives mixture of spin-singlet/spin-triplet pairs, with possibility of broken TRS, gap nodes, multiple gaps.
Topologically non-trivial bands hosting SC.

## Slide 14: Pion → Muon → e+
p+m++nm (26ns)
m+e++ne+nm (2.2ms)
<a> = 1/3

## Slide 15: μSR Technique

## Slide 16: TRIUMF

## Slide 18: Experimental Geometry
τμ=2.2μs

## Slide 19
Zero Field ZF-μSR
Ordered state, ν∝ Moment ∝
Random frozen spins give characteristic relaxation.

## Slide 20
Spin Fluctuations - Dynamics
Longitudinal Field µSR

## Slide 21
Transverse Field µSR
Amplitude: volume fraction of signal.
Frequency: local field at muon site(s): Knight shift
  Field of 8T gives 1GHz precession
  Max field of ~0.2T at pulsed facility due to pulse width, pion lifetime.
Damping: Field inhomogeneity: line shape gives field distribution.

## Slide 22
Quantum Spin Liquid Ground State in Shastry-Sutherland Lattice Material: Yb2Be2GeO7

## Slide 23
Quantum Spin Liquid Ground State in Yb2Be2GeO7
Magnetic Susceptibility
Heat Capacity

## Slide 24
Muon Spin Relaxation in Yb2Be2GeO7
No precession seen at any temperatures
Increasing relaxation with decreasing temperature
  depopulating crystal field levels
  slowing down of spin fluctuations.
Relaxation essentially plateaued below 10K.
At low temperature, LF relaxation rate increases with increasing field indicating increased low frequency spin fluctuations present.
Closing of gap with field above 0.2T.
Yb2Be2GeO7 is a gapped quantum spin liquid candidate
Pula et al., Phys. Rev. B 110, 014412 (2024). (2 days ago!)

## Slide 25: Length Scales in Superconductivity
Penetration Depth & Coherence Length
: length scale for field screening
: variation of SC order parameter
  size of Cooper pair
  size of vortex core

## Slide 26: Type-II Superconductors: Vortex State
2 lengthscales: λ, ξ
Disorder: broadening of line shape features (convolute with Gaussian).
Ceramics - Gaussian
Sonier, Rep. Prog. Phys. 70, 1717 (2007).
J.C. Davis website

## Slide 27: Vortex Lattice Field Distribution
Yaouanc et al., Phys. Rev. B 55, 11107 (1997).
V3Si

## Slide 28: Superfluid density & Vortex Core Size
Curve is ZF μ-wave result. (Hardy et al.)
Linear T-dependence due to d-wave pairing (gap nodes)
High field flattening due to q.p.’s at gap nodes.
Weak dependence of 𝝃 on T indicates absence of bound states in vortex cores.
Sonier et al.

## Slide 29: Spin Orbit Coupling w/o Inversion Symmetry
TaReSi & TaRuSi
Re/Ru
Si
Ta
Sajilesh K P and R.P. Singh, Supercond. Sci. Technol. 34, 055003 (2021).

## Slide 30: Transverse Field SR
Sharma et al., PRB 108, 144510 (2023).
SOC

## Slide 31: Zero Field SR
SOC
Broken TRS in TaRuSi
Conserved TRS in TaReSi
C point group: Broken TRS only with weak SOC
Sharma et al., PRB 108, 144510 (2023).
Quintanilla et al., Phys. Rev. B 82, 174511 (2010)

## Slide 32: Role of Spin Orbit Coupling
DFT (Addison Richards & Erik Sorensen)
TaReSi
TaRuSi
SOC

## Slide 33: Broken TRS in
Hillier, Quintanilla and Cywinski, PRL 102, 117007 (2009).
[ unitary: ]

## Slide 34: Non-Unitary Triplet Pairing in TaRuSi with weak SOC
Isostructural SC’s w/o inversion symmetry
ZF-SR shows broken TRS in TaRuSi, conserved TRS in TaReSi
TF-SR shows isotropic s-wave (conventional) SC in TaReSi
TF-SR shows multi-gap SC in TaRuSi
DFT indicates weak SOC in TaRuSi, strong SOC in TaReSi
Symmetry analysis attributes SC state in TaRuSi to non-unitary triplet pairing state.

## Slide 35: Topological Superconductivity
Majorana Fermions
Normal fermions can be represented as composed of two Majorana fermions (which are their own anti-particles).
Interest comes if Majoranas can be spatially separated, independently probed.
  immune to decoherence
  Possible application to quantum computation.
Exist in vortex cores of chiral superconductors (eg. ): Sr2RuO4?
predicted in vortex cores of topological surface state coupled to bulk s-wave superconductor (Fu & Kane, PRL 100, 096407).
M. Franz, Nature Nanotech. 8, 149 (2013)
Mourik et al., Science 336, 1003 (2012).
Luke et al., Nature 394, 156 (1998).

## Slide 36: Topological Superconductivity?
Hexagonal crystal structure
Hexagonal structure: Dirac cones, flat bands.
BiPt : Superconductivity reported in 1952 (Alekseevskii), 1953 (Matthias).
  only Tc reported (around 1.2K-1.3K)
Cao et al., Nature 595, 526 (2021)
Twisted tri-layer Graphene

## Slide 37
BiPt

## Slide 38
BiPt
Anisotropic (Abrikosov) Lineshape
Anisotropic superfluid density

## Slide 39
BiPt1-xPdx DFT
BiPt1-xPdx changes from topologically trivial to non-trivial around x=0.75.
hexagonal BiPd not stabilized in bulk, but predict Dirac crossing at Fermi level for surface state.
Sharma et al., Phys. Rev. B 109, 224509 (2024)

## Slide 40
BiPt1-xPdx
Hexagonal crystal structure
  predicted to exhibit Dirac band crossings, flat bands which potentially support topologically non-trivial behaviour.

## Slide 41
BiPt0.5Pd0.5 Muon Spin Rotation/Relaxation
Sharma et al., Phys. Rev. B 109, 224509 (2024)
BiPt0.5Pd0.5 fully gapped with preserved time reversal symmetry.
Next steps, proceed to higher Pd substitution levels.

## Slide 42
Current Muon Sources
New sources under development in China, Korea.
3 Sources co-located with neutron sources

## Slide 43
Current CW Muon Sources

## Slide 44
Current Pulsed Muon Sources

## Slide 45: Low Energy Muons - PSI
Conventional surface muons have stopping range of 140 mg/cm2
Thin film samples/surfaces require reduced depth penetration.

## Slide 46: Muon Moderation

## Slide 47: Low Energy Transport

## Slide 48: Muon Trigger

## Slide 49: Low Energy uSR- PSI

## Slide 50: Unconventional Superconductivity
Synthesis, Characterization & Identification
Multiple routes to unconventional superconductivity
Strong correlations, cooperative crystal structure critical.
Muons provide a real space/volume sensitive probe.
Thanks for your attention!

## Slide 51
Coming Soon: TRIUMF M9H
First muon decay channel explicitly designed for delivery of transversely spin polarized beams.
4T 6 port magnet with DR,SiPM spectrometer
High energy decay muons (µ+/µ-), suitable for pressure cells, muonic x-rays for elemental analysis.