## Slide 1: Superconductivity research using muons:
Rhea Stewart, ISIS Muon Group
2nd Workshop on Muon SciEnce TechnoLOgy and InDustrY
CSNS, Dongguan, January 9th – 12th 2025
rhea.stewart@stfc.ac.uk

## Slide 2: Superconductivity research using muons: characterising spin-orbit driven proximity effects in Pt/Nb thin films
Rhea Stewart, ISIS Muon Group
2nd Workshop on Muon SciEnce TechnoLOgy and InDustrY
CSNS, Dongguan, January 9th – 12th 2025
rhea.stewart@stfc.ac.uk

## Slide 3: Central theme of this work
Focus: manipulating the superconductivity in a conventional superconducting thin film using magnetic and high spin-orbit materials and measuring these effects with muons.
Superconducting proximity effects and why they are interesting
Using low energy muons (LEM) to characterise magnetic and superconducting effects at interfaces
A summary of LEM results on ferromagnetic-superconducting proximity effects in Nb thin films
The motivation for moving from ferromagnetism to spin-orbit control of the superconductivity
Results and the development of new theory for spin-orbit driven proximity effects in Pt/Nb thin films
Flokstra, M., Stewart, R., Yim, CM. et al. Spin-orbit driven superconducting proximity effects in Pt/Nb thin films. Nat Commun 14, 5081 (2023)
(and other references as indicated)

## Slide 4
Acknowledgements & contributions
Machiel Flokstra & Steve Lee
Christopher Trainer, Chi Ming Yim & Peter Wahl – STM results to complement MUSR
Nathan Satchell & Gavin Burnell, Sample growth and development
Andreas Suter, Thomas Prokscha & Elvezio Morenzoni Low energy muon instrument scientists
Jos Cooper, Christy Kinane, Nathan Satchell & Sean Langridge PNR measurements on structural and magnetic properties of S/F systems.
Irina Bobkova & Alexander Bobkov Development of quasiclassical theory on high spin-orbit – superconductor interfaces that was key to interpreting the muon data

## Slide 5: Proximity Systems
L1
L2
Symmetry(-ies) broken
Novel effects and even new states of matter can arise at interfaces between materials with different types of electronic order.

## Slide 6: Proximity Systems -> Applications
L1
L2
Symmetry(-ies) broken
Novel effects and even new states of matter can arise at interfaces between materials with different types of electronic order.
For example, combining different superconducting, magnetic and semiconducting materials is a very active area of research as people move towards new electronic devices.

## Slide 7: Superconducting proximity effects
superconductor
ferromagnet
Heavy metal

## Slide 8: Superconducting proximity effects
superconductor
ferromagnet
Heavy metal
Effect of exchange field

## Slide 9: Superconducting proximity effects
superconductor
ferromagnet
Heavy metal
Effect of exchange field
2. Effect of spin-orbit

## Slide 10: Superconducting proximity effects
spin degeneracy lifted
superconductor
ferromagnet
Heavy metal
Effect of exchange field
2. Effect of spin-orbit
Singlet
Triplet
Fermionic statistics require SPOT = -1

## Slide 11: Superconducting proximity effects
spin degeneracy lifted
superconductor
ferromagnet
Heavy metal
Effect of exchange field
2. Effect of spin-orbit
Singlet
Triplet
Fermionic statistics require SPOT = -1
Pairs can gain a magnetisation (spin).
Pairs can become anti-symmetric in time (orbital).

## Slide 12
The TF muon spectroscopy technique
detector A
detector B
muons
NA(t) – NB(t)
NA(t) + NB(t)
‘asymmetry’ (t) =
non-relaxing polarisation
relaxing polarisation
magnetic field
= a0Gx(t) cos(wt)
Oscillation frequency -> magnitude of the local magnetic field
Local magnetic field is altered by the superconducting state, which can be seen as a change in the oscillation frequency.

## Slide 13
The TF muon spectroscopy technique
detector A
detector B
muons
NA(t) – NB(t)
NA(t) + NB(t)
‘asymmetry’ (t) =
non-relaxing polarisation
relaxing polarisation
magnetic field
= a0Gx(t) cos(wt)
Oscillation frequency -> magnitude of the local magnetic field Damping -> field homogeneity
Muons stop in materials at a depth determined by their incident energy and the density of the material.

## Slide 14: Low energy muons applied to superconducting proximity systems
Depth of implantation controlled via selection of the momentum of the incoming muons
Sample local flux density B(x) as a function of depth
Layer 1
Layer 2
Implantation depth
Stopping distribution
7keV, <x>=21 nm
27keV, <x>=82 nm
Muons

## Slide 15: Low energy muons applied to superconducting proximity systems
Depth of implantation controlled via selection of the momentum of the incoming muons
Sample local flux density B(x) as a function of depth
Layer 1
Layer 2
Implantation depth
Stopping distribution
7keV, <x>=21 nm
27keV, <x>=82 nm
Muons

## Slide 16: Low energy muons applied to superconducting proximity systems
Depth of implantation controlled via selection of the momentum of the incoming muons
Sample local flux density B(x) as a function of depth
Layer 1
Layer 2
Implantation depth
Stopping distribution
7keV, <x>=21 nm
27keV, <x>=82 nm
Muons

## Slide 17: Low energy muons applied to superconducting proximity systems
Depth of implantation controlled via selection of the momentum of the incoming muons
Sample local flux density B(x) as a function of depth
Layer 1
Layer 2
Implantation depth
Stopping distribution
7keV, <x>=21 nm
27keV, <x>=82 nm
Muons

## Slide 18: Low energy muons applied to superconducting proximity systems
Depth of implantation controlled via selection of the momentum of the incoming muons
Sample local flux density B(x) as a function of depth
Layer 1
Layer 2
Implantation depth
Stopping distribution
7keV, <x>=21 nm
27keV, <x>=82 nm
Muons

## Slide 19: Low energy muons applied to superconducting proximity systems
Depth of implantation controlled via selection of the momentum of the incoming muons
Sample local flux density B(x) as a function of depth
Layer 1
Layer 2
Implantation depth
Stopping distribution
7keV, <x>=21 nm
27keV, <x>=82 nm
Muons
Spatial average -> full quantitative spatial dependence requires a clear ansatz e.g. asymmetric Meissner profile for S/F:

## Slide 20: Measurable consequences of having manipulated the spin state – a summary of what muons are sensitive to
Importantly, cannot distinguish spin and orbital contributions from LEM alone. Need to model the data with appropriate theory.
In the Meissner state of superconducting proximity systems, we expect changes to both orbital and spin contributions to local flux that the muon experiences due to unconventional superconducting pairs.
This means we can use TF-MuSR to measure the local flux, above and below Tc, as a function of muon implantation energy and characterise superconducting proximity effects at buried interfaces.
Quantitative interpretation of the data often requires application of theory models, and systematic studies where interface properties are tuned to manipulate the measured effects.

## Slide 21
Superconducting proximity – screening effects
superconductor – ferromagnet
Superconductor
Ferromagnet
Paramagnetic screening
A. Di Bernardo, Z. Salman et al., PHYSICAL REVIEW X 5, 041021 (2015).
Matthew Rogers et al, Communications Physics volume 4, Article number: 69 (2021)
Flux profiles across N/S and S
Notes: What is important here?
Typically conventional superconductivity being manipulated by some conflicting state of matter – archetypical example is the FM but a lot of interest in AFM, high S-O etc.
Correlations affected by the material properties of the host they 'leak into' and can become unconventional e.g. Spatial modulation of pair wave function, odd-freq. S-wave pairs that screen with the applied field to add to it. Super weird. Pairs possess NET SPIN.
Why do we do it? Insight into unconventional pairing mechanisms that are not easily realised in bulk system – play with the relevant degrees of freedom. Also, to work towards useful applications – superconducting spintronics where here we care about propagation of net spin pairs over long distances from the superconductor – A CHALLENGE!
But how do we study these systems – obviously a lot of transport measurements (name a couple specifics), PNR is powerful, some SANS, but I will talk about LE-MuSR since that is what I have used most.

## Slide 22
Superconducting proximity – electromagnetic proximity
Superconductor
Typically assume M is trapped for a thin single domain F layer (aside from inverse proximity)
Notes: What is important here?
Typically conventional superconductivity being manipulated by some conflicting state of matter – archetypical example is the FM but a lot of interest in AFM, high S-O etc.
Correlations affected by the material properties of the host they 'leak into' and can become unconventional e.g. Spatial modulation of pair wave function, odd-freq. S-wave pairs that screen with the applied field to add to it. Super weird. Pairs possess NET SPIN.
Why do we do it? Insight into unconventional pairing mechanisms that are not easily realised in bulk system – play with the relevant degrees of freedom. Also, to work towards useful applications – superconducting spintronics where here we care about propagation of net spin pairs over long distances from the superconductor – A CHALLENGE!
But how do we study these systems – obviously a lot of transport measurements (name a couple specifics), PNR is powerful, some SANS, but I will talk about LE-MuSR since that is what I have used most.

## Slide 23
Superconducting proximity – electromagnetic proximity
Appl. Phys. Lett. 115, 072602 (2019)
Ferromagnet
x
z
Superconductor
Vacuum
Applied field
Superconductor
S. Mironov et. al. Appl. Phys. Lett. 113, 022601 (2018)
Zh. Devizorova et. Al. Phys. Rev. B 99, 104519 (2019)
A. F. Volkov et. al. Phys. Rev. B 99, 144506 (2019)
Phys. Rev. Lett. 120, 247001 (2018)
Response of the macroscopic wavefunction to the vector potential due to M in F ​
Direct contact of condensate with M in F
Phys. Rev. B 100, 020505(R) (2019)
Notes: What is important here?
Typically conventional superconductivity being manipulated by some conflicting state of matter – archetypical example is the FM but a lot of interest in AFM, high S-O etc.
Correlations affected by the material properties of the host they 'leak into' and can become unconventional e.g. Spatial modulation of pair wave function, odd-freq. S-wave pairs that screen with the applied field to add to it. Super weird. Pairs possess NET SPIN.
Why do we do it? Insight into unconventional pairing mechanisms that are not easily realised in bulk system – play with the relevant degrees of freedom. Also, to work towards useful applications – superconducting spintronics where here we care about propagation of net spin pairs over long distances from the superconductor – A CHALLENGE!
But how do we study these systems – obviously a lot of transport measurements (name a couple specifics), PNR is powerful, some SANS, but I will talk about LE-MuSR since that is what I have used most.

## Slide 24
Superconducting proximity – spin versus orbital effects
S. Bergeret, Rev. Mod. Phys. 77, 1321 (2005)
Length scale ~x
The above examples of diamagnetic/paramagnetic shielding are orbital effects with a length scale ~l
Can also have spin polarisation contributions to the magnetisation e.g. the inverse proximity effect with a length scale ~ x
B
Penetration depth
l
Cu
Nb
Co
Nb
Cu
Co
Nb
Cu
1
2
3
1
2
3
Cu

## Slide 25: From ferromagnets to high spin-orbit materials
A large body of work on superconductor-ferromagnet interfaces: singlet-triplet pair mixing FFLO analogue, odd frequency pairs, long range triplet pairing, flux logic etc.
Recent experimental and theoretical developments in using interfacial Rashba S-O interaction to generate equal triplet (long range) pairs -> easier route to integrating superconductivity with traditional spintronics devices.
Chunli Huang, Ilya V. Tokatly, and F. Sebastian Bergeret, Phys. Rev. B 98, 144515 (2018) ...and several others
However, theory, and FMR measurements, have suggested these effects can be generated without the exchange field from the ferromagnet layer!
Amundsen et al Colloquium: Spin-orbit effects in superconducting hybrid structures (2022).
Jeon, K.-R. et al, Nat. Mater. 17, 499-503 (2018)

## Slide 26: Sample structures
Cu(40)
Nb(50)
Pt(x)
Nb(50)
Nb(90)
Pt(60)
Cu(40)
SM1
SM2
SM3
}
Reference samples for MuSR measurements on the Pt/Nb bilayer
Layer thicknesses carefully chosen
Sample series developed to introduce, and modify, spin-orbit coupling at the interface between a superconductor and a normal metal.
Build on results for well-characterised Nb, Cu/Nb and Cu/Nb/Co systems measured previously.

## Slide 27: Scanning Tunnelling Spectroscopy Results on Au(5)/Pt(x)/Nb
Temperature dependence in good agreement with calculations using the Usadel theory (with input material parameters extracted from transport measurements).
(almost) fully developed proximity induced gap through 2nm of Pt
reduces to ~10%Nb through 10nm of Pt
Important result is that the coherence length of Pt ~ 10nm and superconducting pairs pass through ~10nm Pt

## Slide 28: Low energy muon results for Cu(40)/Nb(50) and Cu(40)/Pt(10)/Nb(50) – finding a benchmark signal
SM1: without the Pt spacer layer the Cu becomes highly proximitised and a large diamagnetic screening develops due to the long electronic mean free path. (cf Phys. Rev. Lett. 120, 247001 (2018).
SM2: significant reduction in screening both sides of the interface (cf STS results through 10nm Pt).
These effects can be modelled using quasiclassical Usadel formalism (B(x)) WITHOUT S-O.
  Thin platinum spacer layer acts like a vacuum interface.

## Slide 29: Low energy muon results for Pt(60)/Nb(96)
SM3: thicker Nb -> stronger screening-> amplify effects that scale with screening current.
19keV measurement suggests significant discrepancy to expected screening of Nb!
19keV

## Slide 30: Temperature and magnetic field scaling of the muon signal in Pt(60)/Nb(96)
Temperature
Magnetic field
Quasiclassical theory would predict a linear temperature dependence -> not what we observe.
Meissner screening is linear with field -> not what we observe.

## Slide 31: The need to include spin-orbit to describe the data
difference
interface
interface
Pre-existing theory unable to describe the interface contribution or T and B dependence of the signal.

## Slide 32: Adding spin-orbit coupling to the calculation
Convolute with muon stopping profile
A paramagnetic contribution can appear at the interface due to triplet pairs generated by Meissner currents in the presence of S-O coupling (although this doesn’t capture the unusual temperature dependence).
calculated T dependence

## Slide 33: Adding spin-orbit coupling to the calculation
Could instead be a spin galvanic effect due to the interaction between S-O coupling and itinerant electrons in the Pt as in:
S.V. Mironov et al, Appl. Phys. Lett. 124, 252601 (2024)
Convolute with muon stopping profile
A paramagnetic contribution can appear at the interface due to triplet pairs generated by Meissner currents in the presence of S-O coupling (although this doesn’t capture the unusual temperature dependence).
calculated T dependence

## Slide 34: Summary and main conclusions
Low energy muons are a quantitative probe of magnetic interface effects, where full spatial information may be extracted given appropriate theory models.
Superconducting proximity systems host a range of unconventional superconducting states and offer the opportunity to tune superconductivity for fundamental study or application to superconducting spintronics.
Spin-orbit interactions can generate spin polarization in a superconductor even without the presence of a magnetic layer!
We have observed a spin-orbit induced net paramagnetic contribution arising in a Pt/Nb bilayer, where further low energy muon experiments are needed to confirm the origin.
This work is an important step in integrating superconductivity with conventional spintronics since correlations can propagate over long distances, in the absence of an exchange field, and without the need for complicated sample structures.

## Slide 36
Superconducting proximity – screening effects
superconductor – normal metal
Superconductor
Metal
Coherence length
x
xn
Nb (90 nm)
Nb (50 nm)
Cu (40 nm)
Phys. Rev. Lett. 120, 247001 (2018)
* Diamagnetic shielding
* Subtleties depending on how mean free path compares to coherence length
Can be calculated from 'conventional' theory models.
Flux profile across N/S and S
Notes: What is important here?
Typically conventional superconductivity being manipulated by some conflicting state of matter – archetypical example is the FM but a lot of interest in AFM, high S-O etc.
Correlations affected by the material properties of the host they 'leak into' and can become unconventional e.g. Spatial modulation of pair wave function, odd-freq. S-wave pairs that screen with the applied field to add to it. Super weird. Pairs possess NET SPIN.
Why do we do it? Insight into unconventional pairing mechanisms that are not easily realised in bulk system – play with the relevant degrees of freedom. Also, to work towards useful applications – superconducting spintronics where here we care about propagation of net spin pairs over long distances from the superconductor – A CHALLENGE!
But how do we study these systems – obviously a lot of transport measurements (name a couple specifics), PNR is powerful, some SANS, but I will talk about LE-MuSR since that is what I have used most.