## Slide 1
μSR Investigation of Novel Magnetic Semiconductors
Fanlong Ning 宁凡龙
School of Physics, Zhejiang University
(Material synthesis + μSR + NMR)
MELODY – CSNS (Dongguan)
Jan-11th, 2025
Supported by MOST, NSFC and ZJ-NSF

## Slide 2
In collaboration with:
Y.J. Uemura’ Group (Columbia)
G.Luke’ Group (McMaster)
Changqing Jin’s Group (IOP)
Experiments:
Dr. Huiyuan Man (now a postdoc at Standford with Prof. Kathryn Moler)
Dr. Cui Ding (now a postdoc at Tsinghua with Prof. Qikun Xue)
Dr. Shengli Guo (now in industry)
Dr. Licheng Fu, Dr. Yilun Gu, Yao Zhao, Kai Wang
Acknowledgement
TRIUMF: Prof. Jess Brewer, Dr. Syd Kreizman, Dr. Bessam Hitti
Jianhua Zhao(Semi), Kai Chang (Semi), Kaiyou Wang(Semi)，Igor Zutic (Buffalo), S. Maekawa (JAEA), Bo Gu(KITS), Igor Mazin (Navy), Ravin Bhatt (Princeton), Xin Wan (ZJU), Chao Cao (HZNU)

## Slide 3
Outline
Motivations
Introduction of some newly fabricated DMSs
----- Li1+y(Zn1-xMnx)As
----- N-type Ba(Zn1-xCox)2As2
c. Microscopic characterization
----- μSR results on bulk form DMSs
-----NMR results on Li1.1(Cd1-xMnx)P and Li1.15(Zn1-xMnx)P

## Slide 4
Semiconductors
(since 1700s)
Magnetism
(since 400 B.C.)
Magnetic Semiconductors
(since 1960s)

## Slide 5: Spintronics and Magnetic Semiconductors
Electron
Charge
Spin
Electronics
+
Spintronics
Non magnetic
Semiconductor
Condensed Magnetic
Semiconductor
Diluted Magnetic
Semiconductor
We want to create
“spintronics”, and use
not only charge but
also spin information
Notes: 依靠技术的进步和材料的研发

## Slide 6
Concentrated：
EuO、EuS…
Ⅱ-Ⅵ：
(Cd,Mn)Te、(Zn,Co)S…
Ⅲ-Ⅴ：
(Ga,Mn)As、(In,Mn)As、
(Ga,Mn)N …
2D, Topoligcal, Antiferromagnetic：
CrI3、Bi2Se3:Mn、MnPS3…
Bulk form, Decoupled Charge and Spin Doping：
(Na,Ca)(Zn,Mn)2As2, Li(Zn,Mn)As, (Ba,K)(Zn,Mn)2As2
(Ba1-xKx)(Cu2-xMnx)Se2,(La,Ba)(Zn,Mn)AsO…
New, Novel…?
The Development of Magnetic Semiconductors

## Slide 7
Ga1-xMnxAs and Why bulk form DMS?
Ga1-xMnxAs, TC~200K, limited for practical applications; holes and spins are all
introduced by Mn atoms (Jianhua Zhao’s group in Institute of Semiconductor, Beijing)
Currently achieved highest Tc in various
III-V DMS thin films
(Dietl et al, Nature Materials, 2010, (9)965)
Mismatch of valences for Mn2+ and
Ga3+ atoms, chemical solubility is less
than 1% in bulk form
Only low dimensional thin film can be
fabricated with Molecular Beam Epitaxy
Mn2+ substitution for Ga3+ introduces holes and spins
μSR, NMR and neutron scattering are limited to investigate thin film.
Highly debates on the mechanism
DMS in bulk form is highly expected!
Doped with Mn

## Slide 8
Spin Glass Ordering, saturation moment ~0.01μB

## Slide 9
0.003 μB/Mn
Phys Rev B, 58, 12876 (1998)
Zn0.49Mn0.51Te
Zn and Mn valences of “+2”,
No solid solution limit
the doping can be as high as ~70%
Mn ions do not provide carriers,
only provide local moment
Difficult to control density and type
of carriers
ZnSe/ZnTeFeSe
(“11” family of Fe-based SC）

## Slide 11
“III-V” “I-II-V” “II-VI”
LiZnAs (1.6ev)
LiZnP (2.04ev)
LiCdP (1.30ev)
GaAs (1.42ev)
Ga1-xMnxAs: Mn dope both spins and holes
Li1+y(Zn+21-xMn+2x)As, Li1+y(Zn+21-xMn+2x)P, Li1+y(Cd+21-xMn+2x)P (TC ~40-50K)
: decouple spins and carriers
Mn doping induces local moments
Li extra or deficiencies create carriers---use Li to control the type of carriers
(C.Q. Jin’s group in IOP, Z. Deng et al, Nature Comm.,2011, PRB 2013)
LiZnAs  LiFeAs
(“111” family of Fe-based SC）
(Li+Zn2+) = Ga3+
LiZnAs = GaAs
(Li+As3-) = Se2-
 Zn(LiAs) = ZnSe

## Slide 12
“111”- Li1+y(Zn+21-xMn+2x)As （TC ~ 50 K)
Z. Deng et al, Nature Communications (2011)
Saturation moments continuously
decrease with more Mn
Effective moment is 5~6μB/Mn，
high spin state
Coercive field ~ 50 Oe，
for magnetic manipulation

## Slide 13
Deng et al, PRB 88,081203(R) (2013)
Li1+y(Zn+21-xMn+2x)P: Max TC ~ 40 K

## Slide 14
Tc and moment size at 6K
43
35
28
21
Tc
0.75
7.5
0.65
10
0.90
5.0
1.00
2.5
Mn(6K)
x*(100%)
Tc
Li1+y(Cd+21-xMn+2x)P
Wei Han et al, Scientific Reports 9, 7490 (2019)

## Slide 15
(La1-xBax)(Zn1-xMnx)AsO TC ~40K
Isostructral to Fe-based SC
“1111”-LaFeAsO1-xFx
C. Ding and F.L. Ning, PRB 88, 041102 (2013)
LaZnAsO  LaFeAsO
(“1111” family of Fe-based SC）

## Slide 16
(La1-xBax)(Zn1-xMnx)AsO TC ~40K
TC
doping Mn only, paramagnetic state
Only when carriers are doped via Ba
substitution for La, FM ordering is observed
From resitivity, semiconducting behavior
Large coercive field ~ 1 Tesla
C. Ding and F.L. Ning, PRB 88, 041102 (2013)

## Slide 17
K. Zhao et al, Nature Communications, 4, 1442 (2013)
(Ba1-xKx)(Zn1-yMny)2As2 TC ~180K

## Slide 18
(Ba1-xKx)(Zn1-yMny)2As2 TC ~180K
K. Zhao et al, Nature Communications, 4, 1442 (2013)

## Slide 19
TC ~ 230K
BaZn2As2  BaFe2As2
(“122” family of Fe-based SC）
Record TC ~ 200K
Ga1-xMnxAs

## Slide 20
GaAs ------------ (Ga1-xMnx)As ------------------------ MnAs
FM, Tc ~ 210K(film) FM, Tc ~ 320K
LiZnAs --------- Li(Zn1-xMnx)As ----------------------- LiMnAs
“111” FM, Tc ~ 55K(bulk) AFM, TN~ 400K
I-II-V (Nature Comm. 2011, IOP)
BaZn2As2 ---- (Ba1-yKy)(Zn1-xMnx)2As2 ---------------- BaMn2As2
“122” FM, Tc ~ 230K(bulk) AFM, TN~ 620K
II-II-V (Nature Comm. 2013, IOP)
LaZnAsO ---- (La1-yBay)(Zn1-xMnx)AsO --------------- LaMnAsO
“1111” FM, Tc ~ 40K(bulk) AFM, TN ~ 320K
(PRB 2013, Zhejiang)
“32522” ---- (Sr3La2O5)(Zn1-xMnx)2As2 --------------- AFM(?)
FM, Tc ~ 40K(bulk)
(EPL 2014, Zhejiang)
“42622” ---- (Sr1-xKx)4Ti2O6(Zn1-xMnx)2As2 --------------- AFM(?)
FM, Tc ~ 25K(bulk)
(To be submitted, Zhejiang)
Fabricate new DMS and what we have

## Slide 24
Ga1-xMnxAs Tc ~ 200K(film)
Li(Zn1-xMnx)As Tc ~ 55K(bulk)-----”111”
(Ba1-yKy)(Zn1-xMnx)2As2 Tc ~ 230K(bulk)---”122”
(La1-yBay)Zn1-xMnxAsO Tc ~ 40K(bulk) ---”1111”
(Sr3La2O5)(Zn1-xMnx)2As2 Tc ~ 40K(bulk)---”32522”
(Sr1-xKx)4Ti2O6(Zn1-xMnx)2As2 Tc ~ 25K(bulk)---”42622”
P-type DMS
For making junctions, n-type DMS are expected!

## Slide 25
“122” – Ba(Fe1-xCox)2As2- SC
Tc = 25 K
Doping Co,
introduce electrons
F.L. Ning et al, JPSJ 78, 013711(2009)
F.L. Ning et al, PRL 104, 037001 (2010)

## Slide 26
Ba
Zn  Co
As
“122” - BaZn2As2
The idea here is:
---Co introduce both moments and electrons
（Started the work in 2013)

## Slide 27
﻿Ba
﻿Zn/Co
﻿As
Until 2016: Shengli Guo obtained pure phase
S.L. Guo and F.L. Ning et al, PRB 99,155201 (2019).

## Slide 28
S.L. Guo and F.L. Ning et al, PRB 99,155201 (2019).

## Slide 29
S.L. Guo and F.L. Ning et al, PRB 99,155201 (2019).

## Slide 30
Ba(Zn0.96Co0.04)2As2

## Slide 31
Ba(Zn0.96Co0.04)2As2
S.L. Guo and F.L. Ning et al, PRB 99,155201 (2019).

## Slide 32
S.L. Guo and F.L. Ning et al, PRB 99,155201 (2019).

## Slide 34
-n VS. T plot

## Slide 35
Negative Seebeck coefficient
S.L. Guo and F.L. Ning et al, PRB 99,155201 (2019).

## Slide 36
Effects of chemical pressure on Ba(Zn,Co)2As2
Ba(Zn0.96Co0.04)2(As1-ySby)2
(Licheng Fu and Fanlong Ning, Scientific Reports 2022)
Doping Sb  Negative chemical pressure, TC decreases

## Slide 37
(Ba1-xSrx)(Zn0.96Co0.04)2As2
(Licheng Fu and Fanlong Ning, Scientific Reports 2022)
Doping Sr---- Positive chemical pressure, TC increases
Effects of chemical pressure on Ba(Zn,Co)2As2

## Slide 38
(Ba1-xSrx)(Zn0.96Co0.04)2As2
(Licheng Fu and Fanlong Ning, Scientific Reports 2022)
Doping Sr---- Positive chemical pressure, TC increases
TC
Effects of chemical pressure on Ba(Zn,Co)2As2

## Slide 39
(La1-xBax)(Zn1-xMnx)AsO (TC =40K) (PRB，2013)
(SrLa2O5)(Zn1-xMnx)2As2 (TC =40K) (EPL，2014)
Li1+y(Zn1-xCrx)As (TC =210K) (JAP，2014)
Ba(Zn1−2xMnxCux)2As2 (TC =70K) (SR, 2015)
(Ba1-xKx)(Cu1-xMnx)Se2 (TC =18K) ( JMMM, 2016)
Li(Zn1-2xMnxCux)As (TC =33K) (JPCM, 2016)
La(Zn1−2xMnxCux)AsO (TC =8K) (EPL, 2016)
(La1−xCax)(Zn1−xMnx)AsO (TC =30K) (JPCM, 2016)
La(Zn1−2xMnxCux)SbO (TC =15K) (EPL, 2017)
Ba(Zn1-xCox)2As2 (TC =40K) (N-type, PRB, 2019)
(Sr1-xKx)F(Zn1-xMnx)Sb (TC =40K) (JMMM, 2019)
Cu2(Zn1-xMnx)(Sn1-yAly)Se4 (TC =5K) (JMMM, 2022)
(Ba1-xKx)(Zn1-yMny)2Sb2 (TC =275K？ In preparation, 2020)
(Ca1-xNax)(Zn1-yMny)2Sb2 (TC =10K) (CPB, 2020)
New Diluted Ferromagnetic Semiconductors (Zhejing U)

## Slide 40
Sample | TC (K) | Structure | a (Å) | b (Å) | c (Å) | Gap (eV)
Li(Zn,Cr)As | 218 | cubic | 5.929 | 5.929 | 5.929 | 1.6
Li(Zn,Mn,Cu)As | 33 | cubic | 5.941 | 5.941 | 5.941 | 1.6
(Ba,K)(Cu,Mn)2Se2 | 18 | orthorhombic | 9.610 | 4.219 | 10.793 | 1.3
Ba(Zn,Co)2As2 | 45 | tetragonal | 4.125 | 4.125 | 13.571 | 0.2
Ba(Zn,Mn,Cu)2As2 | 70 | tetragonal | 4.140 | 4.140 | 13.300 | 0.2
(La,Ba)(Zn,Mn)AsO | 40 | tetragonal | 4.112 | 4.112 | 9.107 | 1.5
(La,Sr)(Zn,Mn)AsO | 35 | tetragonal | 4.105 | 4.105 | 9.106 | 1.5
(La,Ca)(Zn,Mn)AsO | 30 | tetragonal | 4.102 | 4.102 | 9.076 | 1.5
La(Zn,Mn,Cu)AsO | 8 | tetragonal | 4.101 | 4.101 | 9.073 | 1.5
La(Zn,Mn,Cu)SbO | 15 | tetragonal | 4.228 | 4.228 | 9.565 | 0.3
SrF(Zn,Mn,Cu)Sb | 40 | tetragonal | 4.293 | 4.293 | 9.526 | -
(Sr3La2O5)(Zn,Mn)2As2 | 40 | tetragonal | 4.261 | 4.261 | 27.675 | -

## Slide 41
Sample | TC (K) | Structure | a (Å) | b (Å) | c (Å) | Gap (eV) | group
Li(Zn,Mn)P | 34 | cubic | 5.766 | 5.766 | 5.766 | 2.0 | Jin
Li(Cd,Mn)P | 45 | cubic | 6.071 | 6.071 | 6.071 | 0.6 | Jin
Li(Zn,Co,Mn)As | 40 | cubic | 5.950 | 5.950 | 5.950 | 1.6 | Jin
Li(Zn,Mn)As | 50 | cubic | 5.941 | 5.941 | 5.941 | 1.6 | Jin
(Ca,Na)(Zn,Mn)2As2 | 33 | hexagonal | 4.160 | 4.160 | 7.025 | 0.1 | Jin
(Sr,Na)(Zn,Mn)2As2 | 24 | hexagonal | 4.233 | 4.233 | 7.291 | 1.2 | Jin
(Sr,K)(Zn,Mn)2As2 | 12 | hexagonal | 4.232 | 4.232 | 7.280 | 0.2 | Xu
(Sr,Na)(Cd,Mn)2As2 | 13 | hexagonal | 4.444 | 4.444 | 4.438 | 0.2 | Jin
(Ba,Na)(Zn,Mn)2As2 | 16 | tetragonal | 4.117 | 4.117 | 13.433 | 0.2 | Jin
(Ba,K)(Zn,Mn)2As2 | 230 | tetragonal | 4.130 | 4.130 | 13.509 | 0.2 | Jin
(Ba,K)(Cd,Mn)2As2 | 16 | hexagonal | 4.499 | 4.499 | 7.692 | 0.4 | Xu
(La,Ca)(Zn,Mn)SbO | 40 | tetragonal | 4.228 | 4.228 | 9.566 | 0.3 | Jin
(Ba,K)F(Zn,Mn)As | 30 | tetragonal | 4.241 | 4.241 | 9.538 | 0.9 | Jin
(La,Sr)(Cu,Mn)SO | 200 | tetragonal | 3.996 | 3.996 | 8.519 | 3.1 | Xu

## Slide 42
1, S.L. Guo et al, PRB 99, 155201 (2019)
2, L.C. Fu et al, JMMM 483, 95 (2019)
3, Y.L. Gu et al, JOS 40, 081506 (2019)
4, G.X. Zhi et al, Cond Matt 3, 42(2018)
5, S.L. Guo et al, CPB 27, 097502(2018)
6, Yao Zhao et al, EPL 120, 47005 (2017)
7, F.F. Zhu et al, APL 111, 062106 (2017)
8 S.L. Guo et al, EPL 114, 57008 (2016)
9, S.L. Guo et al, JMMM 400, 295 (2016)
10, Cui Ding et al, JPCM 28, 026003 (2016)
11, S.L. Guo et al, JPCM 28, 366001 (2016)
12, H.Y. Man et al, Scientific Reports 5, 15507 (2015)
13, Cui Ding et al, Science China (2014)
14, Cui Ding et al, EPL 107, 17004 (2014)
15, F.L. Ning et al, PRB 90, 185023 (2014)
16, H.Y. Man et al, EPL 105, 67004 (2014)
17, Q. Wang et al, JAP 115, 083917 (2014)
18, J.C. Lu et al, EPL 103, 67001 (2013)
19, C. Ding et al PRB 88, 041102(R) (2013)
20, C. Ding et al PRB 88, 041108(R) (2013)
21, W. Han et al, Scientific Reports 9, 7490 (2019)
22, Y. Peng et al, CPB 28, 057501 (2019)
23, G.Q. Zhao et al, JPCM 30, 254001 (2018)
24, G.X. Gu et al, APL 112, 032402 (2018)
25, Sun Fei et al, CPL 34, 0256 (2017)
26, R. Wang et al, AIP Advances 7, 045017 (2017)
27, Sun Fei et al, PRB 95, 094412 (2017)
28, B.J.Chen et al, Scientific Reports 6, 36578 (2016)
29, B.Frandsen and Uemura et al, PRB 94, 094102 (2016)
30, F. Sun et al, PRB 93, 224403 (2016)
31, H. Suzuki and Fujimori et al, PRB 92, 215320 (2015)
32, H. Suzuki and Fujimori et al, PRB 91, 140401 (2015)
33, K. Zhao et al, Chin. Sci. Bull. (2014)
34, B.J. Chen et al PRB 90, 155202 (2014)
35, B.J. Chen et al JAP 116,163906 (2014)
36, W. Han et al, Science China (2013)
37, Z. Deng et al, PRB 88, 081203(R) (2013)
38, K. Zhao et al, Nature Comm. 4, 1442 (2013)
39, Z. Deng et al, JPCS 400, 032033 (2012)
40, Z. Deng et al, Nature Comm. 2, 422 (2011)
In past several years, our collaboration team (Uemura & Jin & Ning)
published ~ 60 papers on DMS

## Slide 43
Outline
a. Introduction of some newly fabricated DMSs
“111”, 122”,”1111”, “42622”,”32522”
----- Li1+y(Zn1-xMnx)P
----- n-type Ba(Zn1-2xCoxMnx)2As2
b. Microscopic characterization
----- μSR results on (Ga,Mn)As and Li1.15(Zn1-xMnx)P
-----NMR results on Li1.1(Cd1-xMnx)P and Li1.15(Zn1-xMnx)P

## Slide 44
μ SR experiments were conducted in PSI

## Slide 46
Li1.1(Zn0.95Mn0.05)As (TC ~ 30 K)
as --- relaxation rate (static local field amplitude)

## Slide 47
“122” (Ba1-xKx)(Zn1-yMny)2As2 (TC ~180 K)

## Slide 48
“1111” (La1-xBax)(Zn1-xMnx)AsO TC ~ 40K

## Slide 49
TC: which is a measure of the effective
average ferromagnetic interaction
Static local field amplitude as:
which is proportional to the
individual ordered moment
size multiplied by the moment
concentration
S. Dunsiger, Nature Material, 2009
C. Ding, Physical Review B, 2013
K. Zhao, Nature Communications, 2013
Z. Deng, Nature Communications, 2011
F.L. Ning, Physical Review B, 2014

## Slide 50
Zero field (ZF-) MuSR asymmetry spectra of Ba(Zn0.95Co0.05)2As2 at 2 K
Fitting Function for dilute spin systems: , .
Uemuraet al.Phy. Rev. B 31, 546 (1985).
One component function, no phase seperation

## Slide 51
ZF-MuSR results for Ba(Zn1-xCox)2As2
Static field arises below TC

## Slide 52
Longitudinal field (LF-) MuSR results for
Ba(Zn1-xCox)2As2 at 2 K
The asymmetry is fully decoupled at ~ 100 Oe.
Conclusion: the internal field at 2 K muon suffered is fully static and magnitude is ~ 10 Oe.

## Slide 53
Temperature scan 100 Oe LF-MuSR results for
Ba(Zn1-xCox)2As2

## Slide 54
Ferromagnetic exchange coupling is much larger in this system compared these other p-type systems.

## Slide 55
Several advantages of bulk form DMS materials:
Synthesized in thermally equilibrium condition, less defects are expected;
Bulk form, single crystals are available, for NMR, neutron, μSR measurements;
Carriers can be doped at different ionic sites, for example for BaZn2As2, K
substitution for Ba introduces holes, while Mn substitution for Zn introduces electrons;
Charge and spin doping are decoupled, each can be precisely controlled and tuned;
Iso-structural to its superconductor, antiferromagnet variant, junctions via As layer
can be made;
Thin films of parent compound LaZnAsO and BaZn2As2 have been successfully made;
(Ba1-yKy)(Zn1-xMnx)2As2: TC = 230 K for now, thin film may achieve higher TC? (FeSe-SC)
Share the same origin of ferromagnetism as (Ga,Mn)As, helpful to understand the
general mechanism;

## Slide 56
Series of bulk DMSs with (highest TC = 230 K) have been fabricated, and these DMSs have common mechanism with (Ga,Mn)As, and can serve as model systems to study the ferromagnetism in DMS
A n-type DMS Ba(Zn1-xCox)2As2 (TC = 45K) have been successfully synthesized
NMR and μSR: Mn atoms are homogenously doped, the ferromagnetic ordering is from Mn in the ionic Zn site
NMR results are consistent with a carrier mediated ferromagnetism picture.
Now with the same 122 tetragonal structure, junctions could be made via As layer between following materials:
N-type DMS Ba(Zn1-xCox)2As2 (TC = 45K)
P-type DMS (Ba1-yKy)(Zn1-xMnx)2As2 (TC=230K)
Superconductor Ba(Fe1-xCox)2As2 (Tc=25K)
Antiferromagnet BaMn2As2 (TN=625K)
Paramagnetic BaCo2As2
Conclusions
Thank you for your attention!

## Slide 57
Outline
a. Introduction of some newly fabricated DMSs
“111”, 122”,”1111”, “42622”,”32522”
----- Li1+y(Zn1-xMnx)P
----- n-type Ba(Zn1-2xCoxMnx)2As2
b. Microscopic characterization
----- μSR on Li1.15(Zn1-xMnx)P
-----NMR results on Li1.1(Cd1-xMnx)P and Li1.15(Zn1-xMnx)P

## Slide 58
“III-V” versus “I-II-V” semiconductors
LiZnAs (1.6ev)
LiZnP (2.04ev)
LiCdP (1.30ev)
GaAs (1.42ev)
Li1.1(Cd+20.9Mn+20.1)P and Li1.15(Zn+20.9Mn+20.1)P
decouple spins and carriers
Mn doping induces local moments
Li extra or deficiencies create itinerant or localized carriers
----- use Li to control the type of carriers

## Slide 59
7Li NMR line shape ---- Li1.1CdP
Li
Cd
For 7Li:
Nuclear spin = 3/2
Gyromagnetic ratio = 16.546MHz/Tesla
Bext = 4.5 Tesla  fresonance = 74.457MHz
Single line with line width = 4KHz
No additional Li line found for extra 10% Li
6 Cd atoms at N.N. site, all Li have the same
environment -----define it as Li(0) site
Spin echo inten(arb.)
P
Cd/Mn
Li

## Slide 60
7Li NMR line shape ---- Li1.1CdP
Linewidth:
~7KHz at 4.2K
~4KHz at 280K
Knight shift:
~ 0.001% at 4.2K
~ 0.005% at 280K
Spin echo inten(arb.)

## Slide 61
7Li NMR line shape ---- Li1.1Cd0.9Mn0.1P
10% Mn doped into Cd sites, the probability to find n = 0, 1, 2, 3, 4, 5, 6 Mn atoms at N.N. sites are P(n) = C6n(0.1)n(0.9)6-n
Li
Cd
Li
Cd
Li
Cd
Li
Cd
Li
Cd
Li(0): 53%
Li(1): 35%
Li(3): 1.5%
Li(2): 10%
Li(4): 0.1%
Mn
Mn
Mn
Mn
Li(0):Li(Mn) ~ 50%:50%

## Slide 62
7Li NMR line shape
---- Li1.1Cd0.9Mn0.1P
Key features:
Li(0) line preserve but broaden
Li(Mn) line appears, broad peak at left hand
Li(Mn) line has a large negative shift
Integrated area, Li(Mn):Li(0) = 50:50

## Slide 63
7Li NMR line shape ---- Li1.1Cd0.9Mn0.1P
Li(Mn)
Li(0)
Key features:
Frequency shifts of Li(Mn) follows
a Curie-Weiss law
Li(0) continuously broaden from
20KHz (at 290K) to 240KHz (at 4.2K)
~ 10 times broadening. Line width follow
a Curie-Weiss law
For Li(0) site in the parent
compound Li1.1CdP, only increase from
4KHz (at 280K) to 7KHz (at 4.2K).
Spin echo inten(arb.)

## Slide 64
Frequency VS. Temperature
Negative frequency shift:
---hyperfine coupling constant
between 7Li nuclear spin and
surrounding electrons is negative
73.8
73.9
74
74.1
74.2
74.3
74.4
74.5
74.6
0
50
100
150
200
250
300
Frequency of Li sites VS. T
f(MHz)
T(K)
Li(Mn) of Li
1.1
Cd
0.9
Mn
0.1
P
Li(0) of Li
1.1
CdP
Li(0)
Li
1.1
Cd
0.9
Mn
0.1
P

## Slide 65
Li1.1Cd0.9Mn0.1P
The line broadening of Li(0)
which do not have Mn at N.N.
is the same as the frequency
shifts of Li(Mn).
Li(0) and Li(Mn) sites are
electronically coupled!

## Slide 66
Li1.1Cd0.9Mn0.1P
Li1.15Zn0.9Mn0.1P
Mn atoms are homogenously distributed in the compound, and no Mn clusters exist.
Consistent with 100% magnetic ordered volume from μSR experiment.
The ferromangetic ordering is intrinsic, from the Mn atoms in the ionic sites in I-II-V DMS! It is NOT from spurious phase.

## Slide 67
Spin dynamics----Li1.15Zn0.9Mn0.1P and Li1.1Cd0.9Mn0.1P
Tc = 25K
C. Ding et al., Physics Review B 88, 041108 (R) (2013).
T(K)
T1 of Li(Mn) is 50 times shorter than T1 of Li(0)
Below Tc, for both Li(Mn) and Li(0) sites, T1 decrease

## Slide 68
Spin dynamics----Li1.15Zn0.9Mn0.1P
For Li(Mn) site, 1/T1 ~ constant
Spin fluctuations are locked
at T range ~100 K, J~ 100K
For Li(0) site, 1/T1 ~ a +bT
Korringa relation,
Related to information of carriers
Li(Mn) represent “spins”
Li(0) represent “carries”
Carrier mediated ferromagnetism!
Moriya's Gaussian approximation for the
spin-spin correlation function
Moriya’s exchange narrowed regime
Characteristic frequency of the Mn spin fluctuations
T(K)
Z~ 103 is the number of Mn sites within the
range of Mn-Mn interactions

## Slide 69
Series of bulk DMSs with (highest TC = 230 K) have been fabricated, and these DMSs have common mechanism with (Ga,Mn)As, and can serve as model systems to study the ferromagnetism in DMS
A n-type DMS Ba(Zn1-xCox)2As2 (TC = 45K) have been successfully synthesized
NMR and μSR: Mn atoms are homogenously doped, the ferromagnetic ordering is from Mn in the ionic Zn site
NMR results are consistent with a carrier mediated ferromagnetism picture.
Now with the same 122 tetragonal structure, junctions could be made via As layer between following materials:
N-type DMS Ba(Zn1-xCox)2As2 (TC = 45K)
P-type DMS (Ba1-yKy)(Zn1-xMnx)2As2 (TC=230K)
Superconductor Ba(Fe1-xCox)2As2 (Tc=25K)
Antiferromagnet BaMn2As2 (TN=625K)
Paramagnetic BaCo2As2
Conclusions
Thank you for your attention!