## Slide 1
μSR study on the van der Waals cluster magnet Nb3Cl8
Lin Yang
Institute of Physics, Chinese Academy of Sciences
the 2nd workshop on Muon Science Technology and Industry, @CSNS
2025.01.11
Institute of Physics, CAS

## Slide 2
Quantum Spin Liquid
Resonating Valence Bond (RVB) States in spin-1/2 systems
Geometrical frustrations enhance quantum fluctuations
Rep. Prog. Phys. 80, 016502(2017)
Nature 464, 199–208 (2010)
Properties of QSL:
Strong quantum fluctuations
long-range quantum entanglement
No long-range magnetic order at 0 K

## Slide 3
Breathing Kagome lattice in Nb3Cl8
a2
a1
Breathing Kagome layer in Nb3Cl8
Kagome Lattice
Breathing Kagome Lattice
a1=2.81Å
a2=3.93Å
van der Waals force

## Slide 4
S=1/2
Phys. Rev. X 13, 041049 (2023)
Inorg. Chem. Front. 4, 481(2017)
Mott Insulator
Band structure in Nb3Cl8
single-particle approximation
correlation
Notes: strong correlation effects

## Slide 5
Structural and magnetic transition in Nb3Cl8
Inorg. Chem. Front. 4, 481(2017)
paramagnetic – nonmagnetic in single crystal Nb3Cl8
high temperature magnetic phase
(HTMP)

## Slide 6
T = 0.1K, no magnetic order
large γ
Nb element
= 0.227 J mol/K2
= 0.223 J mol/K2
= 0.01 J mol/K2
Magnetic behavior of HTMP in Nb3Cl8
pressure along c-axis
single crystal
HTMP
HTMP

## Slide 7
4.5%
11%
Nb3Cl8 ~ 1 - 4
Wilson ratio:
influence of spin-orbit coupling
Fermi gas: = 1
Spinon Fermi surface QSL
Magnetic behavior of HTMP in Nb3Cl8
HTMP
HTMP

## Slide 8
NMR results of Nb3Cl8

## Slide 9
μSR results of Nb3Cl8 (zero field)
Static Kubo-Toyabe (KT) damping function：
Oe
Static field distribution：
dynamics
Slow down
No long-range magnetic order down to 75 mK
persistant fluctuation

## Slide 10
Oe, damping static KT function (ZF mode)
Oe，dynamic KT function:
μSR results of Nb3Cl8 (longitudinal field)
Oe, relaxation function：

## Slide 11
μSR results of Nb3Cl8 (longitudinal field)
Oe, relaxation function：
general correlation function:
Redfield formula (x=0, failed):
x = 0.40, 0.41, and 0.61 at 4, 1.8 and 0.075 K, respectively
Notes: Redfield formula:weakly correlated spin dynamic system

## Slide 12
Conclusion
The high-temperature magnetic phase (HTMP) can be realized in polycrystalline or pressure-induced Nb3Cl8
No long-range magnetic order down to 75 mK at HTMP
Persistent fluctuations in Nb3Cl8
Possible quantum spin liquid state at HTMP in Nb3Cl8 – spinon Fermi surface
Further study: inelastic neutron scattering on HTMP
Slow down
persistant fluctuation

## Slide 13
Acknowledgements
Shiliang Li and Huiqian Luo (IOP CAS, supervisors)
Bo Liu (IOP CAS, heat capacity measurements)
Detong Wu and Youguo Shi (IOP CAS, sample synthesis)
Rhea Stewart and Devashibhai Adroja (ISIS RAL, SR measurements and analysis)
Xin Han, Jun Luo and Rui Zhou (IOP CAS, NMR measurements)
Thanks for your attention!