## Slide 1
Sayani Biswas
2nd MELODY Workshop, CSNS, China
11th January 2025
Archaeological artefacts: Probing deep beneath the surface
µ-
Results:
Depth: 1 mm
Element wt%
Cu 68
Sn 21
Pb 3
.
.
.

## Slide 2
Outline
Archaeological artefacts: The approach so far
The μXES technique
Muonic X-ray Emission Spectroscopy
Case studies:
  1) Roman silver coins
  2) Roman gold coins
Take-home messages
- beam
Sample
Ge X-ray detector
0.1-10 MeV
Ge X-ray detector
0.1-10 MeV
Ge X-ray detector
low energy
Ge X-ray detector
low-energy
MuX setup at ISIS

## Slide 3
Archaeological artefacts: The approach so far
A. van der Ent et al., Sci Rep 9, 4746 (2019)
pXRF
LA-ICP-MS
N. L. LaHaye et al., J Anal. At. Spectrom. 29, 2267-2274 (2014)

## Slide 4
The μXES technique
µ- (p, dp/p)
1) The atom:
2) Muon capture by atom:
3) Emission of muonic X-rays:
Chart: 
| 41.820749999999975 | 42.032699999999977 | 42.244649999999979 | 42.45659999999998 | 42.668549999999982 | 42.880499999999984 | 43.092449999999985 | 43.304399999999987 | 43.516349999999989 | 43.72829999999999 | 43.940249999999992 | 44.152199999999993 | 44.364149999999995 | 44.576099999999997 | 44.788049999999998 | 45 | 45.211950000000002 | 45.423900000000003 | 45.635850000000005 | 45.847800000000007 | 46.059750000000008 | 46.27170000000001 | 46.483650000000011 | 46.695600000000013 | 46.907550000000015 | 47.119500000000016 | 47.331450000000018 | 47.54340000000002 | 47.755350000000021 | 47.967300000000023 | 48.179250000000025
 | 0.00086494 | 0.001933 | 0.0040869 | 0.0081747 | 0.015469 | 0.027693 | 0.046901 | 0.075147 | 0.11391 | 0.16335 | 0.22161 | 0.28443 | 0.34537 | 0.39673 | 0.43115 | 0.44327 | 0.43115 | 0.39673 | 0.34537 | 0.28443 | 0.22161 | 0.16335 | 0.11391 | 0.075147 | 0.046901 | 0.027693 | 0.015469 | 0.0081747 | 0.0040869 | 0.001933 | 0.00086494
Momentum, p (MeV/c)
p = 45 MeV/c
dp/p = 2%
Energy ~ 9 MeV
Depth, d (cm)
d ~ 1mm
Pure Cu
(simulation)
Pure Cu (Z = 29)
4) Emission of γ-rays:
HPGe
HPGe

## Slide 5
The μXES technique
µ- (p, dp/p)
1) The atom:
2) Muon capture by atom:
Chart: 
| 41.820749999999975 | 42.032699999999977 | 42.244649999999979 | 42.45659999999998 | 42.668549999999982 | 42.880499999999984 | 43.092449999999985 | 43.304399999999987 | 43.516349999999989 | 43.72829999999999 | 43.940249999999992 | 44.152199999999993 | 44.364149999999995 | 44.576099999999997 | 44.788049999999998 | 45 | 45.211950000000002 | 45.423900000000003 | 45.635850000000005 | 45.847800000000007 | 46.059750000000008 | 46.27170000000001 | 46.483650000000011 | 46.695600000000013 | 46.907550000000015 | 47.119500000000016 | 47.331450000000018 | 47.54340000000002 | 47.755350000000021 | 47.967300000000023 | 48.179250000000025
 | 0.00086494 | 0.001933 | 0.0040869 | 0.0081747 | 0.015469 | 0.027693 | 0.046901 | 0.075147 | 0.11391 | 0.16335 | 0.22161 | 0.28443 | 0.34537 | 0.39673 | 0.43115 | 0.44327 | 0.43115 | 0.39673 | 0.34537 | 0.28443 | 0.22161 | 0.16335 | 0.11391 | 0.075147 | 0.046901 | 0.027693 | 0.015469 | 0.0081747 | 0.0040869 | 0.001933 | 0.00086494
Momentum, p (MeV/c)
p = 45 MeV/c
dp/p = 2%
Energy ~ 9 MeV
Depth, d (cm)
d ~ 1mm
Pure Cu
(simulation)
Counts
Energy (keV)
µ-Lyman
(K series)
µ-Balmer
(L series)
µ-Paschen
(M series)
Pure Cu
(Z = 29)
µ-Kα
µ-Kβ
Kα : 8.0 keV
Kβ : 8.9 keV
µ-Kα : 1514 keV
µ-Kβ : 1844 keV
L. Gerchow, S. Biswas et al, Rev. Sci. Instrum. 94, 045106 (2023)
Non-destructive and depth-selective
Sensitive to all elements
Isotope determination
Oxidation state identification
Pure Cu (Z = 29)
HPGe
HPGe

## Slide 6
T
Creating muons at ISIS
C, 45°
10mm
Currently, we perform the
experiments in port 4
RIKEN-RAL Muon
facility
EC Muon
facility
The μXES technique
MuX setup

## Slide 7
The μXES technique
sample
MuX setup at ISIS and recent developments

## Slide 8
Case Studies
1) Roman silver coins:
denarius of Julia Domna
3rd century (211-217 CE)
Silver coinage formed the backbone of state finance in the Roman Empire
The fineness and quality of a coinage is often taken by historians to be a comment on the fiscal health of the issuing state
Yet very little is really known about its fineness and chemical composition
Many of the existing analyses are inadequate to answer key questions
Samples for analysis are commonly taken from the surfaces, or from just beneath the surfaces, of silver coins, and these are not representative of the original alloys used, leading to erroneous estimates of overall composition
B. V. Hampshire et al, Heritage 2, 400-407(2019)

## Slide 9
Case Studies
1) Roman silver coins:
Image from: Matthew Ponting, Liverpool University
surface
core
SEM-EDS

## Slide 10
Case Studies
1) Roman silver coins:
denarius of Julia Domna
Muon momentum = 17, 18, 19, 20, 22, and 35 MeV/c
35 MeV/c
402±61 μm
107Ag
109Ag
B. V. Hampshire et al, Heritage 2, 400-407(2019)

## Slide 11
Case Studies
1) Roman silver coins:
190 µm
51(1)% Ag
49(1)% Cu
B. V. Hampshire et al, Heritage 2, 400-407(2019)

## Slide 12
Case Studies
2) Roman gold coins:
aurei from the “year of four emperors”
AD 68/9
During the AD 68/9 Civil Wars: Galba, Otho, Vitellius and then Vespasian fought for and gained control over the Roman empire - a period of serious and sustained disruption.
Existing analyses shows a minor reduction in the purity of the gold coinage.
Using X-ray fluorescence and µXES, a number of heavily debased gold coins issued during the AD 68/9 and many slightly debased coins issued in their immediate aftermath.
Debased Civil War gold coinages were indeed produced; that copper was used to debase Roman gold coins during this time, c. 185 years earlier than first shown
The metallurgical evidence from the gold coinage show the AD 68/9 Civil Wars caused significant and sustained disruption to the Roman economic system.
G. A. Green et al, Archaeological and Anthropological Sciences 14, 165 (2022)

## Slide 13
aurei from the “year of four emperors”
Muon momentum = 40 MeV/c
Micro-Analysis Consultants Ltd. (MAC) standards
MAC 1: 94% Au, 4.5% Ag, 1 %Cu
MAC 2: 75% Au, 19% Ag, 5% Cu
Ag70Au30: 30% Au, 70%Ag
44 aurei (measured with XRF) → 12 aurei measured with µXES
G. A. Green et al, Archaeological and Anthropological Sciences 14, 165 (2022)
Case Studies
2) Roman gold coins:

## Slide 14
G. A. Green et al, Archaeological and Anthropological Sciences 14, 165 (2022)
aurei from the “year of four emperors”
Muon momentum = 40 MeV/c
Micro-Analysis Consultants Ltd. (MAC) standards
MAC 1: 94% Au, 4.5% Ag, 1 %Cu
MAC 2: 75% Au, 19% Ag, 5% Cu
Ag70Au30: 30% Au, 70%Ag
44 aurei (measured with XRF) → 12 aurei measured with µXES
Coin 14
(Otho)
Coin 16
(Otho)
Ag
Cu
Case Studies
2) Roman gold coins:

## Slide 15
G. A. Green et al, Archaeological and Anthropological Sciences 14, 165 (2022)
aurei from the “year of four emperors”
Muon momentum = 40 MeV/c
Micro-Analysis Consultants Ltd. (MAC) standards
MAC 1: 94% Au, 4.5% Ag, 1 %Cu
MAC 2: 75% Au, 19% Ag, 5% Cu
Ag70Au30: 30% Au, 70%Ag
44 aurei (measured with XRF) → 12 aurei measured with µXES
Case Studies
2) Roman gold coins:

## Slide 16
  Cultural Heritage
      Bronze Age artefacts
      Mary Rose artefacts
      Baptismal Gates
      Swords
      Cannon Balls
      Sundials
      Coins
      Faience and glass
  Solar cells
  Piezoelectric devices
  Li batteries
  Advanced engineering
Hillier et al in Handbook of Cultural Heritage analysis
Cataldo et al, Appl. Sci 2022
Take-home messages

## Slide 17
Take-home messages
Strengths of the μXES technique:
Non-destructive and depth-selective elemental analysis
Probe deep inside a sample (at least a few centimetre depending on the density of the sample)
Sensitive to all elements in the periodic table (Z ≥ 3)
Negligible radioactivity introduced in the sample
Perform isotopic composition
Possibility to determine the oxidation state of the element
Elemental mapping
Limitations of the μXES technique:
Detection limit ~sub-wt%

## Slide 18
Acknowledgements
Setup R&D (with K. Ishida)
Software Development for MuX
Adrian D. Hillier
Head of muon
group
Software Development for MuX
Matea Bjørklund
Industrial Placement
Student
Setup R&D (with A. D. Hillier)
Software development for MuX
Scheduling of RIKEN beamtimes
Me!
Muon Instrument
Scientist

## Slide 19
µ-XES experiments at ISIS
C, 45°
10mm
Currently, we perform the
µ-XES experiments in port 4
Decay-channel
Muon momentum range:
17 MeV/c – 120 MeV/c
(currently 90 MeV/c)
A. D. Hillier et al, Phil. Trans. R. Soc. A (2019)

## Slide 20
Experimental Setup
- beam
Sample
- beam
Fe
500μm
Zn
500μm
Cu
500μm
Ag
1000μm
Proof-of-concept sample 1
A. D. Hillier et al, Microchemical Journal (2016)
MuX

## Slide 21
Experimental Setup
Proof-of-concept sample 2
K. Ishida et al, in preparation
204Pb
203Tl
279.2
401.4
794.8
1/2+
3/2+
5/2+
7/2+
206Pb
205Tl
203.7
416.0
720.1
1/2+
3/2+
5/2+
7/2+
Proof-of-concept sample 3
Kβ
Kα
M. Aramini et al, Nanomaterials
2020, 10(7), 1260

## Slide 22
HEXITEC Detector
Beam Collimator
Fe2O3
C
Al
Sample face on
CdTe within the detector housing
Sample from above
Experimental Setup
Other technical developments: Elemental Mapping
A. D. Hillier et al, JPS Conf. Proc. 21, 011042 (2018)

## Slide 23
What can we achieve with negative muons (µ-)?
Sample (pure element like gold;
alloy like bronze; compound like plastic)
µ-momentum (p)
-> kinetic energy (T)
(relativistic mechanics)
vµ ~ velocity of atomic electron ~ 2 x 106 m/s
-> atomic capture
of muon
(formation of
muonic atom)
depth
Muonic
X-rays
t ~ 10-13 s
= 10-4 ns
Fate of captured muon ?
Muon decay
~ 100 ns (for high Z)
For Fe
(Z = 26)
9
2) Nuclear capture:
For Fe
(Z = 26)
For Mn
(Z = 25)
→
γ-ray emission